## Slide 1: Solid state detectors part 2
G. Casse
XXXII INTERNATIONAL SEMINAR of NUCLEAR and SUBNUCLEAR PHYSICS "Francesco Romano" June 7-11, 2021

## Slide 2
Lecture 1:
Solid-state tracking detectors (2 hours)
Lecture 2:
Solid-state photon detectors (1 hour)

## Slide 3
Lecture 1:
Solid-state tracking detectors (2 hours)
Lecture 2:
Solid-state photon detectors (1 hour)

## Slide 4
OUTLINE:
Low intensity light (single photon) detection with silicon
Principle of operations
Structure of SiPM
Gate, PDE, Noise
Developments for Physics experimentys

## Slide 5
Energy loss by photon:
Photo-electric effect: Aγ  A+e (E <10-100 keV)
(discontinuities due to ionisation thresholds)
PDG 2001
Mean-free-path for photons is 9/7*X0 (  1/ ), very similar to that for electrons!
A
A
e-

e+
Pair-production
A
e
A
e

Pair-production: γ A e+ e-A (E >1-10 MeV)
(due to E-field nuclei)
Compton scattering: e γ A e γA
(Topologically similar to Bremsstrahlung!)

## Slide 6
Detecting single photons
A mip in a 300mm thick Si-detector releases 24ke, and need low noise amplification. Here we talk about 1 electron.
Need a different mechanism:
Internal amplification multiplication.
Remember the diode IV characteristic:

## Slide 7: Solid-state low-light detectors
SOLID-STATE DETECTORS WITH INTERNAL GAIN
- process: multiplication of carriers via impact ionization
- Advantages: low-bias, compact, rugged, insensitive to magnetic field.
APD
PD
SPAD
VBD
7
SPAD (Single-photon avalanche diode) (GEIGER-MODE APD)
Gain ~106 or more
Timing ~ 20÷50 ps.
Bias voltage <100V
Sensitivity ~1 ph. e.

## Slide 8: SPAD: working principle
Biased (Va) ABOVE breakdown voltage (with excess bias Vex)
Single photon or thermally generated carrier switches on avalanche process (with a certain probability)  macroscopic current
Avalanche has to be quenched by external circuit  quenching circuit:
    Passive quenching in SiPMs (large resistance: usually > 300 kOhm)
Bias reset above breakdown voltage  dead time.
cathode
anode

## Slide 9: SPAD: drawbacks
Limited active area: 20µm ÷ 200µm
Cannot count the number of photons
avalanche
propagates
all over the
diode
avalanche
time
Current
5 photons
1 photon

## Slide 10: The Silicon Photomultiplier (SiPM)
SPAD
SPAD
SPAD
SPAD
SiPMs are arrays of small SPADs connected in parallel.
Each SPAD employs a passive quenching mechanism.
SiPM size:
1x1 mm2 to 10x10 mm2
Microcell (SPAD) pitch:
12 um to 40 um
(typical)

## Slide 11
The Silicon Photomultiplier
A SiPM is a single-photon detector, with internal signal amplification, fabricated on CMOS-compatible silicon wafers.
Capabilities of SiPMs:
Detection of single photons in the visible / NIR range with simple (low power) readout electronics.
Excellent timing performance: down to 50 ps FWHM.
Few-photon or many-photon counting capabilities, depending on design.
Example of few-photon counting
Single photon time resolution (SPTR)
λ = 425 nm

## Slide 12: The Silicon Photomultiplier (SiPM)
Each element is independent and gives the same signal when fired.
Q = Q1 + Q2 = 2*Q1
Output amplitude (and charge)  proportional to the number of triggered cells  proportional to the number of photons.
Flash of
photons

## Slide 13: Silicon Photomultiplier (SiPM)
http://www.ketek.net/
http://advansid.com/
composed of square SPAD e.g. 40x40 µm2
Active area of 1x1mm2 up to 10x10mm2
Different package and connections.
TILE of SiPMs to cover big areas.
Typically coupled to scintillators for gamma-ray detection (e.g. medical imaging, physics experiments)
3.23 cm
8x8

## Slide 14
Typical SiPM Structure with trenches
~ few µm
High-field region
Quenching resistor
Metal
Connections
Microcell (SPAD) of SiPM
High-field region:
is defined with a high-energy ion implant. Avalanche multiplication takes place here.
Deep trenches:
are used to isolate adjacent microcells electrically. Optical isolation depends on filling material.
Superficial implant:
Very thin, constitutes the entrance window for the light into the SPAD
High-dose, partially undepleted.
Epitaxial layer:
The region on which the SiPM cells are built.
Usually fully depleted at breakdown. Close to the interface with the bulk, part of it is undepleted.
Bulk:
(Very) high-doping region upon which the epitaxial layer is built. Never depleted.

## Slide 15
SiPM Gain
7
The Gain in a SiPM is a measure of the number of carriers that pass through the high field region of one microcell during an avalanche.
It can be measured as the integral of the output current of the SiPM when an avalanche is triggered.
Chart: Single photoelectron signal
Gain
Recharge time constant
Parameter | Typical values
Rq | 500 kOhm – 1.5 Mohm
Cd | 15 fF – 150 fF
Cq | 5 fF – 10 fF
Tau | 8 ns – 100 ns

## Slide 16: Photon Detection Eff<iciency
Fill Factor
Quantum Efficiency
Avalanche Triggering Probability
Photon Detection Efficiency (PDE) is a measurement of the probability that a photon impinging on the SiPM surface starts an avalanche.

## Slide 17: Avalanche triggering probability: Pt
Avalanche triggering probability increases with overvoltage, from zero at VBD to 100% at high bias.
At the same level of bias and peak electric field, electrons have a higher probability of initiating an avalanche compared to holes.
Oldham, W. G., Samuelson, R. R., & Antognetti, P. (1972). Triggering phenomena in avalanche diodes. IEEE Transactions on Electron Devices, 19(9), 1056–1060. doi:10.1109/t-ed.1972.17544
High-field region
Electric Field
Red photon
Blue photon
Red photon
Blue photon
Qualitative plot of avalanche triggering probability for holes, electrons and total vs. depth in an p-on-n junction similar to the one used in NUV-HD SiPMs.

## Slide 18: NUV-HD technology: effect of overvoltage on avalanche trigger probability (Pt)
Fast increase of Pt with over-voltage:
 avalanche is initiated by electrons
Slower increase of Pt with over-voltage:
 avalanche is initiated by holes (and electrons)

## Slide 19: Effect of geometry on PDE
SPAD Pitch | 15 µm | 20 µm
Fill Factor (%) | 55 | 66
SPAD/mm2 | 4444 | 2500
25 µm | 30 µm | 35 µm | 40 µm
73 | 77 | 81 | 83
1600 | 1111 | 816 | 625
NUV
SiPM NUV-HD
SPAD pitch (mm)
SPAD size
active area

## Slide 20: Effect of OV PDE
35 um cell pitch
~60% !
Gola, A et al. (2019). “NUV-Sensitive Silicon Photomultiplier Technologies Developed at Fondazione Bruno Kessler.” Sensors, 19(2), 308.
Reduction of PDE because of limited thickness of epitaxial layer (few um)
Pe
Ph
Cutoff because of protective resin

## Slide 21
Noise in SiPMs
Primary
dark counts
DiCT
DeCT
Afterpulsing
Cross-section of the SiPM microcells.
SiPM waveforms acquired with the oscilloscope
Different SiPM noise components are related to different physical phenomena.

## Slide 22
Sources of primary DCR
Entrance window
(un-depleted)
Un-depleted epi
Electric Field
High-Field region
Drift Region
Bulk
SRH, Poole-Frenkel, Trap assisted tunneling
Direct tunneling (dominant at low-Temp)
SRH generation
Diffusion
Diffusion
All these components have different dependence on device parameters and on temperature..
Typically dominant at room T

## Slide 23: SiPM noise: Dark Count Rate and Optical Crosstalk
T = 20 C
Dark Count Rate
80 kHz
Optical Crosstalk
(Correlated Noise)
15%

## Slide 24: Scientific experiment motivated improvement: NUV-HD-LowCT SiPM technologies
NUV-HD-LowCT technology was initially developed for the focal plane of the Medium Size Telescopes (MST) of the Cherenkov Telescope Array.
Reducing crosstalk probability is important to reduce false triggers, especially in presence of strong Night Sky Background.
FBK SiPMs have been employed for the first time in the focal plane of the prototype Schwarzschild-Couder Telescope (pSCT), installed in the VERITAS (Very Energetic Radiation Imaging Telescope Array System) observatory site, in Arizona, USA.
First gamma-ray signals from the Crab Nebula have been recently detected.
Prototype pSCT installed in the VERITAS, equipped with FBK SiPMs.
Representation of the 99 telescoped planned for the southern hemisphere at ESO's Paranal Observatory.

## Slide 25: NUV-HD-LowCT SiPM technologies in FBK
PDE at 420 nm vs. OV
PRELIMINARY
Up to 70%!
DiCT vs. PDE
SEM image of trenches, separating adjacent microcells.
Light absorbing material is placed inside trenches, between adjacent microcells
>60%
Measurements on 40 µm cell size SiPMs, with silicone resin coating
Low optical crosstalk technologies can be obtained by inserting material that absorbs or reflects secondary photons, emitted by the avalanches in the microcells.
Electric field engineering increases PDE compared to standard NUV-HD technology.
Metal in trenches is under development..

## Slide 26
DarksSide-20k Experiment
LAr TPC
DarkSide-50
PMT-based TPC
LSV
WCD
~ 23t of UAr
DarkSide-20k
SiPM-based TPC
TPB WLS: emission at 400 – 450 nm
2 light readout planes: 20 m2 (+ veto)
SiPM tiles
> 3-year long collaboration between FBK and DarkSide to optimize performance of the NUV-HD technology for the specifications of the project.

## Slide 27
Primary DCR reduction
Standard field
Low-field
0.3 counts per day per cell at 77 K!
> 7 orders of magnitude !
Thermal generation
Tunneling
> 20x
A 10x10 cm2 SiPM array would have a total DCR < 100 cps!
25 um cell

## Slide 28
NUV-HD-SF and LF - Afterpulsing
Cell Size = 25 um
AP is maximum at ~ 77 K!
Increase of release time constant of trapping centers at lower temperatures increases AP probability.
AP increase is partially offset by increase of microcell recharge time constant.
A. Gola et al.,Sensors 19, no. 2, (2019), 308

## Slide 29
Photo-detector module
24x 12x8 mm2 SiPMs (~ 1 cm2)
Front-end cryogenic pre-amplifier with differential output
Sensitivity from single photon to few thousands photons
PDM Specifications:
5x5 cm2 active surface
PDE @ 420 nm > 40%
DCR < 0.08 cps/mm2
Baseline hit rate ≤ DCR ↔ SNR > 8
Timing resolution ~ 10 ns
Integration window of 6 μs
20.7 m2 ◦ 6 μs ◦ DCR = 10 pe

## Slide 30
Photon counting with PDM at 77 K
Total Area = 24 cm2
1 readout channel
30 µm cells, 7 V over-voltage
~500 ns recharge time
Good gain uniformity of ~ 3M SPADs at 77 K
Measurements from LNGS

## Slide 31
DarkSide Motherborad
Each motherboard contains 25 Photo Detection Modules
+ power distribution and signal transmitter

## Slide 32
The nEXO experiment
R&D carried out for nEXO to develop SiPMs capable of direct detection of photons at 178 nm and operation at -100°C
TPC Filled with LXe
4-5 m2 SiPM
Single VUV photon sensitive (178 nm)
  > 15% efficiency
  < 20% correlated noise
  < 50 mHz/mm2 DCR
Very low radioactivity
  Silicon is generally very radio pure
0nbb with LXe

## Slide 33
VUV–HD
PDE vs OV (~190 nm)
R&D focused on ARC optimization: Si3N4 removal and preservation of surface passivation quality.
𝜆 = 175 nm
T = -104°C (LXe)
nEXO experiment at Stanford
arXiv:1904.05977
Best result reported in literature

## Slide 34: R&D on SiPM Radiation Hardness
Qualification of radiation tolerance of current SiPM technologies.
Study / modeling of the effects of radiation damage on SiPM characteristics, under different sources of radiation.
Development of a highly customized SiPM technology for optimal performanceafter irradiaiton is most likely needed
LHC
LIMADOU
Calorimeters for collider experiments: from 1010 neq/cm² to >1014 neq/cm²
Geostationary orbit space experiments: ~5∙1010 neq/cm²
Improving radiation hardness of SiPMs is one of the next frontiers of development at FBK for very important applications, both in big science experiments and in space.

## Slide 35
Increase of the primary (Poisson distributed) Dark Count Rate seems the most important effect observed after irradiation.
Faster increase with dose
Saturation effects:
Limited number of cells
Self-heating
..
Slower increase with dose
Example of a broad study of several FBK technologies. 62 MeV proton beam, doses up to 2e13 neq/cm2, RT annealing during 1 month. Data from IV analysis. More information at: https://indico.cern.ch/event/983068/
PRELIMINARY

## Slide 36
SiPMs with extreme radiation tolerance are required for the Barrel Timing Layer of the CMS experiment, at CERN: 1.9×1014 1 MeV neq/cm2.
Custom SiPM technology was developed, combining electric field engineering with small-pitch SiPM technology, for enhanced radiation hardness.
HFF layout
STD layout
FoM measured by from CMS collaboration: A. Heering, Y. Musienko, M. Lucchini et al.)
Chart: Over-Voltage (V)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14
15µm-HFF | 0.037322 | 0.20545 | 0.27436 | 0.32163 | 0.34807 | 0.37691 | 0.38026 | 0.41069 | 0.41443 | 0.42402 | 0.43838 | 0.44729 | 0.46089 | 0.43534
15µm-STD | 0.038763 | 0.16549 | 0.22584 | 0.26542 | 0.28209 | 0.30498 | 0.3134 | 0.32968 | 0.34089 | 0.34644 | 0.34352 | 0.37372 | 0.36794 | 0.38066
The advantage of using small cells for radiation hardness is relevant only if they can still provide very high PDE
NUV-HD-RH SiPMs

## Slide 37
SUMMARY
Silicon PhotoMultipliers (SiPM) are phasing out the previous technology (the PhotoMultiplier Tubes, PMT) for low light intensity detection.
They exhibit increasingly good performance (in terms of PDE and low dark count rate) in the wavelength range from Near Infrared to Vacuum Ultraviolet.
SiPM are the sensor of choice for high sensitivity, large mass physics experiments where the signal is scintillation light.
Interest by medical, automotive and space industries.

## Slide 38: NUV-HD SiPMs for ToF PET
Leading Edge Discriminator
Digital data through Ethernet
1 GHz
10 GS/s
Thermostatic chamber
Scintillator
SiPM
Scintillator readout with SiPMs for ToF-PET
Experimental setup

## Slide 39: Application of NIR-SiPMs
LiDAR for Automotive
Ongoing R&D collaborations with 3 companies