## Slide 1: Testing NIT (Nano Imaging Trackers) films at CNAO
Giovanni De Lellis
University Federico II and INFN, Naples

## Slide 2
AgBr-I: sensitive elements
Organic gelatine: retaining structure
PVA to stabilise the crystal growth
Ag
O
N
C
Recoil energy (MeV)
Track length (micron)
heavy nuclei
light nuclei
2
NIT EMULSIONS
Br
40 nm
25 nm
Crystal size

## Slide 3
Pouring stages
Chemical preparation desk
Production machine
NIT PRODUCTION MACHINE AT LNGS
3
3

## Slide 4
Optical Microscope Read-out: Step 1
Scanning with optical microscope and shape recognition analysis
Bonito CL/CMC-4000
CMOS Camera
4 Mpix, @100 fps
LED Lamp
Nikon Oil Objective
100x, 1.45 N.A., Plan Apo
Magnifying lens,
Nikon VM C-2.5x
Resolution: 28 nm/pixel
View Size: 65.2 x 48.3 µm2
100x objective lens with high N.A.
4

## Slide 5
Resonant Light Scattering From Ag Nanoparticles
Oscillation of e-cloud
Nano-metal in medium εd
Scattering spectrum depends on the light polarization and on the grain shape
El intensity of inside metal
H.Tamaru et al ., Applied Phys Letters 80, 1826 (2002)
El is resonance enhanced
The polarization dependence of the resonance frequencies strongly reflects the shape anisotropy
SEM image
SEM image
Ag 100 nm spherical
no polarizing property
Ag 100 nm spheroidal
polarizing property
λl
5

## Slide 6
30keV Carbon ion
implanted
Surface of
emulsion
500nm
Different orientation
Scattering intensity
polarization direction of incident light
Optical response strongly depends
on the polarization of incident light
TEM image of Carbon track after development
polarization direction
Resonant light scattering: silver grains
6
Resolving two grains closer than 𝛌/2

## Slide 7
30keV Carbon ion
implanted
Surface of
emulsion
500nm
Different orientation
Scattering intensity
polarization direction of incident light
Optical response strongly depends
on the polarization of incident light
TEM image of Carbon track after development
polarization direction
Resonant light scattering: silver grains
7
PTEP (2019) 063H02
Resolving two grains closer than 𝛌/2

## Slide 8
A Track Made Of Two Grains
1μm
e = 1.49
without polarizer
Linear fit slope = track direction
dx ●
dy ○
1μm
Angle of polarization (degree)
Track validated by
elliptical shape analysis
8
PTEP (2019) 063H02

## Slide 9
Colour Camera and Extension of the Plasmon Resonance Analysis
White LED source
Particle tracks displayed in colour
Sample illuminated with white light
Colour camera
9

## Slide 10: LSP (Localized Surface Plasmon) resonance
45x120
45x80
dipole in metallic particle
dipole moment
resonance
Ag grain size → resonance wavelength
R = 45 nm  blue
H = 80 (120) nm  green (red)
metallic particle
100 nm
100 nm
Annu. Rev. Phys. Chem. 58 (2007) 267-297
Appl. Phys. Lett. 80, 1826 (2002)
45x80
45x120

## Slide 11: Silver Nanoparticles for calibration
NP-60
NP-40
7.5 µm x 7.5 µm
7.5 µm x 7.5 µm
40 nm diameter
60 nm diameter
11

## Slide 12: Silver Nanorods for calibration
NR-40x120
NR-40x80
7.5 µm x 7.5 µm
7.5 µm x 7.5 µm
40 nm diameter, 80 nm height
40 nm diameter, 120 nm height
12

## Slide 13: Colour camera Localized Surface Plasmon Resonance
100keV C-ions
Alpha track
Image size 15 µm x 15 µm
Image size 15 µm x 15 µm
13
Head/tail discrimination!

## Slide 14: Testing NIT Films at CNAO (1)
Sensitive layers (tunable, few tens of 𝛍m)
protons
Glass or Plastic (polystyrene) support, 70 to 200 𝛍m
Fragmentation of target (polystyrene) induced by proton collision
100-300 𝛍m
being crystals so small  Large dE/dx is required to sensitize them
 These films are insensitive to mip (cosmic-rays)
σ ~ 6 nm!

## Slide 15: Testing NIT Films at CNAO (2)
Produce the films at Gran Sasso a (few) weeks before
Technical test: check the sensitivity of these films to Carbon ions and protons
Physics goal: use protons to study the fragmentation of the target (emulsions, polystyrene, …?)
Identification of different fragments (charge) through the colour analysis? to be tested
We could expose a few films to test some of the above features