## Slide 1: R&D on Magnets for FCC-hh (and variants)
Lucio Rossi – CERN A&TS
Former LHC Magnet Group Leader – Former HL-LHC Project Leader
(On leave form Univ. of Milano- Physics Dept.)
Giornata sulla European Strategy for Particle Physics @ INFN-Roma1 – 21 Sept.2020

## Slide 2: LHC full energy exploitation
14 T=2x7 TeV operation (8.3 T dipole field)
  Tests before YETS 2016/2017 revealed problem with diode box that prevented termination of the proposed tests  LS2 consolidation of diode boxes.
  The test in sector 1-2 for validating magnet performance at 7TeV prior to LS2 showed that we may need 1 quench/magnet:  1000 quenches, 2-3 months of intense quench campaign.
15 TeV=2x7.5 TeV (ultimate energy, dipoles at 9 T - 93% of intrinsic limit):
  Not impossible but very challenging due to large overhead and possible reduced availability in operation. Some magnets were never trained to ultimate and some may need replacement. Will be a trade off with lumi loss: 20% lost seems the maximum acceptable, difficult to assess today if we are below that level.
Beyond ultimate energy by replacing 1 LHC dipole out of 3 with an 11 T HiLumi dipole:
  15.5 TeV= 2x7.75 TeV at nominal current (2x 8.33 T + one 11.1 T)
  16.6TeV= 2x8.3 TeV at ultimate current (2x9 T + 12 T, since are powered in series)
  Very unlikely: big change, big overheads of de and re-installation (2-3 y?) and very difficult operation. The cost is in the 2-3 BCHF range. Luminosity will be reduced by less avialbility.
  The HiLumi 11 T dipole is not optimized for cost since must be in series with LHC dipoles: big constraints.
LHC was operated in Run2 at 2x6.5 TeV, i.e. dipoles at 7.7 tesla – For 2x7 TeV  8.33 tesla, 86% of the max Ic

## Slide 3: Performance: Integrated Luminosity
Goal of Run1+Run2 was 150 fb-1!
F. Bordry, CERN Director for A&T
Cryo availbility: 97-99 % !

## Slide 4
0.75 1034 cm-2s-1
50 ns bunch high pile up 40
1.4 1034 cm-2s-1
25 ns bunch pile up 40
2 1034 cm-2s-1
25 ns bunch pile up 60
2 1034 cm-2s-1
with levelling, 25 ns b. pile up 60 continuous
Technical limitation on the istantaneous lumi: 1. Collider (cryolimit in the triplet region) at 21034 cm-2s-1 twice the nominal design luminosity)
2. Experiments (pile up in the detectors). Designed for PU 40 they are actually dealing with 60!
Technical limitation on integrated lumi: 1. Collider (radiation damage to the IT magnets – correctors and quadrupoles)
2. Experiments (radiation damage in the Inner Tracker)
Notes: Radiation damage and halveningtime

## Slide 5: Outlook to LHC Run 3 (2021-2023)
9.7 kW/arc (195 W/hc)
Pure BCMS
 | 2021 | 2022 | 2023* | Comment
# bunches | Up to 2748 (BCMS) |  |  | 
 | 1.3 | 1.3 | 1.3  1.55 | Intensity Ramp Up
 | 0 1.4 | 1.4 1.8 | 1.8  2.1 | Max bunch population at the end of each year
 | 2021 | 2022 | 2023* | Comment
# bunches | Up to 2748 (BCMS) |  |  | 
 | 1.3 | 1.3 | 1.3  1.55 | Intensity Ramp Up
 | 0 1.4 | 1.4 1.8 | 1.8  2.1 | Max bunch population at the end of each year
LIU forecast for beam intensity ramp up for HL: can be used in LHC Run3 ?
Approaching cryogenic limitations different heat load emerged in Run2 is to be understood
r=30% decrease
40% increase in integrated luminosity

Swapping the vertical crossing polarity
Pushing present LHC at the limits (using HL-LHC studies and early installation of HiLumi equipment in LS2…: Levelling, collimator low-Z and DS, TDIS…
Lint 160 fb-1 at reach in Run3 with margins
> 350 fb-1 we enter in unknown territory for radiation damage
Run3 WG ,
S. Fartoukh, chair
N. Karastathis

## Slide 6: Why not just keep going with cons?
Upgrade!
Performance improving consolidation
Now performace pushed up to 4000 fb-1 as ultimate value

## Slide 7
> Half way

## Slide 8
Technology landmarks

## Slide 9
LBH_A (11T)
LBH_B (11T)
By-pass cryostat with collimator
Complete 11.2 T cryo-assembly replacing a 15 m long 8.3 LHC dipole
Operation 7 TeV
7 TeV
Hybrid (long proto): Excellent at first ! But strong permanent degradation after thermal cycle. Absence of thermal gradient control in the procedure.
L. Bottura & A. Devred
HiLumi WP11- F. Savary et al.

## Slide 10: 6 11 T to build: 2 pairs to test + 1 pair spare Each pair is 1 MBHA with 1 MBHB
Primo dii serie, tipo B: OK!!!
Secondo di serie, tipo A e ideale da accoppiare con il primo tipo B.
Terzo in test per problemi elettrici: ottimo come quench ma diversi strani segnali elettrici hani richesto tanti test e poi si è degradato
Terzo di serie, tipo A: 1 QH rotto e una bobina degradata
In riparazione
Quarto di series, MBHB-003: OK al primo col down
Ma occorre fare il ciclo termico e nuovo powering e verificare che vada bene!

## Slide 11: 11 T in full swing production: trying to get at least one pair installed during LS2 in 2021!

## Slide 12: IT quadrupole. Increase in field but also in size wrt LHC. Very relevant also for FCC magnets

## Slide 13: Excelent results IT quadrupoles short models (thanks also to US-LARP)
Best HF magnet ever tested in terms of behaviour (not max field)
Final conductor, final prestress procedure
This magnet had a too high prestress The last higher quench have fast ramp rate
All magnets have exceptional memory (no low current quench after thermal cycle)
However we found recently electrical and structural problems on the first two long prototypes (partly seen also on 11 T).
Structural problems on IT Quads understood and being solved: traced to too small margin (in shells). Electrical problem (QH insulation): 2 solutions identified.
Industrialization of long magnets is being more difficult than anticipated! Difference from LHC NbTi.
HiLumi WP3: E. Todesco et al.

## Slide 14: First two US long (4.2 m) IT quads:
Succesful Proto P1 but then voltage breakdown trigged by test at too high Voltage. Repair not successful.
US proto n.2: very bad. Structural failure on a component that was already modified. Howeve triggered a rview and a decise increase of the structural margin.
Primo prototipo lungo CERN (7.2m): degradazione di una bobina: da riparare

## Slide 15: Endurance test on a short IT quad and coil replacement test at CERN
Short models allowed to explore long term behaviour
  MQXFS1 had 8 thermal cycles and 150 quenches, always reched nominal after thermal cycle without quench
  No performance degradation, alwqays reached ultimate after training
Second long term test on MQXFS4
  Special VI measurements - no degradation
  7 thermal cycles done
  Ultimate reached at 1.9 and 4.2 K
Courtesy of E. Todesco
Leader of the HiLumi Magnets for the insertion regions
A weak short model (with cable not conform, was repaired successfully with old coils

## Slide 16: Dec 2019: first US series test: it worked!

## Slide 17: 2st series US quad: 2 weeks ago! Success!

## Slide 18: The US magnets must be paired to have a complete quadrupole set (4.2m+4.2m)
So now they can couple the two magnets, put them into the cryostat and deliver the first IT Quad for the IT string

## Slide 19: P2 IT Quad in CERN; in USA P5/P6
Making long magnets in Nb3Sn is challenging – especially in view of for mass production. We are confident for HiLumi: the project is big but not enormous (about 30 magnets of 4.2, 5.5 and 7.2 m length) by 2024 (2025?). Consider that basic R&D started in 2005 and specific R&D in 2010

## Slide 20: The LHC after HiLumi
LHC as FCC-hh (expensive) injector
  Foreseen to work at low maintenance 3 TeV beam
  Can provide also beam for fixed target at 1..3 TeV
High(er) Energy LHC (for HEP community to assess if interesting or not)
  33 TeV c.o.m. : 20 T magnets (2010 Malta Workshop)
  27 TeV c.o.m. : 16 T magnets (FCC baseline magnet)
  21 TeV c.o.m. : LHC1.5, based on 12 T magnets
LHeC compatible with
  Present LHC (with important modifications)
  New HE-LHC, whatever configuration (a bit easier than present LHC)

## Slide 21: The 25 y LHC construction time line possible only because SSC developed the superconductor…
Only 2 y to make a short magnet «near to final». Conductor available(SSC)
12 y from first working prototype to last magnet
7 years from start R&D to 1st Industry proto

## Slide 22: HE-LHC Malta FP7-Eucard workshop (2010)
Dipole at 20 T
Energy 33 TeV (c.om.)
Where are we?
Little work in that direction.
Magnet technology Hilumi (11-12 T) is taking longer than anticipated
Minimal resources for HTS
It took > 10 years to develop the SC for HiLiumi (2003-2015)
SC for B>12-14 T is not yet there. Effort for a more realistic HE-LHC done in the frame of FCC-hh (since 2013)
L. Rossi & E. Todesco, CERN

## Slide 23: HE-LHC as designed inside FCC-hh project Dipole Field 16 T  27 TeV c.o.m.
M. Benedikt, F. Zimmermann et al.

## Slide 24
Circular hadron colliders: FCC-hh and SppC
circumference 100 km, two high-luminosity experiments up to 3 (1) x 1035 cm-2s-1, two additional experiments possibly combined with injection section, collimation insertions (betatron and momentum cleaning), extraction/dump insertion, RF insertion,
FCC-hh
SppC
new injector chain,
simultaneous operation with e+e- collider
based on existing CERN injector chain,
Luminosity goal ~20 ab-1 per main IP within 25 years
values in brackets refer to CEPC
M.Benedikt @ Granada

## Slide 25: p-p machine CERN
parameter | FCC-hh |  |  | HE-LHC | HL-LHC | LHC
collision energy cms [TeV] | 100 |  |  | 27 | 14 | 14
dipole field [T] | 16 |  |  | 16 | 8.33 | 8.33
circumference [km] | 97.75 |  |  | 26.7 | 26.7 | 26.7
beam current [A] | 0.5 |  |  | 1.1 | 1.1 | 0.58
bunch intensity [1011] | 1 |  | 1 | 2.2 | 2.2 | 1.15
bunch spacing [ns] | 25 |  | 25 | 25 | 25 | 25
synchr. rad. power / ring [kW] | 2400 |  |  | 101 | 7.3 | 3.6
SR power / length [W/m/ap.] | 28.4 |  |  | 4.6 | 0.33 | 0.17
long. emit. damping time [h] | 0.54 |  |  | 1.8 | 12.9 | 12.9
beta* [m] | 1.1 | 0.3 |  | 0.25 | 0.15 (min.) | 0.55
normalized emittance [mm] | 2.2 |  |  | 2.5 | 2.5 | 3.75
peak luminosity [1034 cm-2s-1] | 5 |  | 30 | 28 | 5 (lev.) | 1
events/bunch crossing | 170 |  | 1000 | 800 | 132 | 27
stored energy/beam [GJ] | 8.4 |  |  | 1.4 | 0.7 | 0.36

## Slide 26: The timeline of a FCC-hh is determined by magnet technology wich depends on SC development16 T
Main development goal is wire performance increase:
Jc (16T, 4.2K) > 1500 A/mm2 50% increase wrt HL-LHC wire
Reduction of coil & magnet cross-section
This is difficult
A. Ballarino & L. Bottura, CERN
Present FCC targets

## Slide 27: Conductor R&D
1274 A/mm2 @ 15T, 4.2K
≈ 1000 A/mm2 @ 16T, 4.2K
2850 A/mm2 @ 12T, 4.2K
≈ 1250 A/mm2 @ 16T, 4.2K
≈ 950 A/mm2 @ 16T, 4.2K
1750 A/mm2 @ 15T, 4.2K
≈ 1400 A/mm2 @ 16T, 4.2K
Specification: 1500 A/mm2 @ 16T, 4.2K
Results expected later this year

## Slide 28: FCC Magnet 3 Designs
 |  | blocks |  | cos(q) |  | common coil
Current | (A) | 11230 |  | 10000 |  | 16100
Inductance | (mH/m) | 40 |  | 50 |  | 19.2
Stored energy | (kJ/m) | 2520 |  | 2500 |  | 2490
Coil mass | (tons) | 7400 |  | 7400 |  | 9200
Very efficient use of superconductor
Simplified mechanics and manufacturing ?
Top ≈ 1.9 K
Iop/IC(loadline) ≈ 86 %
Vdump < 2.5 kV
smax < 200 MPa
Thot < 350 K
Dout ≈ 600 mm
From 2013 this the only results!!
(of course nto true: Sc development + small racetracks +… Hilumi
+ launching costruction of 1 m short models
HE-LHC !
Falcon-D

## Slide 29: Highest “dipole” fields
Magnets with “bore”
Field records
LBNL HD1
Record fields for SC magnets in “dipole” configuration
CERN RMC
CERN/CEA FRESCA2
From Luca.Bottura-CERN

## Slide 30: Recent very successful > 14 T magnet reached by US MDP cos dipole at FNAL
But the route is long… a 16 T 100 km accelerator is not yet at hand and a long R&D is necessary.
In May 2020 in Budapest gthe new ESPP will be approved…

## Slide 31
high-field magnet R&D for SppC
10.2 T @ 4.2 K dipole field
in two apertures
(Performance limited by NbTi coils)
Notes: New slide from Davide.
Showing that conductor development is launched at international level, Russia, Japan, (Korea and Europe in preparation)
Underline importance of that development as main cost driver for the hadron collider machine.

## Slide 32
Opening a new page?
High Temperature Superconductors – HTS: next technology step
Plot courtesy of C. Senatore, UNIGE

## Slide 33
High Temperature Superconductors – HTS
The dream of 20-25 tesla! (2 x HilumiLHC!)
A 5 T, 40 mm bore HTS based dipole demonstrator

## Slide 34
Trying the magnets of the future… 20 tesla or more...

## Slide 35
2020
2021
2022
2023
2024
2025
2026
2027
Goal: Demonstrate technology for large scale Nb3Sn accelerator magnets (12 T)
Falcon
WP2/WP3: Nb3Sn Magnets
VE Prototypes
VE Models
SMC, (e)RMC, RMM
HF Models
HF: High Field (16 T target operating field)
VE: Value Engineered (operating field in the 12 T range)
Goal: Evaluate options for ultimate Nb3Sn performance (16 T)
CCT
CCT?
R2D2-FD
F2D2
DEMO
RMC-CC
European Strategy for Particle Physics 2018-2020
European Strategy for Particle Physics 2025-2027

## Slide 36
2020
2021
2022
2023
2024
2025
2026
2027
European Strategy for Particle Physics 2018-2020
European Strategy for Particle Physics 2025-2027
EuCARD2 F2
WP5: HTS Magnets
UHF: Ultra High Field (in excess of 20 T target operating field) GaToroid: funded by KT-MA
SCT: Small Coil Technology Superbend: Part of SLS upgrade at PSI
ASI: Agenzia Spaziale Italiana
Goal: Select options for HTS accelerator magnet design (20 T)
HTS Standalone demonstrators (“cloverleaf”)
EuCARD2
EuCARD2 cosq
HTS Inserts demonstrators
UHF models
Small Coil Technology
SCT for Superbend
New HF test station
Fresca2 at 163
Goal: Assess and quantify potential of HTS for accelerator magnets applications
ASI demonstrator
GaToroid demonstrator
Undulator demonstrator
Self-funded applications

## Slide 37: PERSONAL considerations -1 (Not checked by CERN or INFN management)
The New ESUPP has clarified that the community support the R&D for a new pp collider
EU (and US) has a big advantage in magnet technology: if we want to have the collider better to keep it.
The period 2013-2020 has been useful but now is needed much more focussed R&D
Clearly is different if to work for having an acclerator working at 16 T or 12 T field. The 16 T si compatible only with a start afterr 2050 in my opinion.
But for >2050 a HTS si possible, too (probably) making 20 T and reaching 125 TeV in pp 100 km tunnel
  On a short (2040) time scale only HE-LHC at 20-22 TeV or a FCC-hh with simple NbTi (40 TeV) is possible I believe.
  On a long time scale (>2050) I think a 120-150 TeV shodul be puirsuied ad the highest energy frontier.
  Tthe interemdiate hypothesis a FCC-hh working at 12 T field, i.e. 75 TeV, si possible for somehow 2040-2050…

## Slide 38: PERSONAL considerations -2 Four possibilties for a p-p collider
LHC1.5
12 T Nb3Sn dipoles HiLumi technology in LHC: 21 TeV c.o.m.
7 T Nb-Ti dipole (low cost LHC, 4.2 K):
44 TeV c.o.m. (100 km)
Energy tripler 100km
2040
HTS

## Slide 39
Thanks you

## Slide 40: Pile up
5 events
400
events
Pushing at the maximum the parameters of HL-LHC we would start the fill at L = 15x1034 with 400 events/crossing.
Notes: Ask Rogelio how degrade sensitivity wit pile up and ple up density.

## Slide 41: Long term development of SC is critical for HEP Hadron Collider: Open SC Lab Proposal
L. Bottura and F. Bordry
Phase I - Construction and commissioning (3 years)
• Equipment and labour: 10 MCHF
• Surface: 2000 m2
• Personnel: 10 FTEy (1 project engineer + 2 techn.)
Phase II - Facility ramp-up and initial operation (7 years, processed R&D material of the order of 25 kg/week, operation 40 weeks/year)
• Total cost: 20-30 MCHF

## Slide 42: Great performance of 30 km 1.9 K cryo-system
D. Delikaris
S. Claudet, CERN

## Slide 43: (Peak) Luminosity evolution and limitation
F. Bordry, CERN Director for A&T
2018
Notes: Ask picture of heat exchanger in triplet

## Slide 44
Have optics compatible with HL-LHC ATS optics and β*=0.1m
Head-on collisions mandatory 
High synchrotron radiation load, dipole in detector
Optimize LHeC to LHC ATS optics
Specification of Q1 – NbTi prototype
Revisit SR (direct and backscattered),
Masks+collimators
Beam-beam dynamics and 3 beam operation studies
Beam pipe: in CDR 6m, Be, ANSYS calculations
Composite material R+D, prototype, support..
 Essential for tracking, acceptance and Higgs
Asymmetric IR Design: example LHeC
S. Russenschuck
44
O. Bruning
and M. Klein

## Slide 45: HE-LHC time line and cost
1 TeV beam from SPS
2900 Magnets; 260 for LHC disposal
2020?
2040?

## Slide 46: Consideration on HE-LHC
Assume we want to have for installing in 2035-2040, right after HiLumi
We need to have the magnet proof tomorrow (2023-25)
But for tomorrow we will have «only» the HiLumi Magnets: 30 magnets, 4- to 7.5 m long, B= 11.2-11.5 T operative, B=12.3 T ultimate. I do not think that 16 T dipole industrial construction for HE-LHC can be launched by 2030 (only way to have it by beginning of 2040).
For 16 T dipole project we need a «buy-time project» like LHeC , see later. Or…
With a moderate effort a 12 T operative dipoles can be engineerized with HiLumi SC wire shortly after HiLumi.
  Still SC needs to cost less and needs a small, key, improvements: Deff is  45 µm for HiLumi; we need 20 µm. But we have plenty of Ic…
  Still the magnet technology at 11-12 T level is not yet fully gained, especialy in view of a mass production. We need to understand and improve long term degradation, stress control (mechanical & thermal) and electrical insulation robustness

## Slide 47: Timeline and cost (very rough, no study)
Domain | Cost MCHF | Comments | Wrt HE-LHC
Collider | 4500 | 2400 for Magnets | -500
Injectors | 500 ÷ 1100 | New optimization TBD | 0 ÷ -600
Tech Infr.+C.E. | 900 ÷ 1100 | Probably is less (< Psyn) | ? (-200?)
TOT | 6100 ÷ 6700 | (LHC2008 was 3400) | Cost should be optimized as upgrade
Cost scaled from 2019 HE-LHC study. If it is of real interest the study could be done

## Slide 48: Can LHC system & T.I. be re-used, lasting 15 years more?
YES if proper maintenance and consolidation is done. Already now Consolidation and serious maintenance are keys for the LHC availbilty and success.
Consolidation cost: 15-20 MCHF (10-15 MCHF for LHC and 5-8 for Injectors).
For system the maintenance (under Operation) is critical for duration: cryogenics
40% Tech. Infrastr. & Transp.
33% Magn. & Powering
CONS Budget by system
Courtesy M. Lamont, CERN

## Slide 49: LHeC and LHC1.5
In case of HE type LHC1.5 (realisitic for 2040)
  The option Ring-Ring should be again considered
  It consists of an electron ring in the LHC tunnel on the top of the HE new magnets.
  Certainly possible: was so at the design of LHC (LEP inside). Abandoned in 2001 to make simpler a few points.
  In a new ring design it should be accommodate
  The lepton magnets can be used alosd as LER (Low Energy Ring) for proton injector to avoid upgrade of SPS for post LHC1.5 use: LHC3 with HTS, if anything else is done). We have a (narrow!) tunnel and infrastructure to exploit at the maximum.

## Slide 50: LHeC: RL with ERL Operation as Baseline
Two 1 km long, 10 GeV
SC LINACs with
3 accelerating and
3 decelerating passes in CW operation
SRF sees 6*current
at the IP (≈ 4ns spacing)
 Q0 = 1010 requires
cryogenic system
comparable to LHC
system! Q0 > 1010
Super Conducting Recirculating Linac with Energy Recovery
Choose ⅓ of LHC circumference 
944 cavities; 59 cryo modules per linac
ca. 9 km underground tunnel installation
more than 4500 magnets (same magnet design as for RR option)
1033 cm-2 s-1 Luminosity reach | PROTONS | ELECTRONS
Beam Energy [GeV] | 7000 | 60
Luminosity [1033cm-2s-1] | 1 | 1
Normalized emittance gex,y [mm] | 3.75 | 50
Beta Funtion b*x,y [m] | 0.1 | 0.12
rms Beam size s*x,y [mm] | 7 | 7
rms Beam divergence s’*x,y [mrad] | 70 | 58
Beam Current @ IP [mA] | 430 (860) | 6.6
Bunch Spacing [ns] | 25 (50) | 25 (50)
Bunch Population | 1.7*1011 | (1*109) 2*109
Bunch charge [nC] | 27 | (0.16) 0.32
1034 cm-2 s-1 Luminosity reach | PROTONS | ELECTRONS
Beam Energy [GeV] | 7000 | 60
Luminosity [1033cm-2s-1] | 16 | 16
Normalized emittance gex,y [mm] | 2.5 | 20
Beta Funtion b*x,y [m] | 0.05 | 0.10
rms Beam size s*x,y [mm] | 4 | 4
rms Beam divergence s’*x,y [mrad] | 80 | 40
Beam Current @ IP[mA] | 1112 | 25
Bunch Spacing [ns] | 25 | 25
Bunch Population | 2.2*1011 | 4*109
Bunch charge [nC] | 35 | 0.64
Over 600MW Beam power in electron Beam!!!
Thanks to energy recovery the bill is only 100 MW!
ERL is a must for efficient operation!!!
ERL is new technology for energy efficiency and must be pursued: LHeC is the ideal first HE demonstrator
Cost: 1000-1500 MCHF (30÷60 GeV e- beam)
50
O. Bruning
and M. Klein

## Slide 51
O. Bruning
and M. Klein
The insertion region in LHC must be studied in detail to asses properly the feasibility
S. Russenschuck