## Slide 1
Design of High Temperature ISOL Targets
Mainly taken from M. Manzolaro’s
presentation at the HPTW 2018
S. Corradetti, M. Manzolaro, D. Scarpa, A. Monetti, L. Centofante

## Slide 2
Introduction: the ISOL (Isotope Separation On Line) technique
production target
transfer line
ion source
mass separator
charge breeder (1+ → n+)
& post accelerator
primary beam driver
high temperature
diffusion
effusion
+
+
+
+
+
high temperature
radiative heat transfer
P

## Slide 3
Introduction: the SPES facility @ LNL
New infrastructure for:
Cyclotron
ISOL RIB Facility
Application Facility
SPES is: 1) A second generation ISOL RIB Facility (for neutron-rich radioactive ion beams)
2) An interdisciplinary Application Facility (for p,n applications)

## Slide 4
Introduction: the ISOL RIB (Radioactive Ion Beam) facility
ISOL hall
40 MeV 200 µA primary proton beam
1+ RIB @ LE
to MRMS/HRMS
and n+ RIB @ HE

## Slide 5
40 MeV, 200 µA
proton beam
window (C)
disc (UCx)
dumper (C)
box (C)
heater (Ta)
The SPES target: general architecture and main characteristics
p energy: 40 MeV
p intensity: 200 µA
the whole target system must be operated at extremely high temperature (2000°C and more)

## Slide 6
The SPES target: general architecture and main characteristics

## Slide 7
The SPES target: general architecture and main characteristics
Mattia Manzolaro
before testing
after testing
Endurance tests at high temperature with Joule heating thermal load → 10 kW
(primary proton beam thermal load → 8 kW)
400 testing hours at ≈ 2000 °C → 200 hours at maximum power (10 kW)
80 heating-cooling cycles → 10 with current ramps of 1 s from 0 A to 1300 A (!)
TIS UNIT STILL OPERATIVE !

## Slide 8
Numerical models: a multiphysics approach
particle-matter interaction
thermal analysis
- thermal conduction
- thermal radiation
electrical conduction
structural analysis
ONE-WAY coupling
temperature distribution (x,y,z)
TWO-WAY coupling
temperature distribution (x,y,z)
Joule heating (x,y,z) – ρ (T)
electrical-thermal Finite Element model
power density (x,y,z)
ONE-WAY coupling

## Slide 9
Numerical models: the electrical-thermal Finite Element model
Reference: M. Ballan et al., Nucl. Instrum. Methods Phys. Res., Sect. B 376, 28-32 (2016)
Joule heating thermal load (1300 A) to heat the target during the conditioning phase

## Slide 10
Proton beam thermal load: 40 MeV, 0.2 mA (≈ 8 kW) (power density input for the Finite Element model calculated by means of particle physics MonteCarlo codes)
Numerical models: the electrical-thermal Finite Element model
TEMPERATURE DISTRIBUTION [°C]

## Slide 11
Numerical models: the electrical-thermal Finite Element model
THERMAL STRESS STATE [Pa]
(induced by temperature gradients)
Proton beam thermal load: 40 MeV, 0.2 mA (≈ 8 kW) (power density input for the Finite Element model calculated by means of particle physics MonteCarlo codes)

## Slide 12
homemade materials for the target disks (strong R&D activity required)
main requirements for ISOL target materials @ high temperatures
- open porosity and reduced grain size (diffusion & effusion)
- low vapor pressure (low gas load in the ion source and long term stability at high temperature)
- high emissivity
- high thermal conductivity
- good mechanical properties
total isotope yield deeply affected by open porosity (diffusion/effusion processes)
Target material characterization @ HT
Courtesy of Stefano Corradetti

## Slide 13
Emissivity e (th. radiation) and thermal conductivity l (th. conduction) control the target temperature field
Temperature gradients generate stress states and a good tensile/compressive strength σTS is required
Target material characterization @ HT

## Slide 14
M. Manzolaro, S. Corradetti, A. Andrighetto, L. Ferrari, Rev. Sci. Instrum. 84, (2013) 054902
L. Biasetto, M. Manzolaro, A. Andrighetto, Eur. Phys. J. A 38 (2008) 167-171
Emissivity e meas. method
Thermal conductivity l meas. method
Target material characterization @ HT

## Slide 15
Emissivity measurements for different Uranium Carbides
- Direct emissivity measurements on heated UCx discs using a dual frequency pyrometer
- UCx samples of different composition and synthesis routes produced in different laboratories participating to ActiLab
Target material characterization @ HT
Thermal Conductivity estimations for the SPES Uranium Carbide
- Creation of thermal gradients on UCx disks → thermal conductivity obtained by inverse analysis using Ansys®
- Activity performed in the context of ActiLab Work
Package in ENSAR (7th Framework Program)

## Slide 16
Target material characterization @ HT
average stress level during operation with primary beam
A new method to estimate the Tensile Strength @ HT (Silicon Carbide)
SiC disk (Hexoloy SA) – Matteo Sturaro master’s thesis, University of Padova
Supervisors: G. Meneghetti, A. Andrighetto, M. Manzolaro, M. Ballan

## Slide 17
Target material characterization @ HT
σ1max
Initial propagation direction
Defect
Vpc=0 m/s
Mirror
Vpc=1500 m/s
Hackle Lines
dpc
90°
Peculiar fracture shape
Fracture surface morphology
SiC SA
200X
Defect
G.D. Quinn, Fractography of Ceramics and Glasses, NIST Recommended Practice Guide, 2016
50X
Mirror
Hackle Lines
50X
Silicon Carbide Hexoloy SA
SiC SP

## Slide 18
Target material characterization @ HT
200X
 | Weibull Modulus m | σ0 [MPa]
SiC SA | 9,13 | 413,54
SiC SP | 7,58 | 239,09
 | σlim strength at Ps 99,9% (survival %) [MPa]
SiC SA | 194,07
SiC SP | 96,12
Chart: SiC Hexoloy® SA
| 5.6276211136906369 | 5.7401465473921274 | 5.7918849228777471 | 5.8289456176102075 | 5.8573615625845017 | 5.8681097680778773 | 5.9004451487208129 | 5.9215784196438159 | 5.9215784196438159 | 5.9215784196438159 | 5.9310242832965656 | 5.9310242832965656 | 5.9427993751267012 | 5.9704707106037462 | 5.9737078255187228 | 5.9769091290987832 | 5.9915145458580232 | 5.9915145458580232 | 5.9939614273065693 | 5.9939614273065693 | 5.9939614273065693 | 6.0345958730685858 | 6.0357206383625197 | 6.0629941982469031 | 6.0733209935778145 | 6.0802992608084727 | 6.1208247524136894 | 6.1582282049859876 | 6.1779441140506002 | 6.1844787334406801
σ 1 Max [MPa] | -4.086 | -2.9702 | -2.4417 | -2.087 | -1.817 | -1.5969 | -1.4098 | -1.2459 | -1.0992 | -0.96555 | -0.84215 | -0.72686 | -0.61805 | -0.51444 | -0.41497 | -0.31876 | -0.22501 | -0.133 | -0.04202 | 0.048621 | 0.13968 | 0.23201 | 0.32663 | 0.42487 | 0.52854 | 0.64034 | 0.76474 | 0.91024 | 1.0972 | 1.4096
Linea 3 | 4.3388 | -4.7912
Chart: ln(Ơi)
| 5.1575599288317742 | 5.2315897844973271 | 5.2376114914306422 | 5.2390980068880655 | 5.2390980068880655 | 5.2390980068880655 | 5.2390980068880655 | 5.2956137149737224 | 5.3135507471886259 | 5.3416162909431844 | 5.3648538903482805 | 5.3648538903482805 | 5.437687927995845 | 5.437687927995845 | 5.437687927995845 | 5.4627719215135668 | 5.4627719215135668 | 5.4905892541951591 | 5.4906717590423657 | 5.5014622713555568 | 5.5014622713555568 | 5.5176938312930028 | 5.5176938312930028 | 5.5245760607623922 | 5.6078220835102899 | 5.6701567470065406 | 5.6701567470065406
σ 1 Max [MPa] | -4.0164 | -2.8993 | -2.3695 | -2.0134 | -1.7418 | -1.5201 | -1.3312 | -1.1655 | -1.0167 | -0.88084 | -0.75501 | -0.63706 | -0.52532 | -0.41847 | -0.31538 | -0.21508 | -0.11669 | -0.019357 | 0.077806 | 0.17575 | 0.27559 | 0.37871 | 0.48702 | 0.60329 | 0.7321 | 0.88208 | 1.0739
Linea 3 | 7.7556 | -3.6144
SiC Hexoloy® SP

## Slide 19
Target material characterization @ HT
Type of fracture in TiC
Slow propagation
Fast fracture
TiC thermal conductivity
 | σlim strength at Ps 99,9% [MPa] | σ0 strength at Ps 37% [MPa] | m
TiC | 0,6 | 1,922 | 5,946

## Slide 20
Target material characterization @ HT

## Slide 21
Target material characterization @ HT

## Slide 22
Target material characterization @ HT