## Slide 1
Samples | Energy (MeV) | H+ Fluence (ions/cm2) | Se (keV/nm) | Sn (KeV/nm) | Dose (MGy)
DLC41 | - | - | - | - | 
DLC41 | 2 | 5x1013 | 0.024 | 1.4x10-5 | 1.13
DLC41 | 2 | 5x1014 | 0.024 | 1.4x10-5 | 11.3
DLC41 | 2 | 1x1015 | 0.024 | 1.4x10-5 | 22.6
China | - | - | - | - | 
China | 2 | 5x1013 | 0.024 | 1.4x10-5 | 1.13
China | 2 | 5x1014 | 0.024 | 1.4x10-5 | 11.3
China | 2 | 1x1015 | 0.024 | 1.4x10-5 | 22.6
FTM-NEXT
2020 activity report
Istituto Nazionale di Fisica Nucleare
SEZIONE DI LECCE

## Slide 2
It is well known that the activation of the D peak requires not only the so-called structurally-damaged area but also a surrounding region of crystalline structures. The used dose do not introduce topological disorder into DLC plane layers.
The obtained results, suggest that used ion beams, having a predominantly electronic stopping power, mainly produce ionization processes and emissions of energetic electrons in the interaction process with the DLC films. From literature data, modifications of the features of the Raman spectra can be evident only if the nuclear component of the total stopping power increases too. In this case the nuclear energy release to DLC can, probably, produces collision cascades. These impacts will give rise to carbon atom displacements from the lattice and dislocations, vacancies, defects and damage of the carbon platelets, as break and shrink.

## Slide 3
Raman spectra evolution following irradiation
1E15
PLD DLC (Lecce)
Magnetron DLC (USTC)
1E15

## Slide 4
Effect of irradiation on graphene sheets: an example
High-dose irradiation deeply modifies the features of a Raman spectrum, especially the G and D peaks
16MeV Au ions

## Slide 5
Effect of irradiation on graphene sheets: an example
before irradiation
after irradiation
Courtesy of Prof. Daniela Manno
Courtesy of Prof. Daniela Manno

## Slide 6
Probable low damage is produced by ions on the DLC coating films. An inversion in the structural evolution occurs in the range 10-100 MGy.

## Slide 7
A similar trend was observed on graphene sheets.
A localized energy transfer may originated a thermal annealing. The latter can give rise to a competitive process of partial amorphization and recrystallization

## Slide 8
The resistivity of 41-DLC sample do not vary in a significant manner. The resistivity of the China DLC coating slowly increases as the dose increasing.
Since the electrical transport processes are governed by grain boundary scattering processes, the slight structural evolution could affect the barrier height.
This would explain the slight increase in resistivity, more evident in the China coating.