## Slide 1
Metamaterials

## Slide 2: Proposed solutions
Metamaterials
Engineered material
multiple element assemblies
repeating patterns
properties from new structure
Their smart properties capable of manipulating EM waves: by blocking, absorbing, enhancing, or bending waves, to achieve benefits that go beyond conventional materials.

## Slide 3: Proposed solutions
Pyramidal structures
stacked copper-dielectric layers
broadband response
strong absorption of EM waves
low weight
small volume
Split Ring Resonator
copper strips on dielectric
narrow-band resonator
unit cells of a periodic array
depends on SRR dimensions
simple to manufacture

## Slide 4: Our pillbox cavity
Pill-box material | Aluminium
Cavity length | 100 mm
Cavity radius | 75 mm
Pipe length | 15 mm
Pipe radius | 20 mm
Pipe TM cut-off | 5.73 GHz

## Slide 5: Split Ring Resonators
Alumina SRR sample
(external side 5mm)
# | MODE | 
5 | TM021 | -39.5 @3.68 GHz
# | MODE | 
5 | TM021 | -39.5 @3.68 GHz

## Slide 6: Pyramidal structures

## Slide 7
Dielectric resonant cavity

## Slide 8: Resonant structure methodology
Dielectric resonator: Resonant structure methodology improves the sensitivity
for the electromagnetic characterization of very thin laser surface treated
structures and conductivity close to copper one
CU coated DUT
Sapphire
Hollow
holder
E field distribution
TE011 mode

## Slide 9: Resonant structure methodology
Chart: ∆h (mm)
| 4 | 3.5 | 3 | 2.5 | 2 | 1.5 | 1 | 0.5 | 0
R=2.6mm | 2.7686 | 3.3688 | 4.1233 | 5.0988 | 6.3938 | 7.9627 | 9.6127 | 10.1647 | 7.8725
R=3.5mm | 2.1398 | 3.1265 | 4.2171 | 5.3535 | 7.7865 | 10.0835 | 14.2018 | 17.5692 | 20.5376
Copper vs. molybdenum coated DUT
The maximum Q-factor percentage difference is obtained
with a minimum distance between the DUT and the sapphire
sapphire
radius
Δh

## Slide 10: Resonant structure methodology
The sapphire with
larger radius (3.5 mm)
will be used, because
of its higher sensitivity
in EM characterization
of coating materials
(LESS)
Expected LESS