## Slide 1
15
"Characterization of materials and realization of components in the GHz and THz domain"
Can Koral
13 September 2021
Meeting on “radio frequency activities in the INFN”

## Slide 2
Spectral Fingerprint The photon energy of the THz wave largely coincides with energy levels corresponding to low-frequency motions
Transparency of Materials Nonpolar Materials which are opaque to visible and near-infrared waves, are transparent in the THz range.
Strong Absorption by Polar molecules
(the hydration levels, Icing effects ….)
Time and Spatial Resolution THz spectroscopy permits time-resolved investigations with high sensitivity
Noninvasive and Nonionizing Properties The low-energy photons of THz radiation are suitable for the noninvasive characterization in vivo real-time diagnosis without causing ionization damage.
mm-wave technologies
Frequency:
0.1 THz10 THz 30THz
Wavelength:
3 mm 30 µ m 10 µm
Energy:
0.41meV 41 meV 124meV
Wavenumber:
3.3 cm-1333 cm-1 1000 cm-1
C.Koral,PhD/THz Devices & Characterization/13-09-2021

## Slide 3
The time dependency of the incoming THz electric field is measured by sampling it by a very short optical pulse.
THz Time Domain Spectroscopy
C.Koral,PhD/THz Devices & Characterization/13-09-2021

## Slide 4
THz-Time Domain Spectroscopy
(Transmission mode and Reflection Mode)
THz-Ellipsometry
(Angular Reflection measurements)
THz Fast Mapping and Imaging
Material characterization (dielectrics, doped semiconductors, phase transition and 2D materials, liquid crystals from cryogenic (2 K) to high (700 K) temperatures.
Metamaterial-based and plasmonic devices design and testing
THz Wave-Guide Spectroscopy
C.Koral,PhD/THz Devices & Characterization/13-09-2021

## Slide 5
The THz WAVE-GUIDE SPECTROSCOPY as a novel approach for the evaluation of the surface impedance of coatings in accelerator beam pipes in the sub-THz range.
The electromagnetic characterization of coating materials in the Sub-THz frequency for particle accelerators range used in the accelerators and pipe lines :
Materials for the improvement of ultra-high vacuum(NEG / non evaporable getters)
The reduction of the secondary electron yield(a-C / amorphous carbon)
C.Koral,PhD/THz Devices & Characterization/13-09-2021

## Slide 6: Analytical evaluations (In-house retrieval method)
Waveguide of length lg (TE1,1 mode)
+
pyramidal transitions of length lt (TE1,0 TE0,1 modes)
C.Koral,PhD/THz Devices & Characterization/13-09-2021

## Slide 7: NEG coatings

## Slide 8: Measurement results on Amorphous Carbon Coatings
3 μm of
Amorphous Carbon
on copper bulk
Mechanical stress a-C coating on Cu slab
C.Koral,PhD/THz Devices & Characterization/13-09-2021

## Slide 9
Key Novelty:
Experimentation using electron bunch triggered radiation is that the intense THz emission becomes self-synchronized with all radiation types (from IR to X-ray) emitted with the same electron bunch.
A facile combination of
THz/X-ray pump/probe experiments.
The use of coherent THz pulses for electron beam diagnostics and to reconstruct the charge distribution of the electron bunch.
Accelerator Based
THz Generation

## Slide 10
The BriXSino Project
The BriXSino project exhibits strong potentiality as user facility for both X-rays and THz radiation.
TU (Terahertz Undulator) and IO (Infrared Oscillator) at BriXSino.
Developed by INFN -Milan in collaboration with Italian National Institutions and Universities, and will be located at LASA (Laboratori Acceleratori e Superconduttività Applicata).
C.Koral,PhD/THz Devices & Characterization/13-09-2021

## Slide 11
THz/GHz optics and devices(Devices for THz/GHz beam manipulation)
The technology of active wave-plates based on liquid crystals and operating in the visible/near-infrared
are shifted at THz/GHz frequencies
The polarization of light is an important parameter
entering in many applications.
In the THz range also a simple circular polarization is difficult to obtain due to the lack of efficient wave-plates
C.Koral,PhD/THz Devices & Characterization/13-09-2021

## Slide 12
+Maik Scheller, Christian Jördens, and Martin Koch, "Terahertz form birefringence," Opt. Express 18, 10137-10142 (2010)
2nd order EMT which describes
the effective optical material parameters:
TERAHERTZ FORM BIREFRINGENCE

## Slide 13
3D Printed THz & GHz Wave Plates
C.Koral,PhD/THz Devices & Characterization/13-09-2021

## Slide 14
3D Printed Segmented Wave-Plate (THz &GHz )Design consisting of several specially oriented half-wave plates allows getting radiation with radial and azimuthal polarization from linearly polarized one.
C.Koral,PhD/THz Devices & Characterization/13-09-2021

## Slide 15
3D Printed Segmented Wave-Plate (THz &GHz )Design consisting of several specially oriented half-wave plates allows getting radiation with radial and azimuthal polarization from linearly polarized one.
AZIMUTHAL
(Clock-Wise)
RADIAL (In-Ward)
AZIMUTHAL (Counter-Clock-Wise)
RADIAL(Out-Ward)

## Slide 16
15
"Characterization of materials and realization of components in the GHz and THz domain"
Can Koral
13 September 2021
Meeting on “radio frequency activities in the INFN”