## Slide 1: Morphology effects on desorption processes at cryogenic temperatures
e-cloud’22 workshop
25th – 28th September 2022
Luisa Spallino, LNF-INFN

## Slide 2: Outline
Introduction
Morphology effects on thermal desorption
Morphology effects on electron stimulated desorption: a case of study
Summary and open issues

## Slide 3: Introduction
Extremely Low Pressure (<10-11 mbar) inside beam-pipe
Extremely Low Temperature (40 K /60 K for FCC-hh beam screen)
Advanced technological solutions to match e-cloud, impedance, ...etc
requirements must be compliant with the required cryogenic vacuum
Conditions inside accelerators (HL-LHC,FCC, EIC)

## Slide 4: Introduction
FCC-hh BS
R. Valizadeh et al. , Appl. Surf. Sci. (2017)
LASE-Cu
Engineering the surface morphology
to reduce SEY
(Laser Ablation Surface Engineering -LASE)
LASE-Cu to mitigate e-cloud effects
Low SEY is a
morphological effect

## Slide 5: Introduction
At cryogenic temperature, not only intrinsic properties of surface but also the effects of:
Temperature transients
Photons, Electrons and Ions-surface interaction
Gas Desorption  Pressure transients

## Slide 6: Introduction
At cryogenic temperature, not only intrinsic properties of surface but also the effects of:
Temperature transients
Photons, Electrons and Ions-surface interaction
Gas Desorption  Pressure transients
Independently on the substrate treatment, vacuum stability has to be granted!

## Slide 7: Morphology effects on thermal desorption
LASE-Cu
TPD from Cu and LASE-Cu for temperature induced vacuum transient study: Ar
L. Spallino et al. Appl. Phys. Lett. (2019)
Single TPD peak at ~30 K corresponding to the desorption of a condensed thick Ar layer
Desorption temperature determined by the weak Ar-Ar van der Waals interaction energies
TPD peak at ~30 K corresponding to the desorption of a condensed thick Ar layer together with a broad TPD profiles, whose peak temperatures and widths depend on the Ar dose

## Slide 8: Morphology effects on thermal desorption
LASE-Cu
TPD from Cu and LASE-Cu for temperature induced vacuum transient study: CH4
L. Spallino, J. Vac. Sci. Technol. B (2020); L. Spallino et al., Phys. Rev. Accel. Beams (2020)
TPD from Cu and LASE-Cu for temperature induced vacuum transient study: CO
TPD characteristics of LASE-Cu independent from gas species and determined by sponge-like structural features

## Slide 9: Morphology effects on thermal desorption
LASE-Cu
TPD of 100 L H2 dosed on poly-Cu and LASE-Cu samples held at T~15-18 K
L. Spallino et al., Phys. Rev. Accel. Beams (2020)
No TPD signal should be observed by considering the H2 vapor suture pressure curve!!!
The wide distribution of high energy adsorption sites within the inner pore is responsible for the H2 TPD signal from LASE-Cu sample
Conceptually identical to Ar, CH4 and CO results

## Slide 10: Morphology effects on thermal desorption
LASE-Cu
TPD from LASE-Cu for temperature induced vacuum transient study
Impact on the working conditions
~500 h beam lifetime
Working temperature range foreseen for FCC-hh
L. Spallino et al. Appl. Phys. Lett. (2019); L. Spallino, J. Vac. Sci. Technol. B (2020); L. Spallino et al., Phys. Rev. Accel. Beams (2020)

## Slide 11: Morphology effects on thermal desorption
LASE-Cu
TPD from LASE-Cu for temperature induced vacuum transient study
Impact on the working conditions
~500 h beam lifetime
Working temperature range foreseen for FCC-hh
Further studies on dynamic vacuum behaviour at cryogenic temperature are necessary to completely validate/optimize LASE-Cu
L. Spallino et al. Appl. Phys. Lett. (2019); L. Spallino, J. Vac. Sci. Technol. B (2020); L. Spallino et al., Phys. Rev. Accel. Beams (2020)

## Slide 12: Does the morphology affect electron desorption?
proton bunches
p
e
Beam ionizes residual gas
Electrons (also coming from e-cloud) impact the beampipe
e
e
Electron Stimulated Desorption (ESD)

## Slide 13: Morphology effects on electron stimulated desorption: a case of study
Comparative study of ESD at 500 eV from different Ar doses delivered on flat poly-Cu and LASE-Cu samples
poly-Cu
LASE-Cu

## Slide 14: Experimental set-up at LNF-INFN
Temperature Programmed Desorption (TPD) and Residual Gas Analysis (RGA) measurements
Equipment : QMS (Hiden HAL 101 Pic)
Secondary Electron Yield (SEY) measurements
Equipment : Electron gun, Faraday cup
LNF-cryogenic manipulator
Sample at 15-300 K
Ultra high vacuum systems
main chamber
preparation
chamber
fast-entry lock
X-Ray Photoelectric Spectroscopy (XPS) Equipment : Omicron EAC125 electron analyzer, Mg Kα source (hν = 1253.6 eV)

## Slide 15: Electron stimulated desorption yield (h)
e
Number of desorbed species
Number of incident electrons
LASE-Cu sample
high sensitivity RGA measurements
complex calibration procedures
The direct determination of η is a non-trivial task, requiring

## Slide 16: Morphology effects on Ar adsorption
Electrons, both primary and secondary, are “trapped” by the LASE-Cu highly porous structure
Porous morphological effects

## Slide 17: Morphology effects on Ar adsorption
Electrons, both primary and secondary, are “trapped” by the LASE-Cu highly porous structure
Porous morphological effects
Sub-micrometric structural features
High specific surface accessible to Ar atoms, also inside pores
LASE-Cu sample
SEY contribution of Ar layer adsorbed on the top-most surface

## Slide 18: Morphology effects on ESD
4 L
8 L
40 L
On increasing
Ar dose
M. Angelucci, Il Nuovo Cimento 45 C, 198 (2022)
h from Cu is always higher than h from LASE-Cu
The higher the Ar coverage, the higher is h

## Slide 19: Morphology effects on ESD
Morphological effects of surfaces
LASE-Cu have much greater physical area than that of untreated surfaces where to host gas
One should expect that porous surface adsorbs (desorbs) more than flat substrates
ESD is a surface process mainly governed by the transport of secondary electrons
R. Dupuy et al. , J. Appl. Phys. (2020)
Electrons, both primary and secondary, are “trapped” by the highly porous structure thus leading to a very low LASE-Cu SEY
The lower the SEY, the lower ESD

## Slide 20
A. N. Hannah et al. , Vacuum (2021)
From LASE-Cu the desorption is less efficient, but does it last longer?
The difference in h decreases on increasing the electron dose (scrubbing)
Useful information for vacuum analysis during operation

## Slide 21: Summary and open issues
Porous materials show high pumping capacity
Electron Desorption Yield of porous materials is lower than the one observed from the same dose of gas condensed on the flat counterpart
The Electron Desorption Yield depends on SEY
All these aspects are advantageous for the use of such materials in future accelerators beam screens
Temperature Programmed Desorption shows different desorption temperature range
Further studies are mandatory testing gas species usually composing residual vacuum in accelerators

## Slide 22: Thank you for your attention!