## Slide 1: SEY dependence on overlayer thickness and its relevance for e-cloud studies at various temperatures
M. Angelucci
Ecloud’22 – La Biodola Bay (26-28/09/22)

## Slide 2: Outline
Introduction
Secondary Electron Yield of different surfaces
Structural/Morphological changes
Chemical changes (Cu and SS)
Thickness dependence – Carbon
Cryogenic surface: contamination and SEY changes

## Slide 3: Introduction
sawtooth
surface finishing
LASE-Cu
cooling channels
perforated baffles
FCC-hh BS
LHC BS
Low temperature
(LHC beam screen T~5-20 K)
UHV (P <10-11 mbar)
Different Surface characteristics
    Secondary Electron Emission can drive an avalanche multiplication effect filling the beam chamber with an electron cloud
    Proton bunch
    e- is emitted (photoelectric effect)
    Secondary Electron Emission
LHC
e- cloud phenomenon

## Slide 4: Introduction
Electron mean free path up to ~10 nm
(few monolayers)
Three-step process:
 Production of SE at a depth z
 Transport of the SE toward the surface
 Emission of SE across the surface barrier
Secondary Electron Emission

## Slide 5: Introduction
R. Cimino & T. Demma, Int. J. Mod. Phys. A (2014)
Surface conditions
influence SEY measurements
Energy Distribution Curve (EDC) of the electrons produced by a 112 eV primary energy electron beam impinging on a Cu technical surface
Three-step process:
 Production of SE at a depth z
 Transport of the SE toward the surface
 Emission of SE across the surface barrier
Secondary Electron Emission

## Slide 6
A
B
D
D
SE
R
SE
R
SE
R
SE
R
Energy Distribution Curves at different Primary Energy
SEY of materials
Cimino et al., PRL 93 (2004)

## Slide 7
A
B
D
D
SE
R
SE
R
SE
R
SE
R
Energy Distribution Curves at different Primary Energy
SEY of materials
Cimino et al., PRL 93 (2004)

## Slide 8
A
B
D
D
SE
R
SE
R
SE
R
SE
R
Cimino et al., PRL 93 (2004)
Energy Distribution Curves at different Primary Energy
SEY of materials
Reflected electron component
Low-Energy Range
Sensitive to surface variation

## Slide 9
A
B
D
D
SE
R
SE
R
SE
R
SE
R
Cimino et al., PRL 93 (2004)
Energy Distribution Curves at different Primary Energy
SEY of materials
Total amount of emitted secondary electrons
High-Energy Range
Sensitive to thick layer

## Slide 10
By normalizing to 1 spectra taken with Ep - Ebias < Wf and than plotting together all EDC of clean oriented HOPG
SEY of materials
HOPG

## Slide 11
SEY of materials
SEY
Secondaries
Rediffused
Backscattered
Secondaries
Rediffused
Backscattered
SEY
HOPG

## Slide 12
Differences between “As Received” and Atomically Clean Metals
High-Energy SEY dependence
Contaminants (as received)
Materials (clean)
Ag
Cu
Au
General High SEY
Lower SEY
Characteristic Curves
SEY of materials
AIP Advances 7, 115203 (2017)

## Slide 13
Differences between “As Received” and Atomically Clean Metals
in the Low-Energy range
Evaluation of Work Function
Ag
Cu
Au
General Behaviour
in all clean metals
SEY of materials
AIP Advances 7, 115203 (2017)

## Slide 14
Laser ablation and conditioning
R. Valizadeh et al. , Appl. Phys. Lett. (2014)
Engineering the surface morphology
SEY variation
Morphological
Changes
Modification of surface
R. Cimino et al. PR ST (2015)

## Slide 15
SEY variation
Structural modification
Ar+ Sputtering
Modification of surface
L.A. Gonzalez et al., AIP Adv. 6 (2016) 095117
HOPG

## Slide 16
R. Larciprete et al., Appl. Surf. Sci. (2015)
Modification of surface
Amorphous C-coating
SEY variation
Chemical modification
ultra high vacuum RF magnetron sputtering 50W p(Ar) 6x10-2 mbar
a-C (~ 20 nm)/poly Cu

## Slide 17
R. Larciprete et al., Appl. Surf. Sci. (2015)
Modification of surface
Amorphous C-coating
Thermal graphitization of thin amorphous C layers deposited by magnetron sputtering on Cu substrates
SEY variation
Chemical modification

## Slide 18
SEY Variation
R. Cimino et al., Phys. Rev. Lett. (2012)
e-
sp3  sp2 carbon surface contamination conversion
SEY depends on the surface chemical state
Copper
Chemical variation induced by electron irradiation

## Slide 19
max
SEY Variation
ST. ST.
Chemical variation induced by electron irradiation

## Slide 20
max
SEY Variation
ST. ST.
Chemical variation induced by electron irradiation

## Slide 21
SEY Variation
ST. ST.
Chemical variation induced by electron irradiation

## Slide 22
After Ar
Sputtering
After
10-1 C/mm2
After
1 C/mm2
HOPG Graphite reference
The As received St. St. shows some C in the Bulk + The typical C in sp3 form.
The Semi scrubbed St. St. shows some C in the bulk + most C already in sp2 form.
The fully scrubbed St. St. shows some C in the bulk+ most C already in sp2 form. Identical to the Semi scrubbed
The St. St. shows that C is in the Bulk.
The HOPG Graphite shows the C in sp2 form as a reference.
SEY Variation
ST. ST.
Chemical variation induced by electron irradiation

## Slide 23
ST. St.
C
ST. St.
C
dmax=1.14
dmax=1.55
dmax=1.05
SEY
ST. St.
C
dmax=1.3
Three-step process:
Production of SE at a depth z
Transport of the SE toward the surface
Emission of SE across the surface barrier
SEY electrons are produced within a semi-sphere of about few nm radius
Secondary Electron emission
St. St.
Chemical variation induced by electron irradiation
SEY Variation

## Slide 24
M. Angelucci et. al; Phys. Rev. Research Rapid comm. 2, 032030(R) (2020)
Secondary Electron Yield Reduction
Carbon minimum thickness
Cu KLL
e-beam evaporation from graphite rod
XPS analysis
(Coverage Estimation)
SEY measurements
Minimum thickness evaluation

## Slide 25
Cu KLL
M. Angelucci et. al; Phys. Rev. Research Rapid comm. 2, 032030(R) (2020)
Conversion of deposition time to Carbon Coverage (nm)
Secondary Electron Yield Reduction
Carbon minimum thickness

## Slide 26
M. Angelucci et. al; Phys. Rev. Research Rapid comm. 2, 032030(R) (2020)
Secondary Electron Yield Reduction
Carbon minimum thickness

## Slide 27
M. Angelucci et. al; Phys. Rev. Research Rapid comm. 2, 032030(R) (2020)
Secondary Electron Yield Reduction
Carbon minimum thickness
Low coverage (<6nm): Strong SEY modification

## Slide 28
M. Angelucci et. al; Phys. Rev. Research Rapid comm. 2, 032030(R) (2020)
Secondary Electron Yield Reduction
Carbon minimum thickness
High coverage (>6nm): Stable dmax <1
Low variation in the low ( <50 eV) and high (>500 eV) regions

## Slide 29
Induced SEY variation by external contaminants
Sub-Monolayer Contaminations
Strong Variations
(SEY @10eV from 0.05 to 0.25)
New characteristic structures
Low-Energy Range
Low Variations
(SEY Max from 1.4 to 1.3)
Variation Dependence on Gas contaminant
High-Energy Range
Secondary Electron Yield Variations
at Cryogenic Temperatures
AIP Advances 7, 115203 (2017)

## Slide 30
Sub-Monolayer Contaminations
High-Energy Range
Strong Variations
(SEY @10eV from 0.05 to 0.25)
New characteristic structures
Low-Energy Range
Low Variations
(SEY Max from 1.4 to 1.3)
Variation Dependence on Gas contaminant (?)
Induced SEY variation by external contaminants
Secondary Electron Yield Variations
at Cryogenic Temperatures
AIP Advances 7, 115203 (2017)

## Slide 31
Adsorption process of Carbon Monoxide on Cu sample at 10K
General behaviour
Low-Energy
Evolution
Secondary Electron Yield Variations
at Cryogenic Temperatures
SEY @ 900 eV decreases during adsorption from 1.4 to 1.1
Formation of CO Thick Film (TF)
Characteristic peak of TF at 65 eV
Characteristic peaks at different low energies
Formation of CO Single Layer (SL)

## Slide 32
Not published data
H2O on Cu
H2O on Graphite HOPG
Ar on Cu
L. Spallino et al., Phys. Rev. Accel. Beams (2020)
SEY of gas condensed on a cryogenic surface
Induced SEY variation by external contaminants
Secondary Electron Yield Variations
at Cryogenic Temperatures

## Slide 33: Conclusions
Each system has a different SEY depending on the chemistry and morphology
Overlayers plays a crucial role
The overlayer thickness can induce significant variation in SEY
Contaminant Layer thickness could be responsible of the different sectors behaviour in accelerators

## Slide 34: Thank you for your attention