## Slide 1
NEG As An Anti-Multipactoring Coating: Pro & Cons, Present Limitations & Possible Developments/Applications For Future Machines
Reza Valizadeh, Oleg Malyshev, Adrian Hannah, Sihui Wang,
ASTeC Daresbury Laboratory
Patrick Krkotic, Montse Pont, J.M O’Callaghan
ALBA Synchrotron
Gao-Yu Hsiung
Taiwan Light source

## Slide 2: Outline
Introduction
Non Evaporable Getter As Low SEY Thin Film
NEG Thin Film Pumping Performance
NEG ESD Measurement
Conducting NEG Coating
PSD Measurement of Various NEG Combination

## Slide 3: What is Multipactor
Multipactor is a phenomenon where electron population grows exponentially,
In a positive charge particle accelerator this induces electron cloud.
Ecloud causes beam instability, beam losses, emittance growth, reduction in beam life time, or heat loads on cryogenic vacuum chamber

## Slide 4: Mitigation method
Low SEY Material (Cladding)
Low SEY coating(single/multiple step)
Grooved Surfaces (coated /uncoated)
Special shape of vacuum Chamber
An antichamber allows reducing PEY
Normal
coating

## Slide 5
Non Evaporable Getter As Low SEY Thin Film

## Slide 6: What is NEG?
NEG coating is thin film of one or several reactive metals or alloy which capture gases, such as H2O, CO, CO2, O2 and N2. by a chemical reaction on their active surface.
The reaction generates carbides/oxides/nitrides on the film getter
surface: Gases are permanently removed from the vacuum
system.
Hydrogen does not react to form a chemical compound but
dissolves in the bulk of the getter forming a solid solution.
A getter does not pump noble gases as they do not chemically
react.

## Slide 7: Deposition methods
Commonly used planar magnetron deposition
Cylindrical magnetron deposition for vacuum chambers
Not suitable for coating inside accelerator’s vacuum chambers

## Slide 8: NEG in different structure and layered structure
As Nitride layer it act as a true hydrogen barrier
In a dense structure, it acts as barrier (reservoir) between a vacuum chamber material and an inner vacuum hence even in non-activated state it provides lower residual gas pressure.
In a columnar structure, it has a large surface area, hence, a fully coated vacuum chamber has large distributed pumping speed, the benefit of this is essential for the narrow vessels with a limited vacuum conductance.
In activated state, the NEG coating has low secondary electron (SEY) yield that helps to supress electron multipacting and electron cloud in high intensity accelerators.

## Slide 9: Single Element NEG
Ti
Zr
V
Hf

## Slide 10: Binary and Ternary Alloy NEG
Ti-Zr-V alloy wire
Ti-Zr-V twisted wire
Ti-V
Ti-Zr
Zr-V

## Slide 11: Quaternary TiZrVHf from Alloy rod

## Slide 12
NEG Thin Film Pumping Performance

## Slide 13: Pumping properties measurement method
Pumping properties of NEG coating measured:
a pressure ratio P2/P1 during H2 and CO injection
  to obtain sticking probability 
amount of injected gas
  to obtain sorption capacity
The TPMC results for a pressure ratio P2/P1 as a function of sticking probability α for a tube with d = 38 mm and L = 0.5 m

## Slide 14: Pumping performance of Various Studied NEG
Ti-Zr-Hf-V performed the best
Activated at 150-160 °C for a columnar film
CO  0.4, CO2  0.6, H2  0.03
Hf-Zr-V, Ti-Zr-Hf, Ti-Hf-V and Zr are comparable while Ti-Zr-V is lower
Zr-V is the best binary alloy (has the lowest activation temperature)

## Slide 15: Pumping performance of Columnar vs Dense
Columnar Zr is activated at 160 °C, partial activation at 140 °C activated for 20 hours
R. Sirvinskaite et al. Vacuum 179, 109510 (2020) .

## Slide 16: Effect of activation duration and substrate
The NEG coating activation is usually performed at chosen temperature for 24 hrs.
The activation temperature can be reduced (within some limits) by increasing the duration of heating.
Copper tube with dual dense/columnar NEG
Aluminium tube with dense NEG
Two samples (tubes with d= 36-38 mm, L = 0.5-m)
coated with TiZrV from an alloy target
NEG activations:
  To 140, 160 and 180 C for 24 h
  To 140, 160 and 180 C for 168 h
Increasing the duration of NEG activation at 160 °C can increase both sticking probability and sorption capacity, and can potentially reach the same pumping efficiency as a NEG coating activated to 180 °C for 24 hrs
E.A. Marshall, et al. In Proc. of IPAC'22, p. 1854.

## Slide 17
NEG ESD Measurement

## Slide 18: ESD measurement method
A layout for ESD measurements:
a tubular sample with vacuum conductance Us,
Partial pressure measurements: P1 and pressure P2,
known vacuum conductance U2 and pumping speed S (or effective pumping speed Seff).
The ESD yield, M, is defined as a number of desorbed gas molecules per incident electron:
For non-pumping sample ( = 0):
For pumping sample ( > 0):

## Slide 19: ESD Measurement of TiZrVHf on SS
Electron stimulated desorption (ESD) measurements are quite simple and lower cost than on SR beamline
ESD results allows to compare behaviour of various NEG films at the conditions similar to particle accelerators
H2 ESD is much lower than for 316 LN
Distributed pumping
  => low pressure

## Slide 20: ESD from Zr Coating
ESD results for Zr are comparable with Ti-Zr-V NEG coating
Increasing activation temperature may result in higher ESD!
R. Sirvinskaite et al. Vacuum 179, 109510 (2020)

## Slide 21
NEG coating RF Surface Resistance
Notes: Как я говорил вначале, мв развиваем Новые технологии. Например, мы занимаемся Оптимизацией неиспаряемых сорбирующих плёнок для вакуумных камер ускорителей

## Slide 22: RF Surface Resistance
Beam image current on the beam chamber surface has an RF surface resistance
NEG coating can significantly contribute to the RF surface resistance
  This could one of the main limitation for future machines with
    a small aperture
    a short bunch length
  NEG coating is the only solution for meeting vacuum specification in the narrow beam vacuum chamber with d  25 мм
    Developing of NEG coating with a lower RF surface resistance is required
RF surface resistance (Rs) of NEG film as a function of RF frquency (f)
O.B. Malyshev, Proc. ECLOUD’18, p. 217 (2018).
O.B. Malyshev, et al. Nucl. Instrum. Methods Phys. Res., A 844, 99-107 (2017)

## Slide 23: RF Surface Resistance Measurement at 9 GHz
Bottom | Top | Resonance [GHz] | Unloaded Q | Surface Resistance Top Plate [m
Copper | Copper | 9.05 | 2994 | 26.25
Dense NEG 1 µm | TiZrV/ Cu | 9.06 | 2851 | 30.43
Dense NEG 6 µm | TiZrV/Cu | 9.05 | 1295 | 135.80
Dense NEG 18 µm | TiZrV/Cu | 9.02 | 853 | 235.83
Columnar NEG 18 µm | TiZrV/Cu | 9.05 | 672 | 314.77
Bottom | Top | Resonance [GHz] | Unloaded Q | 
Copper | Copper | 9.05 | 2994 | 26.25
Dense NEG 1 µm | TiZrV/ Cu | 9.06 | 2851 | 30.43
Dense NEG 6 µm | TiZrV/Cu | 9.05 | 1295 | 135.80
Dense NEG 18 µm | TiZrV/Cu | 9.02 | 853 | 235.83
Columnar NEG 18 µm | TiZrV/Cu | 9.05 | 672 | 314.77

## Slide 24
Conducting NEG Coating
Notes: Как я говорил вначале, мв развиваем Новые технологии. Например, мы занимаемся Оптимизацией неиспаряемых сорбирующих плёнок для вакуумных камер ускорителей

## Slide 25: Pumping properties of conductive NEG coating
NEG films were deposited from a twisted Ti-Zr-Hf-V wire target with and without copper wire:
Sample 1 – no Cu, columnar, Sample 2 – no Cu, dense, Sample 3 – 2 mm Cu wire
RF surface resistance of NEG coating can be reduced by adding conductive metal
but at the cost of reduced pumping properties and higher activation temperature
Chart: Ta (°C)
| 140 | 150 | 160 | 180 | 200 | 220 | 250 | 300
NEG col H2 | 0.011 | 0.015 | 0.017 | 0.019 | 0.025 | 0.0251 | 0.028 | 0.04
NEG col CO | 0.0057 | 0.057 | 0.085 | 0.15 | 0.153 | 0.155 | 0.173 | 0.175
NEG col CO2 | 0.076 | 0.195 | 0.22 | 0.19 | 0.2 | 0.23 | 0.24
NEG den H2 | 0.0007 | 0.0006 | 0.00045 | 0.000575 | 0.0012
NEG den CO | 0.00058 | 0.0009 | 0.012 | 0.024 | 0.05
NEG den CO2 | 0.0033 | 0.005 | 0.017 | 0.04 | 0.087
Cu-NEG H2 | 0.002 | 0.0013 | 0.00155 | 0.00165
Cu-NEG CO | 0.0003 | 0.0005 | 0.0075 | 0.015 | 0.05 | 0.08 | 0.085
Cu-NEG CO2 | 0.15 | 0.2 | 0.3 | 0.33
Chart: Ta (°C)
| 140 | 150 | 160 | 180 | 200 | 220 | 250 | 300
NEG col CO | 2.7262e+13 | 7.685e+13 | 2.4269e+15 | 2.346e+15 | 2.0871e+15 | 2932447935244242 | 4.2874e+15 | 4449231350025747
NEG col CO2 | 6.4716e+14 | 4691916696390787 | 4449231350025747 | 4408783792298240 | 4570574023208268
NEG den CO | 3.438e+13 | 8.7771e+13
NEG den CO2 | 7.2401e+12 | 4.4492e+13 | 1.1366e+14
Cu-NEG CO | 1.2072e+12 | 1.8035e+13 | 4.2251e+13 | 1.2072e+14
Cu-NEG CO2 | 1.0985e+14 | 1.1033e+14 | 1.2554e+14 | 2.0473e+14

## Slide 26: SEY and Sheet Resistance of TiZrVHfCu
 | Rs (Ω/□) for NEG | Rs (Ω/□) for NEG +1 mm Cu | Rs (Ω/□) for NEG +2mm Cu
Si/NEG film | - | 7.00 | 1.34
Glass/NEG film | 15.27 | 7.07 | 2.41
Chart: SEY of 1mm Cu + NEG
| 982 | 982 | 932 | 882 | 832 | 782 | 732 | 682 | 632 | 582 | 532 | 482 | 432 | 382 | 357 | 332 | 307 | 282 | 257 | 232 | 207 | 182 | 157 | 132 | 107 | 82 | 62
As received | 1.4139 | 1.4084 | 1.4144 | 1.4274 | 1.4408 | 1.4574 | 1.4776 | 1.5004 | 1.5234 | 1.5508 | 1.5762 | 1.6067 | 1.6366 | 1.6685 | 1.6823 | 1.6961 | 1.7031 | 1.7141 | 1.7157 | 1.7093 | 1.7367 | 1.7114 | 1.7117 | 1.6398 | 1.5535 | 1.42 | 1.3
After heating | 0.99746 | 1.0058 | 1.0143 | 1.0228 | 1.0315 | 1.0404 | 1.0494 | 1.0582 | 1.0673 | 1.0759 | 1.0843 | 1.0914 | 1.0972 | 1.0991 | 1.1002 | 1.0999 | 1.0979 | 1.0929 | 1.084 | 1.0722 | 1.0525 | 1.0349 | 0.99315 | 0.9351 | 0.86572 | 0.78832
Chart: SEY of 2mm Cu + NEG
| 982 | 932 | 882 | 832 | 782 | 732 | 682 | 632 | 582 | 532 | 482 | 432 | 382 | 332 | 307 | 357 | 282 | 257 | 232 | 207 | 182 | 157 | 132 | 107 | 82 | 62
As reveived | 1.145 | 1.1539 | 1.1653 | 1.1774 | 1.1918 | 1.2074 | 1.2243 | 1.2441 | 1.2652 | 1.2851 | 1.3104 | 1.3369 | 1.3631 | 1.3875 | 1.3976 | 1.3755 | 1.4047 | 1.4091 | 1.4078 | 1.4021 | 1.3818 | 1.375 | 1.3221 | 1.2512 | 1.1494 | 1.0503
After heating | 0.91515 | 0.92537 | 0.93515 | 0.94514 | 0.95508 | 0.96533 | 0.97598 | 0.98737 | 0.99883 | 1.011 | 1.0233 | 1.035 | 1.0453 | 1.0495 | 1.0528 | 1.0547 | 1.0547 | 1.0506 | 1.0423 | 1.0312 | 1.0113 | 0.99193 | 0.9492 | 0.89153 | 0.82078 | 0.74377

## Slide 27: Activation of TiZrVAg and RF Surface Resistance

## Slide 28
PSD measurement of Various NEG combination
Notes: Как я говорил вначале, мв развиваем Новые технологии. Например, мы занимаемся Оптимизацией неиспаряемых сорбирующих плёнок для вакуумных камер ускорителей

## Slide 29: Old PSD data
V.V. Anashin, et al. Vacuum 75, 155 (2004).
P. Chiggiato, R. Kersevan, Vacuum 60, 67 (2001).
New PSD data needed for each type of NEG coating:
For various film compositions:
  Ti-Zr-Hf-V, Zr
  NEG + conductive metals
For dense vs columnar NEG film
For different activation temperatures
For different film thicknesses
For NEG films on vacuum fired vacuum chambers
For activation by SR
Etc.

## Slide 30: TLS BL19B Beamline Parameters
SR-Light in the NEG tube
Reducer Tube : Offset 3.5 mm NEG Tube (0.5 m)
Reducer Flange : Tilt 3º
Incident Angle: 3°
Photon Beam Size (W×H) = 23×5 mm

## Slide 31: PSD-Yield vs Photon Dose
η = 𝐷𝛼
Label | Types of NEG-coating | Remarks
SS-1 (NEG) | Conductive NEG (TiZrVAg) - Columnar | NEG Activation (>180 ℃, 24 h) * for decreasing the surface resistance
SS-2 (NEG) | Triple NEG (TiZrVN) - Columnar/Dense/Nitride | Baking (<150 ℃, 24 h) for short- dose (< 1 Ah) exposure NEG Activation (>180 ℃, 24 h) for continuously long exposure
SS-3 (NEG) | Dual NEG (TiZrV) - Columnar/Dense | Baking (80 ℃, 24 h) for short-dose (< 1 Ah) exposure NEG Activation (>180 ℃, 24 h) for continuously long exposure
AL-4 (NEG) | Dual NEG (TiZrV) - Columnar/Dense | NEG Activation (<180 ℃, 24 h) NEG Activation (2) (>180 ℃, 24 h)

## Slide 32: PSD-Yield RGA vs. Beam Dose(Ah)
H2
CH3+
CO
C2H2+
CO2
H2O
84Kr
SS-1 (Cond-NEG)

## Slide 33: Summary
Non-evaporable getter coatings is not a single solution, it is a family of coating with different
  composition, structure and morphology.
NEG coating could be optimised to application in balance between:
  Desorption (PSD, ESD, ISD)
  Pumping properties (, sorption capacity)
  Activation temperature and its duration
  E-cloud mitigation (PEY and SEY)
  Beam impedance (RF surface resistance Rs)
The new PSD and ESD results of various NEG coatings provide new data and more confidence in designing vacuum systems for future particle accelerator

## Slide 34
Thank You