## Slide 1: Impedance characterization of laser structured and coated surfaces
Istituto Nazionale di Fisica Nucleare
The Italian National Institute for Nuclear Physics
28/09/2022
Andrea Passarelli

## Slide 2
Laser structured and coated surfaces
Sample characterization
To avoid undesirable effects on the beam and maximize machine performance
Laser Induced Periodic Surface Structures (LIPSS): e-cloud
Non-Evaporable Getter (NEG): ultrahigh vacuum and e-cloud
Amorphous Carbon (a‐C): e-cloud
SEM
AFM
Raman
XPS
Functional characterization
Morphological
Chemical
Electromagnetic
SEY = Iout/Iin
Electromagnetic characterization in sub-THz region

## Slide 3: CERN and Naples collaboration
Ongoing collaboration among CERN TE-VSC and INFN-Napoli, Napoli University, CNR-SPIN Salerno – Reduction of SEY through Laser Induced Periodic Surface Structures
Electromagnetic characterization (INFN-Napoli):
Andrea Passarelli
Maria Rosaria Masullo
TEAM COORDINATORS
Sergio Calatroni, Marcel Himmerlich (CERN), Carlo Altucci, Salvatore Amoruso, Antonello Andreone (Napoli University) and Maria Rosaria Masullo (INFN-Napoli)
Laser Surface Structuring (Napoli University):
Jijil JJ Nivas
Mohammadhassan Valadan
Meilin Hu
SEM measurements (CNR-SPIN Salerno)
Rosalba Fittipaldi
Antonio Vecchione
AFM and Raman measurements (Napoli University):
Marcella Salvatore
Stefano Luigi Oscurato
XPS analysis, SEY measurements and sample conditioning (CERN):
Sergio Calatroni
Marcel Himmerlich
Martino Rimoldi
Elena Annelie Bez

## Slide 4: Naples laser setup
Processing in vacuum
Chirped pulse amplification Yb:KGW laser source
central wavelength 1030 nm
pulse duration ≈180 fs
maximum rep. rate 200 kHz
Target is mounted on a computer controlled XY-translation stage (PP- 20, Micronix USA) working synchronously with the laser.

## Slide 5: FIRST SET
laser process for different light polarizations and sample conditions (passivation)
Sample Code | Processing conditions (large area raster scanning in ambient air) |  |  |  | 
Sample Code | Laser Polarization | Power [mW] | Energy/pulse [µJ] | Scan velocity [mm/s] | Steps between adjacent lines [µm]
OFC-circ | Circular | 150 | 30 | 1 | 75
OFC-lin | Linear | 200 | 40 | 2 | 110
POFC-circ | Circular | 150 | 30 | 1 | 75
POFC-lin | Linear | 200 | 40 | 2 | 110
Laser: Yb:KGWsystem
λ = 1030 nm
Pulse duration :180 fs
Repetition rate : 5 kHz
Beam radius on target ω0 ≈ 40 µm

## Slide 6: FIRST SET: Morphological & chemical characterization
SEM images: ripple periods from OFC-lin(a) and POFC-lin(c) are of the same order (~800 nm)
OFC and P(assivated)OFC copper samples structured with linearly (a, c) and circularly (b, d) polarized fs laser pulses.
Direction of linear polarization is red/white arrow.
Pulse energy:
Linear E = 40 μJ (Fp=1.6 J/cm2), vs= 2 mm/s, N0=200
Circular E = 30 μJ (Fp=1.2 J/cm2),vs= 1 mm/s , N0=400
AFM images: larger scale surface modulation (channels) induced by the scanning procedure.
Periodicity matches line separation in scanning process (110 µm for linear and 75 µm for circular).
Raman: minimal change to surface composition.
XPS: laser structuring removes the surface passivation.
After 9 months: increase of the hydroxide content and a further uptake of hydrocarbon surface impurities.

## Slide 7: FIRST SET: SEY measurements
SEY measurements: OFC-lin and POFC-lin reduced SEY for primary electron energies <~1000 eV.
After 9 months: SEY increased (>50 and <1000 eV)
Conditioning with a beam of 250 eV electrons.
δmax tends to decrease < 1.0 with an electron dose of ~1 × 10-3 C/mm2, compared with the maximum surface dose of ~5 × 10-3 C/mm2 during 10 days scrubbing procedure at the beginning of LHC Run 2

## Slide 8: FIRST SET: Conclusion
Parallel oriented grating structure (linear polarization) better supress the secondary electron emission with respect to randomly oriented arrangements (circular polarization);
ripples with height of ~200/300 nm and periods of ~800 nm + channels with 2µm height and 110 µm periodicity, generates a surface with higher SEY values compared to laser processing at higher pulse energy (classical LESS process);
the ripples are comparatively cleaner, with less abundance of nanoparticles compared to LESS;
conditioning tests demonstrated that the SEY<1 for an electron dose of ~1×10-3 C/mm2;
surface passivation is not mandatory.

## Slide 9: SECOND SET
laser process in different ambient, wavelength and scanning velocity (article in progress )
λ [nm] | E [µJ] |  [µm] | w0 [µm] | Fth [J/cm2] | fp [kHz] | v [mm/s] | Ambient
515 | 16 | 30 | 35 | 0.14±0.04 | 5 | 1 1.5 2 | Ambient air Vacuum (4×10-3 mbar) Nitrogen
1030 | 84 | 40 | 91 | 0.24±0.03 |  |  | 

## Slide 10: SECOND SET: Morphological characterization
SEM images: λ≈515 nm, rougher surface for air, maybe due to nanoparticles redeposition. In vacuum and nitrogen, rippled surface looks cleaner from nanoparticles redeposition, but ripples very shallow.
λ≈1030 nm, all three cases, rather free from nanoparticulate debris.
AFM images: ripples have no trend with respect to scanning speed. The depth of large scale channels increases reducing beam scanning velocity (j). Channels very shallow for irradiation in vacuum and nitrogen(i).
J. JJ Nivas, et al. Appl. Phys. A Mater. Sci. Process. 124 (2018) 198
J. JJ Nivas, et al., Appl. Surf. Sci. 417 (2017) 149–154 JJ Nivas, et al. Opt. Lett. 42 (2017) 2710

## Slide 11: SECOND SET: SEY measurements
SEY measurements: laser processing in air is most efficient to form LIPSS lower scanning velocity (high aspect ratio)
Conditioning with a beam of 250 eV electrons.
Air: δmax tends to decrease < 1.0 with an electron dose of ~1 × 10-2 C/mm2
Nitrogen: (initial δmax > 2), the SEY stabilized at 1.04 at a dose > 2×10-2 C /mm2

## Slide 12: SECOND SET: Conclusion
Better work in air ambient. In vacuum and nitrogen ambient, roughness parameter does not show any significant pattern and the same is reflected in the aspect ratio.
For decreasing the δmax we have to lower the scan velocity (increasing in the aspect ratio both of channels and ripples) as a greater number of pulses interact with the surface.
Best result: air, at 515nm, v=1mm/s, these working conditions are feasible to be implemented in long vacuum chamber. Simpler with respect into vacuum or nitrogen ambient.
Electromagnetic characterization: See next slides
FUTURE : understand the influence of ripples and channels

## Slide 13: THIRD SET
Processing in air with different lenses and scanning steps at different wavelenght and repetition rate and scanning steps in order to understand the role of surface waviness(channels) and ripples(LIPSS)

## Slide 14: THIRD SET
Spherical
Spherical

## Slide 15: THIRD SET: spherical lens
SEY curves and correlation of dmax with the repetition rate for samples Cu2 (1030 nm) and Cu9 (515 nm)
For both wavelength
Repetition Rate can be increased up to 15kHz, after which the SEY and dmax starts to rise again.
May be seen as a shielding effect due to the plasma formation over the surface during the laser processing.
Effect evident at 1030 nm.
Conditioning: dmax < 1.0 with dose of ~5 × 10-4 C/mm2

## Slide 16: THIRD SET
Spherical
Spherical
Only ripples, no channels

## Slide 17: THIRD SET: cylindrical lens
max on Cu4
Bright
Dark
SEY measurements: dark region (ripples + redeposited particles) with max lower than bright region (only ripples)
max on Cu7
Multiple pass for having more homogeneous structured region.
SEY measurements: not able to lower max
Cu14

## Slide 18: FOURTH SET
New big samples 40 mm x 40 mm pieces of CuOFE with hole pattern: large scale scanning and if holes induce problems
Foreseen a test with the beam at SPS with a bigger piece
Upgrade the experimental set-up with the new stage
6 hours
50 cm x 14 cm

## Slide 19: Electromagnetic characterization: Two different methods
Dielectric resonator
• high sensitivity
Sub-THz waveguide
• small skin-depth
LESS (Laser engineered surface structures)
• conductivity compared with copper
• small samples
NEG (Non-Evaporable Getter)
• homogeneous coating
a-C (Amorphous carbon)
• coating thickness issues

## Slide 20: First method
Dielectric resonant cavity
f [GHz]
𝝀 [mm]
5
20
100
300
1
3
15
60

## Slide 21: Resonant cavity
Modes (electric transverse)
Modes (magnetic transverse)
Cut along z
Electric field
Cut along y

## Slide 22: Dielectric resonator cavity
Electric field mode
Inserting the dielectric:
EM field confinement in a specific region of the cavity
Resonant frequency change as the properties of the dielectric change
Preference to use low loss materials ()
Without dielectric
With dielectric
Cut along y axis
On sample
Inside dielectric
Internal walls
current on sample

## Slide 23: Our methodology and characterized material
Cylindrical copper cavity
Magnetically coupled antennas
Sapphire as dielectric: e
LIPSS:
Laser Induced Periodic Surface Structure
Copper sample , with thickness
Laser structuring with parallel lines over an area of
Average processing depth of the order of

## Slide 24: Simulations: optimization of the cavity structure
Comparison
copper / molybdenum
Dielectric radius

## Slide 25: Simulation results using a calibration curve
Sensitivity in the variation of the quality factor Q is greater for the dielectric with
Losses on the sample
Losses in the rest
of the cavity
Pure copper as reference material

## Slide 26: Measurements
ROHDE& SCHWARZ ZNB 20 - Vector Analyzer 100 kHz-20 GHz

## Slide 27: Measurement results

## Slide 28: Measurement results
LIPSS conductivity value
Estimated average roughness
LIPSS: Linear polarization , in air
LIPSS surface resistance Rs = 76 mΩ
Skin depth = 1.25 μm at 15GHz

## Slide 29: Second method
Sub-THz waveguide attenuation
f [GHz]
𝝀 [mm]
5
20
100
300
1
3
15
60

## Slide 30: The proposed method
Evaluation of the signal attenuation inside a DUT with coating deposited.
Electromagnetic characterization
of coating material.

## Slide 31: The Device Under Test
Methodology advantages: 1)Homogeneous deposition 2)System reusability 3)Large area coating
Copper foil
as
reference
Coated foil
to measure
2
1
3
5
4
6

## Slide 32: Analytical evaluations
In-house retrieval method
Waveguide of length lg (TE1,1 mode) + pyramidal transitions of length lt (TE1,0 TE0,1 modes)
Reliable analytical tool

## Slide 33: Measurement system upgrade
System specifications:
Spectral Range: > 3 THz
Dynamic Range > 70 dB
Scanning Range ~ 300 ps
Spectral Resolution < 3.5 GHz
Upgrade:
> 5 THz
> 90 dB
~ 850 ps
< 1.5 GHz
More accurate guiding system manufacturing

## Slide 34: Measurement results on a-C
Two samples with 3 μm of Amorphous carbon on copper bulk
Mechanical stress a-C coating on Cu slab

## Slide 35: Thank you

## Slide 36: Skin depth
NEG 8e5 S/m
a-C 2.2e3 S/m

## Slide 37: Measurement system upgrade
σa-C = (2.2 ± 0.7) × 103 S/m
σNEG1 = (7.7 ± 1.1) × 105 S/m
σNEG2 = (4.2 ± 0.5) × 105 S/m

## Slide 38: Before LIPSS - History of LESS
ablated region
redeposited dendritic
surface layer
Ablation depth in the order of ~25 μm may be too high, its reduction could be beneficial for surface Impedance
Beam screen SEY higher compared to LESS flat samples, conditioning to SEY<1 for electron doses <10-4 C/mm2
Risk of particle release, that may be source of UFOs in the LHC giving origin to quenches
Laser Engineered Surface Structures
Nanosecond or picosecond pulse duration
100 µm
Beam screen
max.
Thanks to S. Calatroni

## Slide 39: FIRST SET: Chemical characterization
Raman spectra, minimal change to the surface composition induced on the laser irradiated area with respect to the untreated one.
XPS spectra of the Cu 2p, Cu LMM and O 1s emission.
No Cr signal: laser structuring also removes the surface passivation from POFC samples.
After 9 months: increase of the hydroxide content and a further uptake of hydrocarbon surface impurities.

## Slide 40: SECOND SET: Morphological characterization
Aspect ratio reported only for air, since the channels are shallow for vacuum and nitrogen.
For channels (a) shows a clear drop as the scanning velocity increases, evident in the case of λ≈515 nm.
For ripples (b), shows a clear drop as the scanning velocity increases, evident in the case of λ≈1030 nm.

## Slide 41: SECOND SET: Chemical characterization
Raman spectra, for vs=1.5 mm/s.
Air: peaks closely allied the reported peaks of Cu2O are identified. Broad band within 400–600 cm-1 may indicates an amorphous phase or structural defects.
Nitrogen: no considerable oxidation. Peak at 282 cm-1 could indicates CuO nanocrystals formed after the agglomeration of nanoparticles.
Vacuum: induced only a nominal change to surface composition on the laser irradiated area.
The spectra confirm the XPS data: oxide content is maximum when treatment is done in air.
XPS spectra for vs=1.5 mm/s λ = 515 nm. With 1030 nm same trends. Air: higher oxygen content at the surface, either for oxidation during laser processing or oxidization of nanoparticles back-deposited onto surface. The surface mainly composed of Cu2O and slight amount of copper hydroxides.
Vacuum: a partially metallic surface remained.
Nitrogen: reduced surface oxidation, surface hydroxyls is lower and exhibits a proportion of Cu atoms in metallic state. Incorporation of nitrogen at a level of 2-3 at.%.
Similar oxygen content as vacuum case, maybe due to oxidation upon air exposure after the laser treatment, a fraction of the surface atoms remains in metallic state.

## Slide 42: THIRD SET: Conclusion
ONLY RIPPLES
bright region with cylindrical lens
max ≈ 1.9
RIPPLES + NANOPARTICLES
dark region with cylindrical lens
max ≈ 1.6
RIPPLES + NANOPARTICLES + CHANNELS
spherical lens
max ≈ 1.2
Conditioning: dmax < 1.0 with dose of ~5 × 10-4 C/mm2
FLAT SURFACE
max ≈ 2.2

## Slide 43: SECOND SET: Electromagnetic characterization
Electric field
mode
Without dielectric
With dielectric
Cylindrical copper cavity
Magnetically coupled antennas
Sapphire as dielectric: e
Losses on the sample
Losses in the rest
of the cavity
LIPSS: , in air
LIPSS surface resistance Rs 76 mΩ
Skin depth=1.25 μm at 15GHz
Current on sample