## Slide 1
“conclusions”
“there were so many talks !” Vincent Baglin
Frank Zimmermann

## Slide 2
20 years since 1st ECLOUD Workshop ever …
10 years since 1st ECLOUD Workshop in La Biodola
R. Cimino
G. Rumolo

## Slide 3
ECLOUD’02 at CERN

## Slide 4
G. Rumolo
Ex.: PyECLOUD-PyHEADTAIL
  Coupled-bunch instability from e-cloud in LHC dipole on CERN HPC cluster (2019-20)
S. Johannesson
J.-L. Vay

## Slide 5
e-cloud in the LHC
L. Mether
L. Mether
S. Bilgen

## Slide 6
e-cloud in the LHC cont’d
L. Mether
?

## Slide 7
e-cloud incoherent effects – observations & simulations
K. Paraschou

## Slide 8
dipolar or paramagnetic flakes in the LHC?
G. Franchetti

## Slide 9
e-cloud for the HL-LHC
Optimized cryo configuration
e-cloud in quadrup.
e-cloud in dipoles
e-cloud in drifts
Impedance
Synch. rad.
10 kW/arc (~200 W/hcell)
Forecast for scrubbed machine
7 TeV, 5 x 48 b
CO
H2
N2
The HL-LHC beam screen operating temperature must be optimised
100-200 nm thick a-C coated onto 80 μm copper co-laminated beam screen of Inner Triplet
G. Iadarola
V. Baglin

## Slide 10
“Thin“ a-C coating performance at cryogenic temp
4x72 bunches at 1.3 1011 ppb, 25 ns bunch spacing
With BS at 10 K, CB at 3 K, a slight temperature increase (corresponding to ~ 50-100 mW/m) together with pressure increase is observed on the BS at 10 K, but ΔP < 10-10 mbar (H2, CO)
   this would correspond to SEYmax ~ 1.3
Room temperature calorimeter:
  609 mW/m measured on aC coating
RT and cryogenic have different heat load
But possible impact of impedance and different RRR !
V. Baglin, B. Jenninger
Preliminary results !
 More studies needed
V. Baglin
HL-LHC

## Slide 11
surface layers for HL-LHC and others
G. Sattonnay

## Slide 12
e-cloud in the EIC
 | RHIC | LHC | EIC HSR
Bunch spacing (ns) | 108 | 50* -- 25 | 10.15
Bunch charge (x1010 ppb) | 13.5 | 11.5 | 6.9
& 6 cm bunch length
lowest for all hadron machines!
+ changing horizontal offset
SEY<1.02 needed
S. Verdu-Andres

## Slide 13
e-cloud in the EIC cont’d
X. Gu
  For a good copper surface, we expect 0.37W/m from wall resistance, then 0.13W/m cooling available for e-cloud

## Slide 14
e-cloud mitigations for FCC-ee
L. Sabato
R. Valizadeh

## Slide 15
Morphology effects on thermal desorption
LASE-Cu
TPD from LASE-Cu for temperature induced vacuum transient study
Impact on the working conditions
~500 h beam lifetime
Working temperature range foreseen for FCC-hh
L. Spallino et al. Appl. Phys. Lett. (2019); L. Spallino, J. Vac. Sci. Technol. B (2020); L. Spallino et al., Phys. Rev. Accel. Beams (2020)
LESS for FCC-hh (?) – pressure transients? resistivity ? dust ?
L. Spallino

## Slide 16
M. Himmerlich
A. Passarelli

## Slide 17
Carbon-Coated Copper
alternative mitigations
for FCC-hh
A. Liedl

## Slide 18
ion induced pressure - another concern for FCC-hh
O. Malyshev

## Slide 19
e-cloud at former KEKB
K. Ohmi

## Slide 20
e-cloud at SuperKEKB
K. Ohmi

## Slide 21
LHC e-cloud effect
L. Mether
sudden beam loss at SuperKEKB
Y. Ohnishi
eeFACT’22
local e-cloud ?
dust ?

## Slide 22
next ECLOUD workshop?
ECLOUD’24, ECLOUD’25, ECLOUD’26 ?
two candidate sites proposed

## Slide 23
Candidate 1: La Biodola
Cimino theorem:
La Biodola = the best place for ECLOUD’XX
(where XX is any pair of integers)

## Slide 24
Candidate 2: Yucatan
Gerardo Guillermo (CSNS),
Humberto Maury (UGTO),
Karla Cantún (UADY)
2024