## Slide 1: Exploiting Cherenkov radiation and cross luminescence emission with BGO/BaF2 metascintillators
Riccardo Latella
Ph.D. Student & Engineer
Metacrystal & I3M
1
Notes: Welcome everybody. My name is Riccardo Latella, I’m doing my Ph.D. at Polytechnic of Valencia, precisely at the laboratory of i3M, while covering the role of Engineer in Metacrystal company based in Geneva. Today, I’m going to present some of the results we have obtain so far, regarding “Exploiting Cherenkov radiation and cross-luminescence emission with BGO/BaF2 metascintillators”

## Slide 2
Introduction
Testbench setup
Analysis
Results: BGO & BaF2 - VUV – CTR
Discussion & Future Plans
2
Index
Notes: Briefly, I’ll introduce all the sections in which my presentation is divided, starting from the introduction about metascintillators and the possible synergy between Cherenkov and Cross-luminescence emission. Then, I’ll explain in details the testbench setup used in our daily testing, focusing on the electronics, SiPMs, coupling material, pixel/metapixels, and the relative filtering approaches. Moving to the third section, I’ll go through the analysis on the two metapixels based on BGO used in this work. Leading to the results about BGO/BaF2 metapixel using VUV sensors and concluding with the discussion and future plans.

## Slide 3
Which materials give the strongest combination?
3
Metascintillator heterostructures
Good timing resolution & high stopping power.
Thin slices of a dense host material (e.g. LYSO, BGO) and a fast emitter (e.g. EJ232, BaF2)
Share scintillation
Energy-sharing
Gamma energy
Recoil electron
WHY METASCINTILLATORS?
Enhance effective sensitivity
Reduce TB-PET costs
G. Konstantinou 2020
Introduction:
Metascintillators
Notes: So, starting with the introduction, the first generation of metascintillator are composed of thin slices of a dense host material, like BGO or LYSO, and a fast emitter, like plastic or BaF2. The shared scintillation of these heterostructures could break the trade-off between high stopping power and good timing resolution. Indeed, the gamma energy is shared between the two materials thanks to the recoil electron trajectory. This phenomena enhances the total effective sensitivity of the system and, by using cheaper materials than commercial ones, can reduce the costs of large PET scanners like TB-PETs. But, which is the best combination in terms of synergy for metascintillators. This is actually the study we are conduction right now.

## Slide 4
Fast scintillators
as
light-guiding materials
N. Kratochwil 2021
Prove of concept:
EJ232
BaF2
Combination of: - Cherenkov from BGO and BaF2
- Cross-luminescence from BaF2.
Synergy with VUV SiPM!
4
Cherenkov emissions
∝
BGO light absorption
VS
< 300 nm
BGO/BaF2 metascintillators
Introduction:
Cherenkov & Cross-luminescence emissions
Notes: One of the possible scenario is combining Cherenkov and cross-luminescence emissions. But how? Well, I’m not going in the physical details but Cherenkov emissions are produced inside BGO crystal which is also a very dense and well known material. The Cherenkov light produced is inversive proportional to the wavelength squared, while BGO starts to absorb light below 300 nm, which means that the majority of strongest Cherenkov emissions are absorbed inside the crystal itself. To face this problem, fast scintillator can be used as light-guiding materials. To prove this concept, we are combining BGO plates with plastic and in particular with BaF2, that has its fast emission in the deep UV region. A synergy between these two materials can found by using BGO/BaF2 metascintillators coupled with VUV SiPMs. In this way, we can combine Cherenkov from BGO and BaF2 and Cross-luminescence from BaF2.

## Slide 5
Boards
Oscilloscope
Rhode & Schwarz RTP084, high-performance 8GHz bandwidth oscilloscope.
5
Double-channel readout circuit
Timing
channel
Energy
channel
Balun transformer
CTR measurements
Two detectors:
Board
SiPM
Scintillator
Na-22 source (7 μCi)
Low Noise
Baseline
Inspired by Cates and Gundaker’s design
Timing amplification stage modified
Testbench setup
Electronics
Notes: Let’s have a look on which parts our testbench setup is compose of, starting from the electronics. Our boards are inspired by a previous design with some improvements in terms of power consumption and noise level. Each board constitutes a double-channel readout circuit having a dedicated energy and timing channel, based on a balun transformer. These boards are connected to a high-performance 8GHz bandwidth oscilloscope, namely an Rhode & Schwarz RTP084. Our Coincidence Time Resolution measurements are performed initially on the oscilloscope by placing two detectors in front of each other and a sodium 22 source in between.

## Slide 6
Coupling materials used:
Two optical greases:
  SS-988 from Silicon Solution
  Bluesil Paste 7 from Elkem
6
Fondazione Bruno Kessler
NO protective layer
Very fragile!
Improve robustness
Epoxy resin
on
Bonding wires
Good deep UV transmittance
Risk of damaging the SiPM
Testbench setup
SiPMs and Coupling materials
Glycerine bi-distilled
Low temperature

## Slide 7
Metapixels with variable plate materials and dimensions.
7
Reference detector:
3x3x5 mm3 LYSO:Ce,Ca
Bluesil Paste 7
NUV-HD sensor
DTR = 64.7 ps
Metapixels
Metascintillators in pixel configurations
Testbench setup
Pixels and Metapixels

## Slide 8: Filtering methods
Maximum Peak (maxP): Standard energy photopeak filtering
Rise Time (RT): Indicator of initial photon-time density
N. Kratochwil 2020
RTD 2-7mV
8
Photoelectric events can be produced and shared in both materials
Maximum values
Integrated charge
Signal maximum values distribution
surrogate
Integrated charge
distribution
(Pulse energy content)
Metapixels’ spectrums are more complex
Fixing two voltage thresholds, close to the noise level
Rising Time Distribution (RTD)
Choose only the fastest events
5 mV rise time surrogate for energy-sharing
~
Testbench setup

## Slide 9: BGO & Plastic (EJ232) - RTD
BGO, EJ232 & meta with NUV
BGO & meta: NUV vs VUV
Chart: RTD - BGO & EJ232 & BGO/EJ232
Chart: RTD - BGO & EJ232 & BGO/EJ232
The growth of the faster event population can only be attributed to the detection of Cherenkov photons.
9
Test condition:
25ºC
SS-988
Vbias = 39.5 V
Plastic
Meta
BGO
Meta BGO/EJ232 is faster than BGO bulk
VuV less PDE than NUV for λ > 300 nm
Increased population using VUV, even if pulses are weaker
Analysis

## Slide 10: BGO & BaF2 - VUV
Energy Spectrum
Glycerine:
liquid, low viscosity
hard to handle.
10
Test condition:
15ºC
Glycerine
Vbias = 39.5 V
BGO
BaF2
Chart: RTD comparison
Alignment of the energy spectrums
integration window
wavelength-sensitive transfer function
Maximum values
Integrated charge
Maximum values
Integrated charge
maxP usable for metascintillators energy filtering
Sensitive to energy sharing
RTD different between materials:
Energy sharing surrogate
Separate fastest events
Cross-luminescence in BaF2
Cherenkov photons in BGO
Analysis

## Slide 11: BGO & BaF2 – VUV - CTR
 | ER = 20/21% | ER = 24/25% | ER = 16/18%
CTR | BGO [ps] | BGO/BaF2 [ps] | BaF2 [ps]
maxP | 223.1 (0.98) | 186.1 (0.98) | 123.4 (1.00)
RT100ps | 159.9 (0.96) | 138.3 (0.97) | 154.5 (0.99)
CTRs improvements around 25-30%
Most of the BaF2 events are already below 100 ps (62.4 %)
11
Combine
maxP
RT100
Chart: CTR - RT100
Rough results
Time-walk correction: 30% improvement
Reference
Pixel
Metapixel
Results

## Slide 12
Improvement of the CTR of radiation detectors using BGO and fast emission material (CTR = 138.3 ps), especially BaF2 creating a synergy between Cherenkov and cross-luminescence emissions.
COST REDUCTION: these materials have less than half of the LYSO cost, making them a good alternative, especially for larger PET scanners, like TB-PET.
Future improvements are possible by combining maxP and RT filtering approaches and developing/combining new ones, like ToT or neural networks, to have a precise measurement of both energy of interaction and energy sharing.
Further analysis will be conducted on the combination between slabs of various thicknesses, exploiting both materials' characteristics.
REFERENCES:
G. Konstantinou et al., "A novel metascintillator approach for ultra-fast timing in Positron Emission Tomography," 2020 IEEE Nuclear Science Symposium and Medical Imaging Conference (NSS/MIC), 2020, pp. 1-4, doi: 10.1109/NSS/MIC42677.2020.9508015.
P. Lecoq (2017). Pushing the Limits in Time-of-Flight PET Imaging. IEEE Transactions on Radiation and Plasma Medical Sciences.
R. Latella, A.J. Gonzalez, J. Barrio, J.M. Benlloch, P. Lecoq, G. Konstantinou (2021). Test Setup and Data Selection Protocols for the Measurement of Metascintillator CTR. IEEE proceeding, 2021 Tokyo.
A. Gonzalez-Montoro, S. Pourashraf, J. W. Cates, S. Merzi, A. Gola, G. Borghi, C. S. Levin (2021). Physical considerations for Cherenkov radiation-based coincidence time resolution measurements in BGO. IEEE proceeding, 2021 Tokyo.
N. Kratochwil, E. Auffray, S. Gundacker (2020). Exploring Cherenkov emission of BGO for TOF-PET. IEEE Transactions on Radiation and Plasma Medical Sciences.
J. W. Cates, S. Gundacker, E. Auffray, P. Lecoq, C. S. Levin. Improved single photon time resolution for analog SiPMs with front end readout that reduces influence of electronic noise. Physics in Medicine & Biology (63 185022).
Thank you for your attention
12
Discussion & Future Plans