## Slide 1: MT&SA Network Seminar
A. Traverso 1,2,3 , A. Leveratto2 and A. Malagoli2
S. Farinon3, R. Musenich3 and P. Fabbricatore3
1. Università degli studi di Genova
2. CNR-SPIN, Genova
3. INFN, Sezione di Genova

## Slide 2: OUTLINE
The project
Why BiSCCO(2212) and how it’s made?
The GDG process
What have been done in the first two years
New works: whole characterization of a GDG wire
The BiSCCO small coil

## Slide 3: The BISCOTTO project
One structure, plenty of applications
Hadron therapy gantry
Particle physics
Electrical applications
R. Musenich3
M. Statera4, M. Breschi5
3. INFN, Sezione di Genova
4. INFN, Sezione di Milano
5. Università di Bologna

## Slide 4: Why Bi-2212...
Key positives
A flexible conductor technology
  Round, rectangular, square…..
  Fine filaments
  Twisted
  Multiple architecture
Excellent conductivity matrix without any need for diffusion barrier
The fabrication route is the same industrialized for Nb-based and MgB2 superconductors
Critical points
Mechanical properties: low E and low Yield Strength
Wind and react technique like Nb3Sn but more complex
Costs
powders into
a
Silver sheath
POWDER IN TUBE
MECHANICAL DEFORMATION
HEAT TREATMENT
Groove rolling
Drawing
Alternation of
Groove rolling – Drawing – Groove rolling
to realize denser wires
Performed in a atmosphere @ of partial pressure
…and how?

## Slide 5
It has been shown that the main obstacle to current flow through the 2212 filament is the presence of bubbles
(F. Kametani et al., 2011 Supercond. Sci. Technol. 24, 075009)
The pressure caused by them provokes a Bi-2212 movement and an expansion of the wire during the melt stage that makes it very inhomogeneous over lengths longer than 10-15 cm
(A. Malagoli et al., 2013 Supercond. Sci. Technol. 25, 055018)
One problem, two different solutions…
Recently the density of the filaments of a commercial OST wire after drawing was increased using an “over pressure” process at ASC-NHMFL leading to a strong reduction of the bubble density and size and to a strong enhancement of the critical current (D. Larbalestier et al., 2014 Nat. Mat. 13, 375)
Our different approach lies in enhancing the 2212 density of the conductor and getting improved performances, even on long lengths, acting on the wire deformation process – keeping in mind as a key point its straightforward scalability over industrial lengths

## Slide 7: First and second stacked wire
First restack
Second restack
Images are not in scale!!!!!

## Slide 8: heat treatment

## Slide 9
A Malagoli, F Kametani, J Jiang, U P Trociewitz, E E Hellstrom, D C Larbalestier, Supercond. Sci. Technol. 24 (2011) 075016
Performaces drop along a just 1m-long fully drawn wire
Almost the same J_E in short and 1-m-long GDG sample
Measurements performed at ENEA labs in Rome

## Slide 10: What has been done in the past two years
1st year (2018-2019):
huge R&D on wires due to the change of powders supplier.
Enhancement of the transport properties of GDG-BiSCCO wires made at CNR-SPIN in Genoa.
Exceeding of the minimum requirements in terms of the overall critical current density (or Engineering critical current density ) to make a winding. The lower limit is set to at the operative field.
Looking forward
future improvements
and results…
2020
2016
2017
2019
2018
2nd year (2019-2020):
@7T, 4.2K
characterization in function of the temperature (up to 20K) and the applied magnetic field (up to 7 T).
Here a LHC Rutherford cable cross section
In the red boxes are some of the deformed strands composing the cable
Since February 2020 the pandemic issue stop almost all the experimental activities that cannot be done by a single person. The R&D activity on wires was totally stop.
Start of the coding of a Finite Elements code in ANSYS aimed to evaluate the stress accumulation inside of our GDG wires due to the cabling process.
Code refinements and test on flattened samples.
@ the operative field is the minimum request for magnet applications

## Slide 11: FIRST STEP: FOUNDAMENTAL PARAMETERS ESTIMATION
Due to lack of information about mechanical properties, the development of the model required several steps of approximation.
Neither the Young Modulus nor the Poisson's Ratio are known.
Comparing the results of the two different simulations, almost no differences were observed and that suggested that Young Modulus will not affect results for this kind of simulations.
 | Silver | 
Young Modulus |  | 
Poisson's Ratio |  | 
Yield Stress |  | 
 | Silver | 
Material properties involved in the model simulation
First approach: perfect-like geometry. In blue the Silver matrix, in yellow the filaments
Two different simulations on a perfect-like geometry were made: one with a higher and one with a lower Young Modulus than the silver one.
Poisson's ratio was decided to be equal to the Silver one because it was possible that the metal will rules the calculations.
Assumption: Bi(2212) is taken to be elastoplastic Von Mises Theory

## Slide 12: SECOND STEP: SPEEDING UP CALCULATIONS. THE MEAN MATERIAL EXPEDIENT
To speed up the simulation, no filaments were considered and a new model was made with full bundles made by a “mean material”. This model maintains a “perfect” geometry . Mechanical properties of this new material were calculated interfering correctly the Silver matrix and the filaments, so the series and parallels laws for the mechanical properties were applied.
Here on the left, the real cross section of AMBI036 The whole study was tailored on this wire.
Here on the right, the superimposition of the simulated cross sections. The left side of the simulated cross section shows the very first geometry simulated, so a perfect geometry wire with all the filaments (the yellow dots) present.
On the right side just full bundles made by the mean material are present.
Longitudinal Young Modulus:
Transversal Young Modulus:
In the equations, subscripted letters stay for:
composite material, in this case the whole bundle (in Ciano here above);
filaments (the yellow dots here above)
matrix material.

## Slide 13: THIRD STEP:REALISTIC GEOMETRY & TEST
Next step in the model refinement is the construction of a system with a more realistic geometry because, as can be observed in the previous slides, the cross-section of the real wire is not symmetric (due to the shape of the grooves involved in the mechanical deformation process)
Comparison between cross section of the real sample of flattened by of its initial height through a flat rolling (on the left), and the relative calculated cross section (on the right).

## Slide 14: STRESS ACCUMULATION ON GDG FLATTENED WIRES THROUGH FEM APPROACH
10%
15%
20%
25%
Looking at the distribution of the calculated total stress on the bundles induce by the flat rolling, a preferred direction of accumulation is clearly visible.
This shape is related to the “GDG” mechanical
deformation process performed on the wires. The diagonal connecting the two “smoother” edges is the main working direction of the squared grooves.
Colour legend of the Von Mises Equivalent stress

## Slide 15: Evaluation of possible thresholds
Flattening deformation rate | Strain threshold | Stress threshold (MPa) | 
 |  |  | (estimated)
Flattening deformation rate | Strain threshold | Stress threshold (MPa) | 
Considering the drop of the critical current the consequence of loss of effective superconducting area, it is possible to evaluate the bundles’ strain threshold after which the superconducting area is no longer considerable able to carry current.
evaluation of the mechanical properties of GDG wires
Norm (from experiments)
Expected behaviour
Not easy to compare these parameters because mechanical properties of are not known

## Slide 16: Meanwhile in Rome…
Magnetic characterization of performances @ ENEA labs in Frascati
AIM: to fill the literature lack of information with a complete characterization of BiSCCO wire
Kramer (1972) found that for LTS type-II superconductors the normalized pinning force at any temperature can be expressed through a scaling law that Dew-Huges (1974) wrote in the form

## Slide 17: Going from LTS to HTS
determined from loops, while and obtained as fitting parameters 
The pinning force density of wires is often discussed considering the characteristic dependence of grain boundary pinning with and  Evaluation of was performed fitting the experimental curves using p and as fit parameters. q parameter was keep either equal to 3.89, 4, 4.25, 4.5 up to . The final value of was calculated as the average obtained , for any temperature, by the full set of fitting process.
@ 27 K:
p= (0.64 0.01)
q= (3.89 0.01)
Literature: ~ 0.8; from 2 to 5

## Slide 18: Difference due to the powder supplier?
T [K] | Hirr [T] | Hirr [T]
 | SPIN_016nexans | SPIN_036engimat
8 | / | 127±11
10 | 76±5 | 73±5
12 | 50±4 | 48±4
14 |  | 38±3
16 | 22±2 | 22±2
17 |  | 22±1
18 | 16±1 | 17±1
19 |  | 16±1
20 | 11.5±0.7 | 13.2±0.8
23 | / | 8.7±0.5
25 | 6.0 | 7.2±0.5
27 | / | 5.60
30 | 3.52 | 4.89
35 |  | 3.70
40 | 1.34 | 2.79
50 | 0.42 | 1.40
60 | 0.18 | 0.150
69.6 | 0.002 | /
70 | / | 0.08
72.9 | / | 0.002
78.4 | 0 | /
82 | / | 0
Same &
pinning behaviours
“Bi-2212 wires behaviour above liquid Helium temperature for cryogen-free applications,” Sci. Rep, 2021 ( Leveratto A. et al).
differences due to the structure

## Slide 19: What we understood from that characterization?
From the measurements we demonstrated that usual approximation for H_irr in HTS underestimate H_irr
At we still have a at the operative field of and an irreversibility field of
Thinking about a possible device, an operating current as high as 80% of can be sustained at , 7 T with a temperature margin of about 4 K

## Slide 20: What we understood from that characterization? Pt.2 (not published yet)
If we want to think about real applications, we have to take into account that the magnet will be charged/discharged.
In this transient, filaments may couple themselves  heat generation due to the Joule effect
Usually all the weak links that couple filaments inside a wire are suppressed by a small field
But BiSCCO shows a particular weak link behaviour in function of the temperature AND the magnetic field

## Slide 22: What happened in last months??
Mechanical structures (ordered at the end of 2019) for small coils were finally delivered!!!!!! The two mandrels, one in Inconel and one in the cupro-alluminum alloy, are long cylindrical structures with an external diameter of with 15 solenoidal turns carved on.
Built-in-house winding machine
Problem related to BiSCCO: react and wind technique is needed  optimization of the heat treatment is mandatory!
Huge work related to
characterization of the wire performances in function of the maximim temperature of the treatment;
Optimization of the whole treatment ( setpoints & slopes);

## Slide 23: GDG-BiSCCO Coil
Green solenoid
Reacted small coil

## Slide 24: GDG-BiSCCO Coil
The coil has been impregnated with wax to prevent destructive effects on the conductor along the test

## Slide 25: Conclusions
Along these 3 years:
HUGE optimization work of the fabrication process of BiSCCO GDG wires (mechanical deformation process, heat treatment, design…) which led to a raise of the transport properties of GDG BiSCCO wires by a factor 2.
Exceeding of the minimum request (set at at the operative field and temperature) for magnet applications even at temperature higher than liquid helium (performances suitable for applications up to / );
In collaboration with ENEA, whole characterization of BiSCCO wire that filled a lack of information in the literature of this material;
Investigation of the AC losses behaviour and nature in BiSCCO wires (work not published yet)
Development of a preliminary tool that might be involved in the cabling operation; evaluation of mechanical critical threshold for BiSCCO GDG wires;
Realization, treatment and test of the FIRST GDG-BiSCCO(2212) coil.