## Slide 1
SRF cavities for large international projects ESS and PIP-II
Daniele Sertore
INFN Milano – LASA
Paolo Michelato

## Slide 2: Presentation Layout
INFN LASA SRF Group Expertise
  Cavity design
  Prototypes
  2 K Vertical Test
  Path to large project contribution
European Spallation Source
  Challenges
  Status of the contribution
Proton Improvement Plan – II
  Key features
  R&D program
  View into the future

## Slide 3: INFN LASA SRF expertise

## Slide 4: Path towards INFN LASA SRF experties
The First Superconducting Cyclotron in Europe in the ‘80s, now at LNS, was realized at LASA
TESLA and the TESLA Collaboration (90’s …)
  TESLA, a TeV-scale electron-positron collider, was the first accelerator based on SRF. As a funder of the collaboration, INFN LASA contributed to bring SRF to be reliable and usable for acceleration application
European XFEL (from 2000’s …)
  A 17.6 GeV SRF based accelerator feeding a X-Ray Free Electron Laser. This project has succesfully demonstrated the possibility of application of SRF to large projects, paving the way to further challenging accelerators (LCLS-II, SHINE, ESS, PIP-II, ILC, FCC-ee, CEPC, etc.)

## Slide 5: Cavity – Electromagnetic Design
Full parametric model in terms of 7 geometrical parameters
We built a 2D parametric tool for the analysis of the cavity shape on the electromagnetic parameters based on SUPERFISH
A multicell cavity is then built to minimize Field Flatness error, compute b and TTF as well as final performances
The 2D model constitutes the basis for further 3D simulations (HFSS, CST) for HOMs, multipacting, field emission considerations
BuildCavity
Half Cell Parameters
ESS MB Cavity: Example of EM analyses performed: Dipole HOM at 1742.47 MHz
PIP-II LB Cavity: Example of EM analyses performed: Dipole HOM at 1678 MHz showing partial reflections in the FPC

## Slide 6: Cavity – Mechanical Design
The EM design is transferred to mechanical analysis (loop) for estimating critical parameters as:
  Ring radius
  Stiffness
  Tuning sensitivity
  Vacuum sensitivity
  Lorentz Force Detuning (LFD)
  PED, ASME compliance
Developed specific tool
Dynamical analyses: natural modes
LFD

## Slide 7: Cavity - Towards production -> Prototypes
A key element of our expertise consists also in the transfer of the EM and mechanical design to production:
  RF procedures from sheets to cavity
  Define production cycle to guarantee final length and frequency
  Define appropriate treatment (BCP, EP, etc.)
  Mechanical and RF measurement and control plan
  Test of defined scheme on prototypes
  2 K RF test for final acceptance
Cavity EBW
Bulk BCP
180 mm
Annealing
de Hydrog.
Tuning
Final BCP: 20 mm + HPR
Accessories installation
Final Check and delivery
Subcomponents preparation
Cavity integration (He tank)
DESY
Nb sheets and raw materials
CEA
Al1
Al2
Al3
EC
EC
PC
PC
IC
ID
PD
CD
EGP
EGC
Al5
Al4
Cavity tuning machine
Chart: Time [s]
RF Measurements

## Slide 8: Cavity – Cold test @ LASA
8
Clean Room and UPW
  Ultra Pure Water plant
  ISO4/7 clean room, HPR system
  Qualified Slow Pumping Slow Venting system
Cryostat: f 700 mm, 4.5 m length, losses ~ 1 W @ 2 K
Residual magnetic field: < 8 mGauss (single shield). Single mmetal external shield and, second cryogenic shield (Cryoperm) installed.
Sub-cooling system:
  Cooling power: ∼ 70 W @ 2 K
  Lowest temperature 1.5 K.
  Direct filling at 2 K
RF capability: 500 to 3900 MHz
Dedicated inserts with several diagnostics:
  second sound detectors for quench localization
  cryogenic photodiodes
  fast thermometry
  flux gate
X-ray counter and X-ray NaI spectrometer
Real-time Scintillator
Second Sound
Q0 = 4 1010
Internal Magnetic Shield

## Slide 9: Tuners and Blade Tuner
Each SRF cavity must be equipped with a cryogenic tuning device, Cold Tuner, to set the cavity resonant frequency to the project value during operation. Tuners must also compensate detuning.
Among detuning sources:
  Lorentz forces on cavity walls induced by electromagnetic fields
  Microphonics and stochastic noise, strongly correlated to helium bath pressure fluctuations
Tuners control static frequency value (slow action, scale of second to minutes) and suppress dynamic detuning (fast action, scale of milliseconds).
At INFN LASA we designed, developed and experimentally qualified tuners and their control systems for many international projects
Lorentz Force detuning
Slater’s theorem: detuning rises with the square of field
Required power rises with the square of detuning!
Cavity Detuning:
INFN Blade Tuner for E-XFEL, DESY, Germany
E-XFEL Main Linac Tuner
INFN Blade Tuner at S1-Global KEK, Japan
INFN Tuner for the ADS cryomodule at IPN-Orsay, France
INFN Tuner for the ILC cryomodule at Fermilab, USA
Piezoelectric actuators for fast tuning, E-XFEL, DESY

## Slide 10: Cryomodule: TESLA →XFEL→ILC design criteria
High filling factor
  maximize real estate gradient/cavity gradient
    long cryomodules/cryo-units, short connections
Moderate cost per unit length
  simple design, based on reliable technologies
  low static heat losses in operation
Effective cold mass alignment strategy
  room temperature alignment preserved at cold
Effective/reproducible assembling procedure
  clean room assembly just for the cavity string
  minimize time consuming operations (cost /reliability)
Module 1
Module 2
Module 3

## Slide 11: Eu-XFEL 3.9 GHz: cavities and cryomodule results
INFN LASA In-Kind contribution:
  10+10 Cavities, recipe (BCP), PED compliant
  Ancillaries: Blade Tuners, magnetic shields, He-tank, etc.
  Cryomodule: cold mass, thermal shielding, etc.
Y (i.e. t)
X (i.e. E)
RF Curvature Linearization by AH1
On
Off
String Assembly (DESY)
Blade Tuner
3.9 GHz Blade Tuner
3.9 GHz cavities on LASA VT insert
September 23, 2015
3.9 GHz cavity ancillaries

## Slide 12: Photocathodes for High Brightness Photoinjectors
INFN LASA is providing high QE Cs2Te photocathodes since ‘90s (more than 150 photocathode produced) to different labs for high brightness RF electron gun operation, representing the state of the art in this field.
  DESY (FLASH, PITZ, REGAE)
  E-XFEL
  APEX (LBNL)
  FAST (FNAL)
  LBNL for the LCLS II commissioning
VT installation
Preparation Chamber at LASA

## Slide 13: European Spallation Source

## Slide 14: INFN LASA Contribution to ESS
INFN LASA In-Kind contribution for 11.6 M€.
  Fabrication of 36 cavities in the industry, including treatments, tuning and He tank integration.
  Built to Print strategy.
  Cavities delivered ready for the cold test.
    Analogous strategy as for the XFEL successful experience
  Cold test in a qualified infrastructure (DESY).
  Delivery at CEA ready for the cryomodule assembly.
Series cavities production at the industry:
    First cavity cold tested in November 2018
    Cold test at DESY and then CEA delivery
    Delivery rate foreseen: 2 cavities every 3 weeks
ESS Parameters | 
Max Energy | 2 GeV
Average beam power | 5 MW
Peak beam power | 125 MW
Peak beam current | 62.5 mA
Pulse length | 2.86 ms
Repetition rate | 14 Hz
Energy from SC sections | 96 %
LASA contribution
Spokes
Medium β
High β
DTL
MEBT
RFQ
LEBT
Source
HEBT & Contingency
Target
2.4 m
4.6 m
3.8 m
39 m
56 m
77 m
179 m
75 keV
3.6 MeV
90 MeV
216 MeV
571 MeV
2000 MeV
352.21 MHz
704.42 MHz
Berkeley 37-inch cyclotron
350 mCi Ra-Be source
Chadwick
1930
1970
1980
1990
2000
2010
2020
105
1010
1015
1020
1
ISIS
Particle driven pulsed
ZING-P
ZING-P’
KENS
WNR
IPNS
ILL
X-10
CP-2
Fission reactors
HFBR
HFIR
NRU
MTR
NRX
CP-1
1940
1950
1960
Effective thermal neutron flux n/cm2-s
(Updated from Neutron Scattering, K. Skold and D. L. Price, eds., Academic Press, 1986)
FRM-II
SINQ
SNS
J-PARC
LANSCE
OPAL
PIK
2030
CARR
CSNS
Dhruva
IBR-II
NIST
RSG
LVR
JRR-3
Particle driven steady state
Pulsed reactor
HANARO
HIFAR
SAFARI-1
SALAM
ETERR-2
MARIA
HOR
JEEP II
ORPHEE
Reactor Sources
Spallation Sources
Year
ESS

## Slide 15: ESS Medium beta cavities: from design to series
INFN R&D on ESS prototypes
  INFN design, plug compatible with ESS cryomodule.
  Built prototypes at industry with same procedures as for series.
  Test QA/QC plan for future series production
  Final handling and test done in the qualified infrastructure at LASA.
  Successful result well above specification
HOM analyses
Cell shape design
Dumb-Bells
ESS Medium Beta cavity prototype MB001 qualification at 2.0 K
ESS specs
  Eacc >16.7 MV/m
  Q0> 5109
Cold test @ LASA
Cavity tuning

## Slide 16: INFN-LASA ESS cavities production workflow
CEA
Cavities Assembly in criomodules
Not qualified
Eddy current
Scanning (DESY)
Ettore Zanon
Special
diagnostic
Rs vs. T, etc.
Cryomodule test at ESS
Rejected
INFN LASA
Accepted
Vertical TEST @
DESY
Vertical TEST @
LASA
Series
R300 Sheets
Semifinished parts
OTIC Ningxia
Qualified

## Slide 17: MB Cavity 5-Acceptance Levels
Cavity EBW
Bulk BCP
180 mm
Annealing
de Hydrog.
Tuning
Final BCP: 20 mm + HPR
Accessories installation
Final Check and delivery
Subcomponents preparation
Cavity integration (He tank)
DESY
Nb sheets and raw materials
CEA
Al1
Al2
Al3
EC
EC
PC
PC
IC
ID
PD
CD
EGP
EGC
Al4
Al5

## Slide 18: QA/QC and document flow
Managing System
Quality Control
Industry
INFN Managing system
Database:
Parameter Analysis
Process Control
INFN Experts Check
Cavity with Tank
Cavity with Tank
Module
NCR
NCR
NCR
NCR
Document and data management developed in the framework of and LNS collaboration
Cavity Production Data
Cold RF Test
Cavity Assembly
Cavity Acceptance
Q0 vs Eacc RF at Cold
Incoming RF check
INFN Alfresco CMS

## Slide 19: ESS Medium Beta Status
Niobium
  About 4 tons of Nb purchased, eddy current scanned at DESY and delivered to vendor
Series cavities
  All 38 cavities mechanical finished
  28 cavities (7 modules) delivered to CEA for module integration
  8 (+2) cavities still to be qualified
  4 new cavities production in progress, mitigation against possible further delays
ESS Acceptance Goal Eacc = 16.7 MV/m Q0 = 5·109
28 cavities at CEA
3 x goal
4 x goal
Q0 at Eacc target
ECS @ DESY

## Slide 20: Plan for the completion of delivery
  8 (+2) cavities are not yet qualified to ESS specifications. COVID’19 and vendor change of ownership had impact on cavity perfomances. They are limited by the maximum achievabale field, while Q0 at low field is inline with the qualified cavities.
  Actions:
    Optimization of the cleaning process with High Pressure Rinsing
      Recover M006 (already integrated at CEA)
    ElectroPolishing instead of standard BCP
      Recover naked M024
      Integration into He-tank in progress: final test scheduled beginning of May
    Innovative rotational BCP, collaboration with Argonne National Laboratory
      M028 is back from ANL
      test scheduled in the second half of May

## Slide 21: Cavity M024 - Recovery

## Slide 22: Proton Improvement Plan - II

## Slide 23: PIP-II scope
An 800-MeV superconducting H- Linac; CW-compatible
Beam transport of 800-MeV H- from the SRF Linac to the Booster
Modifications to the Booster, Main Injector, and Recycler Ring to enable >1MW power on LBNF target
Associated conventional facilities
SRF Linac
Transfer Line
Booster
Main Inj/Recycler

## Slide 24: PIP-II Superconducting RF CW Linac, 2mA, 800 MeV Consists of Five Types of Cryomodules
2.1 MeV
10 MeV
32 MeV
177 MeV
516 MeV
833 MeV
H- Ion source
RFQ
PIP-II Linac is technically complex, state of the art superconducting RF accelerator.
The world’s highest energy and highest power CW proton linac.
Cryoplant
CDS
HWR
8 Cavities
162.5 MHz
Single Spoke
SSR1 X 2
16 Cavities
325 MHz
Single Spoke
SSR2 X 7
35 Cavities
325 MHz
Elliptical
HB650 X 4
24 Cavities
650 MHz
Elliptical
LB650 X 9
36 Cavities
650 MHz

## Slide 25: PIPII – Challenges
PIP-II LB650 cavities are among the key scientifical challenges of the project, requiring:
an unprecedented quality factor Q0 for these resonators.
Besides accelerating mode and passband, High-Order Modes risks have been assessed so that neither instabilities nor additional cryogenic losses are posing critical issues.
PIP-II operational scenario is an uncharted territory in terms of detuning control, and this requires deep understanding of Lorentz Force detuning, pressure sensitivity and mechanical leading parameters as rigidities, yield limits, stresses.
Extensive finite element analysis to evaluate the challenging potential mutual compliancy to both PED and ASME codes, a first-time for an accelerator project.
Last mode in 2nd monopole passband, +8 MHz away from 9th ML
R/Q of modes in the b range
LFD frequency shift (blue) and pressure coefficient (red) as a function of external cavity stiffness for a cold cavity.
FEM mesh and internal stress analyses

## Slide 26: R&D phase, 2019-2022
A total of 7 LB650 prototype cavities produced (single and multi cell), 3 already shared with Fermilab for a joint development effort:
Two cavities already cold tested at both FNAL and LASA, project goal met for single-cell
Two INFN Bare LB650 Cavities (BCAV) used for qualification and review
Electro-polishing (EP) surface treatment developed jointly with industry and proved with novel diagnostic tools developed at LASA
Test bench for EP and BCP fluid-dynamics simulation validation through PIV camera in collaboration with Politecnico di Milano.
Simulated (sx) vs. Measured (dx) velocity field during etching
Thickness removal during EP
Real-time cavity thickness measurement during EP with US probes
PIV on n-matched cavity
Overview of High-Q activity at INFN | 
Pre-production cavities, Nb order placed | Jan 19
Pre-production cavities, order placed | Jan 19
Acceptance of pre-production cavities at vendor | Mar 20
BCAV#2 tuned for frequency and field-flatness | May 20
Transport and acceptance of BCAV#1 at FNAL | Jun 20
BCAV#2 surface treated with novel EP | Jul 21
BCAV#2 qualified at cold at LASA | Oct 21
JCAV#1 qualified as jacketed at VTS FNAL | Dec 21
JCAV#1 qualified as dressed in HTC FNAL | Apr 22
BCAV#2 jacketing at INFN | Apr 22
Dressed cavity Final Design Review close-out | May 22
JCAV#2 qualified at LASA | Jul 22
High-Q single-cell qualified at LASA | Sep 22
LB650 single-cell during Electro-Polishing

## Slide 27: R&D phase, 2019-2022
INFN cold test infrastructure at LASA is being upgraded in view of the LB650 cavities vertical tests in order to align to state-of-the-art vertical cold test facilities.
Residual magnetic field:
Cylindrical Cryoperm inner shield realized and installed to reduce the average remnant field in the cavity equator region.
Extension of cryogenic plant performances:
Faster cool-down rate, now limited to about 1-1.5 K/min, via a different distribution of helium cold gas flow around the cavity.
Higher cryogenic power, up to 70 W at 32 mbar (2 K), thanks to an increased primary pumping skid throughput.
Sub-atmospheric refilling system installed to extend cavity testing time by means of counter-flow heat-exchanger followed by a Joule-Thomson expander.
Heat-Exchanger as designed, with its process lines
2 K cryogenic system now installed with B61-EZ-002 ready for VT at LASA
New inner Cryoperm magnetic shiled
Refurbished pumping skid for higher cryo power at 2 K

## Slide 28: INFN High-Q activities
Tested at LASA without fast cool down and magnetic field correction
A total of 7 PIP-II LB650 cavities produced, 3 shared with Fermilab for a joint R&D effort.
Single Cell:
B61S-EZ-001 with high-Q recipe treated at FNAL
  180 mm bulk EP + 900 ˚C HT + N-Doping + final EP
  Test at Fermilab-VTS, project goals met
B61S-EZ-002 with baseline recipe qualified at LASA
  200 mm bulk EP + 800 ˚C HT + final EP + 120 ˚C
  High-Q treatment and re-test coming in 2022
B61S-EZ-003 to be prepared by INFN in 2022
  Target recipe is mid-T baking (300 ˚C)
5-cell cavities:
B61-EZ-001 successfully qualified at Fermilab VTS both naked and jacketed at Fermilab
  Accepted for title transfer by Fermilab
B61-EZ-002 successful VT at LASA in October:
  150 mm bulk EP + 800 ˚C HT + final cold EP + 300 ˚C HT
  now targeted for jacketing in industry from April 2022.
B61-EZ-002 installed on vertical insert al LASA
B61-EZ-002 @ LASA

## Slide 29: Production phase, 2021-2025
Major contracts, mainly: cavity material, manufacturing and cold-testing. Expected to be issued by 2022
Two pre-series cavities to be qualified both as naked and as jacketed. Subsequent cavities will reach cold-testing infrastructure as ready for string assembly
First Site Acceptance Review to take place under INFN responsibility at partner testing infrastructure after qualification cold-test. Final Site Acceptance Review to take place at string assembly site.
Production cavities targeted to be delivered at string assembly site in 9 batches from spring 2024 to fall 2025
INFN-Fermilab Project Planning Document (PPD) signed. It accounts for:
  Compliance to the PIP-II Tech. Review Plan
  Scope of Work, Deliverable, Milestones
  Project schedule
Quality Assurance Plan, Risk Management Plan documents finalized and soon released

## Slide 30: Latest News
“Proceed to CD-3”

## Slide 31: Conclusion
INFN LASA has a long experience on cavity design, fabrication and qualification of SC cavities, ancillaries and cryomodules.
We shared with DESY the production of the 800 cavities for European-XFEL cavity production with European companies, 100 cryomodules and tuners.
Afterwards, we have been in charge of the design, production and test of the 20 cavities for the 3.9 GHz module for European-XFEL together with cryomodule and tuners.
We are now involved in the ESS project as responsible for the Italian In-Kind contribution to the Medium Beta Section of the Superconducting Linac with 36 cavities.
We are also starting our activities towards the production of the 38 Low Beta cavities for the PIP-II accelerator at FNAL.

## Slide 32
Thank you for your attention!