## Slide 1: Studies on the Evolution of Mean Transverse Energy (MTE) for Photocathodes Subjected to Controlled Degradation by Gas Exposure
Liam Soomary
Liam.Soomary@cockcroft.ac.uk / Liam.Soomary@Liverpool.ac.uk
EWPAA 2022

## Slide 2: Presentation Outline:
Brief overview of the Transverse Energy Spread Spectrometer (TESS);
Cu polycrystalline degradation;
Cs implanted Cu production and degradation.

## Slide 3: The TESS Instrument

## Slide 4
Optical Power Meter
Brief TESS Overview
*Not To Scale*
TESS Specifications | 
Wavelength | 200 nm to 2000 nm (operation typically 230 nm to 800 nm)
Monochromator Bandwidth | ± 1 nm
Light Spot Size | approx. 100 µm
Camera Exposure | Typically 1s to 120s
Cathode dimensions | 6 mm x 2 mm circular pucks
Chamber Pressure | < 5 x 10-11 mbar
Aggregate error on each MTE measurement = 10 % | 
The TESS instrument at Daresbury Laboratory measures the intrinsic transverse and longitudinal energy distributions of emitted electrons from chosen photocathode candidates.
These studies are important for optimized energy resolution.

## Slide 5: Degradation of polycrystalline Cu
Why polycrystalline copper?
It is a commonly used photocathode material
Easy to prepare, clean and characterise
Surprising lack of literature on degradation in UHV conditions

## Slide 6: Degradation of the Cu polycrystalline Surface
A polycrystalline copper photocathode was prepared in Daresbury’s surface characterisation suite, the Multiprobe system*.
Sample transferred from Multiprobe to TESS via UHV suitcase (<1 x 10-10 mbar).
*T.C.Q, Noakes et al., CERN-ACC-2014-0039, EuCARD2-Mil-MS73-final

## Slide 7: Cu (Poly) Degradation at 256 nm
We see the relative QE plateau shortly after 10 L. This could be due to all active bonding sites being taken.
Cathode subjected to a cumulative gas exposure of 100 L over a 5 hour experiment
O2 is the gas species with the largest negative effect on QE

## Slide 8: Cs implantation into Polycrystalline Cu
Attractive option to lower work function, with a possibly tuneable QE based off implantation depth and number of ions;
Easy to produce;
Potentially rejuvenate samples with additional implantation.
Why study Cs Implantation?

## Slide 9: Experimental Setup
Gate Valve
Cs Ion Source
Callibration Plate
Sample on Transfer Arm
To Picoammeter
Implantation was performed in the cleaning chamber at a pressure of 1 x 10-9 mbar.
Cs ion source brought toward sample, calibrating with drain current.
2 implantation steps: first at 500 eV; second at 300 eV.
Cs Ion Source
Callibration Plate
Gate Valve

## Slide 10: QE Values as a Function of Wavelength
Measured QE using a 405 nm laser gives a QE of 2.4E-2 %
Using the relative QE, we can calculate that at 266 nm the QE is approximately 5.8E-1 %
QE of a previously measured Cs-Cu sample at 266 nm with a UV laser had a QE of 3.1E-1 %

## Slide 11: Implantation Step MTE
Reaches the thermal floor (25 meV) here!
*Herbert B. Michaelson, "The work function of the elements and its periodicity", Journal of Applied Physics 48, 4729-4733 (1977) DOI:10.1063/1.323539 and…
*S Cristofaro et al., 2020, Plasma Res. Express, 2, 035009, DOI:10.1088/2516-1067/abae81
*
*

## Slide 12: What we see on the screen
We see that at short wavelengths, where the Cu poly sample emits, there is a superposition of 2 spots.
This leads to the convolution of the measured MTE , which calls for a difference in analysis method.

## Slide 13
First Implantation Second Implantation
At 266 nm we see differences in the superimposed spots

## Slide 14: O2 Degradation of Cs Implanted Cu
We see over a 60% drop in the QE in under 25 minutes.
This is slightly more robust than negative electron affinity GaAs*
*N.Chanlek et al., (2014), “The degradation of quantum efficiency in negative electron affinity GaAs photocathodes under gas exposure”, Journal of Physics D Applied Physics, 47. 055110. 10.1088/0022-3727/47/5/055110.

## Slide 15
Further studies into Cs implanted Cu, optimizing implantation depth vs QE;
Replantation / rejuvenation experiments;
Medium Energy Ion Scattering (MEIS) studies.
Further Work that can be done.

## Slide 16: Thank you for listening!
The Daresbury Lab Photocathode Team:
Dr. Andrew Vick Hugh Churn
Dr. Lee Jones Liam Soomary (Ph.D. Student)
Dr. Tim Noakes Chris Benjamin (Ph.D. Student)
Dr. Reza Valizadeh
Prof. Carsten Welsch
Lola (Site Overlord)
EWPAA 2022 - Milano

## Slide 17: Additional Slides

## Slide 18: Relative QE Calculation
The gain provided by the MCP was found to double for each increase of 41 V in difference between the MCP back and the MCP front:
Where ∆MCP is the voltage difference between the MCP back plate and the MCP front plate. The estimated relative QE for each wavelength is then calculated using the equation:
Where the Corrected Image Intensity is the intensity of the photoemission after background subtraction, t is the exposure time and (P T) is the power of the transmitted light falling on the cathode.