## Slide 1
Quench Localization in Superconducting Magnets using the Harmonic Field Analysis Method
Samuele Mariotto
on behalf of INFN LASA
Superconducting Magnet Group
Milan, Italy

## Slide 2
The HL-LHC High Order Corrector Magnets
Theoretical Model of magnetic analysis for Quench localization
Experimental Quench Reconstructions
Case of Multi-coil Quench
Conclusion
Structure

## Slide 3
LHC - integrated luminosity 300 fb-1 by 2023
HL LHC - upgrade interacting regions 2025/27
  3000 fb-1 integrated luminosity by 2040
High Luminosity Project

## Slide 4
In kind contribution CERN-INFN (2014-2019)
5 types of NbTi superferric corrector magnets:
Quadrupole, Sextupole, Octupole, Decapole and Dodecapole
Agreement CERN and INFN-LASA (2019-2022)
Construction of all the 54 magnets for the installation in HL-LHC
~70 m
High Order Corrector Magnets

## Slide 5
Superferric design
Compact and modular
Strong contribution of the iron poles
Field quality influenced by the shape of the poles
NbTi superconding coils
Racetrack
Insulation by S2 glass reinforced material
No INFO on which
Coil Quenched!
Design and Quench Protection
MQSXF
MCSXF

## Slide 6
Assumptions
Only Single Coil quench observed during prototype construction phase
  No quench propagation to all the magnet coils
Quenched coils will not have residual magnetization
The all coil volume is not magnetized after the quench
Uniform 2D Model
Single Superconducting coil cross section contribution
New Idea

## Slide 7
Direct calculation of the Harmonic Coefficients
Transformation to calculate the different coils contribution
Each magnetic dipole moment is rotated and inverted in the direction to account for the opposite polarities
FINAL Harmonic Content
Single kth-Coil Contribution
Analytical Model
S. Mariotto and M. Sorbi. “Quench position reconstruction through harmonic field analysis in superconducting magnets”. Superconductor Science and Technology, 35(1):015006, nov 2021.

## Slide 8
Best Harmonic
For Unique Reconstruction
Field Harmonics Phase
4P
6P
n | k=1 | k=2 | k=3 | k=4
1 | 0 |  |  | 
3 | 0 |  |  | 
4 | 0 |  | 0 | 
n | k=1 | k=2 | k=3 | k=4
1 | 0 |  |  | 
3 | 0 |  |  | 
4 | 0 |  | 0 | 
n | k=1 | k=2 | k=3 | k=4 | k=5 | k=6
2 | 0 |  |  |  |  | 
4 | 0 |  |  |  |  | 
5 | 0 |  |  |  |  | 
6 | 0 |  | 0 |  | 0 | 
n | k=1 | k=2 | k=3 | k=4 | k=5 | k=6
2 | 0 |  |  |  |  | 
4 | 0 |  |  |  |  | 
5 | 0 |  |  |  |  | 
6 | 0 |  | 0 |  | 0 | 
Possible Harmonic Phases
b=2
b=3

## Slide 9
Not Allowed Harmonics
Coil 1
Coil 2
Coil 3
Coil 4
No Quench

## Slide 10
5 different OPERA 2D Models
No consideration of 3D coil end shape
ARMCO Iron BH Curve
Imposed permanent magnet strenght based on MQSXFP1c measured data to reproduce the residual magnetization iron
RESULTS:
Negligible iron effect on the not allowed harmonic orders
Permanent Magnet
FEM Model

## Slide 11
Pin for aligment
Connections
Connections
Integrators
Motor
Encoder
Collaboration CERN-INFN LASA
Rotating Coil Design
FFMM framework for the analysis of the signal
Mechanical integration with cryogenic vertical test station at LASA
AD-HOC Design
Rotating Coil Structure
G10 T-beam Support
5 Slots
= 50 mm
PCB lenght: 0.356 m
130 mm
Magnetic Measurement Test Station

## Slide 12
Higher Peak
Coil 1
Lower Peak
Coil 3
Higher Peak
Lower Peak
Coil 4
Higher Peak
Lower Peak
Coil 2
Higher Peak
Lower Peak
Raw Signal Example MQSXF1

## Slide 13
All magnet types have been characterized at least in one cryogenic test at LASA
150 Quench Analyzed ( P = )
  114 Quench (76% of Total)
  Occured in the 4 Tested Skew 4P
Analysis Results
6P
8P
12PS
12PN
4P
S. Mariotto et al. “Quench Localization in the High Order Corrector Magnets using the Harmonic
Field Method”. Accepted by IEEE Transaction on Applied Superconductivity, 2022.

## Slide 14
Why so many Quench in MQSXF1??? How many of them are MULTIPLE-COILS quench?
MQSXF1 Case Study
MQSXF1
MQSXF1b
MQSXF2
MQSXF3
MQSXF5
4.2K
4.2K
4.2K
4.2K
TOT=46
TOT=5
TOT=15
TOT=24
TOT=24

## Slide 15
Coil 2
Coil 3
Coil 4
Coil 1
Quench in Opposite Coils
Continue in the next slide…..
MQSXF1 Case Study

## Slide 16
More multi-coil quench at high current values
  Higher current decay rate
MQSXF1 Case Study
Coil 2
Coil 3
Coil 4
Coil 1

## Slide 17
Single-Coil Quench
Double-Coil Quench
New Harmonic Content:
With Some algebra:
Suppressed
Suppressed
Harmonic Content Comparison
Multi-Coil Quench – 2 adjacent Coils

## Slide 18
Harmonic Content:
With Some algebra:
Suppressed
Suppressed
Suppressed
Harmonic Content Comparison
Single-Coil Quench
Double-Coil Quench
Amplification
Multi-Coil Quench – 2 Opposite Coils

## Slide 19
Harmonic Content Comparison
Single-Coil Quench
Triple-Coil Quench
Quadruple-Coil Quench
Suppressed
Multi-Coil Quench – 3 and 4Coils

## Slide 20
Time Dependance
Main allowed harmonics depends from time after quench event
  Time Constant: order of 100 seconds!!!
  Iron Magnetization Relaxation
    (Current decay rate dependenance)
Three Main Regions of Amplitude
  All Quenched Coils
  Three Quenched Coils
  One Quenched Coil
1
2
3
MQSXF5
MQSXF5

## Slide 21
Time Dependance
1
2
3
1
2
3
Not-allowed harmonics DO NOT depend from time after the quench event
Three Main Regions of Amplitude
  All Quenched Coils
  Three Quenched Coils
  One Quenched Coil
MQSXF5
MQSXF5

## Slide 22
Developed an innovative method for quench localization
  Based on magnetic measurent of the harmonic content produced by the residual superconductor magnetization after the quench event
Both analytical and FEM model are able to reconstruct exactly the quenched coil
  Unique Reconstruction using phase of the harmonic field component
All 150 Quench Events analyzed and reconstructed
  Very good agreement between QDS Va/Vb signal and magnetic measurement
Improved diagnostic system for magnet performances during series production phase
Experimental evidence of multi-coil quench in the skew quadrupole training
  Developed model is able to reconstruct these events too
  Evidence of allowed harmonics time dependance due iron residual magnetization relaxation
Conclusions

## Slide 23
Thank you for the Attention
LASA TEAM
F. Broggi, E. De Matteis, S. Mariotto, A. Paccalini, A. Palmisano, A. Pasini, D. Pedrini, A. Leone, M. Prioli, L. Rossi, M. Sorbi, S. Sorti, M. Statera, M. Todero, C. Uva, R. Valente
22
Seminar Rete MS&TA INFN, 3 March 2022
Samuele Mariotto