## Slide 1: New NbTiN thin films (20 nm) + test structures (resonators)
Goal: determine all material parameters relevant to the design of KI-TWPA
Transition Temperature Tc
Kinetic inductance (per square) Lk
Dissipation/quality factor Q
Nonlinearity
Critical current
Film thickness reduced from 100 nm to 20 nm in order to enhance Lk

## Slide 2: Film parameters
W1
W5
W6

## Slide 3: KID test devices layout

## Slide 4
VNA Characterization

## Slide 5: Kinetic Inductance from f0 and Tc
W1
W5
W6

## Slide 6: Frequency shift vs Power
Film W6 - Resonator 8

## Slide 7: Kinetic Inductance Nonlinearity: first estimation
Need to calibrate:
Need to relate Power in the feedline to I2 in the resonator!
+ Uncertainty  20% on Feedline power
(Attenuators, Cable loss … )
SONNET
QUCS

## Slide 8
SONNET Separate simulation of the L&C elements
Quite Consistent
With full LC !
C (In the resonator there are 2 C in series!)
L

## Slide 9: Lumped model of the system (Qucs)
from
Adapt parameters to experimental fit
Conversion factor

## Slide 10: Finally, Lk vs resonator I2
RESONATOR 1 - f0=4.55 GHz
NbTiN FILM W6 (highest kinetic inductance)
( @NIST: for a 1 um width )

## Slide 11: Results film W6 (resonator width 5 mm)
Resonator |  | 
1 | 4.55 | 19±2
8 | 5.87 | 20±2
Resonator |  | 
1 | 4.55 | 19±2
8 | 5.87 | 20±2
Results film W5 (resonator width 5 mm)
Resonator |  | 
8 | 8.17 | 18±3
Resonator |  | 
8 | 8.17 | 18±3

## Slide 12: Critical current of NbTiN (SC to normal)
Increase current slowly until voltage jumps (normal state)
Measured with film immersed in liquid helium to minimize self-heating effects
Correct to zero temperature with Ginzburg-Landau prediction, modified for thin films:
Roughly expected
(because current density increases at the strip edges … )

## Slide 13: Ratio Ic/I*
MAXIMUM ACHIEVABLE NONLINEARITY =
Why is it important?
NbTiN film (width) | Ic (mA) | I* (mA) | Ic/I*
W5 (5 um) | 4.4 | 18 | 0.25
W6 (5 um) | 2.2 | 20 | 0.09
NIST (1 um) | 2.4 | 7 | 0.34
COULD BE A PROBLEM !
Ic/I* should increase slightly for smaller width
NEED TO EVALUATE Ic & I* FOR THE FINAL WIDTH  1 mm !!