## Slide 1: An Inexpensive Inspection System for Niobium Cavities
Mircea Stirbet and Peter Kneisel
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011

## Slide 2: Optical Inspection Systems for SRF cavities
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011
K. Watanabe, Review of Optical Inspection Methods and Results, TUOBAU01, SRF 2009, Berlin 2009.
Kyoto camera system
DESY system
FNAL system

## Slide 3: Defect localization
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011
W-D. Muller: Review of Results from Temperature Mapping and Subsequent Cavity Inspection, TUOAAU04,SRF 2009 Berlin 2009.

## Slide 4: SRF cavities at JLAB
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011

## Slide 5: 3 1/2-cell photo injector cavities
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011
50 mm
Mechanical marks

## Slide 6: Initial setup for visual inspection on 3 1/2-cell cavities
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011

## Slide 7: Mechanical marks on the endplate of the 3 1/2-cell cavities
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011

## Slide 8: Mechanical marks on the endplate of the 3-cell cavity cont
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011
10 mm

## Slide 9: Image processing using ImageJ software
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011
10 mm

## Slide 10: Image processing using ImageJ software cont.
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011
Density profile along line
Surface plot

## Slide 11: Setup with half-cell for mirror and focus adjustments
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011

## Slide 12: Visual inspection of the endplate after BCP
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011

## Slide 13: Surface details after BCP
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011

## Slide 14: Images in different locations of the 3 1/2-cell cavities
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011
Field probe port
Equator weld
HOM probe
Endplate

## Slide 15: Wish list for an optical inspection system
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011
Illumination: variable intensity, different colors (filters), polarized
Manual focus  auto focus
Optical stand with dampers (System vibrations free)
Optical stand with linear arm movement
Optical system clean room compatible?
Image acquisition via interface to a laptop
Optical wedges for software calibration
Image processing using dedicated software
If in situ cavity repair is intended, the optical system CAN help to
control the operation done in real time, but they should be cheap,
easy to be replaced.
Expensive optical system can be irreversible affected by dust (if grinding is used) or plumes (if local laser healing procedure is intended).

## Slide 16: Miniaturized camera with autofocus features
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011
Olympus IPLEX SA IIR Replaceable optical adapters sharply focus light at the micro-pixel level to realize supremely sharp, vivid detail that contributes precise measurement and inspection.

## Slide 17: Olympus demo

## Slide 18: Conclusions
TTC Meeting Milan, Italy 28th Feb – 3rd Mar 2011
Efficient, inexpensive optical systems for visual inspection
metallic surfaces can be successfully implemented.
These systems can provide valuable information and
defect localization on initial material as well as on the internal cavity surface.
Once data acquisition is done (large cavity production will need TB of storage space), computer assisted analysis can facilitate interpretation and data base mining.