## Slide 1: SiPM@Catania
Measurements and mass test
Claudio Lombardoab
a Dipartimento di Fisica ed Astronomia “E. Majorana” Università degli Studi di Catania
b INFN Sezione di Catania
JUNO-Ita meeting 06/05/2022

## Slide 2: Catania SiPMs test
Preliminary measurements on SiPM
Mass test
Mass test station

## Slide 3: Preliinary measurement on SiPM
Recap on last 2 years measurements at Catania

## Slide 4: Catania and SiPMs
Preliminary measurements on SiPM
Procedure for mass testing
Building of mass test system

## Slide 5: Catania and SiPMs
Preliminary measurements on SiPM→2020-2022
Procedure for mass testing→2021-2022 (FDR ny the end of May)
Building of mass test system→2022-???

## Slide 6: Preliminary measurements on SiPM
Measurements inside and outside climatic chamber
  Staircase, Curve I-V, Dark count, charge spectrum
  Different setup to test different conditions for final setup(measurements with and without lens, dark box, in air...)

## Slide 7: Experimental Setup
Optical Fiber
lens
SiPM
Pitch Adapter Board

## Slide 8: Experimental Setup
LED Dubna

## Slide 9: Experimental Setup

## Slide 10: Experimental Setup
Dark Box “Custom 1”
Dark Box “Custom 2”

## Slide 11: Mass test

## Slide 12: Mass test
Over 4000 SiPMs will be tested:
  Optical test
  Burning test
  Massive test

## Slide 13: Mass test
Over 4000 SiPMs will be tested:
  Optical test
  Burning test
  Massive test

## Slide 14: Mass test@Catania
Writing the FDR before end of May
We studied different hardware setups
We studied the optical part of the mass station

## Slide 15: Mass test@Catania
At the end we decided to use PS and Digit designed by Dubna and produced by Marathon in Russia
Thanks to Arsenij
3 x24 bit ADC on chip

## Slide 16: Mass test@Catania
In the last 6 months we focused on a plan B for the hardware setup using two CAEN solutions
CAEN DT5202
CAEN DT5550W
Common:
Citiroc1A;
SiPM monocanale
HPK S131361-3050-AE08;
Measurements:
at 20 °C and -20 °C
Different optical setups

## Slide 17: HPK S13 8x8
# p.e.

## Slide 18: Mass test@Catania
DT5202 better than DT5550W however PS + digit option is the best solution (acquiring the waveform for further studies, offline integration?)
How can we get the supplies from Russia?(Hard problem for Chinese colleagues)

## Slide 19: Mass test@Catania
Similar but different from the Russian proposal
LED
Environmental Chamber

## Slide 20: Mass test@Catania
Similar but different from the Russian proposal
To be tested at -50 °C
Diffusers at the end?

## Slide 21: Mass test@Catania

## Slide 22: Mass station

## Slide 23: Mass station
New lab @ Dipartimento di Fisica e Astronomia “E.Majorana” in Catania
Environmental chamber room
Lab JUNO

## Slide 24: Mass station
Environmental Chamber Room
Environmental Chamber

## Slide 25: Mass station
16 matrices to test + 16 ref SiPMs:
  Single channel
  HPK S13360-6050CS

## Slide 26: Mass Station

## Slide 27: Conclusions

## Slide 28: Conclusions
Done:
Different plan B have been studied
Draft of FDR
First characterization of ref. SiPM
To Do:
Dark box and mechanical structure
Light field with our splitter
FDR
Characterization of all the ref. SiPM

## Slide 29: Thank You!

## Slide 30: backup

## Slide 31: Spettro a -20 °C HPK S12 8x8

## Slide 32: Prima caratterizzazione HPK S13
CAEN DT5202
CAEN DT5550W

## Slide 33: Cella climatica

## Slide 34: Cella climatica