## Slide 1: Technology and design
The approach within TimeSPOT was to use 3D silicon (and Diamond) sensors to achieve fast timing
  Reducing inter-electrode distance
    Reducing charge collection time
      As well improving intrinsic time resolution
    Increasing radiation hardness
The final geometry selected for the fast timing 3D sensor is the “parallel-trench”
  Already produced in two batches (2019 and 2021) by FBK
55 μm
55 μm
40 μm
First TimeSPOT batch, produced by FBK
Cut along a parallel trench device based strip sensor
150 μm
130 μm
TCAD model of the selected geometry
For more A. Loi https://iris.unica.it/handle/11584/284136

## Slide 2: Measurements
Sensor has been characterised
  Test beams (10/2019, 10/2021 and 5/2022) 
    Intrinsic time resolution
    Performance by tilting the device
    Sensor Efficiency
    Performance after radiation
   Own constructed TCT setup in Cagliari
Customised fast readout has been developed in order to fully explore sensor performance ↓
Test beam setup for intrinsic time resolution characterisation
Dry ice enclosure for rad hard measurements
TimeSPOT fast-electronics
Single pixel test device
TimeSPOT TCT setup
For more G.M. Cossu https://arxiv.org/pdf/2209.11147.pdf

## Slide 3: Results (1)
Intrinsic time Resolution before and after radiation damage above 10¹⁶ n_eq
For more info: A. Lampis https://indico.cern.ch/event/1120714/contributions/4867208/attachments/2472539/4242526/Andrea_Lampis_iworid2022.pdf
https://indico.cern.ch/event/1127562/contributions/4954529/attachments/2511647/4317271/TimeSPOT_TWEPP2022_Final.pdf
No rad damage
After rad damage ↓

## Slide 4: Results (2) and outlook
Sensor behaviour has been studied also by tilting it
  ToA distribution at 20° becomes more gaussian
  The inefficiency (at normal incidence) due to the dead-area of the trenches is fully recovered by tilting the sensors around the trench axis
    It also works for irradiated sensors
Outlook:
  32x32 pixel matrix has been bump-bonded on the TimeSPOT-1 ASIC and currently tested. Future 4D tracking detector and its components are under test and caracterisation (more about it on Lorenzo’s slides)