## Slide 1: Development in dipole magnet technology
Massimo Sorbi
Università degli Studi di Milano – Dip. di Fisica
LASA - INFN – Sez. di Milano

## Slide 2: A few of basic considerations…
B = 0J d
d
d
B = ½ 0J d
CONCLUSION:
Superconducting dipole: less field respect solenoid with same current...
Removing the current in midplane is paid with less field
Other difficulties should be considered (mechanics, thermal design, …)
Magnetic field generated by conducting current
B 0.5  0J d
B =  0J d
  0.20.4

## Slide 3: The conductor: not superconductor only
When we talk of J, we have to consider the overall density in metal part ---> Jeng
Jeng can be between 2 to 10 lower than Jsup
For the cable insulation, Jeng is additionally reduced of kins  0.7  Jeff = kins  Jeng

## Slide 4: Where are we today?
B =  0kins  Jengd
with
0.5
d=100 mm
kins = 0.7
B=4.4 10-2 Jeng
[J] = A/mm2
[B] = T
This means:
10 T -> 230 A/mm2
20 T -> 460 A/mm2
40 T -> 920 A/mm2
Engineering Critical Current Density vs. Applied Field for Superconductors Available in Long Lengths

## Slide 5: Recent achievement in Magnet Community
FP7 EuCARD – WP7 technology R&D 2008-2013
  FRESCA2 dipole 13 T,  100 mm facility Tested in July 2017: 13 T!
  HTS insert + 6 T (no bore) Tested in Juy 2017: 4.52 T @4.2K (power supply limit, no quench)
In 2011 we set the goal for a new EU program FP7-EuCARD2 for enabling HTS in accelerator dipoles.
  Develop a CONDUCTOR of accelerator quality
  Develop a Dipole demo with accelerator characteristics
Fresca2
EuCARD HTS Insert
M. Durante et al. Wed-Af.P03
G. Willering et al. this session

## Slide 6: Conductor cont.
Choice in favor of REBCO tapes assembled in Roebel cable
  REBCO: continuing the route of EuCARD
  EU Industry. Other EU programs (FP7-Eurotapes)
  High current density (use// orientation) & Transposition!
  “Easy” start: conductor in final form, no need high temperature heat treatment of whole coil.
Other types of cable like stacked tape cable with twist on the curvature ends have been investigated. Eyes on CORC®!
Activity on Bi-2212 have been pursued in the collaboration CERN-ASC(Fl) on advanced powder from Nexans with mesurements by Univ. of Geneva on strand and in future U.Twente on cable
W. Goldacker et al., 2006 J Phys. Conf. Ser. 43 901

## Slide 7: Characterization: full campaign @ UniGe
C. Senatore & C.Barth

## Slide 8: From tape to cable
A. Kario & W. Goldacker

## Slide 9: New line for the Roebel
Anna Kario, Simon Otten, Andrea Kling, et al., Wed-Mo-Or21-01

## Slide 10: Aligned Block lay-out
Magnetic Field [T]
Percentage on Loadline [%]
The two plots present flux path variation for insert magnet:
(left) standalone in Iron ,
(right) in 13T ideal background field
Yellow area is the region more near to short sample.
Very different from std. LTS magnets.
e.m. model and e.m. design by J. Van Nugteren @ CERN

## Slide 11: AB dipole magnet
Quench CU bars
G. Kirby, CERN
J. Murtomaki, CERN

## Slide 12: Going in steps:FeatherM0 flat racetrack, 5 m cable

## Slide 13: Magnet technology issues… design & protection issues…
Winding (un)stability : small tension
Impregnation  delamination
QD & QP Studies with strongly anistotropic th. Cond.
and with strong TCS variation inside tape/cable
Current redistribution
e.m. model of J. Van Nugteren, U.T. & CERN
Tampere TUT. J. Ruuskannen
Thu-Af-Po4.09-09,

## Slide 14: FeatherM0.4
Computation showed little time to react to a quench: 20-30 ms:
Quench detection.
Improved voltage taps ( 1 mV)
Array of temp. sensors
Pick-up coil array
Fiberglass in Bragg grating
12.8 kA, cable qualified

## Slide 15: FeatherM2 construction: a complex assembly

## Slide 16: Manufacturing the Eucard2 first dipole FeatherM2
Courtesy of Glyn Kirby

## Slide 17: FeatherM2 AB block dipole construction

## Slide 18: Joints
Classical butlap joint in FM0.4:
>100 n!  40 n
New design, called Fin block joint (G. Kirby).
Improvement by a factor 2, no need of overcooling: do we need it? Certainly it helps to transfer current more uniformly…

## Slide 19
First accelerator-class magnet before going to test:
The Eucard2 FeatherM2.1-2 dipole
April 2017.

## Slide 21
WP1
Project Management and Technical Coordination
WP2 Frascati – Magnetic Measurement Laboratory
WP3 Genova – Superconducting Cables and Material Laboratory
WP4 Milano LASA – Superconducting Magnets Laboratory
WP5 Napoli – Advanced Instrumentation Laboratory
WP6 Salento – Laboratory for Superconductivity and Magnetism
WP7 Salerno – Test facility for large magnet and superconducting line
WP8 Green Superconducting Line at zero emission
WP9 Energy Saving HTS Magnets for Sustainable Accelerators
The IRIS program of the Italian PNRR

## Slide 22
WP9: 10T 20K Test Station Magnet with Cloverleaf-End Design Sketch
Aperture 80X50 mm 700 mm straight section
B3 B5 geometric field quality
12 mm wide REBCO tape (stack)
1.2 MJ stored energy
10 K temperature margin
11 km of HTS tape (~1 M$)
550 A/mm2 cable current density

## Slide 23: what is the limit of our dream of J?
Non-stabilizer Critical Current Density vs. Applied Field for Superconductors Available in Long Lengths
Changing paradigma:
B =  0kins  Jsupd
with
0.5
d=100 mm
kins = 1
B=6.3 10-2 J
[J] = A/mm2
[B] = T
This means:
10 T -> 160 A/mm2
20 T -> 320 A/mm2
40 T -> 640 A/mm2

## Slide 24: No-insulation (NI) coils
Advantages:
Self-protection
Higher Young’s modulus (Lorentz forces cause less movement)
Higher overall engineering current density (no insulation and less stabilizer)
Disadvantages:
Long charging times
Requires more cooling power during ramping since the radial current generates heat
After a quench, the radial current generates new types of forces that can damage the HTS tape
No turn-to-turn insulation
Self-protection: The current can bypass a local quenched part and avoid a local burning
Figure: NI test solenoid produced at CERN;
T H Nes et al. 2022 IEEE Trans. Appl. Superconduc. 32 1-6

## Slide 25: Modeling no-insulation coils
Lumped circuit model: No physical dimensions are considered
Network circuit model: Two physical dimensions are considered
Course network circuit model: One physical dimension is considered (rotational symmetry assumed)
Based on electrical circuit models that considers either 0, 1 or 2 physical dimensions
Couples with models for the temperature and magnetic B-field
Can be expanded to model multi-coil magnets

## Slide 26: Variations of the no-insulation winding technique
Partial insulation (Insulation between selected turns)
Metal insulation (cowound metal tape)
Metal cladding insulation (metal cladding applied to HTS tape surface)
Solder impregnation
Conductive epoxy impregnation
Smart insulation (utilizes the metal–insulator transition of Vanadium(III) oxide)
Varistor insulation (utilizes voltage dependent resistors)
Diffusion bonding (removes contact resistance to obtain predictable turn-to turn resistance)
Aims to control the turn-to-turn resistance and increase mechanical strength

## Slide 27: The HTS Demonstrator Magnet for Space (HDMS) project
Conceptual design of a HTS magnet for the magnetic spectrometer in space ARCOS
Design and manufacture a demonstrator coil AMaSED-2 for the ARCOS magnet
Project webpage: https://knowledgetransfer.web.cern.ch/aerospace/hdms

## Slide 28: AMaSED-2 coil design
Racetrack-like shape, outer dimensions: 480 mm x 256 mm
No-insulation coil
Two cowound HTS tapes (face-to-face)
724 m of 12 mm wide SuperPower HTS tape
Inductance: 46.6 mH
Magnet parameters at Top = 10 K:
Operating current: 2.40 kA
Peak B-field on coil: 9.0 T
Central B-field: 2.7 T
Stored energy: 133 kJ
Notes: AMaSED-2 has a racetrack-like shape and is a small-scale version of a coil from the ARCOS magnet.
The cable will be a tape stack of two HTS tapes. AMaSED-2 requires a total of 750 m of SuperPower HTS tape.
The theoretical maximum engineering operating current density is 2480 A/mm2 at 4.2 K with a peak magnetic B-field of 9.3 T. The coil will be tested at a several different temperatures in the range from 4.2 K to 77 K.
28

## Slide 30: AMaSED-2 completed in October 2021

## Slide 31: AMaSED-2 tested in February 2022
Tested in helium gas at 77 K, 60 K, 40 K, 20 K, and 10 K
Characteristic magnet parameters determined at each temperature
Time constant, radial resistance, and magnet critical current versus temperature.
Maximum achieved B-field in the center (max B0) and on the coil (max Bm) versus temperature

## Slide 32
Conclusion
Dipole field in range of 12-13 T already reached with LTS superconductor. They are heavy magnets (in case of large aperture)
For a spectrometer with 4-5 T·m and 1000-1500 mm length, the actual LTS technology is suitable. Some concerns may be afforded in case of radiation depositions, losses depositions, large forces for large magnet, reduced space availability. Dedicated studies can give reliable solutions.
HTS technology may be a plus for the spectrometer, for energy saving (higher temperature, less consumptions), but strictly is not necessary.
Special dipole dedicated to spin precession in the range of 20 T and bore diameter 20-50 mm for sure requires HTS technology
Now we have HTS program financied for the use of HTS superconductors in dipole for field of 10 T (with insulated cable)
The new technology of non-insulated HTS coil has incredibles potentiability, theoretically with field up to 30 T – 40 T
We hope that this new starting programs will allow to pave the road of HTS, with the possibility to increase the field -> 20 T