## Slide 1: AIDAInnova-WP7.3.2 Industrial engineering of high rate 𝜇-RWELLs
AIDA-Innova General Meeting, CERN - 29th March 2022
G. Bencivenni (LNF-INFN)
on behalf of Bologna-Ferrara-Frascati INFN teams
R. De Oliveira - CERN-EP-DT-MPT Workshop
R. Pinamonti, M. Pinamonti - ELTOS SpA

## Slide 2: Task objectives
Deliverable
D7.3: μ-RWELL prototypes co-produced by industry under the guidance and supervision of the research team. A complete report will be provided (Task 7.3)
Milestone
MS27: Build a 0.3×0.3 m2 prototype and the readout plane with the new structure

## Slide 3: The μ-RWELL (reminder)
The μ-RWELL is a resistive MPGD composed of only two elements:
μ-RWELL_PCB
Cathode
The μRWELL_PCB realized by coupling the resistive grounded amplification stage with the readout PCB through a thin prepreg foil
1
2
3
a resisitive DLC layer(*) (Diamond-Like-Carbon), with ρ~10÷100 MΩ/□
1
a WELL patterned kapton foil (with a Cu-layer on the top) acts as amplification stage
2
3
a standard readout PCB with pad/strip segmentation
(*) DLC foils are currently provided by the Japan Company – BeSputter

## Slide 4: The road-map: R&D + Engineering
IDEA
CERN prototyping
Layout adj.
Layout design
Engineering
Pilot-run
Process adj.
Manufacturing readiness
R&D loop
Engineering loop
QA/QC
LNF validation tests

## Slide 5: Operative meetings
  21 Sept. 2021 - joint INFN-ELTOS-CERN meeting
  standardizing manufacturing procedures of μ-RWELL layout
1-3 Dec. 2021 - CERN-INFN meeting
  status of the R&D on the High Rate layout
  measurement with high intensity X-ray beam
  2D layout based on the readout of a segmented amplification stage
7–10 Dec. 2021 – 1st test batch in ELTOS
  DLC patterning
  PCB planarizing tests
7–8 Mar. 2022 - 2nd test batch in ELTOS
  PCB planarizing tests
  Kapton DLCed foil coupling with PCB-readout
  Mar. 2022 - joint INFN-ELTOS-CERN meeting
    discussion with Rui about the results obtained

## Slide 6: Manufacturing steps
Step 0 - CERN_INFN DLC sputtering machine @ CERN
  bid concluded
  delivery foreseen end of July 2022 – operational within end of 2022
Step 1 - producing PCB readout for μ-RWELL (pad/strip readout) @ ELTOS
  with top patterned (pad/strip side)
  without patterning bottom layer (connector side)
Step 2 - DLC patterning  two options under investigation:
  photo-resist  patterning with BRUSHING-machine (ELTOS)
  photo-resist  patterning with JET-SCRUBBING-machine (CERN)
Step 3 - DLC foil gluing on PCB  three options under investigation:
  double 106-prepreg, ~2x50m thick (by ELTOS - before 2021)
  PCB planarizing w/early-stripping of suitable prepreg (115°C/15min)  single 106-prepreg (by CERN)
  PCB planarizing w/gap filling with epoxy Taiyo THP-100DX1 VF (screen printing)  single 106-prepreg (by ELTOS - NOW)
Step 4 - Top copper patterning for successive kapton etching to create evacuation vias (by CERN and/or ELTOS)
  Step 5 - Amplification stage patterning: kapton etching  plating  ampl-holes (by CERN)

## Slide 7: Starting point (2017-2020): ELTOS vs CERN
DLCed Kapton foil gluing on PCB
The coupling/gluing is performed through a 106-prepreg foil. Main requirements:
good planarity
minimizing the DLC–readout distance (to maximize the signal amplitude):
  PCB planarizing at CERN + prepreg-106
  different approach implemented in the past in ELTOS with a double prepreg-106
50 um Kapton
48 um 1xprepreg-106
16 um Cu
36 um Cu readout pad
Standard CERN stacking
50 um Kapton
80 um 2xprepreg-106
5 um Cu
48 um Cu readout
Standard ELTOS stacking
pad
strip
50 um
58 um 2xpre-preg
5 um Cu
47 um Cu
Standard ELTOS stacking
CERN reference
to be optimized
almost OK
pad

## Slide 8: Tests in ELTOS (I)
  DLC patterning
photo-resist application/developing  patterning with brushing-machine
while at CERN a different approach, based on a JET-SCRUBBING-machine, is implemented
PCB planarizing
PCB planarizing by filling the gap between pads with epoxy resin Taiyo THP-100DX1 VF (screen printing)  PEM planarizer (POLA&MASSA)
  While at CERN a PCB planarizing w/early-stripping of suitable prepreg (115°C/15min)
1
2
3
1
2
24um
29um
28um
gap filling 24 um
pad 29 um

## Slide 9: Tests in ELTOS (II)
DLCed Kapton foil gluing on PCB w/pressing machine
Press-top
Press-down
Stainless steel plates
pacothane
n.1 Pacoflex(1000)–250 um
PCB-1.6mm
n.1 PANASONIC R-1551W tipo106
DLC-Kapton foil
Main parameters:
pressure 180 N/cm2
temperature 210°C
50 um Kapton
55 um 1xprepreg-106
5 um Cu
18 um Cu readout
Good uniformity & DLC–readout distance close to CERN stackout

## Slide 10: NEXT steps
Production of real μ-RWELL_ PCBs (PEP layout w/pad-readout) in ELTOS
  PCB with pad readout
  PCB planarizing
  DLC patterning
  DLCed kapton foil gluing on PCB
Finalizing μ-RWELL_ PCB at CERN
  Top Cu patterning for DLC grounding vias
  Well patterning by Kapton etching
Comparison of joint ELTOS-CERN PCB _RWELL with one manufactured only at CERN
Start operation of the DLC sputtering facility at CERN (techn. Staff to be trained …)

## Slide 11: Spare Slides

## Slide 12: R&D on the PEP high rate layout
PEP – Patterning-Etching-Plating
grid-like DLC grounding from Cu-top
In the framework of the LHCb phase-2 upgrade, in strict collaboration with CERN (Rui), we are developing the PEP (Patterning-Etching-Plating) high-rate layout.
Similarly to the previous SG layout the PEP is based on a grid-like DLC grounding:
in the SG layout the conductive grid was patterned by etching a Cu-layer deposited onto the DLC film
in the PEP the conductive grid is Patterned on the Cu top layer of the kapton foil, connected with the underlying DLC by means a dense blind-vias first Etched then Plated. In this way the DLC is grounded from the top
Advantages:
no Cu deposition on DLC is required
No fine alignment problem between bottom and top
is required

## Slide 13: PEP-1 layout
6 mm
8 mm
A first high rate PEP prototype, developed for LHCb, has been realized and it has been extensively tested (layout optmization in progress)

## Slide 14: PEP-1 layout performance
The rate capability has been measured by irradiating the detector with 5,9 X-ray with Pb collimators with different spot size. The diameter of collimators was larger than the DLC ground pitch. RCmip > 10 MHz/cm2.
A long-term X-ray irradiation is on-going: the current of the detector electrodes (Itop, Icat) as well as ambient parameters (T, P, RH) are constantly monitored.
Qint.  100mC over all the test period.

## Slide 15: PEP-2 layout (geometry optimization)

## Slide 16: 2D – readout layouts
y strip
x strip
y strip
x strip
x strip y strip
PCB_RWELL w/2D readout
X-Y signal pick-up equalization
DLC-readout distance to be minimized
higher gain (2x) wrt 1D-RWELL
more complex PCB manufacturing
2-stacked 1D-RWELL
common light cathode
easy PCB construction
No high gain required
relatively small increase of material budget (0.6% wrt 0.5% X0)
PCB_RWELL w/segmented top
HV on DLC, safer insulation required
TOP to ground
No high gain required

## Slide 17: 2D – readout layouts study
y strip
x strip
y strip
x strip
x strip y strip
PCB_RWELL w/2D readout
higher gain (2x) wrt 1D-RWELL
more complex PCB manufacturing
X-Y signal pick-up equalization
DLC-readout distance to be minimized
2-stacked 1D-RWELL
common light cathode
easy PCB construction
No high gain required
small increase of material budget
PCB_RWELL w/segmented top
HV on DLC, safer insulation required
TOP to ground
No high gain required
Options investigated for RDFCC & CLAS_12-JLAB

## Slide 18: Summary and Outlook
The activity of WP7.3.2 task proceeds on two parallel paths:
the industrialization of some construction procedures of the µ-RWELLs at the ELTOS company (Arezzo - IT), in close collaboration with the CERN-EP-DT-MPT Workshop (Rui):
  good results obtained on several manufacturing steps
  planning the production of high-rate PCB-RWELLs with some construction steps carried out by ELTOS
  kapton etching (+ …) performed at CERN
the R&D with CERN on the high-rate layouts is focusing on different items:
  Design/optimization of the new PEP layout
  prototypes characterization at LNF (gain, rate capability)
  long-term stability test with high intensity X-rays
  test beam at high rate (PSI) for efficiency in 25 ns time window

## Slide 19: Spare Slides

## Slide 20: Comparison single/double press (LR w/pad readout – 2017 batch)
Single press. Ampl. Hole (ELTOS + CERN)
Double press. Ampl. Hole (ELTOS + CERN)
Double press. stackout (ELTOS + CERN)
Single press. stackout (ELTOS + CERN)
70 um
32 um
108 um
108 um
77 um
53 um
5 um Cu
5 um Cu

## Slide 21: Low-rate (RDFCC) vs PEP -1 (LHCb)
RDFCC Low-rate Ampl. Hole (CERN)
PEP - 1 Ampl. Hole (CERN)
PEP -1 stackout (CERN)
RDFCC Low-rate stackout (CERN)
87 um
66 um
40 um
15 um Cu
80 um
100 um
50 um
52 um
15 um Cu

## Slide 22: PEP-0 vs PEP-1
PEP–0 Ampl. Hole (CERN)
PEP-1 Ampl. Hole (CERN)
PEP-1 stackout (CERN)
PEP–0 stackout (CERN)
80 um
100 um
50 um
52 um
15 um Cu
88 um
102 um
55 um
48 um
15 um Cu
DLC grounding vias
DLC grounding vias

## Slide 23: PEP-1 details
PEP-1 Ampl. Hole (CERN)
PEP-1 stackout (CERN)
PEP-1 DLC grounding-hole plating (CERN)

## Slide 24: The High Rate μ-RWELL concept
Ground
Ground
High Rate
Low Rate
half active area: d
A sort of tassellation with little low rate schemes.
spot size: r

## Slide 25: PCB-RWELL w/2D-readout (stackout optimization)
Top strips: 60um (80)
Bottom strips: 350um (350)
Pitch: 400um (400)
Insulator layer between Top & Bottom readout strips: 25um (50)
DLC resistivity: RAB=40MΩ
Insulating layer between DLC and readout strip:
50um Prepreg+12um Kapton+10um epoxy glue
2D-strip μRWELL
Sector 1能谱
Top layer
Bottom layer
Copper
X-Y equal sharing + signal collection optimization  study by Zhou Yi (USTC) w/Rui (CERN)
strip width geometry
top/bottom
thickness
DLC-readout distance  can be reduced down to 28um for signal optimization
X-Y equal sharing