## Slide 1: 𝜇-RWELLs in LHCb & Nuclear experiments
µ-RWELL GM 21-22 June 2022
G. Bencivenni
DDG – LNF - INFN

## Slide 2: LHCb upgrade II (Run5 – Run6)
Current LHCb apparatus
Phase-2 upgrade apparatus

## Slide 3: LHCb upgrade II (Run5 – Run6)
Detector requirements Run5 – Run6
Rate up to 1 MHz/cm2 on detector single gap
Rate up to 700 kHz per electronic channel
Max input capacitance (double gap) ≤ 100 pF
Efficiency (double gap) > 95% within a BX (25 ns)
Long stability up to 1C/cm2 accumulated charge in 10 y of operation (M2R1, G=4000)
Pad cluster size < 1.2
The Muon system (MWPC+GEM) during Run1 & Run2 (1÷4 x 1032 cm-2 s-1)
exhibited tracking inefficiency, from dead time, at level of 1% in Run1
and 2% in Run2
Proposed solution:
µ-RWELL technology
Detector size & quantity (4 gaps/chamber - redundancy)
R1÷R2: 576 detectors, size 30x25 to 74x31 cm2, 90 m2 det.
R3: 768 detectors, siz 120x25 to 149x31 cm2, 290m2 det.
R4 : 3072 detectors, size 120x25 to 149x31 cm2, 1164 m2 det.
Under discussion the replacing of part of R3

## Slide 4: The μ-RWELL
The μ-RWELL is a resistive MPGD composed of two elements:
μ-RWELL_PCB
Cathode
The μRWELL_PCB is realized by coupling the resistive (grounded) amplification stage with the readout PCB through a thin prepreg foil
1
2
3
a resisitive DLC layer(*) (Diamond-Like-Carbon), with ρ~40÷100 MΩ/□
1
a WELL patterned kapton foil (with a Cu-layer on the top) acts as amplification stage
2
3
a standard readout PCB with pad/strip segmentation
(*) DLC foils are currently provided by the Japan Company – BeSputter

## Slide 5: The low-rate layout
Single Resistive Layer (SRL)
2-D current evacuation scheme based on a single resistive layer
grounding around the perimeter of the active area
limitation for large area: the path of the current towards ground connection depends on the particle incidence point  detector response inhomogeneity  limited rate capability <100 kHz/cm2

## Slide 6: High-rate layouts
Double Resistive Layer
3-D current evacuation scheme
two stacked resistive layers connected through a matrix of conductive vias
Resistive stage grounding through a further matrix of vias to the underlying readout electrodes
pitch of the vias with a density less than 1/cm2
The Silver Grid
simplified HR scheme based on a SRL
2-D evacuation scheme by means a conductive grid realized on the DLC layer
grid lines can be screen-printed or etched by photo-lithography
pitch of the grid lines of the order of 1/cm

## Slide 7
High-rate layouts: performance w/X-rays
Rate capability w/m.i.p.  3 times X-rays
3·105
3·106
3·107
3·108
Mip Flux[Hz/cm2]
3·105
3·106
3·107
3·108
Mip Flux[Hz/cm2]

## Slide 8: High-rate layouts: performance w/m.i.p.

## Slide 9: Limitations of DRL/SG layouts
Both DRL and SG show very good performance, but some practical limitations:
both layouts require for DLC+Cu sputtering technology
The DRL based on double matrix of vias require complex manufacturing
The SG layout is more simple than DRL, BUT a bit critical for the alignment of the conductive grid pattern on DLC wrt the amplification pattern on the top (the well-pattern)
New layouts have been proposed in the last year in order to overcome such limitations, further simplifying the PCB manufacturing of the HR layouts.

## Slide 10: The new PEP HR layout
PEP: Patterning – Etching – Plating
Single DLC layer
Grounding from top by kapton etching and plating
No alignment problems
Scalable to large size
DOCA (Distance of Closest Approach): minimum distance between a grounding line and an amplification channel
ACTIVE AREA 30 x 30 cm2
Cathode PCB

## Slide 11: The PEP performance
Because of the common effort in the scientific community to reduce the F-based components, we are changing the gas mixture to Ar:CO2:iC4H10 68:30:2 and starting the stability measurement
3·105
3·106
3·107
3·108
Mip Flux [Hz/cm2]
Rate capability defined as the rate where a 10% of gain drop is observed.
It shoudn’t affect the detection efficiency once chosen a working point well above the efficiency knee

## Slide 12: Time performance (old measurement)
A first measurement of the time resolution has been done at H8C CERN - NA
The detectors were operated with Ar:CO2:CF4 45:15:40 gas mixture (the same used by GEM @LHCb) and equipped with VFAT2. A saturation due to FEE is visible at high gain
There is room to improve the resolution, improving the FEE

## Slide 13
Time performance

## Slide 14: Technology transfer
μ-RWELL technology transfer
DCL foil production
Detector manufacturing
PCB shipping
Completed μ-RWELL_PCB
shipping
DLC sputtering know-how
EU-project
PCB production
Start
*DLC Magnetron Sputtering machine
co-funded by INFN-CSN1

## Slide 15
2022 – 2023 tentative plans
2022
  9/2022 – delivery 10x10 cm2 PEP-RWELL pad layout (LNF)
  11/2022 – assembly, characterization w/X-ray, long-term test w/Xrays (LNF)
  11-12/2022 – FATIC integration & preliminary test w/cosmics (Bari + LNF)
  7/2022 – discussion about eco-gas mix test with Gas – CERN group (B. Mandelli)
  > 9-10/2022 – start eco-gas mix search/test (CERN + ???)
2023
  10/2022 (or 6/2022) Test Beam of 10x10 cm2 PEP-RWELL pad layout (LNF + Bari)
  Design/production of the M2R1 (20x25cm2) PEP-RWELL pad layout following results on 10x10 cm2 (LNF)
  Electronics … (Bari)
  GIF++ (? CERN + ???)

## Slide 16
Open Problems/possible solutions (?)
CF4 is not an eco-gas, responsible of strong kapton etching observed on GEM detectors (STUDY OF ETCHING EFFECTS ON TRIPLE-GEM DETECTORS OPERATED WITH CF4-BASED GAS MIXTURES, M. Alfonsi et al., IEEE Trans.Nucl.Sci.52 (2005) 2872-2878.)
Old GEM detectors at LHCb will be analysed to check for CF4 etching effects (we can learn from this study)
PEP µ-RWELL irradiated with X-Rays at LNF will be analysed to check for CF4 etching effects
Eco-gas mix for GEM/RWELL (?)
RWELL in LHCb (in principle) needs for fast gas mix (?)
Long-term test of a PEP µ-RWELL irradiated with X-Rays will be started soon with Ar/Co2 gas mix (no CF4)
Defining a safe assembly/testing procedure: DI-washing+electrical hot-cleaning, humidity control in the gas line, detector conditioning (in strict collaboration with Rui)
Replacing FR4 frames with PEEK frames, more expensive BUT not hygroscopic and then compatible with CF4 (eventually only in closed mode)
2D readout still to be investigated: 2x1D or 2D w/top readout … capacitive sharing (by Kondo)
Apart APV25 there is no other user-friendly electronics for testing MPGD (not only RWELL).
For LHCb the Bari group is developing a new ASIC, FATIC (still to be tested)
Other ASIC: VMM3 (?)

## Slide 17: µ-RWELL in HEP/NP & beyond
40 cm
5 cm
1
2
3
2, 4
6
5
7
FCC-ee: the muon system of the IDEA apparatus for a Future Collider
CLASS12 @ JLAB: the upgrade of the muon spectrometer
EURIZON: R&D on IT based on cylindrical micro-RWELL for a SCTF
X17 @ n_TOF EAR2: small -TPC for the detection of the X17 boson
UKRI: thermal neutron detection with pressurized 3He-CF4 gas mixtures
TACTIC @ YORK Univ.: radial TPC for detection of nuclear reactions with astrophysical significnace
URANIA-V: funded by CSN5 for neutron detection
Muon collider: HCAL R&D

## Slide 18: 3He operated µ-RWELL for thermal neutron detection
Aim
Neutron scattering applications
Small area (100x100mm2)
High Efficiency(>70% at 25meV)
High Position resolution (<0.5mm FWHM)
Stopping gas to stop the range of the proton and triton of the reaction
n + 3He  1H + 3H + 770 keV
Measurements of the gain with a gas mixture containing 1 bar of 3He and 1 to 6 bar of CF4
To date only MWPC and MSGC could operate at those gas pressures
Setup
50x50 mm2 active area
Active volume 16mm thick
Sealed vessel
(up to 7bar pressure)
Neutrons from AmBe Source
R. Hafeji
D. Raspino
E.M. Schooneveld
N.J. Rhodes

## Slide 19: μ-RWELL for TACTIC (TRIUMF)
TRIUMF Anular Chamber for Tracking and Identification of Charged particles
Active-target detector with cylindrical geometry to study nuclear reactions with astrophysical significance
Aims at efficient small reaction cross-section measurements at low E
Exploiting μ-RWELLs in a curved cylindrical geometry for detection of various reactions of interest with a range of energies (tens keV to few MeV)
Length of detection region (shaded yellow): 251.9 mm
Radius: 53 mm
μ-RWELLs are currently installed inside the apparatus and first alpha signals were seen. Future tests with reference sources and with a stable beam planned
TEST
TPC with planar geometry
Test chamber size: 150 mm x 480 mm x 120 mm
Drift drift gap: 30 mm
μ-RWELL active area dimensions: 35 mm x 251.85 mm; μ-RWELL overall dimensions: 336 mm x 80 mm; Foil thickness: 0.2 mm
Anode is segmented into 60 pads of width 4.2 mm
Designed to test MPGDs and electronics for TACTIC
Ar:CO2; ~103 energy resolution

## Slide 20: Clas12 upgrade @ JLAB
Upgrade phase I: increase luminosity by a factor 2 and improve tracking reconstruction efficiency
  Require additional fast tracking precision layer in the forward region to compensate for drift chamber limitation
Upgrade phase II: Increase luminosity by a factor 10
  Adding several layers to the forward trackers / or replacing drift chambers by fast trackers ➔ MPGD candidate for large area cost effective capabilities
R1
R3
R2
Main efficiency limitation is due to DC occupancy in R1 (up to 3% at high luminosity)

## Slide 21: Clas12 upgrade @ JLAB
R1
R3
R2
Replace tracking planes in DC R1 with MPGD tracker
DC chambers in R1 are made of 2 superlayers, of 6 layers each, and should be replaced with 6 layers of 2D
Requirements
  Tracking resolution: 100
  Timing resolution: 10 ns
  Rate: 100 KHz/cm2
  Low material budget

## Slide 22: Clas12 upgrade @ JLAB
R1 – detector geometry

## Slide 23
2D – readout schemes are being studied in LNF/Rome (synergy w/RDFCC studies)
2 x 1D with common cathode
2D readout: standard X strips on the bottom layer
Y strips on the top layer
Clas12 upgrade @ JLAB
Detectors prototypes will be tested @ CERN test beam run in fall 2022

## Slide 24
2022 – 2023 CLAS12- RM2 tentative plans
2022
  7-8/2022 – delivery 10x10 cm2 PEP-RWELL 1D & 2D w/top readout (RM2 + LNF+ Ferrara)
  9/2022 – assembly, fast characterization w/X-ray (RM2 + LNF + Ferrara)
  10/2022 – joint test beam at CERN (RM2 + LNF + Ferrara)
  > 7/2022 – low mass mechanics simulation and mock-up construction (Ferrara + RM2 + LNF)
  > 7/2022 – 0.8 mm pitch strip simulation w/2021 data set (RM2 + …)
2023
  Design/production of the 50x50cm2 PEP-RWELL 2D layout following results from 2022 TB
  Test beam (?)

## Slide 25: Spare Slides

## Slide 26: LHCb upgrade II (Run5 – Run6)
Detector size & quantity (4 gaps/chamber - redundancy)
R1÷R2: 576 detectors, size 30x25 to 74x31 cm2, 90 m2 det. - 130 m2 DLC
R3: 768 detectors, size 120x25 to 149x31 cm2, 290m2 det. - 414 m2 DLC
R4 : 3072 detectors, size 120x25 to 149x31 cm2, 1164 m2 det. - 1662 m2 DLC

## Slide 27: Starting point (2017-2020): ELTOS vs CERN
DLCed Kapton foil gluing on PCB
The coupling/gluing is performed through a 106-prepreg foil. Main requirements:
good planarity
minimizing the DLC–readout distance (to maximize the signal amplitude):
  preliminary PCB planarizing at CERN + prepreg-106
  different approach implemented in the past in ELTOS with a double prepreg-106
50 um Kapton
48 um 1xprepreg-106
16 um Cu
36 um Cu readout pad
Standard CERN stacking
50 um Kapton
80 um 2xprepreg-106
5 um Cu
48 um Cu readout
Standard ELTOS stacking
pad
strip
50 um
58 um 2xpre-preg
5 um Cu
47 um Cu
Standard ELTOS stacking
reference
to be optimized
almost OK
pad

## Slide 28: Tests in ELTOS (I)
  DLC patterning
photo-resist application/developing  patterning with brushing-machine
while at CERN a different approach, based on a JET-SCRUBBING-machine, is implemented
PCB planarizing
PCB planarizing by filling the gap between pads with epoxy resin Taiyo THP-100DX1 VF (screen printing)  PEM planarizer (POLA&MASSA)
  While at CERN a PCB planarizing w/early-stripping of suitable prepreg (115°C/15min)
1
2
3
1
2
24um
29um
28um
gap filling 24 um
pad 29 um

## Slide 29: Tests in ELTOS (II)
DLCed Kapton foil gluing on PCB w/pressing machine
Press-top
Press-down
Stainless steel plates
pacothane
n.1 Pacoflex(1000)–250 um
PCB-1.6mm
n.1 PANASONIC R-1551W tipo106
DLC-Kapton foil
Main parameters:
pressure 180 N/cm2
temperature 210°C
50 um Kapton
55 um 1xprepreg-106
5 um Cu
18 um Cu readout
Good uniformity & DLC–readout distance close to CERN stackout

## Slide 30: R&D on the PEP high rate layout
PEP – Patterning-Etching-Plating
grid-like DLC grounding from Cu-top
In the framework of the LHCb phase-2 upgrade, in strict collaboration with CERN (Rui), we are developing the PEP (Patterning-Etching-Plating) high-rate layout.
Similarly to the previous SG layout the PEP is based on a grid-like DLC grounding:
in the SG layout the conductive grid was patterned by etching a Cu-layer deposited onto the DLC film
in the PEP the conductive grid is Patterned on the Cu top layer of the kapton foil, connected with the underlying DLC by means a dense blind-vias first Etched then Plated. In this way the DLC is grounded from the top
Advantages:
no Cu deposition on DLC is required
No fine alignment problem between bottom and top
is required

## Slide 31: PEP-1 layout
6 mm
8 mm
A first high rate PEP prototype, developed for LHCb, has been realized and it has been extensively tested (layout optmization in progress)

## Slide 32: PEP-1 layout performance
The rate capability has been measured by irradiating the detector with 5,9 X-ray with Pb collimators with different spot size. The diameter of collimators was larger than the DLC ground pitch. RCmip > 10 MHz/cm2.
A long-term X-ray irradiation is on-going: the current of the detector electrodes (Itop, Icat) as well as ambient parameters (T, P, RH) are constantly monitored.
Qint.  100mC over all the test period.

## Slide 33: PEP-2 layout (geometry optimization)

## Slide 34: 2D – readout layouts
y strip
x strip
y strip
x strip
x strip y strip
PCB_RWELL w/2D readout
X-Y signal pick-up equalization
DLC-readout distance to be minimized
higher gain (2x) wrt 1D-RWELL
more complex PCB manufacturing
2-stacked 1D-RWELL
common light cathode
easy PCB construction
No high gain required
relatively small increase of material budget (0.6% wrt 0.5% X0)
PCB_RWELL w/segmented top
HV on DLC, safer insulation required
TOP to ground
No high gain required

## Slide 35: 2D – readout layouts study
y strip
x strip
y strip
x strip
x strip y strip
PCB_RWELL w/2D readout
higher gain (2x) wrt 1D-RWELL
more complex PCB manufacturing
X-Y signal pick-up equalization
DLC-readout distance to be minimized
2-stacked 1D-RWELL
common light cathode
easy PCB construction
No high gain required
small increase of material budget
PCB_RWELL w/segmented top
HV on DLC, safer insulation required
TOP to ground
No high gain required
Options investigated for RDFCC & CLAS_12-JLAB

## Slide 36: Comparison single/double press (LR w/pad readout – 2017 batch)
Single press. Ampl. Hole (ELTOS + CERN)
Double press. Ampl. Hole (ELTOS + CERN)
Double press. stackout (ELTOS + CERN)
Single press. stackout (ELTOS + CERN)
70 um
32 um
108 um
108 um
77 um
53 um
5 um Cu
5 um Cu

## Slide 37: Low-rate (RDFCC) vs PEP -1 (LHCb)
RDFCC Low-rate Ampl. Hole (CERN)
PEP - 1 Ampl. Hole (CERN)
PEP -1 stackout (CERN)
RDFCC Low-rate stackout (CERN)
87 um
66 um
40 um
15 um Cu
80 um
100 um
50 um
52 um
15 um Cu

## Slide 38: PEP-0 vs PEP-1
PEP–0 Ampl. Hole (CERN)
PEP-1 Ampl. Hole (CERN)
PEP-1 stackout (CERN)
PEP–0 stackout (CERN)
80 um
100 um
50 um
52 um
15 um Cu
88 um
102 um
55 um
48 um
15 um Cu
DLC grounding vias
DLC grounding vias

## Slide 39: PEP-1 details
PEP-1 Ampl. Hole (CERN)
PEP-1 stackout (CERN)
PEP-1 DLC grounding-hole plating (CERN)

## Slide 40: The High Rate μ-RWELL concept
Ground
Ground
High Rate
Low Rate
half active area: d
A sort of tassellation with little low rate schemes.
spot size: r

## Slide 41: PCB-RWELL w/2D-readout (stackout optimization)
Top strips: 60um (80)
Bottom strips: 350um (350)
Pitch: 400um (400)
Insulator layer between Top & Bottom readout strips: 25um (50)
DLC resistivity: RAB=40MΩ
Insulating layer between DLC and readout strip:
50um Prepreg+12um Kapton+10um epoxy glue
2D-strip μRWELL
Sector 1能谱
Top layer
Bottom layer
Copper
X-Y equal sharing + signal collection optimization  study by Zhou Yi (USTC) w/Rui (CERN)
strip width geometry
top/bottom
thickness
DLC-readout distance  can be reduced down to 28um for signal optimization
X-Y equal sharing

## Slide 42: Tentative schedule µ-RWELL in LHCb

## Slide 43
Open Problems/possible solutions (?)
CF4 is not an eco-gas, responsible of strong kapton etching observed on GEM detectors (STUDY OF ETCHING EFFECTS ON TRIPLE-GEM DETECTORS OPERATED WITH CF4-BASED GAS MIXTURES, M. Alfonsi et al., IEEE Trans.Nucl.Sci.52 (2005) 2872-2878.)
Old GEM detectors at LHCb will be analysed to check for CF4 etching effects (we can learn from this study)
PEP µ-RWELL irradiated with X-Rays at LNF will be analysed to check for CF4 etching effects
Eco-gas mix for GEM/RWELL (?)
RWELL in LHCb (in principle) needs for fast gas mix (?)
Long-term test of a PEP µ-RWELL irradiated with X-Rays will be started soon with Ar/Co2 gas mix (no CF4)
Defining a safe assembly/testing procedure: DI-washing+electrical hot-cleaning, humidity control in the gas line, detector conditioning (in strict collaboration with Rui)
Replacing FR4 frames with PEEK frames, more expensive BUT not hygroscopic and then compatible with CF4 (eventually only in closed mode)
2D readout still to be investigated: 2x1D or 2D w/top readout … capacitive sharing (by Kondo)
Low-mass mechanics (Jlab, Eurizon): to be tuned, looking for materials compatible with RWELL DI-washing/hot-cleaning
Apart APV25 there is no other user-friendly electronics for testing MPGD (not only RWELL).
For LHCb the Bari group is developing a new ASIC, FATIC (still to be tested)
Other ASIC: VMM3 (?)