## Slide 1: WP1 Status
Perugia 22/06/2022

## Slide 2: General News
P-i-n devices on Kapton from Nicolas arrived both in Perugia and in Wollongong in two batches
  First batch tested for I/V had no direct current, some channel did not passed the “photovoltaic test”
  Second batch ok from I/V and PV test
  The devices were also tested for bondability yielding negative results.
Good news from the sputtering deposition tests some samples reached 1010 Ω cm resistivity

## Slide 3: I/V characteristics of a p-i-n diode

## Slide 4
Sample | H2 (%) | Ar (%) | Psputtering (mTorr) | Power (W) | Thickness (nm) | Resistivity (Wcm)
# 461 | 5 | 95 | 10 | 500 | 240 | 108
# 463 | 5 | 95 | 10 | 500 | 750 | 107
# 464 | 5 | 95 | 15 | - | - | -
# 465 | 5 | 95 | 7.5 | 500 | 370 | 1010
June 2022
Preliminary sputtering deposition of a-Si:H
First Trial

## Slide 5
7,5 mTorr
10 mTorr
10 mTorr

## Slide 6
Transmission Electron Microscopy Investigation
# 465