## Slide 1: Transients and quantification of Coil Displacement in Accelerator Magnets
Gerard Willering
CERN, TE-MSC
Work done by Marcus Wallin, master student in 2019 CERN and Linköping University
Thesis: EDMS 2254195
https://agenda.infn.it/event/32061/

## Slide 2
Introduction
A quench in superconducting magnets is sometimes preceded by a precursor.
Note that this signal is a generally a filtered signal (300 Hz low-pass) to optimize quench detection.
precursor
Resistive voltage build up (quench)
When measuring during a full ramp of a magnet, we can distinguish sometimes hundreds of these ‘precursors’ without them leading to a quench.
We know that these ‘precursor’ type of events are linked to motion or “mechanical transients” (damped oscillation, accelerometer, acoustic emission sensor, pickup coils).
See seminar by H. Arnestad, https://indico.cern.ch/event/738168/
“Measurement of Electrical and Mechanical Transients in Nb3Sn magnets”, 2018
Intermediate current
Flux jumps
‘precursor’ type of events

## Slide 3
Reminder: Overview of vibrations
When using quench antenna pickup coils, we can map all the mechanical transients longitudinally
Amplitude A
Origin
Each vibration analyzed
Activity mapped
[combination of number and amplitude of the vibrations]
See seminar by H. Arnestad, https://indico.cern.ch/event/738168/
“Measurement of Electrical and Mechanical Transients in Nb3Sn magnets”, 2018

## Slide 4
Example of a ‘random’ slow training MB magnets, with 100 mV precursor.
Further reading:
M. Calvi, Impact of the Mechanical Perturbations on the Performance of the LHC superconducting Dipole Magnets, University of Geneva, PhD thesis, 2004
M. Calvi, et al., Data Analysis of Transient Energy Releases in the LHC Superconducting Dipole Magnets, IMTC conference 2006, Sorrento, Italy.
P. Pugnat, et al., Statistical Diagnosis Method of Conductor Motions in Superconducting Magnets to Predict their Quench Performance, IEEE Trans. Appl. Supercond., Vol 11, No 1, March 2001
P. Pugnat and A. Siemko, Review of Quench Performance of LHC Main Superconducting Magnets, IEEE Trans. Appl. Supercond., Vol 17, No 2, June 2007
M. Calvi, et al., Statistical Analysis of Conductor Motion in LHC Superconducting Dipole Magnets, IEEE Trans. Appl. Supercond., Vol 14, No2, June 2004
M. Calvi, et al., Statistical Analysis of Conductor Motion in LHC Superconducting Dipole Magnets IEEE Trans. Appl. Supercond., Vol 14, No2, June 2004
For LHC MB magnets mainly statistical analysis was done.
Note the use of different words to describe the same phenomenon.
Attempts to predict a magnet quench using these data has not been successful.
Mechanical Perturbations
Quench Precursor
Spike
Transient Energy Release
Conductor Motion
History: Statistics LHC MB magnets

## Slide 5
New in this work
Detailed precision measurements on single spikes for Voltage, Pickup coils and current.
Ignore voltage ‘oscillation’ but focus on integral.
Use the law of conservation of energy
Define a simple physics model to describe mechanical motion qualitatively
Quantify coil motion
precursor

## Slide 6
I
I
Coil 1
Coil 2
Coil 4
Coil 3
Coil 1
Coil 2
Coil 3
Coil 4
differential
absolute
Familiar voltage data as we typically use in presentations/reports:
Differential voltage (C1+C2) – (C3+C4)
Differential voltage is also used for quench detection.
The direct voltage per coil gives additional information.
Example: positive precursor in coil 1 and negative precursor in coil 3 and 4.
Coil voltage measurement
Fresca2. Block coil design. 4 coils, each coil has two layers and 36 to 42 turns per layer.

## Slide 7
Energy calculation
Energy: from voltage measurement
ΔEV_1 = 2.29 J
ΔEV_2 = 0.13 J
ΔEV_3 = -1.37 J
ΔEV_4 = -1.30 J
We know that even 10 µJ to 1 mJ can quench a magnet.
Why does this event not quench the magnet?
Sum of energy is about 0 J → The energy is not dissipated in the coil
Hypothesis → The energy is redistributed due to coil geometry changes
Voltage smoothed &
offset applied
I = 11.7 kA
t0
t1
For reference: Stored energy in this magnet (1/2*L*I^2) is about 4 MJ

## Slide 8: Main assumptions
EV_1 = 2.29 J
EV_2 = 0.13 J
EV_3 = -1.37 J
EV_4 = -1.30 J
Expectations in this case:
Total inductance increases
Total Energy must be conserved:
so magnet current must drop (if faster than PC response)
Redistribution of energy with net increase in coil 1.
Changes in quench antenna pickup coils
Assumptions
Stick-slip is geometry change
Geometry change is inductance change
Outward forces would likely give coil growth.

## Slide 9
Measured current during precursor
Current ramp seems smooth, but we can calculate the deviation of current compared to the linear ramp.
Clear correlation between ‘redistributed energy’ in a ‘precursor’ event and the drops in current.
The power supply has a regulation cycle of 20 to 100 ms and will bring back the current to the requested ramp.
Basic physics:
Conservation of energy
ΔI always negative
→ ΔL positive
→ suggests coil growth

## Slide 10: Quench Antenna pickup coils during precursor
Measurements on FRESCA2 were saturated, so signals cannot be integrated. Measurements for MBHSP 11T are shown.
7 times 3 pickup coils, each 25 cm long.
For this example the A-coils have been used with a direct measurement.
Local effect in quench antenna A5 suggests coil movement is limited to this segment.
Global effect in all other pickup coils: drop in magnet current drops the magnetic field.

## Slide 11: Qualitative summary on measurements of transients
Conservation of energy – no energy deposited
Energy exchange between coils –> Coil geometry change
Current Drop confirmed
Local field change in Quench Antenna
Global field change in Quench Antenna

## Slide 12: Quantification – Modeling with ROXIE

## Slide 13: Quantification – Modeling with ROXIE
Use ROXIE to explore the change in inductance when changing geometry.
Include mutual inductances.
Define the movement modes of interest.
Many thanks to Susana Izquierdo Bermudez for helping set up ROXIE.
Note: There could also be flexing of the coil blocks, or a combination of modes. This has not been investigated.
11T CosƟ
FRESCA2 Block coil
Assumption:
Coil blocks are impregnated and move as one piece.

## Slide 14: How to simulate coil movement
Move part of magnet with various displacements
Calculate field and mutual inductance
Calculated field on a line (quench antenna)
Calculate for several position shifts a it L, B, I and E.
Note: in an 11T single aperture the voltage is measured on the inner and outer layer of both upper an and lower coil.

## Slide 15: Simulation Results – horizontal shift
Simulated movement of entire coil length
 | 10 μm movement
 | 2.73
 | 6.29
 | -6.05
 | -2.97
 | -0.31
 | -4.95E-03
 | -2.88E-03
 | 10 μm movement
 | 2.73
 | 6.29
 | -6.05
 | -2.97
 | -0.31
 | -4.95E-03
 | -2.88E-03

## Slide 16: Normalizing calculated movements
 | 10 μm movement
 | 2.73
 | 6.29
 | -6.05
 | -2.97
 | -0.31
 | -4.95E-03
 | -2.88E-03
 | 10 μm movement
 | 2.73
 | 6.29
 | -6.05
 | -2.97
 | -0.31
 | -4.95E-03
 | -2.88E-03
Normalize result
for all modes
Depending on the mode, the changes in energy, pickup coil and current vary.

## Slide 17: Measurement vs Calculation: Example: 11T model coils
Cosine Theta design

## Slide 18: MBHSP107 example
Gather data from transients and put in same format
40 transients per magnet were analyzed
Voltage
Quench antennas
The 40 events gives a measurement profile:
Blue area contains all transient values
Blue line is the average

## Slide 19: MBHSP107: measurement vs calculation
Angular motion is the most plausible from the studied modes, since the local quench antenna change is positive.
Not a perfect match.
Analyze which profile is matching the measurements the best

## Slide 20: MBHSP109 : measurement vs calculation
Data rather similar to MBHSP107
Angular motion is the most plausible from the studied modes, since the local quench antenna change is positive.
Not a perfect match.

## Slide 21: MBHSP107 vs MBHSP109
Two 11 T model magnets with identical design
Average ‘profile’ rather similar.
A bit more spread in the events of MBHSP109

## Slide 22: Measurement vs Calculation: Example – FRESCA2
FRESCA2 Block coil

## Slide 23: FRESCA2
Single Horizontal or Double Mid Roll have the most characteristics in common with the measurements.
Much larger normalized current drop than expected from any of the motion modes.
Missing direct quench antenna measurement

## Slide 24: Quantifying motion

## Slide 25: Transient Location & Size – 11 T models
MBHSP109
MBHSP107
Dots show transient size
Index is transient number as listed in thesis
Events spread out → indicates cross-section movement
Transients with quench are not necessarily the largest transients.

## Slide 26
Transient Location & Size – FRESCA2
Movements in the middle and where flared ends start

## Slide 27: Movement length – 11T coils
Assume this length moved
Coil near QA 5 moves first, followed by QA 6 and 7

## Slide 28: Movement length
50 cm 11T—max. 10
40 cm FRESCA2—max. 5
Majority much smaller < 1
Off course, if we change the length or the number of turns moving, the displacement length will change accordingly.
If we assume only 1 cable to move (instead of 56 to 80 cables impregnated in one block, the displacement length would be many times larger, and this is deemed impossible.

## Slide 29: Conclusions
Precursors (with significant ∫VIdt in differential voltage) are indeed changes in coil geometry, sometimes leading to a quench, but many times not.
Combining precision measurements and simulations, we can learn something about
- Movement mode
- Displacement length
The size of the precursor (integrated energy displacement) is an important characteristic.

## Slide 30: Possible future work
Only 2D taken into account. 3D calculations are needed for quantifying coil displacement in the magnet head.
The quench antenna pickup coils are mostly used in differential measurement mode, but in direct measurement they give valuable information (We used direct measurements for MQXF magnets)
Looking more often at non-quench data could gives useful insight in magnet mechanics.
Investigate possible coil block changes too, compared to only full block motion investigated now.

## Slide 31: Precursor characteristics for a variety of magnets

## Slide 32: Transient Interpretation Flow Chart
Transient
> 0
~ 0
Damped oscillation?
Single sharp rise followed by decay
Traveling Flux Jump
Coil geometry changed
Impregnation cracking ??
Structural change outside coils??
Localized Flux Jump
Multiple voltage rises, propagation in Quench Antenna
Yes
No
Yes
No
Yes

## Slide 33: MBH – 11T
Example: MBHB-002 (S1)
Reduction of vibration activity while training the magnet.
After thermal cycle small activity.
Conclusion:
Mechanical transients due to structural movements are not an issue for 11T magnets.

## Slide 34: MBH – 11T
Largest precursor: ~5 J
Measured in MBHB-002 in quench 2 at 11.1 kA.
Large precursors only, but not always during training phase of the magnets.
No precursors for quenches at magnet limit.
Differential voltage all quenches in MBH-series

## Slide 35
MQXF-Prototype 1 and 2
No significant precursors during training.
Note: quadrupole configuration has not been investigated and it may change sensitivity of precursor to motion.
No study to movement modes possible/needed without precursors.

## Slide 36
FRESCA2c
Always significant precursor before a quench up to 5 J
Often a double motion: example first in top half (positive) then in bottom half (negative)
Conclusion
Quench limit seems mainly mechanical of origin, so no sign of conductor degradation.
See also: Methods for quench localization and performance diagnostics of Nb3Sn magnets in SM18 https://indico.cern.ch/event/820811/
Study to movement modes gives interesting information.

## Slide 37
eRMC
Sometimes significant precursor before a quench.
Up to 1.5 J
Training stopped at target level.

## Slide 38
RMM
Except for the first quench, always a significant precursor measured.
Training limited by mechanical transients, not conductor degradation.
Largest precursor ~1.5 J
Magnet has a very limited bore, and no quench antenna can be installed to identify displacement mode or location.

## Slide 39
Thank you
TE-MSC magnet seminar contributions on magnet test result interpretation methods
2018, H. Arnestad, G. Willering, Measurement of Electrical and Mechanical Transients in Nb3Sn magnets,
https://indico.cern.ch/event/738168/.
2019, G. Willering, Methods for quench localization and performance diagnostics of Nb3Sn magnets in SM18
https://indico.cern.ch/event/820811/
2021, R. Keijzer, Modelling V-I measurements and characterizing performance degradation in 11T and MQXF magnets
https://indico.cern.ch/event/1025824/
2022, M. Wallin, G. Willering, Transients and Coil Displacement in Accelerator Magnets
https://indico.cern.ch/event/1112725/
Many thanks to the whole team in SM18, always making an effort to get the highest precision measurement.