## Slide 1: Temperature-based quench detection methods via integrated superconducting wires and thermocouple chains
IDSM workshop
April 2023
N. Bykovskiy
H. Bajas
D. Uglietti
P. Bruzzone
K. Sedlak
This work has been carried out within the framework of the EUROfusion Consortium, via the Euratom Research and Training Programme (Grant Agreement No 101052200 — EUROfusion) and funded by the Swiss State Secretariat for Education, Research and Innovation (SERI). Views and opinions expressed are however those of the author(s) only and do not necessarily reflect those of the European Union, the European Commission, or SERI. Neither the European Union nor the European Commission nor SERI can be held responsible for them.

## Slide 2: Outline
Superconducting quench detection wires (SQD)
  State of the art
  Candidate materials
  Experimental demonstration in SULTAN
  Further development
Thermocouple chain
  Detection concept
  First test results
Summary

## Slide 3: Superconducting quench detection wires (SQD)
https://doi.org/10.1109/TPS.2022.3212554
Inductive compensation is not perfect
Slow rise of resistive component in HTS
 How to improve detection sensitivity?
electrically insulated from the main conductor
Electrically insulated from the main conductor, thus operated independently at current ,
In thermal contact with the main conductor:
, assuming
of detection wire T quench,
High voltage along normal zone of the wire due to the absence of low resistivity protection material (copper or silver), and eventually higher operating current ().

## Slide 4: Background
Year | Application | SQD type
2000, 2014 10.1109/77.828253 10.1109/TASC.2013.2286813 | Detector magnets | Nb-Ti wire or foil
2016, 2021 https://cds.cern.ch/record/2228249/files/CERN-THESIS-2016-142.pdf https://patents.google.com/patent/WO2021173216A1 | HTS cables | LTS wires
2019 10.1109/TASC.2019.2900633 | HTS pancakes | Nb-Ti wire
2021 10.1109/TASC.2021.3059602 | CCT coils | Nb3Sn wire
2022 https://doi.org/10.1109/TASC.2022.3171185 | General | LTS wires
2022, 2023 (this work) https://doi.org/10.1109/TASC.2022.3140706 https://iopscience.iop.org/article/10.1088/1361-6668/acb17b | Fusion conductors | Nb3Sn, MgB2, IBS wires

## Slide 5: SQD wires: material selection for fusion conductors
T quench ~15 to 25 K for HTS fusion conductors, thus broad, but still limited choice to fulfill the target
V sqd ~ 1 V/m in order to ensure superior performance
MgB2 wires (not doped)
~2 Ω/m
~14 Ω/m
Cu-Ni matrix
0.5 mm
Nb3Sn wires
SS matrix
0.3 mm
~0.5 Ω/m
~0.3 Ω/m
(after etching)
Internal tin 1.0 mm
Bronze route 0.8 mm
0.5 mm
Iron-based SC wires
~< mΩ/m (Ag and Cu)
Measurements in VTI insert :
 New tool – ‘quench experiment’ in the SULTAN test facility, i.e.
Direct current drive up to 15 kA / 10 V
Temperature from ~5 K up to ~300 K
Helium cooling 1 – 10 g/s at ~10 bar
A pair of 3.6 m-long straight conductors:
https://doi.org/10.1109/TASC.2021.3063997
internal CERNOX

## Slide 6: SQD wires: expected & measured performance
ASTRA2 @12 kA, 10.9 T
SQD integration in the conductor jacket  simple, robust and eventually sufficiently sensitive for the SQD operation at 0.1 A
Conductors for quench experiment in SULTAN:
2 m-long SQD wires
 Summary on conductor stability and quench propagation
https://doi.org/10.1088/1361-6668/acb17b

## Slide 7: Quench experiment on long lengths
Laminated stacked-tape soldered conductor (LASSO)
Task challenges:
HTS conductor development
Ultra-thin SQD wires
Embedded optical fibers
Copper pre-tinning & Cable soldering
Initial Ic reduction ~12% due to self-field effect
By mistake, hard-way deformation at R40  15% Ic drop
Annealed copper to reduce shear stress on ReBCO
Ic bending test at 77 K, self-field

## Slide 8: Quench experiment on long lengths
15 T insert
~1 m
JORDI stand: x-coil dipole
~50 m
SULTAN QE insert: pancake coils
~20 m conductor per coil
* insulated windings
Ultra-thin Nb3Sn SQD wires:
Bronze-route ‘1st stack’ (19 Nb rods in bronze matrix) OD 3.6 mm by JASTEC
  Wire drawing down to OD 0.2 mm by external company and also at EPFL-SPC
Internal-tin etched wire (3000 filaments) OD 0.25 – 0.30 mm by WST
Embedded optical fibers…

## Slide 9: Detection by a twisted pair
Twisted-pair SQD wires in order to enhance cancellation of inductive signal + complete electrical insulation
As an alternative, twisted-pair made of distributed thermocouples?
Conventional thermocouple: response on ΔT only at the ends
 Multiple TC connected in series: response on ΔT along the length
Welded or soldered joints
Continuous response on temperature rise, but discrete sensing locations (i.e. opposite to SQD with continuous spatial sensing at a certain T threshold)
Thermal coupling
V
Twisted pair

## Slide 10: Thermocouple materials
Type K further studied:
+ Chromel Ni90Cr10 – Alumel Ni95Al2Mn2Si1
 OD 0.2 mm, 20 m length procured (10 $/m by a Swiss company, but down to ~0.1 $/m for a km-long order in China)
https://en.wikipedia.org/wiki/Thermocouple

## Slide 11: Test samples
Sample 2:
6-around-1 return wire wrapping (semi-automated)
7 TC joints at 5 cm distance, ~40 cm length in spiral shape
TC joints
Sample 1:
Manual wire twisting
9 TC joints at ~2.5 cm distance, ~25 cm length in spiral shape
Heaters and temperature sensors at 3 locations along the length
TC joints
Heater + CERNOX at each position
‘blind spot’ ? (by symmetry)
2
pos 1
3
Filling port
Test insert:
Central cartridge heater
Impregnation by 62% aqueous glycerol in a steel container

## Slide 12: Voltage response at 77 K and 4.2 K
Voltage response rate (V/K) varies along the length periodically with altering polarity.
Symmetric temperature distribution centered at a blind spot of a symmetric thermocouple chain cannot be detected. In real cases, detection signal is determined by the hottest joint (e.g. see response on the central heater).
Inductive voltage not observed on S2 at ~12 mT/s also using longer integration time (0.1 uV voltage resolution). Assuming negligible inductive contribution, absolute response can be arbitrarily amplified for the desired sensitivity.
Central heater on S1
LN2
LHe
@ LHe
@ LN2
Local heaters on S1 (fired separately)
+12 mT/s
-12 mT/s
S2
S1
Magnet ramp, operation at 4.2 K
V
T1
T2
T3

## Slide 13: Summary
Temperature-based quench detection, nearly immune to mechanical strain and EM noise, is being developed at SPC using superconducting wires and thermocouple chains.
SQD wires can be tuned to a large extent for specific application requirements. Ultimately, one can always use the same sc material for SQD as in the main winding and increase the voltage response by higher current and elimination of low resistivity protection material.
Thermocouple chains offer continuous response on temperature, but long-length manufacturing of a short-segment chain of joints requires further development.
Both can be used in a twisted-pair configuration to exclude electrical contact with the main winding, enhance noise cancellation and allow signal amplification.
THANK YOU FOR YOUR ATTENTION!