## Slide 1: Research on NI HTS Magnet for Quench Simulation, Imitation, Protection, and Detection
Jeseok Bang, Kwangmin Kim, Griffin Bradford, Jonathan Lee, and David Larbalestier
Applied Superconductivity Center
National High Magnetic Field Laboratory
Florida State University
1/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
A portion of this work was performed at the National High Magnetic Field Laboratory, which is supported by the National Science Foundation Cooperative Agreement No. DMR-2128556 and the State of Florida. This work is also supported by the Office of Fusion Energy Sciences Grant DE-SC0022011.

## Slide 2
2/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
Part I. Introduction:
‘Little Big Coil’ Project

## Slide 3: Dream to Reality: High Fields >40 T with NI HTS Magnet
3/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
‘Little Big Coil (LBC)’ framework to explore high fields beyond 40 T
  A stack of 12 double pancake module coils
  Background magnetic field: 31.1 T
  Bore size: 40 mm / cooling mechanism: LHe
LBC1 (40.2 T)
LBC2 (42.5 T)
LBC3 (45.5 T)
LBC4 (44.0 T)—Last Month
Lessons learned from the LBC framework
  Excessive/non-uniform mechanical stress is applied to REBCO CC due to screening current.
  SCS can induce plastic deformation and the consequent magnet quench.
  Slit-edge side and plastic deformation on REBCO CC have a correlation.
  Instrumentation to measure local temperature/voltage/strain is needed.
Now, we are aiming to reach 50 T through the LBC framework!
[ref] S. Hahn et al., “45.5-Tesla direct-current magnetic field generated with a high-temperature superconducting magnet,” Nature, vol. 570, no. 7762, pp. 496–499, 2019
World-record DC field
Slit-edge effect demonstration

## Slide 4: Practical Challenge in Exploring >40 T: LBC1—3 Quench
4/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
Quench @ 40 T (160 A)
Test results of LBC1
Test results of LBC2
Test results of LBC3
Quench @ 42.5 T (200 A)
Quench @ 45.5 T (245 A)
LBC4 also experienced quench at 44 T (not analyzed yet).
We are being trained by LBC1—4 quench data!

## Slide 5
5/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
Part II. Research on Quench:
what we have done and
what we are going to do

## Slide 6: Core Component Technologies to Address Quench Issue
6/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
Detection
Protection
Imitation
Simulation
Voltages
Strains
Temperatures
Vibration
Fields and others
Full-quench
Optimal-quench
Energy transfer
Series-connection
Parallel-connection
Electromagnetics
Mechanics
Thermodynamics
Voltage taps
Strain gauges and others
Thermocouple wires & temperature sensors
Acoustic sensors
Hall sensors & waveguides & optics sensors
Electric heater
Optimized electric heater
Dump resistor & magnetic dam
Local defects & heat source
Selected coil quench or open
Fully-coupled Multiphysics Simulation
Ultimate goal:
  Definition of quench initiation criteria (when, where, why starts?)
  Development of magnet design/analysis program
  Investigation of REBCO CC performance limit

## Slide 7: Research on Quench Detection I: Measurement of Local Voltages, Magnetic Fields, and Temperatures
7/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
Coil mandrel
NI HTS coil (single pancake)
Azimuthal current
Hall sensors
(calibrated)
Radial current
Voltage taps
Six terminals for local voltage measurement
100th turn
200th turn
300th turn
400th turn
1st turn
450th turn
Five terminals for local temperature measurement
100th turn
200th turn
300th turn
400th turn
450th turn
LakeShore
DT-670
Thermocouple wires
10 mm
6 mm
Seven transverse Hall sensors
B1
B2
B3
B4
B5
B6
B7
(>$1000 per each)
6 mm
Three axial Hall sensors
Bcen,1
Bcen,2
Bcen,3
(>$1000 per each)
“Real-time” Monitoring of magnetic fields, temperatures, and voltages in LN2
[ref] J. Bang, S. H. Park, J. Park, G. Kim, J. T. Lee, K. Kim, S. Hahn, and D. C. Larbalestier, “A real-time monitoring system for investigating electromagnetic behaviors of an HTS coil,” IEEE Trans. Appl. Supercond. , vol. 32, no. 6, pp. 1–5, 2022.

## Slide 8: LN2 Test: Measurement of Local Voltages and Fields
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
Charge start
Charge end
The coil was charged up to 100 A with 0.05 A/s, where coil Ic was ~70 A (estimated).
65 A
73 A
81 A
91 A
83 A
Discernible non-linear behaviors were observed.

## Slide 9: Conduction Cooling Test to measure Local Temperatures
9/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
[ref] J. Bang et al., “A customized electric heater to mitigate screening current by optimal control on temperature distribution in a high-temperature superconductor coil,” J. Appl. Phys., vol. 132, no. 18, 2022, Art. no. 183911.
Design, construction, and test
Instrumentation and measurement
Voltage  Temperature
(LakeShore E-type Thermocouple wire)
Feasibility to measure local temperatures confirmed
Not yet proven during the coil/magnet quench

## Slide 10: Research on Quench Detection II: Measurement of Strains at the Outermost Turn of NI HTS Coil
10/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
Small test coil (STC) framework to investigate Ic degradation/Quench of REBCO CC by SCS
Coil parameters | Value
Tape thickness [mm] | 0.045
Tape width [mm] | 4.00
I.R. [mm] | 19.5
O.R. [mm] | 20.4
Hight [mm] | 4.00
Magnet inductance [μH] | 29.95
No. of SPC's turns | 20.00
Total total length [m] | 2.51
Strain gauges (top/bottom)
Periodic one-side edge-wave* (maybe due to SCS) observed
Overstress >0.4%
Flux-flow voltage

## Slide 11: Experimental Results of STC
①
②
③
④
11/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
① Background field test (Time: 0 – 1300 s + 8000 – 9000 s )
② Main test (Time: 1300 – 3500 s)
③ Over current/stress test (Time: 3500 – 5000 s)
④ Post- degradation test (Time: 5000 – 8000 s)
Ox3 magnet was charged only up to 14 T.
Peak strain was 0.15% near the top edge at 14 T.
The measured strain near the bottom edge was negligible.
There was a reasonable agreement with previous STC tests.
STC6 was charged up to 350 A.
Coil voltage spikes and inductive voltage degradation were observed.
The reproducibility of coil behavior was confirmed.
Peak strain was over 0.4%, but no flux flow voltage was measured.
STC6 is charged up to 400 A.
Peak strain is over 0.45% flux flow voltage was measured.
Critical current degradation occurred by excessive stress.
Notable voltage spikes and degradation were not observed.
After critical current degradation, an additional test was performed.
Inductive voltage degradation was observed, compared ② and ④.
Flux flow voltage at the coil current of 300 A.
The reproducibility of coil behavior was confirmed.
: Correlation Confirmed

## Slide 12: Research on Quench Protection: A Customized Electric Heater to Manipulate Local Critical Current
12/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
Key principle: Creation of Pre-determined T(r) using Customized Heater (Thermal Eraser)
Target Temperature: T(r)
Current (A)
Turn (#)
Critical Current
Operating current
Turn (#)
Temperature (K)
Operating temperature
HTS pancake coil
Customized Heater
margin
customized heater

## Slide 13: Instrumentation and Test Apparatus with an In-house Conduction-Cooling System
13/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
Heater current
Thermal Eraser
Hall sensor
Temp.
sensor
Test Coil and Thermal Eraser
Instrumentation
Final Assembly

## Slide 14: Feasibility Demonstration Test: Reasonable Agreement in 𝑻(𝒓) Patterns; Errors in Magnitude
14/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
Turn (#)
71
69
68
67
70
0
200
400
Temperature (K)
100
300
66
65
Target temperature
Measured temperature
64
  Spatially Distributed Temperatures
  Final (measured) Temperature in Test Coil
Temperature (K)
The first turn
The last turn

## Slide 15: Research on Quench Imitation: Preliminary Study with A Stack of HTS Coils Connected in Parallel
15/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
DP 1
DP 6
DP 2
DP 3
DP 4
DP 5
Joint 1
Joint 2
Joint 3
Joint 4
Joint 5
Current lead (in)
Current lead (out)
Conventional coil connection: series
Proposed coil connection: parallel
Ref. Joint
Current bypassing between coils (like no-insulation feature between winding turns), degree of freedom to manipulate coil current in a given coil stack, and feasibility of quench imitation.
What can we demonstrate?
A reference joint resistance of each coil should be measured at preliminary tests (to be used for coil current measurement).

## Slide 16: Experimental Set-up of A Parallel-connected HTS Magnet
16/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
Coil 1
Coil 2
Coil 3
Coil 4
Superconductor current lead (out)
Current Lead (in)
Superconductor current lead (in/out)
Current Lead (out)
Ref. Joints
(intentionally inserted)
Ref. Joints
Each coil current lead (in)
Each coil current lead (out)
Joints (coillead)
Joints (coillead)

## Slide 17: Measurement Results: Non-linear Current and Voltage Behaviors of Individual Coils
17/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
Automatic current bypassing
(measured by a Ref. joint of each coil)
[ref] J. Bang et al., “An HTS magnet with individually controllable coil currents energized by a single power source,” IEEE Trans. Appl. Supercond., vol. 32, no. 4, Jun. 2022, Art. no. 4603005.
Ultimately, we will open a coil in a stack of coils in high fields, and then we will measure I, V, and B.
Feasibility to manipulate coil currents so that to imitate quench confirmed.

## Slide 18: Research on Quench Simulation: FEM-based Model Development for LBC Quench Analysis
18/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
[Conventional] Circuit simulation: Electromagnetics + Thermodynamics coupled
FEM simulation: Electromagnetics + Thermodynamics + Solid-Mechanics coupled (in progress)
  Field/strain/temperature-dependent critical current
  Screening current and the consequent effects
  Field/temperature-dependent contact resistance
Mea.
Cal.
[ref] S. Hahn et al., “45.5-Tesla direct-current magnetic field generated with a high-temperature superconducting magnet,” Nature, vol. 570, no. 7762, pp. 496–499, 2019
To be presented at MT28 Conference in detail:
High Field Magnets - HTS Magnets (3PoA06) session,3PoA06-02, 2023-09-13 14:30 ~ 16:30.

## Slide 19: Discussion and Conclusion: What We Need More?
19/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
Can we define what quench is or when the quench starts in terms of “voltage”?
   Is the critical electric field of 0.1 or 1 indeed “practical” for discussion on quench?
Can we measure local voltages or temperatures without using voltage taps insertion?
  Voltage taps can cause “kinks” in HTS coil exposed to high fields.
Kinks
Can we detect quench with acoustic sensors and waveguides?
  Is it possible to attach the sensors on coils in a limited (small) bore?
Can we do reach 50 T with a superconducting magnet?
  We can do it based on NI HTS and instrumentation/diagnostics technologies!
Can we make an instrument to address/measure local heat dissipation in high fields?
  Helium gas bubbles trapped in liquid helium in a high magnetic field can accelerate local temperature rise, thermal runaway, and the consequent quench.
[ref] H. Bai, S. T. Hannahs, W. D. Markiewicz, and H. W. Weijers, “Helium gas bubble trapped in liquid helium in high magnetic field,” Appl. Phys. Lett., vol. 104, no. 13, Mar. 2014, Art. no. 133511.

## Slide 20
20/20
J. Bang (jbang@asc.magnet.fsu.edu)
ISDM02-2023, Novel quench detection and localization methods, Friday, April 28
Thank you
Q&A