## Slide 1: A CVD diamond detector for (n,α) cross section measurements
C. Weiss 1, 2, G. Badurek 2, E. Berthoumieux 3, M. Calviani 1, E. Chiaveri 1, D. Dobos 1,
E. Griesmayer 4,C. Guerrero 1,E. Jericha 2, F. Kaeppeler 5, H. Leeb 2,T. Rauscher 6, V.Vlachoudis 1 and the n_TOF collaboration
1 CERN, Geneva, Switzerland
2 Vienna University of Technology, Austria
3 CEA Saclay, IRFU, F-91191 Gif-sur-Yvette, France
4 CIVIDEC Instrumentation GmbH, Vienna, Austria
5 Karlsruhe Institute of Technology, Campus Nord, Germany
6 University of Basel, Basel, Switzerland

## Slide 2: Introduction
    CVD diamond as detector material
    The n_TOF experiment at CERN
    10B(n, α)7Li measurement 2011 @ n_TOF, with the prototype detector
    Outlook on future measurements

## Slide 3: CVD diamond as detector material

## Slide 4: CVD diamond as detector material
    Chemical vapor deposition (CVD) diamond is a
    Semiconducting material
        Band gap = 5.5 [eV]
        Energy to create an e--hole pair = 13 [eV]
        typical IV curve (pCVD):
        low leakage current
        sCVD ~ 2E-12
    Particle Interaction with the diamond:
        => Neutrons: nuclear reactions with 12C
      Solid state ionization chamber
Charged particles | Uncharged particles (photons)
Excitation | Photoelectric effect
Ionization | Compton scattering
Bremsstrahlung | Pair production

## Slide 5: CVD diamond as detector material
    Different materials:
      Poly crystalline (pCVD)
      Different charge collection distance
      Single crystalline (sCVD)
      Pulse shapes
grow direction
grown on
non-diamond
Substrate
< 12 cm ∅
< 2 mm thickness
grown on
HTHP diamond
Substrate
~ 1 cm²
< 1 mm thickness
High radiation tolerance
Rapid response (~ ns)
Low dark current

## Slide 6: CVD diamond as detector material
Examples:
Properties are in general not Temperature dependend
Small dark current: Noise comes from the electronics, not the material
Energy resolution sCVD :
  E.Griesmayer et al., CERN BE-Note-2009-028: 0.6 % (22.8 MeV 12C Ions)
  M.Pillon et al., NIM A 640 (2011) 185: 0.3 % (5 – 20.5 MeV Neutrons)
Double pulse discrimination (DPD) vor MIP:
Current Amplifier: CIVIDEC Instrumentation GmbH
    t rise = 180 [ps]
    FWHM (electronic DPD ) = 300 [ps]
  500 μm pCVD with 1V / μm
    DPD = 2 [ns]
  500 μm sCVD with 0.8 V / μm
    DPD = 6 – 9 [ns]

## Slide 7: The n_TOF Experiment

## Slide 8: The n_TOF experiment

## Slide 9: The n_TOF experiment
High
instantenous flux
Wide energy range
Neutron Fluence

## Slide 10: 10B(n, α)7Li Measurement 2011
with the prototype detector

## Slide 11: The CVD Diamond Detector
20 mm
20 mm
Metallization:
In coll.with CEA Saclay
4 pads of 100 nm Al
d = 500 μm

## Slide 12: The Detector Prototype
10B4C sample
PCB structure with diamond
Neutron Beam
Distance Sample to Diamond
d = 0.5 mm

## Slide 13: 10B (n, α) 7Li measurement @ n_TOF
    16.June 2011 – 29.June 2011
    OBJECTIVES OF THE TEST MEASUREMENT :
    Investigate the background level in the region of interest
    Identify aspects to be improved for the future detector
    Investigate the detection efficiency for the (n, α) reaction
Reaction Yield:

## Slide 14: 10B (n, α) 7Li measurement
Neutrons
Detector box with
Sample inside
    Preamplifiers *
Preamplifiers *

## Slide 15: Preliminary Results – TOF Pad 2

## Slide 16: Preliminary Results – Reaction Yield

## Slide 17: Outlook
Intended Measurements

## Slide 18: Proposed Isotopes
keV < En < MeV Candidates:
  33S
  59Ni
  67Zn
  95Mo
  149Sm
En > MeV Candidates:
  16O
  25Mg

## Slide 19: Prototype: Expected Counting rates

## Slide 20: Intended Measurements
2011: Background measurement at PTB Braunschweig
2012: 33S (n, α) 30Si
  30 x 30 [mm2] pCVD diamond detector
  For background reduction: thickness only 250 μm
  33S sample at both sides of detector
  Assembly under Vacuum
Future (2014?):
  Ringdetector with sCVD diamonds
    Elimination of 12C induced background
    Reduction of in-beam γ-ray background at n_TOF

## Slide 21
Thank you for your attention!

## Slide 22: Backup

## Slide 23: Diamond Properties
Property | Diamond | Silicon | 
Band gap [eV] | 5.5 | 1.12 |  Low leakage
Breakdown field [V/cm] | 107 | 3x105 | 
Intrinsic resistivity @ R.T. [Ω cm] | > 1011 | 2.3x105 | 
Intrinsic carrier density [cm-3] | < 103 | 1.5x1010 | 
Electron mobility [cm2/Vs] | 1900 | 1350 |  Fast signal
Hole mobility [cm2/Vs] | 2300 | 480 | 
Saturation velocity [cm/s] | 1x 107 | 0.82x 107 | 
Density [g/cm3] | 3.52 | 2.33 | 
Atomic number – Z | 6 | 14 | 
Dielectric constant - ε | 5.7 | 11.9 |  Low capacitance
Displacement energy [eV/atom] | 43 | 13-20 |  Radiation hard
Thermal conductivity [W/m.K] | ~2000 | 150 |  Heat spreader
Energy to create e-h pair [eV] | 13 | 3.61 | 
Radiation length [cm] | 12.2 | 9.36 | 
Spec. ionization loss [MeV/cm] | 6.07 | 3.21 | 
Aver. signal created / 100 μm [e0] | 3602 | 8892 |  Low signal
Aver. signal created / 0.1 X0 [e0] | 4401 | 8323 | 

## Slide 24: CVD diamond as detector material
sCVD typical pulse shapes: Testbeam Oct.2010 @ n_TOF
Triangular ≈ pCVD signal
Rectangular

## Slide 25: CVD diamond as detector material
Successfully used in various applications, for example:
  CERN: RD42 => ATLAS, CMS, ALICE, LHCb
  CERN: LHC – beam loss monitor => cryogenic applications under investigation at the moment
  Geel: Fission fragment monitor
  CEA: Neutron applications
  Beam position monitors at synchrotrons
  Industrial applications: Cyclotron - Phase monitor
  …

## Slide 26: Preliminary Results – Pad 2
n_TOF
γ –Background - Moderation

## Slide 27: Suggested Isotopes @ n_TOF

## Slide 28: 2012: 33S

## Slide 29: Abstract
In astrophysics, the determination of the optical α-nucleus potential for low α energies has turned out to be a challenge, crucial in understanding the origin of the stable isotopes. Theory still cannot predict the optical potentials required for the calculation of the astrophysical reaction rates in the Hauser-Feshbach statistical model and there is scant experimental information on reactions with α particles at the relevant astrophysical energies. Measurements of (n, α) cross sections offer a good opportunity to study the α channel.
At the n_TOF experiment at CERN a prototype detector, based on the chemical vapor deposition (CVD) diamond technology has been developped for (n, α) measurements. A reference measurement of the 10B(n, α)7Li reaction has been performed in 2011 at n_TOF as a feasibility study for this detector type.
The preliminary results of this measurement and an outline for future experiments will be presented.