## Slide 1: An overview of photosensors testing and DU integration at CAPACITY lab in Caserta
Andrea Simonelli INFN sezione di Napoli
15.11.2022

## Slide 2
Part one:
New measurements on an improved 3" Hamamatsu photomultiplier for the KM3NeT Neutrino Telescope
Part two:
DU integration at CAPACITY LAB

## Slide 3: New measurements on an improved 3" Hamamatsu photomultiplier for the KM3NeT Neutrino Telescope
Andreino Simonelli
INFN-Napoli
on behalf of KM3NeT
collaboration

## Slide 4
Describe the new setup for Quantum Efficiency at INFN-Capacity lab in Caserta
Show the QE measurements and compare the OLD R12199 (cfr. 2018 JINST 13 P05035) to the NEW R14374 PMTs
Describe the special R14374 UBA increased QE PMT under test for possible future improvements
Compare the time characteristics of a 500 set of new R14374 PMT using the Dark box apparatus to the old 3’’ PMT
Conclusions
Summary of part one

## Slide 5: Experimental apparatus at CAPACITY lab of Caserta - INFN
Pico-ammeter Keythley
Power meeter control
Xenon lamp 300 W
Filters wheel
HV power supply
Metallic parabolic collimator
launch monochromatic light in air
Motorised 2d movements
Power meter PD

## Slide 6
Experimental solutions
2D cathode scan is performed by programming the head motion in a comb movement shape.
Custom code to read the Keythley pico ammeter via RS232 with instrument control toolbox.
Cathode at -100 V respect to the first dynode grounded together with all the 9 remaining dynodes and anode in order to collect all possible electrons escaping from the first dynode

## Slide 7
to electrons #
to # photons
Special UltraBialkali 14374
under test, later we will see more details
Method
We acquire a reference power spectrum every ten current spectra and measure PMT current vs Wavelength (use the monochromator scan function) and store it for post processing.

## Slide 8: Former measurements on the R12199 performed at ECAP on a 46 pcs. set

## Slide 9: Comparing former measurements of ECAP with the new ones performed over a set of 200 PMTs

## Slide 10
Small subset comparison :
average values of QE for OLD and NEW pmt by using
THE SAME EXPERIMENTAL SETUP in CASERTA

## Slide 11
Spatial uniformity
By using the 2D stage it was possible to
program and execute the scan of the photocathode.
The central part is less sensitive than the borders where
there is a clear increase, mainly due to reflected light that stimulates the photoelectric emission twice.
NEW PMT QE at 450 nm

## Slide 12: Radial uniformity vs wavelength
E
e
e
Evidences:
The QE is minimal at the center at normal incidence
The inner borders of the PMT “mushroom” is internally coated with a metal sheet (i.e a perfect mirror for all the wavelengths)
This effect is documented by producers but not fully explained
30
15
0

## Slide 13
Radial homogeneity comparison
between old (red) and new (blue) PMTs

## Slide 14
Crystallinity of the Antimony coating plays the fundamental role of improving QE in bialkali photocathodes
A special version of 14374 with increased QE
is under test

## Slide 15: Total efficiency comparison
+41%
A special version with increased QE
is under test
Standard R14374
Special R14374

## Slide 16
A special version with increased QE
is under test
Special R14374

## Slide 17
Dark counts comparison with
standard R14374
Special R14374

## Slide 18
The DARK box apparatus for timing properties measurements
M.C. Mollo et al.
The Dark Box instrument for fast automatic testing of the photomultipliers for KM3NeT
Volume 236 - The 34th International Cosmic Ray Conference (ICRC2015)

## Slide 19
The DARK box apparatus for timing properties measurements
M.C. Mollo et al.
The Dark Box instrument for fast automatic testing of the photomultipliers for KM3NeT
Volume 236 - The 34th International Cosmic Ray Conference (ICRC2015)

## Slide 20
Some Time characteristics of concern
After-pulses: are spurious pulses that appear in the wake of true pulses.
they can limit the number of true pulses that can be registered.
After-pulses have two main causes:
  light emitted by electrodes due to electron bombardment.
  ionisation of residual gas traces.
Dark counts: A small amount of current flows in a photomultiplier tube even when operated in a completely dark state.
  Thermionic emission
  Leakage current
  Photocurrent produced by scintillation from glass envelope or electrode supports
  Ionisation current from residual gases (ion feedback)
The transit-time spread: variations in the single photoelectron transit time

## Slide 21
Overview of the existing equipment
DB
QE
Single photon camera

## Slide 22
After-pulses measurements
between 100 ns and 10 μs

## Slide 23
Delayed pulses
between 15 ns and 60 ns

## Slide 24
Dark counts rate

## Slide 25
Transit time spread comparison
R14374 (new)

## Slide 26: Conclusions of part one
The new QE setup in Caserta is now fully operative
New R14374 shows a better spatial QE uniformity and same QE over wavelength
A comparison between old and new PMT with the same setup is done
The DarkBox is again operative in Capacity lab for PMTs timing characterisation
500 pcs of R14374 PMTs have been measured showing far better timing properties
A dedicated variation to the QE setup is near to completion for QE measurements of the Assembled DOMs

## Slide 27: DU integration at CAPACITY LAB
in Caserta

## Slide 28
The team

## Slide 29
Overview
For M01- 2023 6 DUs are expected: 40, 45, 52, 61, 63, 65

## Slide 30
DU 52
DU 63
DU 61
DU 45
The DU integration LAB
Curious Lello

## Slide 31
DU 45
Opened BM
OT shows 2 DOM missing
OTDR test will occur on 31/10-1/11 with J.W. visiting CAPACITY
We plan to purchase an OTDR tester

## Slide 32
DU 45
OTDR test and fault locator revealed a problem
at 70 meters from the light injection point

## Slide 33
DU 45

## Slide 34
DU 52
Opened BM
OT shows 8 DOM missing
OTDR test will occur on 31/10-1/11 with J.W. visiting CAPACITY
We plan to purchase an OTDR tester

## Slide 35
DU 52

## Slide 36
DU 52

## Slide 37
DU 40
OTDR test
OT

## Slide 38
DU 61
STATUS: P1
BASE CONTAINER

## Slide 39
DU 63
STATUS: P4
BASE CONTAINER

## Slide 40
Other current activities
Damaged spheres NRB on LOMs :
investigations and removal
Modifications
on new LOMs
Caserta LOMS status |  |  |  |  | 
LOM UPI | single hemisphere (position) | full hemisphere (position) | total hemispheres | picture number | needs rubber ?
6.6.2.3/R2/2.8 | 1/18 9/6 |  | 2 | 1.1 1.2 | y
6.6.2.3/R3/1.22 | 15/10 15/4 | 3/16 | 4 | 2.1 2.2 2.3 2.4 | y
6.6.2.3/R3/1.17 | 3/16 18/7 15/10 |  | 3 | 3.1 3.2 | y
6.6.2.3/R1/1.45 (DU 45 on it) | n.a. | n.a. | 5 | 4.1 4.2 4.3 4.4 4.5 | n
6.6.2.3/R2/1.18 |  |  |  |  | y
6.6.2.3/R2/1.15 |  |  |  |  | y
6.6.2.3/R2/1.23 |  |  |  |  | y
TOTAL |  |  | 14 | minor=5 medium=2 large=7 | 
large
medium
medium
minor

## Slide 41: Conclusions for part two
8 DUs deployed
3 DUs in refurbishment
2 DUs in integration
new LOMs modifications ongoing
Broken bentospheres on LOMs classified
  and documented
For M01- 2023 6 DUs are expected

## Slide 42
            General conclusions
The equipment for QE measurements and time properties of the PMTs are fully operative
The measurements obtained are and will be of great importance for the KM3NeT telescope and for the experiments using this kind of photosensors
The DU production process is well established and will expand the production capacity in the next future, for M1 2023 we plan to ship six Due