## Slide 1: Multilayer coatings and their use in spectroscopic applications
Maria Guglielmina Pelizzo, A.J. Corso, P. Zuppella, P. Nicolosi
National Research Council of Italy
Institute for Photonics and Nanotechnologies, Lab. LUXOR
Padova
2nd International Conference Frontiers in Diagnostic Technologies
28-30 Novembre 2011

## Slide 2: What is a multilayer?
Multilayer is a nanostructured stack based on two or more materials
The layer thickness is regulated in such a way that all the reflected component at each interface add in phase
A capping layer (i.e. structure on top of it) can be deposited to improve performances or for protection

## Slide 3: When is it necessary to use a multilayer?
Instruments at normal incidence operating at shorter wavelengths then 30 nm
  Mirrors and gratings for normal incidence configuration spectrograph limited by mechanical constraints, high resolution spectrograph
  Mirrors for spectro-imaging
  Mirrors for EUV Projection systems
  Mirrors for short pulse beam manipulation/spectral selection (using the filter properties without affecting the beam shape)
  Mirrors for short pulse re-shaping

## Slide 4: Applications
Solar observations from space
EUV Large scale facilities
Lithography
Atto-physics
Plasma
Condenser
optic
Collection
optic
Mask
Wafer
Projection
optic

## Slide 5: State of art

## Slide 6: Standing wave in periodic Mo/Si MLs (=13.5 nm)
When the EUV radiation interacts with the ML structure, the superposition of the incident and reflected electromagnetic wave generates a standing wave field distribution in the ML. An aperiodic design allows the regulation of the distribution of this field, attributing specific properties to the ML.
In the case of a quarter wave stack anti-nodes of the standing wave are placed in the absorber material with a consequent high absorption of radiation in the first layer.
In the case of a periodic stack with  = 0.6, anti-nodes of the standing wave are placed in the spacer material with less absorption and consequent deeper penetration of the radiation into the stack.
=0.5
=0.6

## Slide 7: Standing wave distribution in with CL (1)
If on top of the structure a capping layer (CL) is deposited, the maximum of the standing wave coincides with this layer. In case this one is an absorbing material, the radiation is strongly weakened.
For example: 2.3 nm RuO2 on top of 2 nm Mo; total CL thickness is 4.3 nm > dn-a=3.3 nm —> the standing wave anti-node is placed inside the RuO2 layer.
Mo/RuO2 CL
No CL
EUV MLs for lithography or astronomic application in harsh space environment require capping layers

## Slide 8: ML with CL and pre-capping layer(2)
By varying the thickness of the last top layers underneath the capping layer, the standing wave field is shifted; the anti-node is placed outside the CL, obtaining a reduction of the absorbance.
B4C/RuO2 CL
Mo/RuO2 CL
Two layers varied (pre-CL)
Two layers varied (pre-CL)
Structures claimed in patent PCT/EP2007/060477, University of Padova, CNR-INFM, RXOLLC (N.Y. USA), 2007

## Slide 9: Optimization of MLs for EUV lithography
The MF used to maximize the EUV lithographic apparatus flux is
where is the source spectrum, is the reflectivity of the structure, N is number of mirror in the apparatus; in this work we have assumed N=10 and as a source a Sn laser produced plasma
Pelizzo M.G. et al., Optics Express, vol. 16(19), pp. 15228-15237, 2008.
Suman M. et al, Applied Optics. vol. 47(16), pp. 2906-2914, 2008
Structures claimed in patent PCT/EP2007/060477, University of Padova, CNR-INFM, RXOLLC (N.Y. USA), 2007
Mo/RuO2 CL
Mo/Pt CL
Experimental
results
Max gain of total throughput for a 10 mirrors lithographic system with respect to a standard ML:
Aperiodic:118%
Last top layer varied (pre-CL): 109%

## Slide 10: On-going projects
Developement of multilayer mirrors for METIS coronagraph on board of Solar Orbiter ESA mission
Developement of multilayer mirrors for Free Electron Laser applications

## Slide 11: Development of ML for FERMI@ELETTRA
Developement of multilayer mirrors for Free Electron Laser applications
Activity carried on in a collaboration framework with FERMI@ELETTRA
Funded by FONDAZIONE CARIPARO, Research Project 2009-2010

## Slide 12: Why multilayers?
High Gain Harmonics Generation provide a more compact and fully temporally coherent source, control of pulse length and control of spectral parameters.
Thanks to the filter properties, ML can use for selecting proper harmonic, without affecting temporal shape of the beam
Li-Hua Yu DUV-FEL
represents the intrinsic phase shift, and therefore does not have any effect on the pulse
represents the group delay
represents the phase chirping, which can effect the pulse shape
For Mo/Si multilayer optimized for 20 nm third harmonics reflection at 45° incidence angle, for an impulse of =100 fs duration, a delay time of 0.3 fs; in case of four ML mirrors reflections, the delay time is around 1% of the pulse duration

## Slide 13: FERMI@ELETTRA Delay line scheme
Application to: DiProI, LDM, Timer beamline
Key third harmonics wavelength: 6.7 nm, 13.5 nm, 16 nm, 21 nm
Multilayer with high efficiency at the working wavelength (s polarization)
Multilayer with high
Pulse delay:
-1 ps < t < 15 ps without multilayers (achromatic no polarizing dependent)
t up to 1 ns with multilayer

## Slide 14: Structures for 6.7 nm third harmonic selection

## Slide 15: Experimental results
ELETTRA- BEAR
45°
45°

## Slide 16: New Frontier EUV photolithography
From Takamitsu Otsuka, Deirdre Kilbane, John White, Noboru Yugami, Weihua Jiang, Akira Endo, Padraig Dunne, and Gerry O'Sullivan, Rare-earth Plasma Extreme Ultraviolet Sources at 6.5-6.7 nm for Next Generation Semiconductor Lithography, EUVLitho 2010, http://www.euvlitho.com/2010/2010%20EUV%20Source%20Workshop%20Proceedings.pdf:
Our goal: apply the ML concept design developed at 13.5 nm to 6.7 nm, using aperiodic design and the new ML structure obtained.
10°

## Slide 17: Damage of MLs by EUV high energy short pulses
Fig.5
Collaboration with Laser-Laboratorium Göttingen e.V (K. Mann, F. Barusky)
Image at microscope showing the surface of an Mo/Si ML + Ir capping layer damaged by E=2-6 J/cm^2, # of pulses: 1 to 10

## Slide 18: New optical configuration for polarization state control

## Slide 19: Framework
METIS, THE MULTI ELEMENT TELESCOPE FOR IMAGING AND SPECTROSCOPY for the SOLAR ORBITER MISSION (PI: E. Antonucci, INAF Osservatorio Astronomico Torino)
SCORE Sounding rocket – METIS Coronagraph Prototype (PI: E. Antonucci, INAF Osservatorio Astronomico Torino)
GOAL: Full Imaging of the extended corona (1.5 – 3.5 Ro) in EUV (30.4 nm), UV (121.6 nm), and visible light
30.4 nm
121.6 nm

## Slide 20: METIS and SCORE optical design

## Slide 21: METIS Multilayer optics and requirements
MLs have to be deposited on M1, M2 and grating
Mirrors Requirements
  High reflectivity at 30.4 nm, 121.6 nm and in the VIS spectral range for simultaneous observations METIS
  Stability over time LONG TERM MISSION
  Stability to ion-bombardment
  Thermal stability
M1 and M2 are ML coated
MO sun disk rejection mirror
SOLAR ORBITER orbit
ML

## Slide 22: Multilayer prototypes considered
Standard Mo/Si (nominal coating - REF) – R 30.4 nm = 20%
ML with different capping layers (CL) materials (4 different types):
  Mo/Si + CL1 Ir/Mo (R 30.4 nm = 26%)
  Mo/Si + CL2 Ir/Si (R 30.4 nm = 26%)
  Mo/Si + CL3 Ru/Mo (R 30.4 nm = 25%)
  Mo/Si + CL4 W/Si (unstable)
  Corso, Alain Jody; Zuppella, Paola; Nicolosi, Piergiorgio; Windt, David L; Gullikson, E; Pelizzo, Maria Guglielmina, Capped Mo/Si multilayers with improved performance at 30.4 nm for future solar missions, Optics Express, Vol. 19 Issue 15, pp.13963-13973 (2011)
Ir/Si ML (R 30.4 nm = 24%)
P. Zuppella, G. Monaco, A.J. Corso, P. Nicolosi, D.L. Windt, V. Bello, G. Mattei, M.G. Pelizzo, “Iridium/Silicon multilayers for extreme ultraviolet applications in the 20-35 nm wavelength range”, Optics Letters 36(7), 1203-1205 (2011).
SiC/Mg ML (R 30.4 nm = 40%)

## Slide 23: Multilayer prototypes considered

## Slide 24: Multilayer reflectance curve
NSLS – Beamline X24C

## Slide 25: Multilayer prototypes considered

## Slide 26: Four years after….(1)
The amount of degradation seems more related to the structural parameters of the multilayer and the characteristic of the capping layer. In particular:
samples with an Si top layer degraded
samples with a SiC top layer deposited onto the last SiC layer have unaltered performances
samples with varied  ratio show a partial degradation, which can be put in correlation with the thickness of the Mg in the bilayers
 varied
SiC cap
Si cap

## Slide 27: Four years after….(2)
ELETTRA BEAR

## Slide 28: AFM analysis (1)
AFM of reference sample A06012.
AFM of samples with Г varied

## Slide 29: AFM analysis (2)
AFM of samples with SiC additional top layer.
AFM of samples with a Si additional top layer.

## Slide 30: XPS analysis
BEAR – ELETTRA
Sample A06011

## Slide 31: Multilayer prototypes considered
Standard Mo/Si (nominal coating - REF) – R 30.4 nm = 20%
ML with different capping layers (CL) materials (4 different types):
  Mo/Si + CL1 Ir/Mo (R 30.4 nm = 26%)
  Mo/Si + CL2 Ir/Si (R 30.4 nm = 26%)
  Mo/Si + CL3 Ru/Mo (R 30.4 nm = 25%)
  Mo/Si + CL4 W/Si (unstable)
Ir/Si ML (R 30.4 nm = 24%)
SiC/Mg ML (R 30.4 nm = 40%)

## Slide 32: Multilayer prototypes considered
Standard Mo/Si (nominal coating - REF)
ML with different capping layers (CL) materials (4 different types):
  Mo/Si + CL1 Ir/Mo
  Mo/Si + CL2 Ir/Si
  Mo/Si + CL3 Ru/Mo
  Mo/Si + CL4 W/Si
Ir/Si ML

## Slide 33: Reflectance tests prior thermal cycling and proton bombardment
Tests at 30.4 nm (large band) performed at ELETTRA- BEAR beamline + some tests at ALS 6.3.2 Beamline
Tests at 30.4 nm (peak) in Padova, using our grazing incidence facility equipped with an hollow cathode lamp

## Slide 34: Si/Mo ML + CL W instability

## Slide 35: Ir/Si analysis

## Slide 36: SOLO operation environment
SOLO will be the closest mission to the sun
Minimum perihelium will be 0.23 AU
Temperature of MO: 236°
Low energy Ions bombardment
 | At 1AU (in the earth) | average
H+ Density (cm-3) | 8,7 | 25
H+ Speed (km/s) | 468 | 468
Nalpha/Nproton | 0,047 | 0,047
NO6+/Nproton | 0,0003 | 0,0003
NFe10+/Nproton | 8,77 x 10-6 | 8,77 x 10-6
ESA Solar Orbiter Enviromental Specification, Issue2, 2008

## Slide 37: Analysis of SOLO orbit and temperatures determination
The gradient at which the optics will be subjected would be 42° ( 15°) in 14 days
The multilayer will be heated and cooled for 5 time from 20 to 77 °C in a vacuum chamber
Performances will be re-tested after cycling
20°
62°
Active T control

## Slide 38: Thermal cycling
The ML samples have been placed on a substrate holder by clamping them with a stainless steel screw
The have been heating with 3 quartz halogen lamps
5 cycles between 20°C and 77°C have been carried on, with a gradient slope increased by six time in order to compress the time duration of the experiment
The vacuum pressure in chamber was 5x 10-7 mbar at 20 ° C
The experiment lasted about 570 hours (more than 23 days)

## Slide 39: Re-tested reflectance after thermal cycling

## Slide 40: Protons implantation experiment
The ion implantation experiment has been performed at Ion beam implantation in the Forschungszentrum Dresden-Rossendorf in Germany (ex Helmholtz-Zentrum Dresden-Rossendorf) using the LE implanter facility.
The chamber of the LE implantation facility and the ML samples fixed in the support inside the chamber
The vacuum in the chamber during the implantation was lower than 10-7 mbar.
The protons current was measured and integrated in order to evaluate the total dose provided to the samples.

## Slide 41: Reflectance after proton implantation (I)
A witness sample has also been re-tested to verify that non natural aging degradation occurred
CL1 (Ir/Mo)
CL2 (Ir/Si)
3 months exposure dose
1 year exposure dose

## Slide 42: Reflectance after proton implantation (II)
REF
3 months exposure dose
1 year exposure dose
CL3 (Ru/Mo)

## Slide 43: Reflectance after proton implantation (III)
After 3 months
After 1 year
Ir/Si

## Slide 44: Experimental evidences
Mo/Si REF shows an increased R after 3 month; due to C overlayer deposition (XPS); this does not explain change in R observed in other samples
TEM show damage on CL3 Ru/Mo
Pelizzo, M G; Corso, Alain Jody; Zuppella, Paola; Windt, D L; Mattei, G; Nicolosi, P, «Stability of extreme ultraviolet multilayer coatings to low energy proton bombardment», Optics Express, Vol. 19 Issue 16, pp.14838-14844, 2011

## Slide 45: AFM on Ir/Si
AFM of an Ir/Si sample after session A (left) and B (right)
3D-AFM of image B
SPIE paper 8148-32, San Diego 2011

## Slide 46: Anyone interested?
A post-doc position available at CNR-IFN UOS Padova
Please, send your CV to the following address: pelizzo@dei.unipd.it

## Slide 47: Acknowledgements
D. Windt, RXO LLC
D. Cocco, M. Zangrando, F. Parmigiani, FERMI@ELETTRA TS
E. Antonucci, S. Fineschi, Osservatorio Astronomico di Torino
A. Giglia, N. Mahne, S. Nannarone, BEAR Beamline, ELETTRA TS
Sh. Akhmadaliev, Institute of Ion Beam Physics and Materials Research Research Center Dresden-Rossendorf
G. Mattei, Unversity of Padova
F. Barusky, K. Mann, Laser-Laboratorium Göttingen e.V
John Seely, Naval Research Laboratory, Space Science Division
Benjawan Kjornrattanawanich, USRA and NSLS, Brookhaven National Laboratory
E. Gullikson, ALS, Berkeley
F. Barusky, K. Mann, Laser-Laboratorium Göttingen e.V
Italian Space Agency (ASI/INAF/015/07/0 and Solar Orbiter - METIS)
Scientific Framework CNR-IFN and ELETTRA Trieste
This work has been supported by the European Community as an Integrating Activity “Support of Public and Industrial Research Using Ion Beam Technology (SPIRIT)” under EC contract no. 227012.
FONDAZIONE Cassa di Risparmio di Padova e Rovigo, Progetti di Eccellenza 2009/2010
COST MP0601 for scientific support