## Slide 1: HASPIDE – WP3 Device Simulations Status Activities & Future Plans
02/02/2023
Tecnologo
0.25
0.65

## Slide 2
2

## Slide 3
The initial activities rely upon the INFN 3D-SiAm background.
The a-Si:H band-gap engineering was codified according to Wollongong studies and the literature.
The a-Si:H material has been implemented within the TCAD environment (bang-gap definition, trap level parametrization, …) (-> a-Si:H.par)
Different carriers’ mobilities models have been developed and implemented within the TCAD as external add-on PMI (Physical Model Interface) (.c)
An extensive comparison between measurements (test structures) and simulations has been carried out, aiming at validation and optimization of the modeling scheme.
3

## Slide 4
Charge Transport and Carriers Mobility Models
An extensive acvitity has been devoted to the modeling of the charge transport within the a-Si:H, relying on standard transport equations for monocrystlline silicon - drift-diffusion (DD) approximation and using a custom defined charge mobility, looking at the current-voltage responses at different temperatures.
4
  Custom mobility model (PMI)
  Embedded Transport Models (DD, TD, HD)
m
n
= Electric Field
= Potential
= Temperature

## Slide 5
5
Current vs. Voltage Simulations @ mobilities models
Current vs. Voltage Simulations vs. Measurements
Model validation: Simulations vs. Measuremens (I-V)
The effects of changing the exponents of V and T have been studied.
Notes: Immagine a sx Na=0 (intrinsic). Immagine a dx Na=4e15 cm-3

## Slide 6
I-V @T ok
I-T @ Voltage…
6
Model Predictivity….

## Slide 7
I-V @T ok
I-T @ Voltage…
7
Model Predictivity….
(a.u.)

## Slide 8
TCAD Modelling scheme evolution
Area Factor
Capacitance-Voltage simulations:
    small-signal analyses
    comparison with measurements.
a:Si-H: band-gap re-engineering (trap definition  … equivalent donor/acceptor modelling).
    De-activation / wipe out of not effective levels?
  Parametric Analysis: leverages
8

## Slide 9
Area Factor
9

## Slide 10
Capacitance-Voltage simulations
Comparison with measurements (small-signal analyses)
Simulations vs. Measurements
Simulations @ differente frequencies (detail)
10

## Slide 11
a-Si:H.par: Effect of the Traps: Original vs. Simplified model
11
ORIGINAL
SIMPLIFIED

## Slide 12
Model validation: eMobility and current variations (Δμ - ΔI)
Expected mobilities (cm2/Vs) range average μn = 0.1 μp = 10-4
12
T4
Notes: Mobilità calcolate a 40V Na=4e15 cm-3

## Slide 13
Parametric Analysis: leverages on simulations outcomes
Analysis of the Fermi level’s position
Introduction of an “artificial” p-type doping
Optical Generation (additional charge – workaround for large band-gap materials).
Impact Ionization activation
Increase of the (effective) trap concentration
13

## Slide 14
Expected EF values
The intrinsic a-Si:H material has been modeled by considering an “artificial” p-type doping concentration in order to fix the Fermi level’s position within the bang-gap, according to experimental findings.
The activation of the Impact Ionization model (Avalanche) enables a more realistic carrier generation and recombination processes -> more realistic trend of the I-V curves.
14

## Slide 15
Good agreement between measurements and simulations
Accounts for a more realistic traps occupation probability
Increase of the of the Acceptor and Donor trap concentration
15
Notes: La ragione più fisica dell’incremento della concentrazione delle trappole risiede nel fatto che le trappole per come sono definite nel TCAD e per come il TCAD le considera hanno una probabilità di occupazione che sottostima quella reale e quindi è necessario tenere in considerazione un fattore di normalizzazione.

## Slide 16
WP3 Budget & Dissemination
Dedicated WorkStation DELL
Abstract submitted to
16
You will be notified about its acceptance by the chairpersons of symposium you choosed by MARCH 10 at the latest.
2x AMD EPYC 7443 2.85GHz, 24C/48T, 128M Cache (200W) DDR4-3200 2x 16GB RDIMM, 3200MT/s, Dual Rank
Notes: Workstation DELL: - 2x AMD EPYC 7443 2.85GHz, 24C/48T, 128M Cache (200W) DDR4-3200 -2x 16GB RDIMM, 3200MT/s, Dual Rank

## Slide 17
WP3 Future Plans
Additional model improvement (see paper
Introduction of charge selective contacts model.
Study of the active behaviour of the device: TCAD transient analysis (response/charge collection to a single particle stimulus).
17