## Slide 1
MeV-scale simulations and fabrication tests of silicon slot and woodpile-based waveguides for Dielectric Laser Accelerators
Giuseppe Torrisi
giuseppe.torrisi@lns.infn.it
MIniaturised aCceleRatOrs Network
μICRON
On behalf of MICRON collaboration, INFN Comm-V
15th Workshop on Breakdown Science and High Gradient Technology (HG2023) 16–20 Oct 2023 INFN Frascati National Laboratories

## Slide 2
DLA
Co-prop. schemes
Design
Conclusions
schematic overview of the accelerating gradient for different types of accelerators
laser-plasma interaction
[1] R. Joel England et al., Rev. Mod. Phys. 86, 1337-2014
[2] R. J. England, D. Filippetto, G. Torrisi et al; “Laser-Driven Structure-Based Accelerators”,
arXiv:2203.08981 [physics.acc-ph], 2022 White Paper for Snowmass 2021
Topical Group AF06 - Advanced Acceleration Concepts ]
[3]E. Nanni, et al., Nat Commun 6, 8486 (2015).
[4] F. Lemery, et al.” Commun Phys 3, 150 (2020).
AIM of this session:
To examine Novel Schemes to go “beyond the X-band”

## Slide 3
DLA
Co-prop. schemes
Design
Conclusions
schematic overview of the accelerating gradient for different types of accelerators
on-chip optical-wavelength
DLA [1,2]
laser-plasma interaction
[1] R. Joel England et al., Rev. Mod. Phys. 86, 1337-2014
[2] R. J. England, D. Filippetto, G. Torrisi et al; “Laser-Driven Structure-Based Accelerators”,
arXiv:2203.08981 [physics.acc-ph], 2022 White Paper for Snowmass 2021
Topical Group AF06 - Advanced Acceleration Concepts ]
[3]E. Nanni, et al., Nat Commun 6, 8486 (2015).
[4] F. Lemery, et al.” Commun Phys 3, 150 (2020).
AIM of this session:
To examine Novel Schemes to go “beyond the X-band”
This talk
THz-driven
DLW LINAC [2,3]

## Slide 4: Laser particle accelerators: from RF to laser drive – based on the same operating principle
RF cavity (TESLA, DESY)
Conventional linear
accelerator (RF)
Laser-based dielectric
accelerator (optical)
Based on
Peak field limited by
Max. achievable
gradients
(Supercond.) RF cavities
Quartz grating structures
Surface breakdown:
200 MV/m
Damage threshold:
10 GV/m
100 MeV/m
= 0.1 GeV/m
5 GeV/m
= 5 000 MeV/m
Principle: a nearfield scheme generates the required electromagnetic mode to continuously accelerate charged particles in vacuum – the particle is surfing the mode
DLA
Co-prop. schemes
Design
Conclusions

## Slide 5: From Radio Frequencies to Infrared Light
Simple idea: Use scale-invariance of Maxwell equations and shrink down size of particle accelerators by 4 orders of magnitude.
Replace RF power (cm-wavelength) with laser (um-wavelength)
Material properties are frequency dependent -> dielectrics
Beam dynamics challenges
[Rasmus Ischebeck, Structure-based accelerators (e.g. ACHIP) and advanced radiation generation schemes, talk @the 2022 EuroNNAc Italy 18- 24 September 2022] [https://agenda.infn.it/event/28376/contributions/178676/
Parameter | RF | DLA
Power Source | Klystron | laser
Wavelength | 2-10 cm | 1-10 µm
Bunch Length | 1-5ps | 10-100 as
Bunch Charge | 0.1- 4 nC | 1-10 fC
Norm. Emittance | 0.1-1 µm rad | 1-10 nm rad
Rep Rate | 1-1000 Hz | 100 MHz
Material | Metal | Dielectric
Unloaded Gradient | 10-50 MV/m | 1-10 GV/m
DLA typical parameters
DLA Operating Principle
DLA
Co-prop. schemes
Design
Conclusions

## Slide 6: Experiments have demonstrated record gradients and energy gain
gradient
SLAC/UCLA: 0.3 MeV energy gain**
SLAC/UCLA: 0.85 GeV/m*
Geff = 850 MV/m
Kerr
saturation
e-
E0
k0
800 nm
Interaction length > 500 um
pulse front
tilted laser
electron energy spectrum
* D. Cesar et al, Communications Physics 1(4), 1-7 (2018)​​
** D. Cesar et al, Optics Express 26 (22), 29216 (2018)
DLA
Co-prop. schemes
Design
Conclusions
Notes: D. Cesar, S. Custodio, J. Maxson, P. Musumeci, X. Shen, E. Threlkeld, R. J. England, A. Hanuka, I.V. Makasyuk, E. Peralta, K.P. Wootton, and Z. Wu, "Nonlinear response in high field dielectric laser accelerators," Nature Communications Physics 1(4), 1-7 (2018).​​ D. Cesar, J. Maxon, P. Musumeci, X. Shen, R. J. England, K. P. Wootton, and S. Tan, "Enhanced energy gain in a dielectric laser accelerator using a tilted pulse front laser," Opt. Exp. 26 (22), 29216 (2018).

## Slide 7: Limiting Factors for MeV Energy Gain
Laser-electron interaction time
Total structure length
Dynamic effects – over longer lengths, e- will defocus
Extending Structure Length Non-Trivial: Nanofabrication techniques are typically not concerned about long range wafer distortions
[Pietro Musumeci, Accelerator on a chip program overview
invited talk @the 2022 edition of the EuroNNAc European Network for Novel Accelerators La Biodola Bay, Isola d'Elba, Italy 18- 24 September 2022]
https://agenda.infn.it/event/28376/contributions/179636/
[Rasmus Ischebeck, Uwe Niedermayer with contributions by the ACHIP collaboration ”Dielectric Laser Accelerators,” Townhall Meeting High Gradient Acceleration Plasma/Laser 30-3-2021]
Small beam apertures (Wakes, Halo)
Long-distance transport
Focusing and beam transport
Power delivery
Instrumentation and feedbacks
DLA
Co-prop. schemes
Design
Conclusions

## Slide 8
“transverse-illuminated” Phase Reset Device
Laser
beam
[New Acceleration Concepts.
“Dielectric Laser Acceleration”, Joel England (SLAC) Snowmass AF6 Meeting Sept 23, 2020]
low energy gain per stage
(few keV)

short interaction region
(few µm)

Laser
beam
[N. V. Sapra et al; Science, 367, 6473, 79-83 2020]
[E. A. Peralta et al; Nature, 503(7474):91–94, 2013.]
[Kent P. Wootton et al; Opt. Lett., 41(12):2696, 2016]
[D. Cesar et al; Nature Comm. Phys., 1(4):1–7, 2018]
[K. J. Leedle et al; Opt. Lett., 40(18):4344, 2015]
cascading stages of acceleration is
very challenging

Cross-propagating schemes
DLA
Cross-prop. schemes
Design
Conclusions

## Slide 9: This talk
Hollow-core waveguides for high power handling
Collinear co-propagating laser and particle beam
High interaction impedance Zc and accelerating gradient
Continuous wave (CW) laser operation (1-5 µm)
DLA high-Q photonic-crystal cavity
[courtesy of C2N]
Laser
beam
[G. S. Mauro et al., " in IEEE MTT, 68, 5, 1621-26, 2020]
[G. S. Mauro et al;. 15th Metamaterials Conf. (Aug. 2021)]
[Ziran Wu et al; Phys. Rev. ST Accel. Beams 17, 081301
Co-propagating/Collinear schemes
DLA
Co-prop. schemes
Design
Conclusions
Laser
e-beam
Ez
Laser
e-beam
Ez
laser power flow propagates in the same direction as the electron beam
co-propagation designs have the potential to increase the interaction length between electrons and the laser beam.

## Slide 10: side-pumped configurations Power Delivery
pulsed Laser
Particle
quasi-1D topology, based on hollow-core waveguides
reaching a final energy scales linearly with the structure length L
require a complex 2D feeding network with a large footprint proportional to L2
the input facet becomes a bottleneck for damage and nonlinear effects
Dispersion Management is needed
CW collinear hollow-core scheme Power Delivery
CW Laser
Particle
[Tyler W. Hughes et al. Phys. Rev. Applied, 9:054017, 2018]
CW DRAWBACKS:
Power Losses
Efficiency
Copropagating schemes
Cross-propagating schemes
vs
DLA
Co-prop. schemes
Design
Conclusions

## Slide 11
DLA
Co-prop. schemes
Design
Conclusions
In silicon:
Kerr nonlinearity
For example, at 2 µm, the Kerr nonlinear coefficient of 7.62 m2/W would result in a refractive index variation of 0.4% for large power (200 W). it can be considered and addressed.
2. two-photon absorption (TPA).
TPA phenomenon, that leads to a prohibitively high losses. Multiple options can be explored to mitigate the effects of
TPA. The pump wavelength can be slightly changed to take advantage of the fact that silicon exhibits no TPA beyond 2.2 μm.
CW DRAWBACKS
[DOI: 10.1515/nanoph-2013-0020 Nanophotonics 2014; 3(4-5): 247–268]
Red bars indicate high-loss wavelength bands for each material

## Slide 12
Copropagating schemes for Dielectric Laser Accelerators
What we mean for schemes?
We require
an optical waveguide that is constructed of dielectric materials
transverse size on the order of a wavelength
supports a mode with speed-of-light phase velocity in vacuum.
Our goal:
  Definition of guidelines for the design of
  optical dielectric accelerating waveguides
R.J. England et al., Dielectric laser accelerators, Rev. Mod. Phys., 2014
DLA
Co-prop. schemes
Design
Conclusions

## Slide 13
For particles that are sub-relativistic, the beam velocity β = v/c changes rapidly as the particle accelerates
One of the Key focus areas identified for scaling to multi MeV energy gains
chirped DLA geometry in which the excited accelerating mode has a phase velocity that increases as nonrelativistic electrons are accelerated (here we use lithography-based structural chirping of chirped DLA geometry)
phase velocity tapered structures:
match the phase velocity of the accelerating wave to the electron beam velocity
DLA
Co-prop. schemes
Design
Conclusions

## Slide 14
3) 3D PhC Woodpile
1) Slot waveguide
2) 2D Photonic Crystal (PhC) waveguide
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile

## Slide 15
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile
each one is different and optimized for a specific region of energy variation

## Slide 16
3) PhC Woodpile
[]
Tapered Slot-waveguide
[]
Tapered Photonic Crystal (PhC) waveguide
[
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile

## Slide 17
3) PhC Woodpile
[]
Tapered Slot waveguide
[]
Photonic Crystal (PhC) waveguide
[
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile

## Slide 18
Slot waveguides
- by inserting a slot within the central part of a Si wire
- consists of two strips of high-index material that enclose a sub-wavelength low-index slot region
Discontinuities of the normal components of the electric field at the high-index-contrast interfaces between silicon area and the slot lead to a partial mode confinement effect within the slot, i.e. within the low-index material
Interface conditions
for the Electric displacement field
normal component
Schematic of a slot waveguide
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile

## Slide 19
[“Design of a tapered slot waveguide dielectric laser accelerator for sub-relativistic electrons”
Zhao et al., Opt. Express 26, 22801, 2018]
tapered slot waveguide DLA structure for sub-relativistic electron acceleration with continuous phase synchronization
It shows 10 keV of energy gain within 30 µm (0.33 GeV/m)
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile

## Slide 20: Synchronicity
Electron traveling with velocity ve(z)
SYNCHRONOUS CONDITION IS FULFILLED WHEN:
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile
For a varying particle velocity, we need a non-uniform slot waveguide
Wave with phase velocity vϕ(z)

## Slide 21: Synchronicity
Electron traveling with velocity ve(z)
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile
For a varying particle velocity, we need a non-uniform slot waveguide
non-uniform slot waveguide
SYNCHRONOUS CONDITION IS FULFILLED WHEN:

## Slide 22: Tapered slot waveguide for sub-relativistic electrons
variation vs. rib width size a
Phase velocity variation along the waveguide
a
a
af
af
“Tapered” Geometry
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile
non-uniform
slot waveguide

## Slide 23: OPTIMUM TAPER PROFILE: Procedure
1) KNOWING THE RELATION
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile

## Slide 24
THE CORRECT TAPER PROFILE CAN BE ACHIEVED BY:
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile
a= 0.44 µm
OPTIMUM TAPER PROFILE: Procedure

## Slide 25
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile
a= 0.44 µm
OPTIMUM TAPER PROFILE: Procedure
THE CORRECT TAPER PROFILE CAN BE ACHIEVED BY:

## Slide 26
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile
Derived optimal taper

## Slide 27: What happens for a uniform (NON-TAPERED) slot waveguide?
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile
PHASE SPACE AT ACCELERATOR’S EXIT
Large Energy spread
No particle in the accelerating RF bucket!

## Slide 28: LINEARLY TAPERED SLOT WAVEGUIDE
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile

## Slide 29: Performance comparison
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile

## Slide 30
Approximate solutions and approximate technique to solve guidance problems in dielectric waveguide –> EFFECTIVE INDEX METHOD
Reducing complexity in electromagnetics problems
The effective index method (EIM) is used to reduce 3D structure to 2D for calculating the propagation constant (or effective refractive index) of a simpler two-dimensional structures in place of the starting complex 3D structure

## Slide 31
The starting 3D problem has a stratification along y
b) The starting 3D structure can be divided in three regions where a 2D problem can be solved to compute the three effective indices: neff1, neff2, neff3, where neff = β/k0 , (β ≡ kz).
c) A 2D simpler problem can be solved having a stratification along x
Effective Index Method (EIM)
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile

## Slide 32: Slot waveguides (“effective index” approximation)
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile
3D REAL
“2D “EFFECTIVE”

## Slide 33: Simplex optimization
Nelder - Mead method
  Local optimum in multidimensional space
    Quadratic taper profile
  Good for nonlinear optimization, but slow convergence rate
    No gradient is calculated!
  Optimization procedure
    NM algorithm chooses and ( is fixed)
    Batch script calls COMSOL to calculate the 2D accelerating field
    Batch script evaluates the objective function
    Repeat until convergence ...
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile
Comparison of the obtained acceleration profile and output energy with the different
optimization strategies.

## Slide 34
Tapered Slotted
waveguide
Tapered PhC waveguide
[
Me & My Lab
DLA
Co-prop. schemes
Conclusions
DESIGN

## Slide 35
1 GV/m
@ P_inj=1 kW
OK
3) Woodpile
[]
1) Slotted waveguide
[]
2) Tapered 2D photonic crystal waveguide
[
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile

## Slide 36
|Ex|
|Ey|
|Ex|
|Ey|
Phase of Ex along x vs.
x
2D photonic crystal waveguide design procedure
TM01-like mode (longitudinal Electric field Ex0)
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile
W

## Slide 37
0.85
0.7774
0.85
0.7774
Phase advancement variation by varying the defect size W
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile
W1
W2
W3

## Slide 38
3) Woodpile
[]
1) Slotted waveguide
[]
2) 2D photonic crystal waveguide
[
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile

## Slide 39
Woodpile
[
Tapered Slotted
waveguide
Tapered PhC waveguide
[
Me & My Lab
DLA
Co-prop. schemes
Conclusions
DESIGN
FABRICATION

## Slide 40: Woodpile waveguide
Composed by a “pile” of rectangular w × h bricks disposed in layers stacked in the vertical direction, each layer rotated of 90° with respect from the layer below, whose centers are distant a period d.
Creating a so called “defect channel”, one or more modes can be trapped inside the defect and thus a waveguide is obtained.
‘Hollow-core’defect channel
Woodpile waveguide
Electric field inside defect channel
G. S. Mauro et al., "Fabrication and Characterization of Woodpile Waveguides for Microwave Injection in Ion Sources," in IEEE Transactions on Microwave Theory and Techniques, vol. 68, no. 5, pp. 1621-1626, May 2020, doi: 10.1109/TMTT.2020.2969395.
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile

## Slide 41
The periodic structure repeats in the stacking direction each four layers, creating a frequency band-gap where the EM propagation is suppressed.
The band-gap can be calculated considering an unit cell with periodic boundary conditions.
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile
frequency band-gap
'Projected' band diagram of the accelerating waveguide, calculated along the defect propagating axis (z axis).
The confined TM01-like mode (red line) is clearly visible.

## Slide 42: hollow-core woodpile coupler
The side-coupler consists of:
a right-angled bend mode converter, from TE10-like launch mode to TM01-like mode suitable for particle acceleration;
an accelerating waveguide whose length can be tuned in order to obtain the final energy.
Wave is injected (and extracted) into the woodpile coupler by using two waveguide splitters (or optical fibers at optical frequencies).
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile

## Slide 43
From the electric field plot along the accelerating waveguide, it can be seen that:
the longitudinal component |Ez| is predominant;
the transversal components |Ex|, |Ey|, are almost equal to zero.
Acc. gradient of 2 GV/m along hollow-core channel with 500 W input power.
hollow-core woodpile coupler
TM01-like mode synchronous with
speed of light @ 193.66 THz.
G. S. Mauro et al; Numerical Simulation of a Hollow-Core Woodpile-Based Mode Launcher for Dielectric Laser Accelerators Appl. Sci. 2022, 12(5), 2609; https://doi.org/10.3390/app12052609
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile

## Slide 44
Inspired by the RF METALLIC counterpart….
hollow-core woodpile coupler
X-band mode launcher
Courtesy of D. Alesini

## Slide 45
Inspired by the RF METALLIC counterpart….
Courtesy of D. Sertore,
Standing-wave, multigap SW cavities-like, woodpile-based accelerating structure
Next step: design of a proper Dielectric cavity coupler.
3-cell SW structure working in the TM010-like mode, λ0 = 5 μm.
woodpile cavities connected by
silicon ‘junction blocks’ of proper length.
superconducting cavities @1.3 GHz
λ0 = 23 cm.

## Slide 46
Preliminary example of sub-relativistic to relativistic PhC-based transition design
Sub-relativistic (0.4 < β < 0.75) Silicon on Silica slotted waveguide
Sub-relativistic to relativistic (0.75 < β < 1)
Silicon triangular lattice PhC accelerating waveguide
E-field plot (back-to-back simulation)
DLA
Co-prop. schemes
Fabrication
DESIGN
TRANSITION
Conclusion

## Slide 47
Slotwg2PhCwg Transition
PIN = 100 W
DLA
Co-prop. schemes
Fabrication
DESIGN
TRANSITION
Conclusion

## Slide 48: Fabrication overview
Me & My Lab
DLA
Co-prop. schemes
Conclusions
DESIGN
FABRICATION
3) PhC Woodpile
[]
Slot waveguide
Photonic Crystal (PhC) waveguide

## Slide 49: Fabrication overview
Me & My Lab
DLA
Co-prop. schemes
Conclusions
DESIGN
FABRICATION
3) PhC Woodpile
[]
Slot waveguide
Photonic Crystal (PhC) waveguide
✓
✓
silicon waveguides can be readily/easliy fabricated from Silicon-on-Insulator (SoI) wafers using standard CMOS (complementary metal-oxide-semiconductor) processes.
Optical lithography and etching techniques are used to form the silicon waveguide.
cost efficient mass production environment for such integrated photonic devices.

## Slide 50: Fabrication overview
Me & My Lab
DLA
Co-prop. schemes
Conclusions
DESIGN
FABRICATION
3) PhC Woodpile
[]
Slot waveguide
Photonic Crystal (PhC) waveguide
✓
✓
silicon waveguides can be readily/easliy fabricated from Silicon-on-Insulator (SoI) wafers using standard CMOS (complementary metal-oxide-semiconductor) processes.
Optical lithography and etching techniques are used to form the silicon waveguide.
cost efficient mass production environment for such integrated photonic devices.
x

## Slide 51
Layer deposition (min. feature size: 450 nm)
General process involves building up the structure layer by layer, using silicon dioxide as a matrix in which silicon features are embedded.
Then, a selective etch is done to remove the silicon dioxide, resulting in a free standing structure of silicon and vacuum.
2. Direct laser writing (min. feature size: 100 nm)
By moving the focus of the laser beam three dimensionally, arbitrary 3D structures can be written into the volume of the material.
Woodpile structure fabrication - overview
C. McGuinness, R.L. Byer, E. Colby, B.M. Cowan, R.J. England, et al., “Woodpile structure fabrication for photonic crystal laser acceleration”, AIP Conf. Proc. 1086 (2009) 1, 544-549, DOI: 10.1063/1.3080965;
I. Sakellari, E. Kabouraki, D. Gray, C. Fotakis, A. Pikulin, N. Bityurin, M. Vamvakaki, M. Farsari, "High-resolution 3D woodpile structures by direct fs laser writing," Proc. SPIE 8456, Nanophotonic Materials IX, 84560E (15 October 2012); https://doi.org/10.1117/12.930155.

## Slide 52
3D printing at the micro- / nano- scale
Two photon polymerization (TPP)
Femtosecond pulsed laser to induce resist polymerization
100x objective
M4D System by Laser nanoFab
TPP setup
Laser nanoFab
Single photon polymerization (standard): lower resolution, surface polymerization
Two photon polymerization (2PP) : higher resolution, polymerization inside volume
DLA
Co-prop. schemes
Conclusions
DESIGN
FABRICATION

## Slide 53
CVD / PECVD deposition of Si
AIM: obtain the designed Dielectric PC structure starting from the TPP printed structure
PECVD
Fabrication of the Si woodpile micrometric structure by covering the polymeric structure obtained by TPP with Si deposited by CVD techniques as
PECVD (a-Si:H)
LPCVD (a-Si:H or polySi)
DLA
Co-prop. schemes
Conclusions
DESIGN
FABRICATION

## Slide 54: 2PP Fabrication
Chemiresistive devices for room-temperature gas sensing applications: from LPs and ICPs to LDHs
Lorenzo Vigna
Sample preparation by drop-casting characterized by solvent evaporation
2PP direct writing, which polymerizes the resin through a fs-laser
Development
54
DLA
Co-prop. schemes
Conclusions
DESIGN
FABRICATION

## Slide 55: 2PP Fabrication
Chemiresistive devices for room-temperature gas sensing applications: from LPs and ICPs to LDHs
Lorenzo Vigna
Drying process by using a CPD instrument
FESEM characterization
55
DLA
Co-prop. schemes
Conclusions
DESIGN
FABRICATION

## Slide 56: Latest Results
56
DLA
Co-prop. schemes
Conclusions
DESIGN
FABRICATION
start

## Slide 57
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile
Conclusion
Dielectric laser accelerators (DLA) represents a significant advancement and promising opportunity for future high gradient accelerators
Co-propagating structures can scale well towards “useful” energies
Successful design and implementation DLA is challenging
The development of a 2D reduced model enables automatic optimization and simplifies the design process
Next steps:
prototype realization
overall numerical study of a co-propagating S2E structure

## Slide 58
MeV-scale simulations and fabrication tests of silicon slot and woodpile-based waveguides for Dielectric Laser Accelerators
MIniaturised aCceleRatOrs Network
μICRON
THANK YOU!
G. Torrisi, A. L. Genre, G. S. Mauro, D. Mascali, S. Quevedo, G.R. Rizzoli, V. Bertana, S. L. Marasso and G. Sorbello
15th Workshop on Breakdown Science and High Gradient Technology (HG2023) 16–20 Oct 2023 INFN Frascati National Laboratories
DLA
Co-prop. schemes
Conclusions
DESIGN
1) Slot waveguide
2) 2D PhC waveguide
3) 3D PhC Woodpile