## Slide 1
Daisuke Satoh, Chief Researcher.
National Institute of Advanced Industrial Science and Technology (AIST)
Tetsuo Abe, associate professor.
High energy accelerator research organization (KEK)
19 Oct 2023, 11:50 – 12:10
Developments of Dielectric-Assist Accelerating structure at C-band and beyond
The 15th Workshop on Breakdown Science and High-Gradient Technology (HG2023)

## Slide 2
【Outline】
Motivation
Operation principle of DAA structure
Proof of principle study
✓Design and fabrication
✓Low power test
✓High power test
Toward improving DAA performance
Research plan
Dielectric assist accelerating structure, DAA

## Slide 3
【Motivation】
Dielectric loaded cavity has potential to become a high Q value and high Zsh
Metallic
cavity
Dielectric resonator
104
105
108
1010
Q0
Normal conductor
Superconductor
Low-loss Dielectric
（Al2O3, MgO etc…）
N. McN Alford, et al., J Eur. Ceram. Soc. 21, 2605 (2001)
Temperature
High
Low
1-order higher Q0@RT
Started the development of a high power efficiency accelerating structure focusing on the low RF loss characteristics of the dielectric.
Dielectric Assist Accelerating (DAA) Structure
【Comparing the Q0 of the metal cavity and the dielectric resonator】

## Slide 4
【 Operation principle of DAA structure】
[1] D. Satoh, et al., PRAB 19, 011302 (2016)
[2] D. Satoh, et. al., PRAB 20, 091302 (2017)
DAA consists of dielectric cylinders and disks with irises which are periodically arranged in a metallic enclosure.
Higher order TM02n mode is used for beam acceleration.
→ Wall loss on conducting surface is drastically reduced in DAA structure
Dielectric cylinder
Dielectric disk
【Conceptual diagram of DAA structure】
TM01 – π mode like
Patent : PCT/JP2016/087683

## Slide 5
【 Mechanism of high-Q0 】
Wall loss on a conducting cylinder: Pwall
Pwall ∝c1 ×|Hθ(c1)| 2
* c1: inner radius of conductive cylinder
【Pillbox cavity】
【DAA structure】
|Hθ(c1)| in DAA structure is almost 1/4 that of pillbox cavity
→ The wall loss on conducting cylinder is drastically reduced !
【Pillbox cavity】
c1 = 0.39λ0
|Hθ(c1)|
|Hθ(rmax)|
= 0.89
【DAA】
c1 = 0.82λ0
|Hθ(c1)|
|Hθ(rmax)|
= 0.23
rmax
rmax

## Slide 6
【 Design and Fabrication of prototype 】
【5 cell DAA structure[2]】
【Cavity parameters[2]】
[2] D. Satoh, et. al., PRAB 20, 091302 (2017)
【Dielectric cells[2]】
【DAA structure assembly[2]】

## Slide 7
【 Low-power test of the prototype 】
Parameters | Designed values | Measured values
f0 (GHz) | 5.7120 | 5.71192
Q0 | 125,000 | 119,314
Qext | 48,803 | 46,246
QL | 35,112 | 33,328
β | 2.56 | 2.58
【Experimental Results[2]】
[2] D. Satoh, et. al., PRAB 20, 091302 (2017)
Zsh = 617 MΩ/m
【Eacc field along beam axis[2]】

## Slide 8
【 High power test of the prototype】
【Test stand @KEK】
Eacc,max = 2 MV/m (@ Tp = 2 μs) achieved.
But, it did not rise to any higher Eacc,max after operating for more than 6×106 shots.
The longer the pulse width, the slower the progress of cavity conditioning and the lower Ez, max was.
Trig.
KL HV
Pfoward
Preflection
【Results】
High power tests were performed with pulse width of Tp = 2 - 7.5 μs.
Multipactor

## Slide 9
【 Diamond like carbon coating on DAA】
DLC coating is known to reduce secondary electron yield while not increasing dielectric losses.
H. Xu et al., PRAB 22, 021002 (2019).
[3] S. Mori, M. Yoshida, D. Satoh, PRAB 24, 022001 (2021)
【Secondary electron yield of MgO and DLC surface】
【Low power test[3]】
Q0-uncoated : 112,000
Q0-DLC(a-C:H) : 113,000
Eacc,max = 11 MV/m (@ Tp = 5.4 μs) achieved.[3]
However, a large breakdown caused irreversible deterioration in accelerator performance.
Chart: Ein (keV)
| 0.6 | 1 | 1.2 | 1.4 | 1.6 | 1.8 | 2
MgO | 4.5 | 4.2 | 5 | 4.5 | 4.6 | 4.1 | 4.3
a-C:H on MgO | 1.4 | 1.3 | 1.01 | 1.03 | 0.9 | 0.85 | 0.75 | 0.71 | 0.675
【DLC coated dielectric cell & DAA structure】
Maintaining a high Q0 value !
Succeeded in significantly reducing SEY of MgO !
【High power test of DLC-DAA structures[3]】
DLC, Tp = 5.4 μs
DLC, Tp = 0.5 μs
bare, Tp < 2.5 μs

## Slide 10
【 Toward improving DAA performance】
【 Dielectric cells after high power tests 】
Discharge traces were observed on the edge and surface of the dielectric disk and on the outer wall surface of the dielectric coaxial structure.
A deep understanding of discharge phenomena in these points of DAA structures is important for higher gradient.
Chart: Hydrogen Contents (at. %)
| 0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 100
a-C
a-C:H
GLC
PLC
Previous work
New work
Diamond
Graphite
CVD
Ion gun
【DLC film forming equipment】
【 Optimization of DLC coating】
Ref [3]

## Slide 11
【X-band DAA @Nextef2】
High gradient was realized by beam-driven and short pulse dielectric accelerators
●320 MV/m@422GHz, - B.D. O’Shea et al., Nat. Comm. 7, 12763 (2016).
●102 MV/m@X-band, - B. Freemire et al., PHYS. REV. ACCEL. BEAMS 26, 071301 (2023)
→ Short pulse excitation by X-band＋step pulse input → high Zsh + high Eacc
Parameters | MgO
εr | 9.64
tanδ | 6.0×10-6
Frequency | 11.424 GHz
Q0 | 6.55×105
Zsh | 600 MΩ/m
【 Single cell X-band DAA structure】
【 Nextef2/Shield-B@KEK】
Discharge
【 previous study @KEK】
Side-view camera
Observation of discharge occurring in DAA cavities from many point.
Update of the internal structure based on the observation record to achieve higher gradient.
Chart: Time (ns)
Chart: Time (ns)
【 Step-pulse input 】
TM01 mode launcher
DAA
On-axis camera
Acc. structure
Very short pulse

## Slide 12
【 Summary】
We proposed the DAA structure and have been performed a proof-of-principle study.
The DLC coating lowerers the SEY of MgO cells while maintaining a low tanδ. → Eacc,max = 11 MV/m (@ Tp = 5.4 μs)
It is important to understand in detail where and what causes the discharge in the DAA structures in order to further increase the Eacc.
A new research program is currently underway to develop an X-band DAA structures (2023); short pulse excitation of the DAA structures with step-pulse input and monitoring of the discharge inside the cavity is planned for April 2024.

## Slide 13
Thank you for your attention.
【Acknowledgment】
This work has been supported by 【MEXT Development of key element technologies to improve the performance of future accelerators Program】 Japan Grant Number JPMXP1423812204 and Grant in Aid for JSPS Fellows Grant No. 13J08681, 16H02134, 19K20609 and 22684010, .
【Special Thanks】
N. Hayashizaki (Tokyo Thech.), S. Mori, Y. Yamamoto, M. Yoshida, T. Natsui, N. Toge (KEK), S. Miura, N. Shigeoka (MHI), H. Ogawa, Y. Hakuta, H. Mano(AIST)

## Slide 14
Ba(Mg, Ta)O3
(BMT) Ceramics
MgO
【 Improvement of the power efficiency】
【 Optimum dielectric material selection】
【cooling】
Shunt impedance can be improved by 38% compared to the prototype.
6.6×10-7@27K
Parameters | BMT | MgO
εr | 24.2 | 9.64
tanδ | 2.5×10-5 | 6.6×10-7@27K
Acc. type | Standing wave type | 
Acc. Mode | TM02 - π mode | 
Num. of Acc. cells | 5 | 
Frequency | 5.712 GHz | 5.712 GHz
Temperature | 20 ℃ | 27 Kelvin
Q0 | 121,200 | 7.65×106
Zsh | 870 MΩ/m | 3.8 GΩ/m
The cryogenic temperature operating DAA structure is expected to have 6 times higher Q0 and Zsh than that of RT operating DAA prototype.
Under development
BMT sample
[4] D. Satoh et al., Nucl. Instrum. Methods Phys. Res. B, 459, 148 (2019).
14