## Slide 1: An Advanced X-ray Spectromicroscopy of Bi2Se3 Ultrathin Films on SiO2/Si Substrates
M. Azizinia, M. Salvato, M. Amati, L. Gregoratti, R. Parmar, S. J. Rezvani, P. Castrucci and R. Gunnella
High Precision X-Ray Measurements 2023 Conference
19-23 June 2023

## Slide 2: A Brief Introduction
VdW Heterostructures
The use of van der Waals force to assemble low-dimensional materials.
Structures made by stacking different nanomaterials on top of each other (multiple heterojunctions together).
Liu, Yuan et al., Nature Reviews Materials 1.9 (2016): 1-17.
Martanov, et al., Nanomaterials 10.11 (2020): 2305.
Fabrication of heterostructures based on the artificial stacking of 2D materials
PDMS and Pick-up transfer methods
Polydimethylsiloxane (PDMS)
Polypropylene carbonate (PPC)
 All-dry, since no chemical/water is in contact with the flakes.
Fabricated by incorporation of (at least) two distinctive nanomaterials.
Possess merged properties superior to those of the individual counterparts.
2D-2D
Heterostructures

## Slide 3: Bismuth Selenide (Bi2Se3)
Se
Bi
1QL
Layered structure (alternating Bi and Se in the sequence of Se-Bi-Se-Bi-Se) in which five atomic layers are covalently bonded  Quintuple (QL).
Van der Waals interactions between QLs.
Bi2Se3 is known to be a strong 3D topological insulator:
Its bulk is insulating
Conducting surface states (symmetry protected) Prevented charge backscattering
Application in optoelectronic and/or opto-spintronic devices based on Si
Broadband photo detection (ultraviolet (UV) to infrared (IR))
Small band gap (ca. 0.3 eV)
Se vacancies are the most abundant intrinsic defects in Bi2Se3  n-type defects  Fermi level crossing the conduction band
Almost in all the cases reposted, the correct stoichiometry is not achieved.
Image taken from: https://www.ossila.com

## Slide 4
A method by Salvato et al. in 2020.
A two-step physical vapor deposition (PVD) procedure:
1) Deposition of Bi2Se3 nanowires/nanobelts inside a quartz tube,
2) re-evaporating the Bi2Se3, stuck on the inner surface of the quartz tube (plus some pure Se).
The nanofilms with different thicknesses are deposited on various substrates including glass, Si-Pt and Si-Au substrates (for optoelectronic device applications) and to be specific single photon detectors
It is expected that the samples achieved correct stoichiometry.
SiO2
n-Si
Cr
Active window
Pt
Our Samples
Salvato, Matteo, et al. Nanoscale 12.23 (2020): 12405-12415.
Far Downstream Region

## Slide 5
ESCA Microscopy Beamline
Hosting Scanning Photoelectron Microscope (SPEM)
Third generation X-ray source and a beam diameter reduced down to 120 nm High spatial resolution at submicron scale
The overall energy resolution better than 200 meV
Two available measuring modes:
1) Imaging spectromicroscopy  XPS spectra
2) Microspot spectroscopy
A 48-channel hemispherical electron energy analyzer (HEA) mounted at 30° angle with respect to sample surface to collect the emitted photoelectrons
Experimental
Pre-measurement treatments: thermally, in-situ in the preparation chamber at 115 °C overnight under 10−9 mbar ultra-high vacuum,
The incident photon energy 650 eV
Elemental/or chemical distribution maps of the sample surface
Image taken from: https://www.jbarisk.com

## Slide 6
Presence of Si 2s in sample B, as well as, higher Si 2p and O 1s peak The film thickness is different and/or the film on B is not continues
Estimated thickness of the sample A = about 2 nm (i.e. 2QL) due to presence of the Si 2p feature;
Different Bi/Se ratios  Different stoichiometry
Undesired components C 1s and O 1s  due to exposure to air
No other evidence of possible contamination
Broad Spectra of the Bi2Se3 Films

## Slide 7
More Detailed Spectra
In a general view:
Dissimilarities in Bi 4f core level photoemissions
Resemblance in overall characteristics of the Se 3d core level emissions
A higher intensity of the Bi-O peak in samples A
Larger Si-O component of sample B, indicating a stronger interaction with the Silicon region underneath thinner and less uniform nature of the film .
Binding Energy (eV)
Intensity (counts/s)

## Slide 8
a) Bi 4f and b) Se 3d SPEM images (peak/background, i.e., Chemical
Mapping) of sample A:
Bi and Se are almost homogeneously distributed on the Si oxide substrate
c) Bi 4f and d) Se 3d SPEM images of sample B:
Bi atoms are present only in certain areas, while Se atoms are distributed quite homogeneously.
Se atoms are the first sticking on the Si oxide surface.
SPEM Images

## Slide 9
Bi 4f 7/2 |  |  |  | 
 | Sample A |  | Sample B | 
Peak | Center | FWHM | Center | FWHM
Bi ⁰ | 157.21 | 0.73 | 157.23 | 0.72
Bi-Se | 158.09 | 0.75 | 158.30 | 0.75
Bi-O | 158.91 | 0.86 | 159.08 | 0.86
Bi-O | 159.97 | 0.86 | 160.02 | 0.86
Fitted Peaks and Stoichiometry
Se 3d 5/2 |  |  |  | 
 | Sample A |  | Sample B | 
Peak | Center | FWHM | Center | FWHM
Se-Bi | 157.21 | 0.73 | 157.23 | 0.72
Se ⁰ | 158.09 | 0.75 | 158.30 | 0.75
Intensity (counts/s)
Binding Energy (eV)
Sample A: mainly Bi2Se3, a small percentage of Bi-O and an extremely low presence of Bi ⁰ and Se ⁰
Sample B: larger percentages of Bi⁰ and Bi oxide and a well higher percentage of Se ⁰
Binding energies are comparable with those reported in literature  no charge transfer at the interface with Si oxide surface, which should have been clearly detected for such an ultrathin Bi2Se3 film.
Stoichiometric Ratios X(Bi)/X(Se) | 
Sample A | Sample B
0.65 ± 0.02 | 0.54 ± 0.02

## Slide 10
Confirming the ability of this two-step PVD growth technique to produce stoichiometric Bi2Se3 films
No serious contamination
No charge transfer has been detected between the substrate surface and the Bi or Se atoms
Note: a small fraction of the bismuth oxide formation is due to the interaction of the Bi2Se3 film with environment and substrate
Importance of the position of the substrate inside the quartz tube
Fermi level correctly positioned in the middle of the bulk bandgap as for topological semi conductors
Conclusion
Next…
Building up heterojunctions using Bi2Se3 and different 2D materials e.g. graphene
Exploring the interaction between topology and magnetism by Bi2Se3/ CrCl3 Generation of various novel topological quantum states.
Investigating the interplay between topological insulators and superconductors by Bi2Se3/ NbSe2 junctions