## Slide 1: Update on mechanical structure for the ENDCAP calorimeter

## Slide 2
Status report on:
mechanical properties of LYSO
mechanical structure for EMC forward
Test to measure elastic properties along cut direction.
Non destructive measurement of the elastic module
Via ultrasounds qualitative investigation of crystals
    high anisotropy has been observed
2) Quantitative measurements with
    Laser vibrometer for Laser Doppler Vibrometry (LDV)
    Hammer with charge amplifier
  Measurement of the velocity of the propagation of the perturbation induced by the hammer along the longitudinal dimension of the crystal
  4200m/s --> 131 12 GPa what does it means???
Destructive test are ongoing in these days to study to study resistance to stress
and breaking points.

## Slide 3
It is very important in the simulation of the geometry to take into account the gap between crystals that has to be filled with the structure.
Deformation of the structure < gap between edge of the crystal and structure itself
It is possible to build CFC structure 100um thick
If structure is 1/10 mm  tolerance 1/100 mm
Same or even better tolerance between modules (5x5 crystals) related also to the positioning of the module on the structure.
Geometry now takes into account 400um between crystals and 400um between modules

## Slide 4
Project and design for the module of the beam test: better to have it of the same dimension as in the whole calorimeter (5x5), it can be used ad prototype.
Contact industry for construction of CFC (we can have a list of name)
Simulation of CFC different from other mechanical simulation:
stratification of material and at the same time study of the property of the material and then tuning
Support behind calorimeter in Babar 2.5 cm thick, is this also a mechanical support
for the IFR?
If yes discuss with them the project for the new support.
If APD will be used to read crystals, a study for the thermal control is necessary (cooling system), what about FE electronics in terms of space?