## Slide 1: Investigation of residual nuclide inventory of the storage ring of the Swiss Light Source (SLS)
Roman Galeev, Sophie Harzmann, Eike Hohmann, Lisa Pedrazzi, Sabine Mayer Department of Radiation Safety and Security :: Paul Scherrer Institute (PSI), Switzerland
SATIF-16, May 2024, INFN
Frascati, Italy

## Slide 2: Swiss Light Source
Electron energy: 2.4 GeV
16 operational experimental beamlines
In operation since December 2000
Upgrade since October 2023
Circumference: 288 m
Over 500 beamline components in storage ring
Aim:
  Study of nuclide inventory is necessary for clearance process -> first results are presented
Booster
Storage ring
Bird's-eye view of PSI
SLS tunnel
https://www.synchrotron-analysis.ch
https://www.psi.ch

## Slide 3: Activation of materials at electron accelerators
Considering material composition and previous studies, expected inventory includes:
  Isotopes of Co, Mn, Ni, Fe, V, Cr, Sc, Na
High activation gradient expected in vicinity of beam loss location
Different activation processes for different materials
Electromagnetic shower
Photonuclear reactions
Neutron capture
Activation mechanisms at high energy electron accelerator

## Slide 4: Studies of nuclide inventory
Study is done in 2 main stages:
During operation:
  Pre-study. Dose rate survey (“Hot Spots”)
  In-situ gamma spectrometry (relative)
  Material sampling (absolute)
After shutdown, 6 months of cooling time:
  In-situ gamma spectrometry (relative)
  Material sampling (absolute)

## Slide 5: Studies of nuclide inventory
Study is done in 2 main stages:
During operation:
  Pre-study. Dose rate survey (“Hot Spots”)
  In-situ gamma spectrometry
  Material sampling
After shutdown, 6 months of cooling time:
  In-situ gamma spectrometry
  Material sampling

## Slide 6: Dose rate survey. Hot Spots search
Repeated measurements for 8 years for more than 350 positions
Measured in contact with beam pipe
Background is about 70 nSv/h
Hot spot: dose rate above 100 nSv/h
Hot spot locations are constant
>100 nSv/h after 1 hour
Scheme of SLS

## Slide 7: Studies of nuclide inventory
Study is done in 2 main stages:
During operation:
  Dose rate survey (“Hot Spots”)
  In-situ gamma spectrometry
  Material sampling
After shutdown, 6 months of cooling time:
  In-situ gamma spectrometry
  Material sampling

## Slide 8: In-situ spectrometry at hot spot, 1 hour after shutdown
6 cm
https://www.kromek.com/product/gr1/
Used spectrometer
Spectrometer at measurement position
Energy [keV]
Counts

## Slide 9: In-situ spectrometry at hot spot, 1 hour after shutdown
6 cm
Used spectrometer
Spectrometer at measurement position
https://www.kromek.com/product/gr1/
Energy [keV]
Counts

## Slide 10: In-situ spectrometry at hot spot, 1 hour after shutdown
6 cm
Used spectrometer
Spectrometer at measurement position
Relevant nuclides:
Mn-54
Co-57
Co-58
Co-60
https://www.kromek.com/product/gr1/
Energy [keV]
Counts

## Slide 11: Studies of nuclide inventory
Study is done in 2 main stages:
During operation:
  Dose rate survey (“Hot Spots”)
  In-situ gamma spectrometry
  Material sampling
After shutdown, 6 months of cooling time:
  In-situ gamma spectrometry
  Material sampling

## Slide 12: Material sampling during accelerator operation
Hot spot
Beam direction

## Slide 13: Samples from magnets: screws
9 stainless steel samples from same magnet
Measurements were done with high purity Germanium detector (HPGe)
Measurements results:

## Slide 14: Studies of nuclide inventory
Study is done in 2 main stages:
During operation:
  Dose rate survey (“Hot Spots”)
  In-situ gamma spectrometry
  Material sampling
After shutdown, 6 months of cooling time:
  In-situ gamma spectrometry
  Material sampling

## Slide 15: Features for measurements after shutdown
Measurable activation only in few locations
Limited accessibility
Destructive methods possible
>100 nSv/h after 1 hour

## Slide 16: Features for measurements after shutdown
Measurable activation only in few locations
Limited accessibility
Destructive methods possible
>100 nSv/h after 1 month

## Slide 17: Studies of nuclide inventory
Study is done in 2 main stages:
During operation:
  Dose rate survey (“Hot Spots”)
  In-situ gamma spectrometry
  Material sampling
After shutdown, 6 months of cooling time:
  In-situ gamma spectrometry
  Material sampling

## Slide 18: In-situ spectrometry, 6 months after shutdown
Measurements are done in 5 reachable hot spots
Short living nuclides already decayed
Co-57
Mn-54
Counts

## Slide 19: In-situ spectrometry, 6 months after shutdown
Comparison of normalized spectra
Channel counts/total counts

## Slide 20: In-situ spectrometry, 6 months after shutdown
Comparison of normalized spectra
Channel counts/total counts

## Slide 21: In-situ spectrometry, 6 months after shutdown
Comparison of normalized spectra
Channel counts/total counts

## Slide 22: In-situ spectrometry, 6 months after shutdown
Comparison of normalized spectra
Channel counts/total counts

## Slide 23: In-situ spectrometry, 6 months after shutdown
Comparison of normalized spectra
Co-57
Mn-54
Channel counts/total counts

## Slide 24: Studies of nuclide inventory
Study is done in 2 main stages:
During operation:
  Dose rate survey (“Hot Spots”)
  In-situ gamma spectrometry
  Material sampling
After shutdown, 6 months of cooling time:
  In-situ gamma spectrometry
  Material sampling

## Slide 25: Sampling of materials. 6 months of cooling
Magnet yokes:
  Ferromagnetic steel

## Slide 26: Sampling of materials. 6 months of cooling
Vacuum chamber:
  Stainless steel 316LN
Magnet yokes:
  Ferromagnetic steel
Magnet coils:
  Copper

## Slide 27: Vacuum chamber. Indicated nuclides
Nuclide | Co-57 | Mn-54 | Co-60

## Slide 28: Vacuum chamber. Identified nuclides
Nuclide | Co-57 | Mn-54 | Co-60
Hot spot 1 | ✓ | ✓ | ✓

## Slide 29: Vacuum chamber. Identified nuclides
Nuclide | Co-57 | Mn-54 | Co-60
Hot spot 1 | ✓ | ✓ | ✓
Hot spot 2 | ✓ | ✓ | x
*Minimal Detectable Activity
- below minimal detectable activity

## Slide 30: Vacuum chamber. Identified nuclides
Nuclide | Co-57 | Mn-54 | Co-60
Hot spot 1 | ✓ | ✓ | ✓
Hot spot 2 | ✓ | ✓ | x
Hot spot 3 | ✓ | ✓ | x
- below minimal detectable activity

## Slide 31: Vacuum chamber. Identified nuclides
Nuclide | Co-57 | Mn-54 | Co-60
Hot spot 1 | ✓ | ✓ | ✓
Hot spot 2 | ✓ | ✓ | x
Hot spot 3 | ✓ | ✓ | x
Hot spot 4 | ✓ | ✓ | x
- below minimal detectable activity

## Slide 32: Vacuum chamber. Identified nuclides
Nuclide | Co-57 | Mn-54 | Co-60
Hot spot 1 | ✓ | ✓ | ✓
Hot spot 2 | ✓ | ✓ | x
Hot spot 3 | ✓ | ✓ | x
Hot spot 4 | ✓ | ✓ | x
Hot spot 5 | ✓ | ✓ | x
- below minimal detectable activity

## Slide 33: Vacuum chamber. Identified nuclides
Nuclide | Co-57 | Mn-54 | Co-60
Hot spot 1 | ✓ | ✓ | ✓
Hot spot 2 | ✓ | ✓ | x
Hot spot 3 | ✓ | ✓ | x
Hot spot 4 | ✓ | ✓ | x
Hot spot 5 | ✓ | ✓ | x
Hot spot 6 | ✓ | x | x
Predominant nuclide
- below minimal detectable activity

## Slide 34: Vacuum chamber. Activity ratios
Nuclide | Co-57 | Mn-54 | Co-60
Hot spot 1 | ✓ | ✓ | ✓
Hot spot 2 | ✓ | ✓ | x
Hot spot 3 | ✓ | ✓ | x
Hot spot 4 | ✓ | ✓ | x
Hot spot 5 | ✓ | ✓ | x
Hot spot 6 | ✓ | x | x
- below minimal detectable activity

## Slide 35: Vacuum chamber. Activity ratios
Nuclide | Co-57 | Mn-54 | Co-60
Hot spot 1 | ✓ | ✓ | ✓
Hot spot 2 | ✓ | ✓ | x
Hot spot 3 | ✓ | ✓ | x
Hot spot 4 | ✓ | ✓ | x
Hot spot 5 | ✓ | ✓ | x
Hot spot 6 | ✓ | x | x
- below minimal detectable activity

## Slide 36: Magnet yoke. Identified nuclide
Identified nuclide: Mn-54

## Slide 37: Magnet coils. Identified nuclides
Sample | Co-57 | Mn-54 | Co-60
Hot spot 1 | ✓ | ✓ | ✓
Hot spot 2 | ✓ | x | ✓
Hot spot 3 | x | x | ✓
Hot spot 4 | x | x | x
Hot spot 5 | x | x | x
Predominant nuclide
- below minimal detectable activity

## Slide 38: Copper coils. Activity ratios
Sample | Co-57 | Mn-54 | Co-60
Hot spot 1 | ✓ | ✓ | ✓
Hot spot 2 | ✓ | x | ✓
Hot spot 3 | x | x | ✓
Hot spot 4 | x | x | x
Hot spot 5 | x | x | x
- below minimal detectable activity

## Slide 39: Copper coils. Activity ratios
Sample | Co-57 | Mn-54 | Co-60
Hot spot 1 | ✓ | ✓ | ✓
Hot spot 2 | ✓ | x | ✓
Hot spot 3 | x | x | ✓
Hot spot 4 | x | x | x
Hot spot 5 | x | x | x
- below minimal detectable activity

## Slide 40: Summary and conclusions
Studies of nuclide inventory are done in two steps with two approaches
Predominant nuclides are identified for most used materials of storage ring. Namely, they are:
  For vacuum chamber: Co-57
  For magnet yoke: Mn-54
  For magnet coil: Co-60
Nuclide inventories obtained in different locations are comparable
First results need to be confirmed by further investigation

## Slide 41: Wir schaffen Sicherheit– heute für morgen
Thank you
Dr. Roman Galeev
Department of Radiation Safety and Security (ASI), PSI
roman.galeev@psi.ch