## Slide 1: Exploring the Durability of thin carbon-backed lithium fluoride targets bombarded by 68 MeV 17O beams: A Theoretical and Experimental Analysis
Yong Hyun Kim1,2, Hee-Seock Lee1, Mahdi Bakhtiari1, Barry Davids 3
The 16th workshop on Shielding aspects of Accelerators, Targets and Irradiation Facilities, May 28-31, INFN-LNF, Italy
May 31, 2024
1 Pohang Accelerator Laboratory (PAL), South Korea
2 Hanyang university, South Korea
3 TRIUMF, Canada

## Slide 2
1. Introduction
2. Analysis on the target degradation
a) Thermal evaporation (Sublimation)
b) Sputtering
c) Radiation damage
3. Result & discussion
4. Conclusion
Table of Contents

## Slide 3
Experiment to investigate the effect of oxygen on massive stars in the early universe:
measuring the fusion reaction of 17O (α,)21Ne at EMMA, TRIUMF
7Li(17O,t)21Ne*()21Ne reaction rate measured indirectly
EMMA
7Li(17O,t)21Ne*()21Ne reaction
Target chamber
Electromagnetic recoil mass spectrometer
TIGRESS & SHARC
17O
SSB detector (particle rate in detector)
- Detecting elastically scattered beam and target ions to monitor the beam flux and target content degradation
W : solid angle
: target mass density
x : target thickness
R : count rate
I : beam intensity
: differential elastic scattering cross section,
R/I ∝ (areal mass density of target)
Introduction
01
Target
7LiF 100ug/cm2
+ C 30ug/cm2

## Slide 4
Count rate from SSB, R
Three identical targets were prepared in case of targets destruction
For each target, three areas could be selectively irradiated.
Target #1
Target #2
Target #3
left
center
right
Running HISTORY about SSB(14th/12/2019~ 19th/12/2019)
Running number (each run ~ 1 hour)
During 6-day experiment, areas where beam hit were changed 10 times due to target degradation, which limited data acquisition
After experiment
Target #1
Target #2
Target #3
Experiment was postponed around 1 year due to target destruction
Time consuming & Costly
-> Each targets were rejected after 5~20 hours irradiation
Introduction
01
Notes: This is the plot about count rate history for each run from SSB detector during the measurement.

## Slide 5
5
To analyze the cause of the destruction of the target bombarded with 17O beam,
a) Thermal evaporation (sublimation),
b) Sputtering (erosion rate), and
c) Radiation lattice damage
were explored.
Target lifetime was theoretically calculated by these three factors and was compared with the experimental target lifetime
Approach
Started to figure out the cause of target destruction (hole)
Introduction
01

## Slide 6
6
a) Thermal evaporation (sublimation)
Energy deposition –> Temperature -> Evaporation(sublimation)
Analysis flow
(Tool: FLUKA)
(Tool: ANSYS)
Thermal evaporation was calculated to estimate target lifetime
Thin target lifetime with respect to evaporation can be expressed as:
: target lifetime
N0 : atomic number density
d : target thickness
V(T) : evaporation rate of target atoms (or molecules) per unit area
By F. Nickel (1978)
Evaporation lifetime
02
Analysis on the target degradation
Energy deposition v.s. radius
Energy deposition 2D map
Energy deposition
Assumption: beam intensity = 1.0 ions/s
out: 67.42 MeV
in: 68 MeV
(By FLUKA)
the largest value used in the experiment
Beam intensity profile during exp.
17O4+ 2~7 nA

## Slide 7
 | Thermal sublimation, V(T) [1/scm2] (at r = 0, under 10-6 Torr vaccum) | Calculated lifetime, [hour] | Experimental lifetime, [hour]
C | (5.28 ± 1.53)ⅹ10-95 | 1.6ⅹ10108 | 5 ~ 20
7LiF | (2.94 ± 3.19) ⅹ10-9 | 1.18ⅹ1034 | 
 | Thermal sublimation, V(T) [1/scm2] (at r = 0, under 10-6 Torr vaccum) |  | 
C | (5.28 ± 1.53)ⅹ10-95 | 1.6ⅹ10108 | 5 ~ 20
7LiF | (2.94 ± 3.19) ⅹ10-9 | 1.18ⅹ1034 | 
7
-> No effect on target degradation and target lifetime
Temperature
Background Temp. : 22 ͦC
steady-state thermal analysis
Center (r =0) of C : 58.16 oC
Center (r =0) of 7LiF : 58.10 oC
By ANSYS
R=0.4 cm
Sublimation can occur in vacuum at temperature below melting point
02
Analysis on the target degradation
a) Thermal evaporation (sublimation)
Thermal sublimation (evaporation) flux, V(T)
Vapor pressure
- Hertz-Knudsen Equation
NA : Avogadro number
Pv : the vapor pressure
M : molecular mass
: gas constant
[1/s·cm2]
Calculated lifetime determined by sublimation
Assumption: beam intensity = 1.0 ions/s
Beam intensity= ions/s

## Slide 8
8
02
Analysis on the target degradation
b) Sputtering
Nuclear Sn & electronic Stopping power Se at target
Beam energy
(By SRIM[1] stopping range table)
-> Electronic stopping power in C and LiF was predominant at 68MeV
Representing the erosion of surface atoms by particle bombardment
A target atom is sputtered when the kinetic energy associated with its motion normal to the surface is larger than the surface binding energy
Defined as the mean number of emitted atoms (or molecule) per incident particle
Thin target lifetime with respect to sputtering can be expressed as:
s: sputtering (=erosion) yield [emitted /incident particle]
(s = nuclear Yn+electronic Ye+ chemical sputtering Ych)
: averaged beam flux density
Sputtering lifetime
By J. Yntema, F. Nickel (1978)
Sputtering
Electronic
sputtering
Nuclear
sputtering
Chemical
sputtering
→ governed by Se
→ governed by Sn
→ governed by chemical reaction
Sputtering consists of three types: Electronic, Nuclear, and chemical sputtering
Total sputtering is calculated as the sum of these types
[1]J.F. Ziegler, The Stopping and Range of Ions in Solids, SRIM Co. (2008).

## Slide 9
9
Electronic sputtering
Electronic sputtering Ye: energy deposition from high-energy ions (>1 A MeV) through ionization and electronic excitations leads to surface evaproation
i-TS model used to calculate electronic sputtering yield (i-TS model : best explains observed electronic sputtering yields quantitatively)
02
Analysis on the target degradation
for C
for 7LiF
Temperature as a function of time at different radial distances from ion in nm.
Numerically solved using an explicit method
b) Sputtering
Carbon film
-> Ye_c = 9.74e-4 [emitted /incident particle]
7LiF film
-> Ye_LiF = 4.8e-7 [emitted /incident particle]
: local evaporation rate
Calculated electronic sputtering yield
,
- Heat diffusion in the electron & lattice subsystems by two coupled differential equations:
: heat capacity
: thermal conductivity
g: electron-phonon coupling for energy transfer
- Deposited energy per ion v.s. radial distance to the ion path
Initial energy on electron
(Heat source by inelastic collision (i-TS model))
Ref.: M. R. P. Waligorski(1986)
incident ion
electron subsystem
Te
Ta
lattice subsystem
energy
electronic sputtering

## Slide 10
10
 | Nuclear sputtering 𝑌n | Electronic sputtering 𝑌e | chemical sputtering 𝑌ch | Total sputtering 𝑌s | Calculated lifetime, [hour] | Experimental lifetime, [hour]
 | [emitted/incident particle] |  |  |  |  | 
C | 3.50E-03 | 9.74E-04 | 1 | 1 | 650 | 5~20
7LiF | 2.05E-02 | 4.80E-07 | 0 | 2.05E-02 | 90,100 | 
 | Nuclear sputtering 𝑌n | Electronic sputtering 𝑌e | chemical sputtering 𝑌ch | Total sputtering 𝑌s |  | 
 | [emitted/incident particle] |  |  |  |  | 
C | 3.50E-03 | 9.74E-04 | 1 |  |  | 5~20
7LiF | 2.05E-02 | 4.80E-07 | 0 | 2.05E-02 | 90,100 | 
Assumption: beam intensity = 1.0 ions/s (the largest value used in the experiment)
02
Analysis on the target degradation
Calculated lifetime determined by sputtering (𝑌s = nuclear 𝑌n + electronic 𝑌e + chemical sputtering 𝑌ch)
-> No meaningful effect on the degradation or longevity of the target
b) Sputtering
Ref.: A. Guentherschulze, Vacuum. 3 (1953) 360–374
Chemical reaction only between 17O beam and carbon film :
17O + C -> CO or CO2
-> Chemical erosion in the form of volatile CO and CO2
Total yield from both reactions is approximately 1, independent of the oxygen beam energy
Carbon film
Ych_C = 1 [emitted /incident particle]
7LiF film
Ych_LiF = 0 [emitted /incident particle]
Chemical sputtering
Reported chemical sputtering yield
Nuclear sputtering
Carbon film
Yn_c = 3.5e-3 [emitted /incident particle]
7LiF film
Yn_LiF = 2.05e-2 [emitted /incident particle]
(by TRIM MC Simulation)
Calculated nuclear sputtering yield
Caused by atomic collision cascades between the incoming particles and the atoms in the surface layers of a solid
heavy ions in the MeV energy region, the transmission sputtering and back sputtering occur
beam intensity range: ions/s

## Slide 11
02
Analysis on the target degradation
c) Radiation damage
11
Displacements of target were calculated using TRIM, FLUKA[1,2], PHITS[3] codes for estimation of target lifetime.
Different radiation damage models used for each simulation. In case of TRIM, threshold displacement energy could not be adjusted by the user
The energy loss of energetic heavy ions caused by elastic atomic (nuclear stopping power) leads to atom displacements in solid-state targets.
Displacements used to measure the amount of radiation damage, which can change the mechanical properties; ex) tensile strength, embrittlement, cracks, swelling, elongation, irradiation creep, etc.
Thin target lifetime with respect to radiation damage can be expressed as:
=
Radiation damage lifetime
: atomic desnity number
: displacements rate per unit volume
: displacements per unit volume per incident particle
(= ∙ dpa/particle)
: beam intensity
By F. Nickel (1978)
- Number of displacement (NRT model)
Displacements : The number of interstitial atoms and vacancies in the lattice
: Frenkel pairs (number of defects)
:displacement efficiency
: Lindhard partition function
T : energy transfer
: Threshold displacement energy
limitation of target lifetime
 | Used model for radiation damage | Threshold displacement Energy, Ed (eV) | 
 |  | C | 7LiF
TRIM | Full damage cascade (Binary collision approximation, BCA simulation) | 21[4] | 1.40[5]
FLUKA 4-4.0 | NRT using restricted loss | 21[4] | 1.40[5]
PHITS-3.34.1 | NRT | 31 | 22
 |  | (built hard-coded variable) | 
[4] F. Vuković, J.M. Leyssale, P. Aurel, N.A. Marks, Evolution of Threshold Displacement Energy in Irradiated Graphite, Phys. Rev. Appl. 10 (2018) 1–12.
[5] F. Herrmann, P. Pinard, Y. Farge, About the displacement of the lithium ion in lithium fluoride by accelerated electrons, J. Phys. C Solid State Phys. 7 (1974).
[2]T. Sato et al, J. Nucl. Sci. Technol. 61, 127-135 (2024)
[1] C. Ahdida et al, Frontiers in Physics 9, 788253 (2022).
[2] G. Battistoni et al, Annals of Nuclear Energy 82, 10-18 (2015).
[3]T. Sato et al, J. Nucl. Sci. Technol. 61, 127-135 (2024)

## Slide 12
03
Radiation damage
LiF
C
Displacements per unit volume for each simulation
11
Result & Discussion
Average displacements results of TRIM were 2 to 3 times higher than FLUKA results and 10 to 100 times higher than PHITS results.
Target material | Average displacements per unit volume [displacement/cm3/incident particle] |  |  | Ratio | 
 | TRIM | FLUKA | PHITS | (FLUKA/TRIM) | (PHITS/TRIM)
C | 4.82106 | 1.98106 | 6.76105 | 0.41 | 0.14
7LiF | 9.48107 | 2.98107 | 2.13106 | 0.31 | 0.02
Target material |  |  |  | Ratio | 
 | TRIM | FLUKA | PHITS | (FLUKA/TRIM) | (PHITS/TRIM)
C |  |  |  | 0.41 | 0.14
7LiF |  |  |  | 0.31 | 0.02
Based on the calculations, LiF film seems to be degraded due to lattice damage, and the moment the LiF film is perforated or torn, the carbon film which was intact may also be torn. Lifetime of the target was determined by radiation lattice damage to the 7LiF film
Target material | Calculated Target lifetime [hour] |  |  |  | 
 | Evaporation lifetime, | Sputtering lifetime, | Radiation damage lifetime, |  | 
 |  |  | TRIM | FLUKA | PHITS
C | 1.60E+108 | 650 | 293 | 712 | 2,089
7LiF | 1.18E+34 | 90,100 | 8 | 26 | 359
Target material | Calculated Target lifetime [hour] |  |  |  | 
 |  |  | TRIM | FLUKA | PHITS
C | 1.60E+108 | 650 | 293 | 712 | 2,089
7LiF | 1.18E+34 | 90,100 | 8 | 26 | 359
Assumption: beam intensity = 1.0 ions/s (the largest value used in the experiment)
Experimental lifetime, [hour]
5 ~ 20
5 ~ 20
beam intensity range: ions/s

## Slide 13
03
11
Result & Discussion
Experimental and calculated lifetime for thin LiF targets on carbon backings
The theoretically calculated lifetime of the target was compared to the experimental lifetime which was the period of use before disposal.
In this study, the lifetime calculated with TRIM agreed well with the observed target lifetime during the experiment.
Discrepancy in displacements occurred in different radiation damage models.
FLUKA and PHITS provide an average estimate of atomic displacements, but they do not detail the complex chain of successive collisions as TRIM's radiation damage model does. TRIM keeps track of all displaced atoms and counts them.
In the case of PHITS, the simulation results differed significantly from the other two simulations due to the use of an inherent higher threshold displacement energy.
Comparison between the calculated lifetime at the beam spot and the experimental time |  |  |  |  |  | 
 | Sample#1 center | Sample#1 right | Sample#1 left | Sample#2 center | Sample#2 right | Sample#3 center
Average intensity [ions/s] | 3.90E+09 | 4.72E+09 | 6.07E+09 | 5.35E+09 | 3.18E+09 | 5.39E+09
Fluence [ions/cm2] | 4.09E+16 | 4.82E+16 | 3.73E+16 | 4.34E+16 | 2.90E+16 | 1.19E+16
Calculated DPA by TRIM [Displacements/atom] | 5.55E-01 ±2.04E-01 | 6.54E-01 ±2.23E-01 | 5.06E-01 ±1.82E-01 | 5.89E-01 ±2.12E-01 | 3.93E-01 ±1.41E-01 | 1.61E-01 ±5.80E-02
Experimental time to rejection [hours]* | 22.8 | 22.3 | 13.4 | 17.7 | 19.9 | 4.8
Calculated lifetime [hours] | 22.9±8.2 | 18.9±6.8 | 14.7±5.3 | 16.7±6.0 | 28.1±10.1 | 16.6±6.0
* Experimental time to rejection is the time it takes for the SSB count to reach 0, after which the target is replaced.

## Slide 14
Conclusion
04
14
The cause of the destruction of thin, carbon-backed lithium fluoride targets during a measurement of the fusion of 7Li and 17O were analyzed.
The lifetimes of carbon and LiF films due to thermal evaporation, sputtering, and lattice damage were estimated and compared with the lifetime observed in the experiment.
Thermal evaporation and sputtering did not affect the target degradation
The lifetime of LiF film is calculated for the first time using the radiation lattice damage model suggested by Nickel et al.
It was confirmed that the radiation damage and target life estimation using TRIM closely matched the experimental results, compared to those using FLUKA and PHITS.
Radiation damage calculation varied according to the model used and the threshold displacement energy set by user.
This study suggested methods for predicting the lifetimes of thin LiF films, which are used to induce nuclear reactions, allowing for increased experimental efficiency.
Kim, Yong Hyun, et al. Nuclear Engineering and Technology 55.3 (2023): 919-926.
Details in the published paper

## Slide 15
Thank you for attention
E-mail: kimyh0411@postech.ac.kr
Yong Hyun Kim

## Slide 16: Support
FLUKA : NRT model using restricted loss (stopping power)*
where =Sn’/S,
where Sn’(E,Eth)= N
: number of defects by Norgert, Robinson and Torrens (NRT)
:displacement efficiency
: Lindhard partition function
Sn’ : restricted nuclear stopping power(energy loss)
N : atomic density
T : energy transfer
: differential scattering cross section
Eth : displacement damage threshold
where
A : mass number
Avogadro number
: Frenkel pairs (number of defects)
: density
*Ref: Fasso, Alberto, et al., Progress in Nuclear Science and Technology 2 (2011): 769-775.
restricted loss (stopping power)
adjustable
TRIM(Full Cascade calculation) : Binary collision approximation (BCA) simulation model

## Slide 17: Support
Two peaks comes from?
Displacement and ion(17O)&recoil(Li,F) distributions according to depth were examined for each particle. And, simulations were performed according to the thickness of LiF. As a result, the bonding force between Li and F on the surface is rather weak compared to that one in the bulk, so it is estimated that vacancy and replacement increased near the boundaries by recoil of Li and F from the surface.

## Slide 18
Forward Difference :
= +
=
Symmetric Central difference :
= - +
= - +
FDA-Explicit scheme (electronic system)
= - ++
= [
]
= = T0
, = 0
= = T0
(rmin=0.1 nm, rmax=100 nm)
Boundary Conditions
Convergence Conditions
2De / ()2 < 1
= 0.1 nm
= 2.0 x10-17 s
0.1< r <100 nm
2.0x10-17< t < 2.0x10-11 s
Ref: [1]Thermal spike model interpretation of sputtering yield data for Bi thin films irradiated by MeV 84Kr15+ ions [2] Transient thermal process after a high-energy heavy-ion irradiation of amorphous metals and semiconductors[3] Bell, R. O., M. Toulemonde, and P. Siffert. "Calculated temperature distribution during laser annealing in silicon and cadmium telluride." Applied physics 19.3 (1979): 313-319.[3] THERMAL SPIKE MODEL OF TRACK FORMATION IN YBa2Cu3O7−x
the classical equations of heat flow according to Fick’s law

## Slide 19
= +
= [
]
= = T0
, = 0
= = T0
(rmin=0.1 nm, rmax=100 nm)
Boundary Conditions
Convergence Conditions
2De / ()2 < 1
= 0.1 nm
= 2.0 x10-17 s
0.1< r <100 nm
2.0x10-17< t < 2.0x10-11 s
= +
= +
Forward Difference :
= +
=
Symmetric Central difference :
FDA-Explicit scheme (lattice system)
the classical equations of heat flow according to Fick’s law
Sol.1
Sol.2
= N(r,t)
L = 0.15 nm (z= end of target)
De = 2 cm2/s
dE/dx = 1.1E+10 ev/cm
= [
+
a : electron-lattice
relaxation time(1E-12s )

## Slide 20
FDA-Explicit scheme (calculation)
= = T0=320 K
, = 0
= , = 0
= = T0 = 320 K
= = = T0=320 K
Boundary Conditions
= / +
= - +
= 0
= +
= + (1-) + ) + )
1. = N(r,t)
L = 0.15 nm (z= end of target)
De = 2 cm2/s
dE/dx = 1.1E+10 ev/cm
= [
+
= +
2. = 0
= +