## Slide 1: LBNF – Long Baseline Neutrino Facility Department of Particle Physics Division Decay Pipe Concrete Shielding – Placing Sequence
Supervisors: Tracy K Lundin, Thomas J Hamernik
Presenter: Lisa Favilli
2014 CNI-ISSNAF Internship Final Presentation
December, 11th, 2014

## Slide 2: What is the LBNF?
The Long-Baseline Neutrino Facility (LBNF) is designed to send neutrinos straight through the earth from Batavia, Illinois, to Lead, South Dakota. It will include a beamline to create the neutrinos and a near and far detector to detect them for physics studies.
The scientists make the neutrino beam in a three-step process:
Using the Fermilab’s main injector accelerator as a proton source, they extract the proton beam and smash it into a target.
The protons interactions with the protons and neutrons in the target material produce new, short-life particles as pions and kaons.
These particles travel a short distance trough a decay pipe, and as they do, a good fraction of them decays into neutrinos that continue on in the same direction, forming a neutrino beam.

## Slide 3: What is the Decay Pipe Shielding?
The project would require the construction of three buildings, a 52-foot-high hill made of compacted soil and a 680-foot long tunnel. This tunnel is the Decay Pipe (DP), placed between the Absorber Hall and the Target Hall complex.
The decay pipe is the part of the beamline in which
the protons and neutrons decay into neutrinos.
This process releases radiation,
which need to be shielded.
The area of concern is the design of a concrete structure
with the role to shield the radiation.

## Slide 4: Decay Pipe Concrete Shielding – About material
EFFICIENCY
OF SHIELDING
DENSITY
CONCRETE IS A HIGH DENSITY MATERIAL
GEOMETRY
5.6 m RADIUS
THE DP CONCRETE SHIELDING IS A MASS CONCRETE

## Slide 5: Decay Pipe Concrete Shielding – Typical Cross Section
CONCRETE
SHIELDING
CENTER OF THE BEAM
DECAY PIPE
GEOMEMBRANE
GRAVEL LAYER
SAND LAYER
COMPACTED
BACKFILL SOILS
IN SITU SOILS
AND ROCK
15.5 m (51 ft)
15.5 m (51 ft)

## Slide 6: Decay Pipe Concrete Shielding – The Goal
+
+
+
RADIATION SHIELDING
DENSITY
GEOMETRY
MASS CONCRETE
HEAT OF HYDRATION
LOW EXTERNAL TEMPERATURE
DIFFERENT COOLING BETWEEN INTERIOR AND EXTERNAL SURFACES
VOLUME CHANGES
RESTRAINTS
CRACKS
NON-HORIZONTAL
PLACING PLAN
SEGREGATION
FAILURE OF THE SHIELDING
GOAL: DEFINE A VIABLE SEQUENCE FOR PLACING THE SHIELDING, TAKING MEASURES TO CONTROL THE HEAT OF HYDRATION AND TO PLACE AT A 10 % SLOPE

## Slide 7: Project of the Decay Pipe Concrete Shielding - Summary
ONE CROSS SECTION FOR THE ENTIRE LENGTH
CRACKING AND TEMPERATURE CONTROL
HEAT OF HYDRATION CONTROL
ASSUMPTIONS
GOAL
INTERCONNECTED ASPECTS
METHODS
REPORT
DRAWINGS
TO DETERMINE A VIABLE SEQUENCE PLACING THE DECAY PIPE CONCRETE SHIELDING
NO RESTRICTIONS ON THE AVAILABILITY OF CONCRETE
THE GEOMEMBRANE IS NOT CONSIDERED IN THIS EFFORT
THE PLACING PLAN IS A 10% SLOPE
CONCRETE COMPOSITION PROPERTIES
CONCRETE MASS PROPERTIES
VOLUME CHANGES CONTROL AND JOINTS CONSTRUCTION
EVALUATION OF AN ALTERNATIVE CONCRETE
DEFINITION OF THE PHASES OF PLACING
TO USE AN ORDINARY PORTLAND CONCRETE

## Slide 8: Project of the Decay Pipe Concrete Shielding – Report
PARAMETERS
REQUIREMENTS
RECOMMENDATIONS
Elements composing
each aspect
Needs of the project
How to reach the
needs of the project.
REPORT: the document that contains suggestions and recommendations regarding materials and phases of construction.

## Slide 9: Heat of hydration control
TO HAVE LOW HEAT OF HYDRATION
PARAMETERS
AGGREGATES SIZE
POZZOLAN TYPE
CEMENT TYPE
WATER/CEMENT RATIO
AGGREGATES TYPE
NATURAL COARSE VOL.
POZZOLAN PERCENT
CEMENT CONTENT
REQUIREMENTS
IMPROVE WORKABILITY
CEMENTITIOUS PROPERTIES
LOW HEAT OF HYDRATION
LOW CONTENT
RECOMMENDED FOR MC
HIGH
MEDIUM - HIGH
LOW
RECOMMENDATIONS
3 in. - 4 in. (80 mm-100 mm)
CLASS C
PORTLAND TYPE II
0.20
CRUSHED
82 %
35 %
240 kg/m3 (405 lb/cy)

## Slide 10: Cracking and temperature control
TO CONTROL CRACKING AND TEMPERATURE
PARAMETERS
CRACK RESISTANCE
REQUIREMENTS
RECOMMENDATIONS
CRACKING AND TEMPERATURE
HIGH
CEMENTITIOUS MATERIAL CONTROL
COOLING OPERATIONS
CONSTRUCTION MANAGEMENT
PLACING IN BLOCKS
DEGREE OF RESTRAINTS
LOW
THIN LAYERS
1.5 – 2 m (5 – 6.6 ft)
NO. OF BLOCKS: 10
LENGTH: 20.3 m (67 ft)
PRE-COOL INGREDIENTS
POST-COOL CONCRETE
INSULATE EXT. SURFACES
SLOW
STRAIN APPLICATION
LAYER NUMBER | DIMENSIONS m (ft) | Q.TY OF CONCRETE m3 (yd3)
1 | 15.5x1.5x20.3 (51x5x67) | 472 (617)
2 | 15.5x1.5x20.3 (51x5x67) | 472 (617)
3 | 15.5x1.5x20.3 (51x5x67) | 472 (617)
4 | 2x6.5x20.3 (6.6x21x67) | 264 (345)
5 | 2x6.5x20.3 (6.6x21x67) | 264 (345)
6 | 2x6.5x20.3 (6.6x21x67) | 264 (345)
7 | 2x6.5x20.3 (6.6x21x67) | 264 (345)
8 | 7.5x6.5x20.3 (25x21x67) | 677 (885)
9 | 15.5x1.5x20.3 (51x5x67) | 472 (617)
10 | 15.5x1.5x20.3 (51x5x67) | 472 (617)
11 | 15.5x1.5x20.3 (51x5x67) | 472 (617)

## Slide 11: Concrete mass properties
TO HAVE SHIELDING EFFICIENCY
PARAMETERS
TYPE OF CONCRETE
DIMENSION
AGGREGATES PROPERTIES
REQUIREMENTS
NORMAL DENSITY
LOW THERMAL
EXPANSION COEFFICIENT
NORMAL WEIGHT
LOW MODULUS
OF ELASTICITY
RADIUS ENOUGH TO SHIELD
RECOMMENDATIONS
MINIMUM VALUE:
2350 kg/m3
4.5 X 10-6 F-1
LIMESTONE
14000 MPa (2 X 106 psi)
5.6 m

## Slide 12: Concrete composition properties
COMPLETION OF THE PREVIOUS RECOMMENDATIONS
PARAMETERS
REQUIREMENTS
RECOMMENDATIONS
SLUMP RANGE
RECOMMENDED FOR MC
LOW
COMPRESSIVE STRENGTH
DRYING SHRINKAGE
PERMEABILITY
LOW
4 X 10-4
LOW RANGE
1 in. – 2 in.
MEDIUM VALUE
1500 psi – 2000 psi
5 X 10-10 cm/sec
TEMPERATURE DIFFERENTIAL
35 °F

## Slide 13: Volume changes control and joints construction
JOINTS MATERIAL
WITH THE SAME DENSITY OF CONCRETE
DENSITY
SHIELDING EFFICIENCY
TO PREVENT AND CONTROL CRACKS
VOLUME CHANGES
PARAMETERS
PLACING IN BLOCKS
REQUIREMENTS
CONTRACTION JOINTS
CONSTRUCTION JOINTS
RECOMMENDATIONS
VERTICAL BETWEEN BLOCKS
HORIZONTAL AND
VERTICAL CONSTRUCTION BETWEEN LAYERS
TWO CONTRACTION JOINTS
HORIZONTAL AND VERTICAL “LINES” ARE CONSTRUCTION JOINTS

## Slide 14: Definition of the phases of placing 1/2
PARAMETERS
THICKNESS OF LAYERS
POST PLACING OPERATIONS
PLACING PLAN
REQUIREMENTS
THIN LAYERS
10 % SLOPE
CONTROL
HEAT GENERATION
RECOMMENDATIONS
1.5 – 2.0 m (5.0 – 6.6 ft)
USE 4 in. VIBRATORS
INSULATE EXTERNAL SURFACES
POST COOL
TO HAVE BEST PLACING SEQUENCE
SETBACK OF 1.5 m (5 ft)
LARGE DIMENSIONS
ROUGH BACKGROUND SURFACE
DIVIDE INTO 10 BLOCKS

## Slide 15: Defining of the phases of placing 2/2
Operations | Recommendations | Reference item
Pre cooling ingredients |  | 
Placing gravel and sand layers |  | 
Building concrete rough surface (30 cm) | Clean surface with wet sandblasting | Figure 1
Placing layers 1-2-3 of the first block | Divide the length into 10 blocks Setback toward the successive edges of 1.5 m (5 ft) Clean surface with wet sandblasting before placing the next layer Insulate the external surface of concrete Use vibrators diameter of 4 in. (100 mm) | Figures 1-2
Placing layers 1-2-3 for each block |  | Figure 3
Placing layers 4-5 of the first block |  | Figure 4
Placing layers 4-5 for each block |  | Figure 5
Placing layers 6-7 of the first block |  | Figure 6
Placing layers 6-7 for each block |  | Figure 7
Placing layer 8 of the first block |  | Figure 8
Placing layer 8 for each block |  | Figure 9
Placing layers 9-10-11 of the first block |  | Figure 10
Placing layers 9-10-11 for each block |  | Figure 11
Post cooling with embedded pipes |  | 
Insulate external surfaces |  | 

## Slide 16: Evaluation of alternative concrete
MORE WORKABILITY
LESS SEGREGATION
LOWER HEAT OF HYDRATION
LARGER LAYERS AND
FEWER BLOCKS
FEWER JOINTS
COOLING OPERATIONS REDUCED/ELIMINATED
TESTS AND
INFORMATION ON:
THERMAL BEHAVIOUR
CHEMICAL PROPERTIES
PHYSICAL PROPERTIES
MECHANICAL PROPERTIES
PARAMETERS
REQUIREMENTS
RECOMMENDATIONS
TO COMPARE POSSIBILITIES
HEAT OF HYDRATION CONTROL
CRACKING AND TEMPERATURE CONTROL
PLACING PROCEDURE
PLACING PLAN
THERMAL PROPERTIES
RADIOLOGICAL PROPERTIES
LEACHING TEST

## Slide 17: Summary and Conclusions
CRACKING AND TEMPERATURE CONTROL
HEAT OF HYDRATION CONTROL
CONCRETE COMPOSITION PROPERTIES
CONCRETE MASS PROPERTIES
VOLUME CHANGES CONTROL AND JOINTS CONSTRUCTION
EVALUATION OF AN ALTERNATIVE CONCRETE
DEFINITION OF THE PHASES OF PLACING
REPORT AND DRAWINGS
DISCUSSED ASPECTS
STATUS
METHODS
TESTS
REPORT AND DRAWINGS
REPORT AND DRAWINGS
REPORT AND DRAWINGS
REPORT AND DRAWINGS
REPORT AND DRAWINGS

## Slide 18: Sources and References
ACI 116R-00 “Cement and Concrete Terminology”
ACI 207.1R-96 “Mass concrete”
ACI 211.1-91 “Standard practice for Selecting Proportions for Normal, Heavyweight and Mass Concrete”
ACI 214-77 “Recommended practice for Evaluation of Strength Test Results of Concrete”
ACI 224R-90 “Control of Cracking in Concrete Structures”
ACI 224.3R “Joints in concrete construction”
ASTM C150 “Standard specification for Portland Cement”
ASTM C618 – 08 “Standard specification for Coal Fly Ash and Raw or Calcined Natural Pozzolan for Use in Concrete”
ASTM C637 – 09 “Standard specifications for aggregates for radiation – shielding concrete”
Barite Analysis – Thomas Hamernik
Memorandum – Thomas Hamernik

## Slide 19
Thank you all
for your attention!