## Slide 1: Magnets Part II
Luca.Bottura@cern.ch
Erice, Sicilia, 27 July - 2 August 2023

## Slide 2: Superconductors JE
Graphics by courtesy of C. Senatore, University of Geneva
Can we really achieve 1000 A/mm2 ???

## Slide 3: Overview
Accelerator magnets and examples
HEP detector magnets and examples
Resistive and coil magnet designs
Superconductors and their delicacies
Performance limits of accelerator magnets
Muon collider magnet challenges
Summary and perspective

## Slide 4: Overview
Accelerator magnets and examples
HEP detector magnets and examples
Resistive and coil magnet designs
Superconductors and their delicacies
Performance limits of accelerator magnets
Muon collider magnet challenges
Summary and perspective

## Slide 5: Stability and quench event-tree
Stable operating condition
External perturbation:
flux jump
conductor motions
insulation cracks
AC loss
heat leaks
nuclear heat
(degradation)
…
Approach Jc(T, B, …)
Quench
yes
no
Stable operating condition
Transition to normal state and Joule heat generation in current sharing
heat generation >
heat removal
stability analysis
Heat balance
Perturbation spectrum
quench analysis

## Slide 6: Perturbation overview

## Slide 7: Is it stable ?
Superconductor stability is the art of balancing large stored energies (and potential for energy release) with a little capital
Extremely important in LTS-based magnet to reach the desired performance (10 MJ vs 10 mJ)
  Generally not an issue for HTS-based magnets
Stability is not absolute, it implies comparing the perturbation spectrum to the available margin
Several strategies can be applied to achieve stable operating conditions under the envelope of foreseeable perturbation spectrum

## Slide 8: Adiabatic heat balance
The simplest (and conservative) approximation for the evolution of the temperature during a thermal transient is to assume adiabatic behavior at the location of the perturbation:
Average heat capacity:
Average resistivity:

## Slide 9: Adiabatic stability
Stable operation is possible only if the superconductor is below its critical surface
  No resistivity, hence no Joule heating
Integrate the adiabatic heat balance:
energy margin
volumetric enthalpy

## Slide 10: Enthalpy reserve
2
30
2
3
Enthalpy reserve increases massively at increasing T: stability is not an issue for HTS materials ?!?
do not sub-cool if you can only avoid it !
Enthalpy reserve is of the order of the expected perturbation spectrum: stability is an issue for LTS magnets
2
100

## Slide 11: A summary of LTS strategies
Operating current density (A/mm2)
Energy margin (mJ/cm3)
1
10
100
1000
1
10
100
1000
CICC
Adiabatic
Cryostable
Cold end
MPZ/MQE

## Slide 12: Limit 1 – Operating margin
A superconductor requires a minimum operating margin to run stably
Stable operation in the vicinity of the critical current is not practical, it will lead to inevitable resistive transitions and down times
The margin should not degrade as the magnet goes trough its normal operating life (including CD/WU, powering, quenches), lest the operating point will need to be lowered
Corollary – for a given superconducting material this sets an upper limit on the field

## Slide 13: What is a quench ?
Quench is the result of the resistive transition, leading to appearance of voltage, temperature increase, thermal and electro-magnetic forces, and cryogen expulsion
This is a quench of a GE MRI magnet during tests at the plant
This is the result of the chain of events triggered by a quench in an LHC bus-bar

## Slide 14: Why is it a problem ?
Magnetic energy stored in the field:
  converted to heat through Joule heating RqI2
If this process happened uniformly in the winding:
  Cu melting temperature 1356 K
  corresponding Em=5.2 109 J/m3
  limit would be Bmax  115 T: NO PROBLEM !
BUT
the process does not happen uniformly: as little as 1 % of the magnet mass may absorb the total energy – damage potential !
L
Rq

## Slide 15: Detection, switch and dump
precursor
propagation
detection
detection threshold
trigger (t=0)
fire heaters
switch
dump
tdetection
tdelay
tswitch
tdump
tquench ≈ tdetection + tdelay + tswitch +f tdump
tdischarge
Example of an LHC dipole magnet training quench

## Slide 16: Hot-spot limits
the quench starts in a point and propagates with a quench propagation velocity
the initial point will be the hot spot at temperature Tmax
Tmax must be limited to:
  limit thermal stresses (see graph)
  avoid material damage (e.g. resins have typical Tglass of 100 ∘C)
Tmax < 100 K for
negligible effect
Tmax < 300 K for well-supported coils (e.g. accelerator magnets)

## Slide 17: Hot spot temperature
adiabatic conditions at the hot spot :
can be integrated:
cable operating current density
total volumetric heat capacity
stabilizer resistivity
B.J. Maddock, G.B. James, Proc. IEE, 115 (4), 543, 1968
The function G(Tmax) is a cable property
The integral of J depends on the circuit quench integral
Perturbation is over

## Slide 18: G(Tmax) for pure materials
Assume that the cable is made of stabilizer only (good first guess):
G(Tmax) is a material property and can be tabulated
A useful approximation is:
Copper at B=0 T
Wilson’s Gamma

## Slide 19: Quench Capital vs. Tax
The real problem is to determine the integral of the current waveform: how much is the quench time tquench ?
Consider two limiting cases:
  External-dump: The magnet is dumped externally on a large resistance (Rdump >> Rquench) as soon as the quench is detected
  Self-dump: The circuit is on a short circuit and is dumped on its internal resistance (Rdump = 0)

## Slide 20: External dump of a magnet
The magnetic energy is extracted from the magnet and dissipated in an external resistor:
The quench integral is:
and the quench time is:
B.J. Maddock, G.B. James, Proc. Inst. Electr. Eng., 115, 543, 1968
L
Rdump
S
normal operation
L
Rdump
S
Rquench
quench

## Slide 21: Protection at high fields
Energy per unit length in a sector coil of inner radius Rin, outer radius Rout, coil width w = Rout-Rin producing a dipole field B
A simple exercise:
JCu ≈ 1000…1250 (A/mm2)
dT/dt ≈ 1000…2000 (K/s)
t(300 K)≈ 0.15…0.3 (s)
Iop ≈ 15 (kA)
E/l ≈ 1000 (kJ/m)
V/l ≈ 500…1000 (V/m)
It is not possible to protect accelerator magnet strings using an external dump
Voltage per unit length for an external dump with time constant t

## Slide 22: Magnet strings
Magnet strings (e.g. accelerator magnets, fusion magnetic systems) have exceedingly large stored energy (10’s of GJ):
    Energy dump takes very long time (10…100 s)
    The magnet string is subdivided and each magnet is by-passed by a diode (or thyristor)
M1
M2
M3
MN
normal operation
quench

## Slide 23: Quench heaters
The quench is spread actively by firing heaters embedded in the winding pack, in close vicinity to the conductor
Other methods can be used to trigger a distributed quench
advantages:
  homogeneous spread of the magnetic energy within the winding pack
disadvantages:
  active
  high voltages at the heater
winding
heater

## Slide 24: Self dump of a magnet
The magnetic energy is completely dissipated in the internal resistance, which depends on the temperature and volume of the normal zone
In this case it is not possible to separate the problem in quench integral and cable property, but we can make approximations
Assume that:
  The whole magnet is normal at tdischarge (perfect heaters)
  The current is constant until tquench then drops to zero
  Wilson’s Gamma and the power resistivity
L
Rquench
S2
S1
normal operation
quench

## Slide 25: Scaling for self dump
Temperature
Quench time
magnet bulk
hot-spot
C/h
J and t

## Slide 26: Sample scaling study – self dump
Cu/Nb3Sn
fCu = 0.55
fSC = 0.45
Iop = 10 kA
tdischarge = 0.1 s
Tmax
em limited
Jop limited

## Slide 27: Hot spot temperature limits
Courtesy of S. Izquierdo Bermudez, PhD, 2023
The material enthalpy in a self-dumped magnet limits the stored energy density

## Slide 28: Limit 2 – Quench protection
An upper bound on hot spot temperature sets a limit on the current density and the magnetic energy density of a coil
Corollary – this sets an upper limits to the maximum affordable field
HL-LHC (12 T, Thot ≈ 300 K) achieves an overall current density in the coil of 520 A/mm2 and a stored magnetic energy density of 100 MJ/m3
FCC-hh (16 T, Thot ≈ 350 K) is designed for a current density in the coil of 500 A/mm2 and a stored magnetic energy density of 160 MJ/m3

## Slide 29: Forces
An electric charged particle q moving with a velocity v in a field B experiences a force FL called electromagnetic (Lorentz) force (N):
A conductor carrying current density J (A/mm2) experiences a (Laplace) force density fL (N/m3):
(O. Heaviside) E.A. Lorentz, P.S. Laplace

## Slide 30: Electromagnetic forces - solenoid
The e.m. forces in a solenoid tend to push the coil
  Vertically, towards the mid plane (Fy < 0)
  Radially, outwards (Fr > 0)
The radial force produces a hoop stress
Field
Force
Fy
Fr
Fr
Fy
Graphics by courtesy of P. Ferracin, S. Prestemon, E. Todesco

## Slide 31: Magnetic pressure
Ideal case of an infinite solenoid
    Vertical and uniform magnetic field
    Radial and uniform electromagnetic force
Magnetic pressure
r
z
B0
fr
t
J
B0 = 16 T  p = 1000 bar
fr

## Slide 32: Electromagnetic forces: dipole
The electromagnetic forces in a dipole magnet tend to push the coil:
  Vertically, towards the mid plane (Fy < 0)
  Horizontally, outwards (Fx > 0)
Tevatron dipole
Fy
Fx
Field
Force
Graphics by courtesy of P. Ferracin, S. Prestemon, E. Todesco

## Slide 33: Forces in dipole coils
Force increases with the square of the bore field
  Requires massive structures (high-strength materials, volume, weight)
  The stress limit is usually in the superconducting coil (superconductor and insulation, mitigated by Je≈1/B)
In practice the design of high field magnets is limited by mechanics
Force per coil quadrant in high-field dipoles built or designed for accelerators applications and R&D
Lorentz forces in the plane of a thin coil of radius Rin generating a dipole field B (thin shell approximation), referred to a coil quarter

## Slide 34: Magnet structures
mid 1970’s, FNAL: Collared coils
A. Tollestrup, Proc. Int Conf. on the History of Original Ideas and Basic Discoveries in Particle Physics, Erice (1994).
2002, LBNL: Bladder and keys
R.R. Hafalia, et al., IEEE TAS, 12(1) (2002), pp. 47-50.
1998, TAMU: Stress management
N. Diaczenko, et al., Proc. PAC, Vancouver (1997), pp.3443-3345.
2014, LBNL: CCT
S. Caspi, et al., IEEE TAS (2014), p. 4001804.
1975, MIT: CICC
M.O. Hoenig, et al., Proc. 5th Magn. Tech. Conf., Frascati(1975), p. 519.
2017, FNAL: SM cos(q)
V. Kashikin, et al., Proc. IPAC, Copenhagen (2017), pp. 3597-3599.

## Slide 35: Stress in high field magnets
LHC
11T
QXF
FCC
HE-LHC
Unconstrained scaling
Stress limited
reducing J
High field superconductors (Nb3Sn, REBCO, Bi-2212, Bi-2223, …) are brittle materials and stress/strain sensitive
Cracks development

## Slide 36: Limit 3 – Stress and strain
Allowable stress sets an upper limit to the maximum current density and field
Corollary – this sets an upper limits to the maximum affordable field
HL-LHC (12 T) achieves a design electromagnetic stress of approximately 100 MPa
FCC-hh (16 T) is designed for electromagntic stress of 150 MPa (limit of Nb3Sn)

## Slide 37: High field solenoids
HTS is the only path beyond 16 T
Superconducting
All SC 32 T HTS insert
Hybrid HTS 45.5 T insert

## Slide 38: High field dipoles (FCC-hh)
Upper limit of LTS (Nb3Sn)
HTS is the only path beyond 16 T

## Slide 39: Overview
Accelerator magnets and examples
HEP detector magnets and examples
Resistive and coil magnet designs
Superconductors and their delicacies
Performance limits of accelerator magnets
Muon collider magnet challenges
Summary and perspective

## Slide 40: Muon Collider magnets
> 40 T, 60 mm
RCS
20 T, 200 mm
Radiation heat load ≈ 5…10 kW
Radiation dose: 80 MGy
NC ±1.8 T, 400 Hz 100 mm x 30 mm
SC < 10T
100 mm x 30 mm
SC dipole
NC dipole
NC dipole
SC dipole
16 T peak, 150 mm
Radiation heat load ≈ 5 W/m
Radiation dose ≈ 20…40 MGy
HTS !
HTS !
HTS ?
HTS ?

## Slide 41: Target and capture solenoid (20 T)
Operating field: 20 T
Operating temperature: 20 K
M. Takayasu et al., IEEE TAS, 21 (2011) 2340
Z. S. Hartwig et al., SUST, 33 (2020) 11LT01
MIT “VIPER” conductor
Strong connection to HTS magnets for fusion
A Portone, P. Testoni, J. Lorenzo Gomez, F4E
MuCol HTS conductor
Operating current: 61 kA

## Slide 42: Final cooling (40 T)
B. Bordini, CERN
Inner Ring
Outer Ring
‘Modular’ Coil
1 % Field Homogeneity
Bore
Support Plate
‘Correction’ Coil
T. Mulder, CERN
B. Bordini, CERN
A. Dudarev, CERN
smax = 600 MPa
40 T solenoid design
Strong connection to HTS magnets for science

## Slide 43: Back to the future – NI coils
Non-insulated winding
Nb3Sn tapes (12 mm width, 0.1 mm thickness) produced at RCA, 1965

## Slide 44: Accelerator magnets (±1.8 T)
F. Boattini, CERN
5.07 kJ/m
5.65…7.14 kJ/m
5.89 kJ/m
Warm dipoles are pulsed from
-Bmax to +Bmax at high speed (0.35 to 6.37 ms) every 200 ms
Cold dipoles provide a steady baseline field of about 10 T
The main challenge is the management of the power in the resistive dipoles (several tens of GW):
Minimum stored magnetic energy
Highly efficient energy storage and recovery
HTS flat racetracks
Rectangular magnet bore 100 mm x 30 mm
peak field
10.4 T
b3 = -7.2 units
b5 = -1.4 units
b7 = -0.03 units
A simple HTS racetrack dipole could match the beam requirements and aperture

## Slide 45: Collider magnets limits (Nb3Sn)
Work in progress to provide analytical expression for the magnet design limits (including protection and cost)
  Maximum field and gradient vs. magnet aperture in LTS and HTS
  Combined function limits B+G and B/G
Margin limit
Stress limit
Dipoles
Quadrupoles
Stress limit
Margin limit
Present design range
Present design range

## Slide 46: The need for energy
CERN uses today 1.3 TWh per year of operation, with peak power consumption of 200 MW (running accelerators and experiments), dropping to 80 MW in winter (technical stop period)
Electric power is drawn directly from the French 400 kV distribution, and presently supplied under agreed conditions and cost
Supply cost, chain and risk are obvious concerns for the present and future of the laboratory

## Slide 47
Future helium supply is limited and entails a substantial economical and availability risk
Courtesy of F. Ferrand, CERN

## Slide 48: Energy efficient cryogenics
The 60…80 K range would be a dream…
LHC
(FCC)
ESS
Need efficient cryo-plant and heat removal scheme in the range of 10…20 K (see work at ESS)
This could be the best range of operating temperature of a future HEP collider
RHIC
Tevatron
HERA
LHC
HTS may be the only path towards a future collider
Nb-Ti
8T
5T
Nb3Sn
16T
12…14T
HTS
40…60T
20…40T
a few T
1.9
4.2
77
Credits to P. De Sousa and R. Van Weelderen, CERN
W/Q = (Th-Tc)/Tc

## Slide 49: Conductor cost
Grateful thanks to fusion !
Impressive cost reduction in HTS !
Based on CERN orders and requests for quotations 2010-2022
Normalised costs are not aligned to currency, nor corrected for inflation

## Slide 50: Compact windings
350 A/mm2
500,000 km
950 A/mm2
150,000 km
We need to increase the winding current density to fall in a reasonable range of tape length (the same applis to conductor mass for LTS)
Unresolved issues:
  Winding geometry for tapes and stacks (ends, alignment, transposition possibly superfluous ?)
  Mechanics of coils under the exceptional electromagnetic loads (longitudinal stress in the range of 600 MPa, transverse stress in the range of 400 MPa)
  Quench management at high current and energy density (above 100 MJ/m3)
  Radiation hardness of materials and coils (40…80 MGy and 1022 n/m2)

## Slide 51: The HEP push towards HTS
Reduce energy consumption
(FCC-ee 350 MW, FCC-hh 580 MW)
Increase energy efficiency
(COP at 1.9 K is about 1000)
Risk with helium supply chain
(FCC-hh would require 900 tons of lHe)
Infrastructure (magnet) cost
(FCC-hh quoted at 9 BCHF)
Operate SC magnets at higher cryogenic temperature (gas)
Avoid large liquid helium bath and operate with gas (lower density)
Reduce SC cost per unit length and current
Increase coil current density to decrease conductor inventory
Compact HTS windings
Target JE 1000 A/mm2
Operation in gaseous He
Range of 15…25 K
5 T at 2800 A
JE = 250 A/mm2
16 T at 2800 A
JE = 850 A/mm2
Calculation example
(T. Lecrevisse, CEA)

## Slide 52: Overview
Accelerator magnets and examples
HEP detector magnets and examples
Resistive and coil magnet designs
Superconductors and their delicacies
Performance limits of accelerator magnets
Muon collider magnet challenges
Summary and perspective

## Slide 53: Summary and perspective
Superconducting magnets, one of the key technologies of accelerators, may be on the verge of a grand change. Thanks to HTS, and driven by:
  Needs for yet higher fields, as usual, but also …
  … considerations of energy efficiency, supply chain risk reduction and sustainability
This will be possible overcoming known limitations from mechanics and quench protection by:
  Innovation (e.g. non-insulated windings), that …
  … break the scalings I discussed here
These are exciting times for all, for you foremost !

## Slide 54: Magnetars – the ultimate frontier !
108…1011 T
Magnetar found very close to the supermassive black hole, Sagittarius A*, at the center of the Milky Way
Image courtesy of NASA