## Slide 1: Joule-class Yb:YAG lasers for driving plasma-modulated plasma accelerators
by Mathias Krüger
A. Münzer and S. Karsch, S. Hooker and R. Walczak

## Slide 2
Concept of a Plasma-Modulated Plasma Accelerator (P-MoPA) [1]:
  Collaboration with University of Oxford / Group of S. Hooker
  Ultimate goal: 1 kHz, >1 J drive pulses for 0.5 GeV electron bunches
  Modulator: ps-scale laser pulse converted to burst of fs-scale pulses
  Accelerator: burst of pulses used as kHz driver for wakefield acceleration
  Medium: cm-scale plasma waveguide
        Good scalability with energy and average power (> 1 kHz, > 1J)
                [1] Phys. Rev. Let. 127, 184801 (2021)
kPAC - kHz Plasma Accelerator Collaboration
Notes: Low energy 100 mJ sub 100 fs driving wakefield (1-2%)
Followed by high energy picosecond beam, travels in the wakefield
Modulated spectrally
Temporally still smooth

## Slide 3
PFS and PFS-pro at CALA
Notes: Kurze Kachelübersicht PFS – PFS pro mit Kerndaten der beiden Systeme gegenübergestellt / \

## Slide 4
PFS and PFS-pro at CALA
PFS-pro
(1 kHz)
PFS
(10 Hz)
Notes: Bild ändern mit Frontalaufnahme aus Kontrollraum, Kästen mit farbiger Füllung einfügen für PFS und PFS pro

## Slide 5
The PFS System
(10 J, 10 Hz, <700 fs)
Notes: Nur Einleitungsfolie

## Slide 6
The 10 Hz PFS System
Notes: Übersicht zu PFS mit Kenndaten der Verstärker
-> Farben der letzten beiden Boxen ändern!

## Slide 7
The 10 Hz PFS System
Main amplifier key figures:
  Concept: 44 pass, double Type 2 imaging [2]
  Gain medium: 2x D38x3 mm 2% Yb:YAG @ 20°C cooling
  Pump per medium: 27 kW @ 940 nm, 1 ms, 10 Hz
    Output: 8.7 J +- 0.5 % @ 10 Hz, 60 mJ seed
[2] J. Körner, Applied Sciences, vol. 6, no. 11, 2016
Notes: Leistungsdaten des komprimierten Lasers inklusive NF Beam profile, FROG

## Slide 8
The 10 Hz PFS System
Thermal lens / LIDT limited operation:
  Cooling: Active mirror, liquid metal interfaced water cooling @ 20°
  Issue: Too efficient cooling, steep thermal gradients at 10 Hz // 270 W pumping
    Solution: Modified heatsink design with negligible gradients
Notes: Leistungsdaten des komprimierten Lasers inklusive NF Beam profile, FROG

## Slide 9
The 10 Hz PFS System
Compression:
  >3.1 nm bandwidth @ 10 J, 2.5 Hz
  86 % compressed to 672 fs
  FL: 652 fs
  G-error: 6%
Notes: Leistungsdaten des komprimierten Lasers inklusive NF Beam profile, FROG

## Slide 10
The PFS-pro System
(120 mJ, 1 kHz, 1.3 ps/37 fs)
Notes: Nur Einleitungsfolie

## Slide 11
The 1 kHz PFS-pro System
Notes: Prinzipieller Aufbau des Systems in Kacheln, von links nach rechts, sodass auf folgenden Folien jede Kachel beleuchtet werden kann und der entsprechende Teil des Lasers beschrieben werden kann

## Slide 12
The 1 kHz PFS-pro System
Main amplifier key figures:
  Concept: Ring type regenerative amplifier
  Gain medium: 2x Yb:YAG Thin-Disks (TRUMPF GmbH)
  Pump per medium: 1.5 kW @ 969 nm, CW/1 kHz
  Output @ 5 kHz: 200 mJ // 1000 W
  Output @ 1 kHz: 120 mJ // 120 W, non-optimized)
  0.3 % RMS power stability over 5h
Notes: Regen

## Slide 13
The 1 kHz PFS-pro System
Compression:
  Grating compressor 94% eff.
  Normal operation (no PreAmp):
    1.1 nm FWHM
    1.3 ps
  Broadband operation with old PreAmp:
    2 nm FWHM
    750 fs
Notes: Kompression

## Slide 14
The 1 kHz PFS-pro System
Multipass Cell (Herriott Cell):
  Nonlinear broadening by self-phase-modulation in gas (Argon, Helium)
  Resonator-like, up to 45 roundtrips
  8 m long chamber for 100+ mJ
Beam on
Mirrors 2/3
Input pulses
Broadened pulses
Foci
8 m
Notes: HC

## Slide 15
The PFS-pro System
Multipass Cell (Herriott Cell):
  Use of TEM11 mode via vortex phase plates
    2x bigger beam size with 2.5x less peak intensity
    Less ionization and LIDT issues, more throughput
TEM11*-like
560W (112 mJ)
1.3 ps
TEM00
Vortex phase plate
(SiO2 plates with a vortex surface)
Focus at 540W
(108 mJ)
>70% of Energy
within 1/e²
250 mBar Argon
Notes: HC

## Slide 16
The 1 kHz PFS-pro System
HC output and compression [3]:
  On record 108 mJ @ 5 kHz, ~75 nm, 96% eff.
  Compression of low energy fraction in CM compressor to 37 fs
    12 bounces on 4“ mirrors with -500 fs²
[3] Vol. 46, No. 5 / 1 March 2021 / Optics Letters
Notes: HC

## Slide 17
The PFS lasers for kPAC
Notes: Nur Einleitungsfolie

## Slide 18
kPAC @ CALA
Concept of P-MoPA experiment at CALA:

## Slide 19
First results of kPAC
First results:
  Pointing fluctuation: 10-30 % of respective focus diameter
  Timing jitter: 92 fs Std. Dev
  Stability of Herriott Cell: +-10 % bandwidth over 10 months (no maintenance)
  Timing jitter PFS / PFS-Pro
  Spectral stability Herriott Cell
  First hydrogen plasma channel