## Slide 1: Highly efficient proton acceleration from solid ultra thin plastic foils
Isra Salaheldin, M. Shi, P. Hilz, A. Sävert, G. Schäfer & M. Zepf
6th EAAC Workshop
19 September 2023

## Slide 2: Overview
Experimental campaign at HI-Jena with thin plastic foils
High-quality proton beams (20 MeV/J) via …
  … high laser contrast
  … high focus quality
  … thin plastic foils
Results from the experiment

## Slide 3: JETi200 laser system
Wavelength: 800 nm
Medium: Ti:Sapphire
Energy on target: up to 5 J
Pulse duration: 17 fs Peak power: 300 TW
Repetition rate: 5 Hz
Probe beam: 5 fs @ 750 nm
Double CPA system + XPW

## Slide 4: Plasma mirror for high laser contrast

## Slide 5: Deformable mirror for high-quality focus

## Slide 6: Ultra-thin foil fabrication in Jena
Fabrication Method:
Spin coating
Solution:
Formvar powder
Solvent:
Dichloroethane
Formvar Structure :
Target floating
30 nm target on the target holder
Thickness of 10 nm – 1 µm
Spin coating
Glass substrate

## Slide 7: Experimental parameters
for LP = 30
for CP = 21
Pulse duration = 25 fs
Energy on target = 1.23 J
Focal spot size = 1.7 µm
Target: Ultrathin (Formvar) foils
Foil thickness range = (10-200) nm

## Slide 8: Energy spectrum with LP from solid foils

## Slide 9: Energy spectrum with CP from solid foils

## Slide 10: Scaling with Intensity (LP)
LP

## Slide 11: Scaling with Intensity (CP)
CP

## Slide 12: Summary
Experimentally obtained monoenergetic proton beams (~35 MeV)
High energy conversion rate (~20 MeV/J)
TNSA for thicker targets with LP
Hybrid (RPA-CE) thin targets with CP
Reproduceable results
LP
CP

## Slide 14: Aluminum step filter
(a) (b) (c)
Aluminum step filter
raw data
front top

## Slide 15: Target thickness scan with CP laser

## Slide 16: 40 nm target under CP laser incidence