## Slide 1
Community Report on Accelerators Roadmap
Prospects of High Temperature Superconductors
Anna Kario, Simon Otten, Amalia Ballerino, Christian Barth, Carmine Senatore, Bernhard Holzapfel, Bernhard Auchmann, Jaap Kosse, Yifeng Yang, Andrea Malagoli, Thibault Lecrevisse, Andrzej Siemko

## Slide 2
High temperature superconductors – future for 20 T + (accelerator) magnets
D. Larbalestier, et al. Nat. Mater. (2014)
L. Rossi, C. Senatore, https://doi.org/10.3390/ instruments5010008
Mechanical stress limitation of superconductors
Coils structural materials constrains
Material tailored magnet designs
High Field Magnets
2

## Slide 3
HTS Enabling Technology
The physics landscape
 | Dipoles | Quadrupoles | Undulators/Wigglers | Detectors | Field (T)
FCC-ee |  | IR Quad |  |  | < 3 T
CEPC |  | IR Quad |  |  | < 5 T
ILC |  |  |  |  | < 2 T
CLIC |  |  |  |  | < 2.5 T
FCC-pp |  |  |  |  | 16 T -20 T
SppC |  |  |  |  | 12 T- 24 T
Muon Collider |  |  |  |  | Solenoids 20 T, 55 T
Higgs Factories
Energy Frontier
High Field Magnets
3
Notes: Future circular collider
Circular Electron Positron Collider
International Linear Collider
Compact Linear Collider
Super Proton-Proton Collider

## Slide 4
The High Temperature Superconductors workshop at CERN in 2023
High Field Magnets
4
https://indico.cern.ch/event/1220254/
Notes: Future circular collider
Circular Electron Positron Collider
International Linear Collider
Compact Linear Collider
Super Proton-Proton Collider

## Slide 5
Where do we stand with the ReBCO conductor for accelerator magnet application?
High current capability
Long lengths of ReBCO > 300m from several companies worldwide for demonstrator usage
High temperature margin (Tc~90 K)
React and wind technology
Mechanical properties: tensile stress ~600 MPa, transverse stress >300 MPa
High Field Magnets
5
Current homogeneity as function of length, temperature and field
- measurements (l,α, T, B)
- modelling
Quench protection
- mitigation of Normal Zone Propagation velocity
- novel protection methods
- partial insulation, cable, coil
Shear stress sensitivity
- conductor architecture
- delamination
Magnetization and the other AC loss components
- conductor, cable, coil architectures

## Slide 6
ReBCO transport critical current measurements
Various orientations in magnetic fields up to 19 T/21 T and variable temperatures
Characterisation of samples from different manufacturers, batches
Comparison of Ic / width – high performance tapes
High Field Magnets
6
T = 4.2 K
T = 20 K

## Slide 7
ReBCO tapes and cables mechanical properties
High Field Magnets
7
C. Zhou et al., IEEE TAS, Vol. 26, No. 4, June 2016.
Bruker
SuperPower
P. Gao et al 2019 Supercond. Sci. Technol. 32 055006.
Importance of study ReBCO tape mechanical properties, together with simulations, for understanding limits for future high-current cables and further high-field magnets.
Important study ReBCO cables under transverse stress to understand the limits in high-field magnets

## Slide 8
“New architectures” ReBCO synthesis laboratory
High Field Magnets
8
Intermediate 20 m length scale
Short length 0.5 m experiments to optimize deposition conditions for regular Y123 coatings
IBAD tapes from Faraday Inc., SuNAM and Shanghai SC under investigation
Jc (self-field, 77 K)>1MA/cm2 for 0.5 micrometers samples reached (inductively measured)
10 m>1 micrometer until June
Laboratory for testing at a small scale new scientific ideas, both on ReBCO tape and cables
PLD600
Substrate drum

## Slide 9
Bi-2212 has become a magnet conductor after more than 10 years of coordinated university-lab-industry support through DOE-OHEP and the CDRP
It has great advantages – genuinely multifilament with low AC loss, macroscopically isotropic, round and available in single pieces now > 1 km length in multiple architectures and variable diameters
It has major too –it requires Wind and React route for HEP and lab magnets at almost 900°C and now optimized Jc requires ~50 bar overpressure (1 bar O2 and balance Ar)
Wires have a breaking strength of ~170 MPa, well below the stresses foreseen for many magnets
BSCCO-2212 wire potential - USA effort
D. Larbalestrier, HiTAT Workshop, CERN, March 2023
High Field Magnets
9

## Slide 10
Drawing machines
Groove rolling machines
Flat rolling machine
R&D on Iron Based 122 PIT wires
Critical current density (Jc) through reliable, simple and scalable techniques that could enable industrialization
Target Jc  103 A/mm2 at 16 T
From mono to multi-filamentary wire
Target unit length  100 m
Iron Based Superconductors (IBS) Laboratory
High Field Magnets
10
A Gurevich, Ann. Rev. Cond. Matt. Phys 5 (2014) 35
C Yao and Y Ma, iScience 24 (2021) 102541
Ba-122:
Tc  38 K
Hc2(20 K) > 70 T

## Slide 11
ReBCO – different cables architectures
ReBCO Roebel flat cables
for EU Eucard 2
CORC® round cables
Advanced Conductor
Technologies
STAR® REBCO Wire
(0.8 mm)
University of Houston
Stack of tapes
MIT, CEA (I-FAST), ENEA, SPC, KIT, North China Electric Power University
MIT
High Field Magnets
11
Roebel bar, Martin Wilson
Bi-2223 tapes, Sumitomo
ReBCO: KIT, Robinson Research Institute, SuperOx

## Slide 12
3 kA @ 60 K (B = 0.7 T)
Round, flexible, electrically insulated REBCO cables
No measurable critical current degradation of tapes after cabling
Current rating of ReBCO cables: 600 A, 3000 A, 7000 A and 18000 A @ 60 K ( 0.7 T)
Cabling machine designed and constructed at CERN
Two layers of tape
On-line Polyimide insulation
…and ReBCO round Cables for HL-LHC
High Field Magnets
12

## Slide 13
REBCO CORC® CCT, LBNL
ReBCO Conductor On Molded Barrel (COMB)
Fermilab, STAR Wires
ReBCO Cloverleaf, CERN and UTwente
PhD Thesis of Th. Nes
BSCCO-2212 CCT, LBNL and ASC
Rutherford cable
High Field Magnets
13
Superconducting coil, ReBCO
Dummy coil
Feather-M2
Feather-M0
ReBCO Cloverleaf demonstrator CERN
Recent accelerator type HTS magnet developments

## Slide 14
High Field Magnets
14
Recent accelerator type HTS magnet developments
R. Gupta et al., IEEE TAS, Vol. 28, No. 3, April 2018
Chart: year
| 2012 | 2014 | 2016 | 2017 | 2018 | 2018 | 2018 | 2019 | 2019 | 2020 | 2020 | 2022 | 2023
REBCO | 2.6 | 0.2 | 3.03 | 0 | 4.52 | 3.1 | 8.6 | 2.4 | 1.2 | 4.5 | 2.91 | 0.5 | 0.79
Bi-2212 | 2.6 | 3.5 | 1.34 | 1.64
Bi-2223 | 1.9 | 1.19 | 1.61
 | 4.5
L. Rossi, C. Senatore, https://doi.org/10.3390/ instruments5010008

## Slide 15
Prototype ReBCO coils at CERN
Winding machine - up to 14 tapes
160
Electrically insulated stacks
of REBCO tapes
Ø int 37 mm
Ø ext 57 mm
Objective: demonstrator of 5 T in a background field of 15 T
Development of electrically insulated cables. Target: 10 kA @ 20 T, 5 kV
Model racetrack coils
Common coil design
Common-coil design, R. Gupta
High Field Magnets
15

## Slide 16
Prototype ReBCO coils at CEA
High Field Magnets
16
Phase 1 (KE5647) 2023-2025:
Simple or double Racetrack MI
Phase 2 :
magnet MI 16 T+
« EuCARD V2 »
Phase 3 :
« EuCARD V3 »
MI cold bore 16 T+
magnet
Aperture +
Field quality measurements
Models + techno
Global roadmap phases
Mechanics + high field +
Quench + assembly
CEA PEEC model
Technology
Notes: Use «Metal-insulated (MI)» winding:
  No need for insulation nor Cu stabilizer
  Considerable increase of the current density in the coil to reach very high fields

## Slide 17
Solenoid magnet 7 T
NI dry wound double ReBCO pancake coil
ReBCO coil mechanical support
146 mm
HTS/vapor cooled current leads
Prototype ReBCO coils at University of Twente
High Field Magnets
17
Chart: Current [A]
Non-insulated ReBCO coil at 4.2 K in background field
ReBCO Clovearleaf demonstrator test at 77 K

## Slide 18
MagDev Laboratory
REBCO, 2 tapes
18.2 T in the center, 20.3 T on the conductor
2 kA and 12 K
Aperture: 50 mm
Prototype ReBCO coils at PSI
NI coil technology license agreement with Tokamak Energy
High Field Magnets
18

## Slide 19
Summary
High Field Magnets
19
Current homogeneity as function of length, temperature and field
- measurements (l,α, T, B)
- modelling
Quench protection
- mitigation of Normal Zone Propagation velocity
- novel protection methods
- partial insulation, cable, coil
Shear stress sensitivity
- conductor architecture
- delamination
Magnetization and the other AC loss components
- conductor, cable, coil architectures
Improvements of the conductor architecture and realization of the protection
Quantification of the current homogeneity, setting the requirements
Enhance shear stress trough conductor architecture and prototype design
Advance conductor and cables architectures lowering magnetization and other AC losses