## Slide 1: Resistive read-out Silicon Detectors with internal gain
Luca Menzio
VERTEX 2023 - 32nd International Workshop on Vertex Detectors
Sestri Levante, 16-20th October

## Slide 2: Introduction

## Slide 3: 4D Tracking
Luca Menzio – INFN Toino
Adding the time information allows resolving events overlapping in space
If the timing information is present on each point along the tracks, the reconstruction can be performed employing only the compatible times
Non-compatible tracks are discarded at the trigger level – online rejection allows for reducing the amount of saved data
This work aims to describe the development of an option of silicon detector for 4D tracking
VERTEX 2023
17th October 2023
Notes: Resistive read-out devices are capable of measuring both time and space

## Slide 4: 4D Tracking Silicon Detectors - Overview
Luca Menzio – INFN Toino
VERTEX 2023
17th October 2023
No gain
Low-gain (LGADs)
No gain
Low-gain (LGADs)
BiCMOS
(SiGe)
3D
Si/Diamond
Resistive read-out
BiCMOS
(SiGe)
Standard read-out
CMOS
Planar
CMOS
Hybrid
Monolithic
Sensor
ASIC
Sensor
ASIC

## Slide 5: Resistive read-out in LGADs

## Slide 6: Resistive Read-out
In resistive read-out, instead of many p-n diodes, there is a single diode.
The n-doped implant is resistive and acts as a signal divider
Very uniform electric and weighing fields, perfect geometry for timing
Luca Menzio – INFN Toino
VERTEX 2023
17th October 2023

## Slide 7: Resistive Read-out Principles of Operation
e-h pairs are produced by the impinging particle in the sensor volume
Electrons are multiplied (LGAD)
Charge is induced in the n+ layer (resistive layer)
Nearby electrodes see a fast signal
Charges in the n+ flow to ground
AC-coupled electrodes
50 μm
Time resolution typical of thin LGADs
Luca Menzio – INFN Toino
Signal sharing
AC-coupled signals
VERTEX 2023
17th October 2023
In normal pixel detectors with
Resistive read-out sensors have

## Slide 8: Resistive Read-out
Charge sharing over silicon surface
Internal gain (LGAD)
Excellent position resolution with large pads
Excellent Timing
Low power consumption
Low material budget
+ 100 % intrinsic fill factor!
Luca Menzio – INFN Toino
VERTEX 2023
17th October 2023
Pros
Low channel density
Thin sensors

## Slide 9: Standard Silicon Detector vs RSD
Standard Silicon Detector
Resistive Read-out Detector
Resistive implant
~ 50 mm
---
- --
++
+++
Pixel size
~ 250 x 250 mm2
Silicon bulk
Contacts
Electronics
~ 150 mm
Gain implant
--
---
- --
+
++
+++
Pixel size
~ 25 x 25 mm2
Luca Menzio – INFN Toino
VERTEX 2023
17th October 2023
Notes: Parametrizzazioni prossima

## Slide 10: Active Foundries
The first AC-Coupled Resistive read-out LGAD sensor has been developed by Fondazione Bruno Kessler (FBK)
RSD1 prototype production [2]
Shortly after, other foundries manufacturing LGAD started producing LGADs based on resistive read-out:
Hamamatsu Photonics K.K. (HPK)
Brookhaven National Laboratories (BNL)
Institute of High Energy Physics (IHEP-IME)
Centro Nacional de Microelectrónica (IMB-CNM), the first batch production was just delivered
Relevant expertise is being gained!
Luca Menzio – INFN Toino
VERTEX 2023
17th October 2023
Notes: “info about HPK sensors will be brought in the next talk”

## Slide 11: Performance

## Slide 12: FBK Pixels Results
Two prototype runs of Resistive Silicon Detectors have been characterized:
RSD1 – proof of concept
RSD2 – aimed at improving the spatial resolution among the whole sensor area
  Optimized metal layouts to achieve more efficient signal sharing
Luca Menzio – INFN Toino
VERTEX 2023
17th October 2023
1.3 mm pitch
450 µm pitch
Chart: RSD2 crosses: spatial resolution for 4 different pitch sizes
| 29 | 53 | 69 | 154
1300 um | 95 | 50 | 33 | 15.4
450 um | 34 | 25.3 | 19.9 | 15.5 | 10.6 | 10.1 | 8.4 | 7.9 | 10.6
340 um | 44.8 | 34.1 | 21.87 | 19.9 | 13.85 | 12.8 | 10.6 | 7.4 | 6.33
200 um | 45.9 | 26 | 24.13 | 18.5 | 15.9 | 10.5 | 8.5 | 7.8 | 5.2 | 4.4
gain = 30
Tested with laser setup

## Slide 13: FBK Pixels Results
Two prototype runs of Resistive Silicon Detectors have been characterized:
RSD1 – proof of concept
RSD2 – aimed at improving the spatial resolution among the whole sensor area
  Optimized metal layouts to achieve more efficient signal sharing
Luca Menzio – INFN Toino
Time resolution typical of traditional LGADs
Spatial resolution ~5-10% of the pixel pitch
VERTEX 2023
17th October 2023
1.3 mm pitch
450 µm pitch
Test beam results

## Slide 14: BNL Strips Results
Devices produced by BNL with best results consist in resistive strip layout devices with different pitches.
Following laser and test beam campaigns, these devices demonstrated to be able to reach great spatial and temporal resolutions.
Luca Menzio – INFN Toino
Future studies are concentrated to improve the spatial resolution uniformity among the whole device surface (e.g. narrower metal pads).
VERTEX 2023
17th October 2023
Test beam results [4]

## Slide 15: IHEP-IME Results
The IHEP-IME foundry produced AC-coupled resistive detectors with different shapes and implant doses.
These devices have been tested employing a laser and beta setup [5], indicating the ability to achieve results comparable with the other producers.
Luca Menzio – INFN Toino
VERTEX 2023
17th October 2023

## Slide 16: Future Developments

## Slide 17: Future Developments
DC-RSD
Improvement of the RSD sensors aiming at addressing drawbacks of the AC-LGAD (see yesterday’s poster and [3]).
Buried layer LGAd
Sensors based on a continuous gain layer positioned deeper into the bulk to improve radiation resistance.
One batch was already produced but suffered from poor epitaxial deposition [7].
Luca Menzio – INFN Toino
DC-RSD
VERTEX 2023
17th October 2023
Signal confinement in DC-coupled devices brings:
Fewer electrodes involved in the reconstruction – better S/N
Smaller area covered by the signal – better performance in high-occupancy environments
Notes: Signal confinement parlare di piu’

## Slide 18: Conclusions
Resistive read-out prototypes have already demonstrated to be able to reach exceptional performance with low channel density
Provided by multiple producers – multiple R&D paths
Excellent performance in terms of spatial and temporal resolution
Margins for improvements:
Signals confinement – DC-RSD
Resistive read-out in LGADs looks like a very promising technology for 4D Tracking

## Slide 19: Thank you!

## Slide 20: Special Thanks to
We kindly acknowledge the following funding agencies and collaborations:
INFN - Gruppo V, UFSD and RSD projects
INFN – FBK agreement on sensor production (convenzione INFN-FBK)
Horizon 2020, grant UFSD669529
Dipartimenti di Eccellenza, Univ. of Torino (ex L. 232/2016, art. 1, cc. 314, 337)
Ministero della Ricerca, Italia , PRIN 2017, progetto 2017L2XKTJ – 4DinSiDe
Ministero della Ricerca, Italia, FARE, R165xr8frt_fare
Marta Tornago for all the nice drawings
Luca Menzio – INFN Toino
VERTEX 2023
17th October 2023

## Slide 21: References
  Resistive Read-out in Thin Silicon Sensors with Internal Gain, N. Cartiglia (2023) https://arxiv.org/abs/2301.02968
  Resistive AC-Coupled Silicon Detectors: Principles of operation and first results from a combined analysis of beam test and laser data, M. Tornago et al., NIM A (2021)
  Development of Resistive Silicon Detectors for 4D tracking, L. Menzio, PhD Thesis (2023)
  Characterization of BNL and HPK AC-LGAD sensors with a 120 GeV proton beam, R. Heller, JINST (2022)
  Timing and spatial performance of IHEP AC-LGADs, X. Zhang et al., JINST (2022)
  4-Dimensional Trackers, V. Cairo, R. Heller, S. Mazza A. Schwarzman et al, Showmass 2021 (2022)
  Buried Layer Low Gain Avalanche Diodes, Ronald Lipton, TIPP 2021 https://indico.cern.ch/event/981823/contributions/4293564/attachments/2251204/3818882/BL-LGAD-TIPP.pdf
VERTEX 2023
17th October 2023

## Slide 22: Requirements
The requirements for future facilities are
Plus the usability of the detectors up to 1017 neqcm-2
Nowadays sensors have
  5 µm obtainable with 25x25 µm2, but the number of channels is too high
  Better spatial resolutions are possible with charge sharing due to external magnetic field, but sensors become too thick
And they lack the desired temporal resolution (now )
A new solution is needed → 4D Tracking = Different sensor design
Luca Menzio – INFN Toino
VERTEX 2023
17th October 2023

## Slide 23: Timing in Silicon Devices
Until ten years ago, silicon devices were not employed for particles timing measurements
With the advent of the Low Gain Avalanche Diodes (LGAD) technology it became possible to achieve tens of picoseconds time resolution in silicon detectors
  The addition of a p+-doped region allows achieving electron multiplication leading to moderate gain (10-30) - large signals with low noise
  Thin (~50 μm) active thickness yields to fast signal rising edge
Electric Field
Electric Field
PiN
LGAD
Luca Menzio – INFN Toino
“recipe” of the Ultra Fast Silicon Detectors
VERTEX 2023
17th October 2023

## Slide 24: Low-Gain Avalanche Diode(s)
The LGAD technology has been optimized for timing in HEP.
Luca Menzio – INFN Toino
They can achieve when new
Can withstand radiation damage up to fluences of
Provide large signals, easily processable by electronics
Are thin ( 50 µm) - low material budget
But
Have no-gain area 70 µm → they cannot reach good enough spatial resolution with high fill factor
VERTEX 2023
17th October 2023

## Slide 25: RSD1 Radiation Hardness
Luca Menzio – INFN Toino
25
Similar to traditional LGADs
The space and time resolutions decrease due to the signal being smaller
No “RSD specific” effects have been found, resistive read-out is not sensitive to radiation damage up to 1E15 n/cm2
VERTEX 2023
17th October 2023

## Slide 26: Resolutions parametrization
due to the variation in the signal amplitude caused by the electronic noise ~ noise/(dV/dx)
accuracy of the reconstruction method
related to eventual variations in the signal sharing due to the experimental setup (i.e. amplifiers)
all sensor imperfections that could contribute to differences in signal sharing
Space
similar as before, ~ noise/(dV/dt)
non-uniform ionization contributes with ~30 ps in 50 μm thick sensors
propagation time from the impact point to the read-out pad. It is correlated to the precision of the hit position reconstruction
Time
Luca Menzio – INFN Toino
VERTEX 2023
17th October 2023
Notes: To produce the best possible sensor, one should keep in mind the physics behind

## Slide 27: “Traditional” Tracking in HEP
Tracking systems are a fundamental part of HEP experiments
Nowadays are composed by mainly silicon pixel or strips detectors positioned close to the collision point
Can measure primary and secondary interaction point(s)
Right now, at LHC vertexes do not overlap in space (pileup 50) and tracking resolves all vertexes
In future facilities such HL-LHC (pileup 150-200) standard trackers will not suffice
Luca Menzio – INFN Toino
CMS tracker
Thanks to the precise measurement of hit position on a surface, charged particle tracks are reconstructed
Measurement of charged particle momentum by curvature in magnetic field
VERTEX 2023
17th October 2023
LHCb VELO modules