## Slide 1: Development of HPK Capacitive-Coupled LGAD (AC-LGAD) detectors
Tomoka IMAMURA, Sayuka KITA, Junya NISHINO,
Yua MURAYAMA, Issei HORIKOSHI,
Koji NAKAMURAA, Kazuhiko HARA
University of Tsukuba, KEKA
32nd International Workshop on Vertex Detector
17/Oct/2023

## Slide 2: Detectors with high timing resolution
Future high energy physics experiments
Higher Energy
Higher luminosity
Event pile-up will be an issue
Solution
Timing information
More robust reconstruction!
140pileup@HL-LHC
1500pileup@FCC-hh
Detector with…
Good spatial resolution
Good timing resolution

## Slide 3: LGAD technology
Low-Gain-Avalanche-Diode
n+
p+
Al electrode
Oxide film
e
h
Elec Field
Operation principle of LGAD
p+ implantation below the n+ implantation to make gain layer
Local high electric field in p+ layer develops avalanche
Large amount of e/h pairs are created per initial electron
Creation of large signal in the vicinity
Good timing resolution
Gain layer
p-

## Slide 4: AC-LGAD detector
AC-LGAD detector has been successfully developed down to 100um pitch pixel detector with 100% fill factor
Uniform gain layer under segmented electrodes
n++
n+
p++
n++
p+
Al electrode
Oxide
n+
p++
n+
p++
n+
p++
DC-LGAD
Each electrode has individual gain layer
With Junction Termination Extension and p-stop
Low fill factor
AC-LGAD
n++
n+
p+
n++
p-
Al electrode
Oxide
e
h
arxiv:2305.12355

## Slide 5: Measurement setup
Beta-ray
IR laser
Electron from 90Sr beta decay
In the bath to keep the temperature
DAQ system
Sensors on amplifier board
Wire-bonded sensor electrodes to amp inputs
Each amp channel employs two-stage fast charge sensitive amp IC
16 channels available for one board
LeCroy Waverunner 8000
350MHz – 2GHz
10GS/s
8ch
Infra red laser (1065nm)
Laser size σ~1um
Inject through slit made in the sensor
MCP-PMT 240
as timing reference
Wire bonding
90Sr
LGAD Sensor
MCX cable
MCX cable

## Slide 6: Timing resolution
Time walk
Minimize contribution
by adopting constant
fraction
50% of
Max pulse height
Use a fraction of pulse height max instead of a fixed threshold
Jitter
Big signal size is important to reduce jitter effect
+ the smaller noise as well
Determine the best bias voltage
Landau noise
Non uniform energy deposition of MIP
Laser measurement results do not include this effect
Thinner sensors should reduce this effect
: noise sigma , : rise time
: signal size

## Slide 7: Timing resolution results
●landau
＊jitter
○Time reso.
Lab meas | 50um | 30um | 20um
Timing resolution | 38.8ps | 31.5ps | 31.2ps
Jitter | 9.8ps | 11.8ps | 15.9ps
Landau noise | 37.5ps | 29.2ps | 26.8ps
Laboratory measurement
+ +
+ +
IR laser
Beta
Beam test measurement
Uniform timing resolution over the detector has been observed
2x2 pad with 500um square electrodes
Injected 120GeV Proton beam at FTBF
Thinner samples have better timing resolution due to landau noise
~20ps
TB meas

## Slide 8: Radiation damage on LGAD
Future high energy physics experiments
Higher Energy
Higher luminosity
Detectors will be exposed to large amount of radiation
2×1016 neq/cm2
10MGy
e.g. Inner trackers in HL-LHC ATLAS at 4000fb-1
Acceptor removal
Single Event Burnout
For bias voltage with average E-field of >12V/um, a large energy deposit happens to create a crater
Our sensors are 50um upper limit is 600V
n+
p+
e
h
p-
  One of the major effects of radiation damage of LGAD
  Acceptor doping concentration in gain layer is reduced by radiation damage
Shallow dope
Radiation damage
Defect complexities
need to apply higher bias voltage

## Slide 9: Ideas to improve radiation hardness
Need to reduce the bias voltage after the irradiation
need to reduce the effect of acceptor removal
Compensation
Partially-Activated-Boron
Irradiation test
  CYRIC at Tohoku University
  70MeV proton beam at 7nA~1600nA
  Temperature was set to -15℃
  Uniform scanning over the sensors
  7×1015, 3×1015, 6×1014,
  8×1013 neq/cm2
Made samples Irradiation test IV & Signal measurement
Samples

## Slide 10: Compensation(I)
Amount of effective p+ may not reduce if donor removal is fast enough
Donor removal
Acceptor removal
Both p and n are reduced
Dope quantity
depth
Radiation damage
Dope quantity
depth
n+
p+
e
h
p-
Result of first samples
Non-irrad
6×1014
3×1015
No significant improvement has been observed
 | p+ Boron | n+ Phosphorous | effective p+
2.5B+1.5P | 2.5a | 1.5a | a
1.5B+0.55P | 1.5a | 0.55a | 0.95a
Reference | a | 0 | a
Tested samples
IV curves are overlapped with reference sample

## Slide 11: Compensation(II)
Higher dope concentration will help suppressing acceptor removal effect
  Reduce the reduction factor of acceptor
Dope concentration
Reduction factor of acceptor
Result of higher dope concentration samples
Signal measured using 90Sr β
Operation voltage is defined as the voltage with the largest S/N
IV measurement
Compensation with high dope concentration reduces acceptor removal effect
 | p+ Boron | n+ Phosphorous | effective p+
10B+9.2P | 10a | 9.2a | 0.8a
5B+4.05P | 5a | 4.05a | 0.95a
Reference | a | 0 | a
➡No signal have been observed
Non-irrad
6×1014
3×1015
Fluence dependence of increment of operation voltage
IEEE Transactions on Nuclear Science , 65, Issue: 8, 2018

## Slide 12: Compensation – MPV of non-irradiated samples
Signal MPV dependence on dope concentration
Signal size is reduced by total dope concentration of gain layer implantation
Higher dope concentration seems reduce acceptor removal more
No signal has been observed with 10B+9.2P sample…
Only for non-irradiated samples
Relative dope concentration is the dope concentration normalized by reference one
Difficult to improve by simply increasing dope concentration
Compensation method will be developed with carbon dope as the next step…

## Slide 13: Partially-Activated-Boron(I)
Conduction Band
Valence Band
Bs
acceptor
Bs ➡ Bi
Bi + O ➡BiO
Conduction Band
Valence Band
donor
BiO
Boron inactivation
Inactivated Boron combine with Oxygen
Clean up the oxygen before irradiation to prevent Bi from becoming BiO - new donor
Bi deliberately left in p+ layer takes oxygen with it
Result of first samples
Break down voltage was ~50V
Not enough to observe signal
Break down voltage of irradiated samples seem less than reference sample …?
Break down voltage tuned samples have been tested as second samples
Non-irrad
6×1014
3×1015
BS substitutional Boron
Bi interstitial Boron

## Slide 14: Partially-Activated-Boron(II)
Result of break down voltage tuned samples
IV measurement results
Bs
Bs
Bi
Fully activated
Injected Bi the same amount as activated Bs
1PAB
Bs
Bs
Bi
Injected Bi the half amount as activated Bs
0.5PAB
Fully activated
Second samples … Inject additional boron over fully activated boron
No significant improvement has been observed
Fluence dependence of increment of operation voltage
Signal measured using 90Sr β
Operation voltage is defined as the voltage with the largest S/N
BS substitutional Boron
Bi interstitial Boron

## Slide 15: Conclusion
Detector with high timing resolution is needed
  LGAD detector is being investigated as a detector with superior timing resolution
AC-LGAD detector is successfully developed
  Finely segmented pixel sensor solving fill factor problem
  ~30ps timing resolution with laboratory measurement setup
  ~20ps timing resolution with 120GeV proton beam
  Uniformed timing resolution
Two novel ideas to improve radiation hardness have been tested
  Compensation method
  higher dope concentration seems effective in reducing acceptor removal
  effect, but shows smaller pulse
  Partially-Activated-Boron method
  No significant improvement has been observed so far

## Slide 16: Back up

## Slide 17: Bias voltage dependence of signal and noise

## Slide 18: Tested samples and results
Compensation
Partially-Activated-Boron
 | p+ Boron | n+ Phosphorous | effective p+
10B+9.2P | 10a | 9.2a | 0.8a
5B+4.05P | 5a | 4.05a | 0.95a
2.5B+1.5P | 2.5a | 1.5a | a
1.5B+0.55P | 1.5a | 0.55a | 0.95a
Reference | a | 0 | a
1PAB
  Once the activation is complete, inject an equal amount of Boron and left inactivated
0.5PAB
  Once the activation is complete, inject a half amount of Boron and left inactivated
Fluence dependence of increment of operation voltage
Dope concentration dependence of MPV

## Slide 19: Degradation due to radiation damage
Increase in operation voltage – non-linear function of fluence
Reduction of signal size

## Slide 20: TID damage
Already studied
  Gamma ray irradiation with 60Co
IV measurement
Pulse height distribution
Cross talk
The effect of TID damage is small*
*Compare with proton irradiation

## Slide 21: Dosimetry
Method
Calibration
Al
Sensor
P
Proton irradiation to Al
２４Na are produced
1.37MeV&2.75MeV γ-ray
Decay with half-lifetime 15hrs
Ge detector
Efficiency due to solid angle
  Depending on the distance
    10mm
    30mm
    60mm
Energy efficiency
  - γ→ photoelectric absorption + Compton scattering
*with 60Co，137Cs
→extrapolation
Ge detector

## Slide 22: CA and CD relations
Assuming an exponential reduction in irradiation dose[2]
Using the relation from the IV measurement results
  Overlap among all three conditions
p+
n+
reduction factor of donor
irradiation dose
effective p+
p+
effective p+
=
Reference
Compensation

## Slide 23: Signal measurement setup
Signal measurement with Sr90
HV
Sr
sensor
Amplifier board
PC
PMT
LV
HV
trigger
bath
Oscillo
scope
Lead shield
Non-irradiated samples : 20℃
Irradiated samples : -20℃

## Slide 24: Cross talk of AC-LGAD
Larger n+ resistivity
smaller cross talk
JFY2019
sample
JFY2020
sample
E-b
D-b
D-a
C2-b
C2
NIMA 1048(2023) 168009

## Slide 25: Gain of LGAD detector

## Slide 26: Some dependence of break down voltage
low
mid
high
Dope concentration dependence
Thickness dependence