## Slide 1: Measurements at the SIRAD irradiation facility
Luca Silvestrin
Università di Padova, Dipartimento di Fisica e Astronomia
INFN Sezione di Padova
LNL User Meeting LNL, November 17 2023

## Slide 2: Radiation Effects in electronics
TID - Total Ionizing Dose
  Small Eionization deposited uniformly and delivered over a long time
  Slow drift of device parameters due to charge accumulation in SiO2
V
+
-
V
+
-
V
+
-
V
+
-
Poly
SiO2
Si
e
h
e
h
h
h
h
h
h
h
SEE - Single Event Effects
  Effect due to the passage of a single energetic ionizing particle
  Sudden large Eionization deposited in the “wrong” place at the “wrong” time (sensitive junction)
Interstitial and vacancy defect creation.
exiting
particle
incident
particle
interstitial
vacancy
Frenkel pair
DDD - Displacement (Bulk) Damage Dose
  Non-ionizing E transfers to atomic nuclei (Coulomb nuclear interactions).
  Cumulative displacement damage of silicon lattice
Ionization
Cumulative

## Slide 3: Radiation environments of interest
High Energy and Nuclear Physics Environments
Space environments
Everyday environments
NASA Curiosity rover on Mars

## Slide 4: Single Event Cross section curve
Cross section curve of the ESA-SEU monitor.
Simulatio of the sensitivity to single event upset of a SRAM memory cell. (Courtesy of prof. Barney Doyle)

## Slide 5: The SIRAD irradiation facility
  SEE tests with heavy ions
  DDD with protons and lithium ions
  TID with heavy ions
  Material modification with heavy ions
Beam
diagnostics

## Slide 6: SIRAD technical characteristics
The irradiation chamber
(active since 2006)
Diameter : 80 cm
Depth: 80 cm
It is used for global SEE tests, bulk damage and TID studies
The chamber is open with the sample holder exposed

## Slide 7: SIRAD technical characteristics
Motorized sample holder
Horizontal transl. 30 cm
Vertical transl. 15 cm
Resolution 10 µm
Rotation axis vertical, +/-80o (1o steps)
The dosimetry systems inside the irradiation chamber
Fixed PIN Silicon diodes board
Faraday cup
Pointing laser
Mirror of the optical inspection system
http://www.youtube.com/watch?v=sKPew-nnfog

## Slide 8: Ion beams available at SIRAD
Ion Species | Energy [MeV] | q1 | q2 | Rigidity [T∙m] | Range in Si [m] | Surface LET in Si [MeV×cm2/mg]
1H | 28 | 1 | 1 | 0.77 | 4340 | 0.02
7Li | 56 | 3 | 3 | 0.95 | 376 | 0.37
11B | 80 | 4 | 5 | 0.86 | 185 | 1.13
12C | 94 | 5 | 6 | 0.81 | 164 | 1.53
16O | 108 | 6 | 7 | 0.86 | 107 | 2.95
19F | 122 | 7 | 8 | 0.87 | 95 | 3.90
28Si | 157 | 8 | 11 | 0.87 | 61 | 8.58
32S | 171 | 9 | 12 | 0.89 | 54 | 11.1
35Cl | 171 | 9 | 12 | 0.93 | 50 | 12.7
48Ti | 196 | 10 | 14 | 1.00 | 40 | 20.9
51V | 196 | 10 | 14 | 1.03 | 38 | 22.6
58Ni | 220 | 11 | 16 | 1.02 | 37 | 29.4
63Cu | 220 | 11 | 16 | 1.06 | 34 | 31.9
74Ge | 231 | 11 | 17 | 1.11 | 33 | 36.9
79Br | 241 | 11 | 18 | 1.10 | 33 | 41.8
107Ag | 266 | 12 | 20 | 1.21 | 29 | 58.4
127I | 276 | 12 | 21 | 1.28 | 30 | 65.4
197Au | 275 | 13 | 26 | 1.52 | 26 | 79.1
Typical ions available at SIRAD serviced by the XTU-Tandem accelerator, assuming:
  Tandem voltage at 14 MV,
  the most probable charge state using two strippers.
Note: The range and surface LET are in silicon (SRIM).
The magnetic rigidity is also tabulated. The rigidity limit of SIRAD is ~ 1.6 T-m
1st multi-source
(19F, 35Cl, 79Br, 127I)
2nd multi-source
(16O, 28Si, 58Ni, 107Ag)
f = 0.25

## Slide 9: SIRAD collaboration in 2013-2023
Univ. e INFN Padova
Univ. e INFN Milano-Bicocca
Univ. e INFN Torino
Univ. e INFN Ferrara
INFN Pisa
INFN Trieste
Univ. and INFN Padiva
INFN Roma-Tor Vergata
Univ. Cassino
INAF IAPS
ENEA
CERN
EPFL
IFIN-HH
Micron Technology
ESA
NASA-JPL
Technical University of Braunschweig
CEA-LETI
STMicroelectronics
Saphyrion (Lugano)
LUGANO
CASSINO

## Slide 10: SEE tests in Non-Volatile Memories
Non-volatile memories are used in almost all electronic applications, from smartphones to servers, and from microwave ovens to cars
3D devices are the last frontier to reach ever-increasing levels of integration and capacity
Numerous irradiations performed on state-of-the art non-volatile memories, using heavy ions
Spokepersons: Marta Bagatin and Simone Gerardin, Università and INFN Padova
Channel
K. Parat et al., IEDM 2015
32 layers (WL)
few mm
The floating gate (annulus shaped) is sandwiched between the tunnel oxide and the interpoly dielectric.

## Slide 11: SEE tests in Non-Volatile Memories
Particles create clusters of cells with shifted threshold voltage
Different cell technologies tested: floating gate vs charge trap
Tests at SIRAD by the UniPD Information Engineering Department were instrumental to assess the performance of 3D non-volatile memories in harsh environments
Spokepersons: Marta Bagatin and Simone Gerardin, Università and INFN Padova
Nickel (LET 29 MeV cm2/mg) at 0°
Nickel (LET 29 MeV cm2/mg) at 30°

## Slide 12: SEE tests in SiC Power Devices
A high-resolution measure of gate and drain leakage currents during irradiation.
A synchronized time base
The collection of drain and gate current pulses during each irradiation step.
Experimental Set Up
SiC power devices are the primary candidates to integrate/replace standard Si-based devices in applications where high frequencies, high operating temperatures, and reduced volumes are required.
The experimental set-up is designed to achieve the best behavior in terms of signal-to-noise ratio, allowing the measurement, during irradiation, of the gate leakage current down to the hundreds of picoamperes, range and the drain leakage current down to the nano amperes range. The circuit acquires the current pulses at both gate and drain terminals and, finally, a synchronized time base, allows us to correlate the leakage current jump to the current pulse that caused it.
Courtesy of Francesco Velardi, University of Cassino

## Slide 13: SEE tests in SiC Power Devices
Main results
1.2 kV SiC Schottky diode
Thermal Burnout
1.2 kV SiC Power MOSFET
The failure critical voltage is related to the different penetration ranges of the bromine ions.
The plasma filament, created by the ionizing particle perturbing the electric field, forces it beyond its track. If the ion traverses the entire epitaxial layer, the simultaneous presence of a very high conduction current density and an intense electric field results in a considerable power density at the metal/epitaxy interface, leading to a thermal failure.
The experimental data evidence three critical regions in terms of SEE sensitivity.
At very low bias voltages, the gate latent damage severely compromises the oxide integrity, reducing the maximum operating voltage to a value lower than 100V.
Starting from about VDS= 350V, the sudden increase of the drain leakage current reveals progressive drain damage, injuring the drain structure.
At about VDS=500V, a classical burnout takes place.
The burnout is not related to the progressive drain injury.
Ion | Energy [MeV] | Critical VDS [V]
127I | 276 | 65 – 80
79Br | 240 | 70 – 85
58Ni | 220 | 75 – 85
Gate Latent Damage
Courtesy of Francesco Velardi, University of Cassino

## Slide 14
Beamtime allocation (2013-2023)
Chart: Days of beamtime allocated for SIRAD
| 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019 | 2020 | 2021 | 2022 | 2023
 | 20 | 24 | 25 | 21 | 6 | 14 | 1 | 2 | 0 | 3 | 11
Courtesy of prof. S. Mattiazzo - University of Padova
and O. Carletto - LNL accelerator division.
Beamtime shortage
Pandemic
Tandem stop

## Slide 15: International School on detectors and radiation damage
October 23–25, 2023
Padova, Palazzo della Salute
… and its legacy
The school, will review and explain the latest advancements in solid-state sensors design and manufacturing and their applications.

## Slide 16: Conclusions
SIRAD is a strategic facility for INFN, to validate electronics which has to survive in radiation harsh environments in HEP experiments;
After thirty years of activity, the SIRAD collaboration is well established and still growing.

## Slide 17: The end backup slides follow

## Slide 18: SEU Test on the ALICE ITS ALPIDE DTU
Data Transmission Unit (DTU) for the ALPIDE ASIC for the ALICE experiment
Data rate : 1.2 Gb/s
Input clock : 40 MHz
Double Data Rate
SEU tolerant (tested at SIRAD)
Installation ongoing
Ag 0°
Ni 45°
Ni 0°
Ni 20°
Si 45°
Si 20°
Si 0°
O 45°
Ag 0°
Ni 0°
Ni 45°
Si 45°
Spokeperson: Gianni Mazza, INFN Torino

## Slide 19: 2013-2019: space and other applications
Università di Padova – DEI (Dipartimento di Ingegneria dell’Informazione)
  SEE on non volatile Flash memories, non volatile phase change memories (PCM), non volatile resistive memories (RRAM), SRAM and flip flop in BCD technology, GaN transistors and MIM capacitors, in collaboration with Micron Technology, ESA, NASA-JPL, Technical University of Braunschweig, CEA-LETI, STMicroelectronics
IXPE (INFN Roma Tor Vergata, INFN Pisa, INAF IAPS)
  Single Event Latchup (SEL) and SEU sensitivity of the ASIC in the Gas Pixel Detector of the X-ray Imaging Polarimetry Explorer satellite mission
Università di Cassino e del Lazio Meridionale (Dipartimento di Ingegneria Elettrica e dell’Informazione)
  Single Event Effects in Power MOSFETs
ENEA
  Investigation of the effect of high fluence irradiation on the swelling and microstructural behavior of DS4 steel and on of anti corrosion coatings for high temperature operation
TERA (INFN Torino)
  SEU test of the Tera ASIC (hadron beam monitoring in cancer treatment)
space
other
See Gerardin’s talk
See Velardi’s talk

## Slide 20
Chart: year
| 2000 | 2001 | 2002 | 2003 | 2004 | 2005 | 2006 | 2007 | 2008 | 2009 | 2010 | 2011 | 2012 | 2013 | 2014 | 2015 | 2016 | 2017 | 2018 | 2019
 | 7 | 17 | 25 | 26 | 20 | 12 | 6 | 12 | 6 | 8 | 8 | 7 | 22 | 20 | 24 | 25 | 21 | 6 | 14 | 0
2013-2019
Beamtime allocation (2000-2019)
Chart: 
Chart: 
| INFN | DEI Padova | Cassino | Enea | Others
INFN DEI Padova Cassino Enea Others | 54 | 19 | 22 | 12 | 3
Chart: 
| HEP | SPACE | Other
HEP SPACE Other | 54 | 27 | 29

## Slide 21: SEU Test on GBLD chip
GBLD is a radiation tolerant laser driver for the GigaBit Transceiver (GBT) project (which, in its turn, is part of the “Radiation Hard Optical Link Project” which aims at developing a radiation hard bi-directional optical link for use in the LHC upgrade programs)
Data rate : 5 Gb/s
Laser types : EE and VCSEL
Technology : CMOS 130 nm
SEU tolerant (tested at SIRAD)
~91000 chips produced
Spokeperson: Gianni Mazza, INFN Torino
Notes: the GBT part of the “Radiation Hard Optical Link Project” which aims at developing a radiation hard bi-directional optical link for use in the LHC upgrade programs. The link targets data transmission between the on-detector and off-detector electronics serving simultaneously applications such as data acquisition, timing, trigger and experiment control. The GBT Project it self aims at the development of radiation hard chipset that will allow the implementation of such a link. The project aims also at the development of HDL code to enable FPGAs to interface directly with the links based on the GBT chip set.

## Slide 22: 2013-2019: HEP applications
CHIPIX65 (INFN Padova, INFN Torino, INFN Bari, INFN Pavia, INFN Pisa, INFN Milano, CERN)
  Study of Single Event Effect (SEE) on pixel readout integrated circuits in 65nm for HL-LHC upgrade
LHCb (INFN Ferrara, CERN, IFIN-HH)
  Radiation hardness tests and qualification for SEE of the read‐out electronics chain for the Upgrade of the LHCb RICH detectors at CERN and Radiation hardness (SEE) on FPGAs in the context of LHCb Upgrade
PANDA (INFN Torino)
  Single Event Upsets (SEU) in the ToPix4 ASIC for the pixel detector readout of the PANDA experiment
ALICE (INFN Padova, INFN Torino, CERN)
  Study of proton-induced bulk damage on the prototype pixel and SEU tests of the GBLD laser driver for sensors for the ALICE ITS upgrade
CMS (INFN Padova, INFN Pavia, INFN Trieste, CERN)
  TID effects on CMS muon barrel detector Electronics, bulk damage on SiPM for the CMS HCAL upgrade and SEE on RPCs (Resistive Plate Chamber) Front-End Board for the CMS Muon System at HL-LHC
SCALTECH28 (INFN Padova, INFN MI Bicocca, CERN, EPFL)
  Study of Single Event Effects (SEE) on a flip flop based shift register in a 28nm High-K CMOS technology for future HEP experiments
APOLLO (INFN Padova, INFN Roma, CERN, Cassino University, Padova University)
  SEE tests on LV Power Supplies for the next High Energy physics experiments

## Slide 23: SEU Test on the PASTA chip
PASTA: custom readout circuit of silicon double-sided micro-strips of the PANDA MVD
  ASIC developed by JLU Giessen, FZ Juelich and INFN Torino
  Chip developed in 110 nm UMC technology
  Radiation tolerant circuits to Single Event Upset (SEU) effects are implemented
Test on the channel configuration register have been performed at SIRAD
The obtained result is adequate since the number of upsets expected in the micro-strip detector equipped with 3112 electronics readout chips, is less than 1 bit flip per hour taking into account that an evaluated particle flux of 5× 104 hadrons/cm2 contribute to upset effects.
“Study of SEU effects in circuits developed in 110 nm CMOS technology» D. Calvo, et al. Presented at TWEPP2019
Spokeperson: Daniela Calvo, INFN Torino

## Slide 24: SEU Test on MZMD chip
  The MZMD chip has been designed and produced for the PHOS4BRAIN INFN Gr V experiment: PHOtonic Systems for Broad Rad HArd INterconnect
It implements two 5 Gbps drivers for Silicon-Photonics Mach Zehnder Modulators and a high-speed serializer
It is fabricated in 65 nm TSMC technology implementing RHBD techniques like Enclosed Layout, CML and double-long transistors.
Chart: LET(Mev*cm2/mg)
| 3.1579999999999999 | 3.1579999999999999 | 3.1579999999999999 | 8.7899999999999991 | 8.7899999999999991 | 13.2 | 13.2 | 28.4 | 42 | 57.01 | 62.5
 | 1e-09 | 1e-09 | 1e-09 | 7.0316e-06 | 7.2257e-06 | 7.9906e-06 | 8.0796e-06 | 4.2449e-06 | 3.3039e-06 | 2.1834e-06 | 2.5023e-06
O16
Si28
Cl35
Ni58
Br81
Ag109
I127
Spokeperson: Guido Magazzù, INFN Pisa

## Slide 25: SEU test for LHCb RICH Detector Upgrade
Different irradiations performed in the period 2014-2018
  Heavy ions and 28 MeV protons
Radiation hardness characterization of the prototype and production versions of the CLARO ASIC (8 ch. ampl./discr. designed by INFN Ferrara/Milano-Bicocca/AGH-Krakow) and PMT glass transmittance
Tests at SIRAD were instrumental to assess the CLARO performance
Spokeperson: Massimiliano Fiorini, Università and INFN Ferrara

## Slide 26: The Ion Electron Emission Microscope
Time resolved ion induced SEE-micromapping with the IEEM:
  single energetic heavy ion impact points are reconstructed with a resolution of a few microns at a rate of 1kHz over a circular area of 180 µm diameter.
power MOSFET device with 223 MeV 79Br ions.