## Slide 1
Comparative Experimental and Simulation DOI
Analysis on Semi-Monolithic Metascintillators
Riccardo Latella, Lei Zhang, Antonio J. Gonzalez, Member, IEEE, Paul Lecoq, Fellow, IEEE,
Andrea Gonzalez-Montoro, Member, IEEE, Marta Freire, and Georgios Konstantinou, Member, IEEE
Riccardo Latella, PhD Student
Multiwave Metacrystal SA
Institute for Instrumentation in Molecular Imaging, i3M
Isola d’Elba, Italy, May 21st, 2024

## Slide 2
Index
Results
Flood Map and Energy Spectrums
Discussion and Future Works
Introduction
PET, Corrections, and DOI
Metascintillators
Materials and Methods
SMMS Structure
Scintillators & Photodetectors
Setup Description
Collimation Points
Estimator and Interpolation
Centroid Comparison
Regression/Conversion Methods
DOI Average Results
Timing Simulation
Timing Setups
SMMS-slab
Final Remarks

## Slide 3
Introduction
Corrections:
Scatter Filtering
Attenuation Correction
Random Coincidences Filtering
Depth-of-Interaction (DOI)
...
DOI Correction
Occurs when:
Imaging a curved surface
The detector angle is not perpendicular to the surface being imaged.
Benefits:
Reduces parallax error.
Enhances image resolution
ToF improvement
CT or MRI
t1 - t2 < time_window
The sole Line Of Response (LOR) is not enough to achieve significant improvements in terms of spatial resolution
Positron Emission Tomography (PET)
Precise timing
Good energy resolution
High-quality imaging
https://metacrystal.ch/

## Slide 4
Metascintillators
PATENT: González Martínez, A. J., Lecoq, P., Benlloch Baviera, J. M., Konstantinou, G., & Barrio Toala, J. (2023). Device for the detection of gamma rays based on segmented metascintillator block detectors.
Semi-Monolithic MetaScintillators (SMMS)
Metascintillators:
Combine dense host material with a fast emitter
Heterostructure with complementary properties
Based on the shared events concept
Exploiting the recoil electron trajectory
Light guide
G. Konstantinou et al.
doi: 10.1088/1361-6560/acac5f
P. Lecoq et al.
doi: 10.1140/epjp/s13360-022-03159-8
R. Latella et al.,
doi: 10.1109/TRPMS.2023.3310581
G. Konstantinou et al.
doi: 10.1109/TRPMS.2024.3368802
F. Pagano et al.,
doi: 10.1088/1361-6560/ac72ee

## Slide 5
SMMS Structure
Key components:
- LYSO:Ce plates (25.4 × 24 × 0.3 mm3)
- EJ232 plates (3 × 24 × 0.1 mm3)
Each SLAB contains:
8 LYSO:Ce semi-monolithic plates
8 layers of Ej232
8 EJ232 pixellated plates for each layer
Total of 64 EJ232 pixelated plates.
x8
ESR inter-slabs
SLAB
Everything coated in ESR,
Except the extraction surface

## Slide 6
Scintillators & Photodetectors
Hamamatsu SiPMs (HPK) S14
Semi-Monolithic MetaScintillators (SMMS)
Standard
Semi-MONolithic
(SMON)
Scintillators
Silicon Photomultipliers
Custom made readout:
Rows and columns reduction circuit (Patented)
M. Freire et al.,
doi: 10.1088/1361-6560/aca389
Dimensions:
25.4×25.4×24 mm3
100 μm Ej232 pixelated plates
300 μm LYSO:Ce semi-monolithic plates
25.4×25.4×20 mm3
8 bulk LYSO slabs

## Slide 7
Setup Description
Setup Description:
Sodium-22 radioactive source
Tungsten collimator
Temperature sensor
Compressed air system
Two detectors in coincidence
Custom-made analog frontend (Oncovision partnership)
Temperature Sensor
Compressed Air
Reference Detector
Testing Detector
Collimator
Radioactive Source

## Slide 8
Index
Custom-made analog frontend (Oncovision partnership)
12-bit 66-channel ADCs
Gbit connection
Integrated Charge
Trigger: 3-5-7ns coincidence time window

## Slide 9
Collimation Points
SMMS: 16 collimation points
SMON: 12 collimation points
Collimation:
Parallel incidence to the SiPMs
Perpendicularly to the monolithic side of the scintillator
Distance from the SiPMS
DOI1 = 3 mm
DOI2 = 9 mm
DOI3 = 15 mm
DOI4 = 21 mm

## Slide 10
Estimator and Interpolation
DOI Estimator (E/I or N/I):
E (or N) is the total energy of all the SiPMs (summation of all rows or columns)
I is the energy of the row or column with the most energetic signal
R. Pani et al., doi: 10.1109/TNS.2016.2539287
Convert
Interpolation:
Using the centroid position of the DOI E/I Distribution:
Linear Interpolation
Exponential-Tangent Interponation
[a.u.]
[mm]
FWHM: Full-Width at Half Maximum
mlog: Fitting function slope or angular coefficient of specific points

## Slide 11
Flood Map and Energy Spectrums
source
source
SMMS
SMON
x
y
x
y
Raised To the Power (RTP)
R. Pani et al., doi: 10.1088/1748-0221/11/01/C01061

## Slide 12
Centroid Comparison
DOI4 = 21 mm
DOI3 = 15 mm
DOI2 = 9 mm
DOI1 = 3 mm
Distance from the SiPMS
col0
col1
col2
col3
SMMS
SMON
0
SiPM

## Slide 13
Centroid Comparison
DOI4 = 21 mm
DOI3 = 15 mm
DOI2 = 9 mm
DOI1 = 3 mm
Distance from the SiPMS
col0
col1
col2
col3
Column 0
Column 1
Column 2
Column 3
0
SiPM

## Slide 14
Chart: Exponential-Tangent Conversion
Chart: E/I [a.u.]
| 4.42 | 5.57 | 6.16 | 6.41
col0 | 3 | 9 | 15 | 21
Regression/Conversion Methods
DOI4 = 21 mm
DOI3 = 15 mm
DOI2 = 9 mm
DOI1 = 3 mm
Distance from the SiPMS
Both report Gaussian-like distributions without major distortions
Linear
Exponential
0
Chart: Linear Regression Conversion
SiPM

## Slide 15
DOI Average Results
SMON SMMS
(4 DOI)
Linear 4.7 mm 6.2 mm
Expo 5.2 mm 7.4 mm
(3 DOI)
Linear ‘’ 5.3 mm
Expo ‘’ 5.7 mm
GOAL:
- Achieve similar results in terms of DOI
- Not to achieve the best DOI
SMMS: 4 DOI Layers
SMON: 3 DOI Layers

## Slide 16
Timing Simulation
Simulation & Experimental Data
SMMS simulation results match experimental data regarding the logarithmic behavior of centroid positions.
Timing Improvements:
Correction based on 8 DOI categories.
After DOI time-walk correction, CTR improvement from 136 ps to 98 ps
A potential 28% improvement in timing.
Simulation
Experimental

## Slide 17
Timing Setups
PETsys TOF-PET2
CAEN A5202+A5251
(Citiroc-based readout)

## Slide 18
SMMS-slab
Key components:
- BGO plates
- EJ232 plates
Each SLAB contains:
8 BGO semi-monolithic plates
7 layers of Ej232
8 EJ232 pixellated plates for each layer
Total of 56 EJ232 pixelated plates.

## Slide 19
Discussion and Future Work
Key Findings:
Comparable performance of SMMS and SMON in DOI capabilities, despite the 20% discrepancy in scintillation block height.
SMMS structure does NOT compromise the semi-monolithic DOI performances.
Exponential regression DOI resolution: 5.7 mm for SMMS vs. 5.2 mm for SMON.
Simulation Insights:
Simulation aligns with experimental data, following the same logarithmic behavior of centroid positions.
Main discrepancy noted in FWHM trends: experimental data decreases, simulation increases with distance from SiPM.
Timing improvements: potential 28% enhancement in coincidence time resolution after DOI time-walk correction.
Future Directions:
Continued validation of SMMS architecture for PET applications.
Explore SMMS timing capabilities using PETsys or Weeroc ASICs

## Slide 20
Thank you
Thank you for your attention!
Q&A