## Slide 1: High loading nanocomposites of cesium lead halide nanocrystals for fast timing
Jan Král1,2, Vojtěch Zabloudil2,3, Fiammetta Pagano4, Václav Čuba2, Eva Mihóková1,2, Kateřina Děcká1,2, Etiennette Auffray3
1 Institute of Physics of the Czech Academy of Sciences, Prague, Czech Republic
2 Czech Technical University in Prague, Prague, Czech Republic
3European Organization for Nuclear Research (CERN), Meyrin, Switzerland
4 Instituto De Instrumentación Para Imagen Molecular, Valencia, Spain
Email: kralja13@fjfi.cvut.cz
10th Conference on PET, SPECT, and MR Multimodal Technologies, Total Body and Fast Timing in Medical Imaging, 21.5.2024

## Slide 2: Cesium lead halide nanocrystals
ABX3 (A=Cs+, MA+; B=Pb2+ ; X=Cl-, Br-, I-)
excitonic luminescence, weak quantum confinment
narrow tunable emission peak
1
Protesescu et al. Nano Lett. 2015, 15, 6, 3692–3696

## Slide 3: Fast timing potential
2
bi- and multiexcitonic decay comp. (A. Erroi et al., ACS Energy Lett. 2023)
Prompt photons to scintillation puls of composite scintillators
K. Děcká et al. Nanomaterials 2022, 12, 14.

## Slide 4: Radiation detection
TOF-PET – 10ps challange
TOF-CT
  J Rossignol et al 2020 Phys. Med. Biol. 65 085013
Real-time single-proton counting
  Mi, Z., Bian, H., Yang, C. et al. Nat. Mater. (2024).
HEP- nanocal
  https://ep-news.web.cern.ch/content/birth-nanocalal. npj
Fast timing capabilities
Cheap nanocomposite detectors
3
F. Pagano et al. 2022 Phys. Med. Biol. 67 135010
coincidence time resolution
rise time
decay time
photon density
R.M. Turtos et 2D Mater Appl 3, 37 (2019)

## Slide 5: Timing performance under X-rays
DTR (detector time resolution) = FWHM of the time delay peak
significant improvements in timing performance under X-ray excitation
F. Pagano et al.(2022). In Frontiers in Physics (Vol. 10).
4
F. Pagano et al. Adv. Mater. Interfaces 2023, 2300659.
Notes: Fig. in right—these are different results than those published in our Adv. Mater. Interf.? If not, add the reference

## Slide 6: TOF – PET energy sharing
F. Pagano et al. Adv. Mater. Interfaces 2023, 2300659.
5
Shared events between NC layer and bulk scintillator under 511 keV excitation
Embedding nanocrystals in the matrix for chemical and mechanical protection to prepare nanocomposite material

## Slide 7: Embedding nanocrystals into a matrix
Needed: high loading (stopping power) and high transparency
6
Main goal: improving nanocrystal dispersion

## Slide 8
Allyltrimethoxysilane (ATMOS)
Allyltrichlorosilane (ATS)
Introduction of copolymerizable functional groups
7
ACS Appl. Mater. Interfaces 2016, 8, 50, 34762-34769

## Slide 9: Nanocomposite preparation
8
styrene purification and prepolymerization
Hot-injection synthesis and functionalization
Sample preparation
+ thermal initiator
Polymerization at 80°C

## Slide 10: Nanocrystal characterization
9
partial ligand exchange and introduction of allyl groups to the surface successful
tunable emission of the samples
CPB = CsPbBr3
CPBC = CsPb(Br/Cl)3

## Slide 11: Nanocomposite samples
Samples with 1 wt% loading
  CPB@PS different ligands
Samples with high loading (>10 wt%)
  CPB and CPBC samples with different loading and composition
10

## Slide 12: CPB@PS 1% - ligand comparison
11
improvement in transparency and blue-shift of emission when ATMOS ligand applied

## Slide 13: CPB@PS 1% confocal Raman microscopy
12
decreased agglomeration with ATMOS ligand

## Slide 14: Nanocomposites with high loading
200 µm
14
thickness 200 µm
High loading up to 40 wt% with some transparency

## Slide 15: Decay under X-ray excitation
CPB decay kinetics mostly unaffected with increasing content up to 20 w%
Increased share in the slowest component for 40 w%
Significantly faster decay kinetics for increasing chloride content
15

## Slide 16: Time resolution under X-rays
16
significantly decreased light output with increased chloride content
comparable timing of CPB and CPBC nanocomposite under X-ray excitation
Significant improvement vs previously reported DTR for CPB nanocomposite ~ 300 ps K. Děcká et al., J. Mater. Chem. C 10, 12 836 (2022)

## Slide 17
Conclusions
  functionalization by allylsilanes was successful
  introduction of allyl group improved transparency and dispersion of nanocrystals in the matrix
  high loading up to 40 wt% was achieved
  timing capabilities of CsPb(Br/Cl)3 nanocrystals is comparable with CsPbBr3 nanocrystals
  improved timing for CPB nanocomposites under X-rays, significant increase in stopping power
Outlook
  determination of nanocomposite light yield
  utilization of high loading samples in heterostructures
  preparation of high loading nanocomposites with newly modified NCs
17

## Slide 18
It was funded by OP JAC project financed by ESIF and the MEYS SENDISO (CZ.02.01.01/00/22_008/0004596), Czech Science Foundation (GA23-05615S), Grant Agency of the Czech Technical University in Prague (SGS23/189/OHK4/3T/14), and CERN Budget for Knowledge Transfer to Medical Applications
This work was carried out in the frame of Crystal Clear Collaboration.
Acknowledgements
18