## Slide 1: Amorphous Silicon Microchannel Plates: A new photon detector with 10 ps timing and 15 μm spatial resolution
Samira Frey, Georgios Konstantinou, Luca Antognini, Christophe Ballif and Nicolas Wyrsch

## Slide 2: Contents
Micro-Channel Plates: A short functionality and structure introduction
Amorphous Silicon Micro-Channel Plates (AMCP)
Simulation and experiment
Design for spatial resolution
Functionality fit to new generation of scintillators

## Slide 3: MCPs: A guide to functionality
R. Paschotta, RP Photonics Encyclopedia
Reverse Vbias
Ground
Elba PSMR 2024
Photon
Photocathode
Broad application in low light environments (microscopy, LIDAR, night-vision)
Cost as the main barrier of entry for scintillator readout

## Slide 4: aSi-Based MCPs
[1] A. Franco et al. Sci. Rep. 1 (2014).
Advantages of AMCP vs. conventional MCP:
Monolithic Integration
Flexibility in fabrication
a-Si:H tunable resistivity
Miniaturization

## Slide 5: Fabrication process
Metal deposition (sputtering, evaporation)- Cr or Alu (or both)
Photolithography:
  PR spin-coating, laser exposure, PR development, Chemical etching
Plasma enhanced chemical vapor deposition (PECVD):
  Different recipies of H and SiH4
Deep Reactive Ion Etching (DRIE): Bosch process
Si isotropic etching
c-Si wafer
a-Si:H
Cr
a-Si:H
Al Electrode
SiO2
Cr
Cr
Sulfur hexafluoride [SF6]
Octafluorocyclobutane [C4F8]

## Slide 6: AMCPs: A history of development
S. Frey PhD Thesis, 2023
Developed for Cherenkov TOF PET:
SNSF Synergia project
Funnels
2011

## Slide 7: Gain and efficiency Simulation
*For an incoming particle with 200eV
 | AMCP Straight Channel | AMCP Funnel Channel | AMCP Funnel Channel (+ MgO)
Gain (500 V) | 1515 | 1109 | 1712
Time Jitter [ps] | 6.1 | 6.3 | 5.5
Rise Time [ps] | 4.31.2 | 4.31.4 | 4.71.1
Det. Efficiency (Inside channel)* | 79.8% | 91.8% | 99%
 | AMCP Straight Channel | AMCP Funnel Channel | AMCP Funnel Channel (+ MgO)
Gain (500 V) | 1515 | 1109 | 1712
Time Jitter [ps] | 6.1 | 6.3 | 5.5
Rise Time [ps] |  |  | 
Det. Efficiency (Inside channel)* | 79.8% | 91.8% | 99%
MgO can compensate for loss in gain due to channel broadening
Time Resolution not affected by funnel
MgO sputtering

## Slide 8: Characterization - Gain Measurements
Newest Generation of Devices : Aspect ratio 25  Gain 1500
Notes: After the optimization we measured the gain of the new samples both under continuous and pulsed illumination. Few things I want to point out here. A gain of around 1500 could be measured which is quite an increase to the previous maximum of around 100 in the older generation. The increase in gain is due to the increase of aspect ratio and also because the structural defects in the amorphous silicon layer were reduced we were able to apply a high bias voltage of 500V on the 40um thick amorphous silicon layer. I again plotted the gain bias relationship in a log log plot.

## Slide 9: Integration on CMOS camera
To add high spatial resolution to this system, a matrix of read-out channels is necessary
Such approach is commonly followed on CMOS cameras
A CMOS tile with 4x4 um2 active area and 15x15 um2 pitch was chosen for prototyping
0.35 Mpix
Source: Wikipedia

## Slide 10: Design compromise of hexagonal and square grids
Hexagonal array is necessary to maintain geometrical coverage of the funnels (and improved packing fraction)
Design of the bottom electrode requires isolation between readout pixels to avoid cross-talk
It is important that the same number of microchannels are read-out by a single pixel

## Slide 11: Design compromise of hexagonal and square grids

## Slide 12: Design compromise of hexagonal and square grids
We slightly adapt the hexagonal grid to have the same pattern for each pixel
10% change is within specifications of design
The new pixel design interlocks with a critical distance of ~1.2 um and 15 um pitch

## Slide 13: Design compromise of hexagonal and square grids
We slightly adapt the hexagonal grid to have the same pattern for each pixel
10% change is within specifications of design
The new pixel design interlocks with a critical distance of ~1.2 um and 15 um pitch

## Slide 14: New design fabrication
Secondary changes to the fabrication process (design, bottom pad thickness and material (Cr/Al/Cr  Cr)
Criticality of alignment  more robust exposure laser process (no need for mask)
<300 nm misalignment, within specs

## Slide 15: Timing characterization
Two different configurations - Chip + ext. amplifier / Chip LNA on board

## Slide 16: Timing results: External Amplifier board
12.6 ps
(FWHM)
Low Flux / NO PC / Ext. Amplifier

## Slide 17: Timing results: LNA on board
(Note : Bias only up to 300V – Gain reduced)
6.1 ps
(FWHM)
Low Flux / NO PC / Amplifier on the same board
Notes: Which brings me to the final measurement- now this is the configuration where the AMCP and the amplifier were placed close to each other on the same board inside the vacuum chamber. Now there were a few problems with this AMCP chip- we could only bias up to 300V instead of the usual 500V which means the gain was significantly reduced. The reason for this was again due to electrical breakdowns that occured in this chips. But what we can see is even though the gain was low and the signal was amplitude was very low the time resolution was still good with 6.1picoseconds. So we can still increase the resolution a lot by having amcp and amplifier close or ideally in the future fully integrated.

## Slide 18: Simulation: Metascintillators on AMCPs
LYSO:Ce, (24x9.6x0.25 mm3)
PEA2PbBr4 perovskite (24x9.6x0.1 mm3)
Good energy resolution/ energy sharing resolution
Down to 1 mm Spatial Resolution
8 mm DOI
90 ps CTR
No need for 15 um2 pixelation, 150 um2 would render similar results  Digital SiPM people?

## Slide 19: Next steps
Migrate the technology from the test design to the CMOS design
Confirm timing and spatial resolution characteristics through the dedicated low-noise CMOS readout
Experiment and integrate AMCP with a photocathode
  standard solution: Photonis Planacon
  Possible solutions: Bi-alkali sputtering, oxides, silicon
Navigate design specs for optimal PET application

## Slide 20: Conclusions
MCPs have already proven their capabilities as TOFPET photon-detectors
AMCPs have the potential to improve the state of the art in MCP and photon detection timing
AMCPs on CMOS set the state of the art in spatial resolution
Fabrication is complex but versatile, allowing devices with variable and application specific specifications
Potential fit for scintillator read-out to be explored

## Slide 21: Thank you for your attention