## Slide 1: Characterization of SiPMs and performance studies for the dRICH detector of the ePIC experiment
Luisa Occhiuto, University of Calabria & INFN Cosenza
luisa.occhiuto@cern.ch INFN 2024

## Slide 2: THE ELECTRON-ION COLLIDER AND THE ePIC EXPERIMENT
Key capability: particle tracking and identification (PID), aiming to separate electrons from pions, kaons and protons.
dRICH detector
Two radiators: aerogel (), C2F6()
Mirrors: 6 large open sectors with radius 220 cm
SiPM sensors
luisa.occhiuto@cern.ch INFN 2024 1

## Slide 3: Nσ SEPARATION OF π AND K
Momentum for the gas [13.0 , 60.0] GeV in steps of 5 GeV.
Momentum for the aerogel [1.0 , 19.0 ] GeV in steps of 2 GeV.
Pseudorapidity () [1.5, 2.0] , [2.0, 2.5] , [2.5, 3.5].
From geometrical consideration Cerenkov angles.
Gaussian fit on distribution of Cerenkov angle.
Mean and sigma from these fits.
Evaluation of the separation between pions and kaons as a function of the particle momentum with:
N
Identification of particles with momentum from a few GeV/c up to about 50 GeV/c.
luisa.occhiuto@cern.ch INFN 2024 2

## Slide 4
N
Momentum (GeV/c)
Momentum (GeV/c)
Momentum (GeV/c)
N
N
Resolution of Cerenkov angle (π)
luisa.occhiuto@cern.ch INFN 2024 3

## Slide 5: I-V CHARACTERIZATION
Costum made portable Peltier box
Ultra pure air tanks
Multiplexer
Source Meter
Power supplies
Adapter board
SiPM board
Characterization setup for I-V characteristic installed in Cosenza, University of Calabria.
5 boards analyzed.
Data acquisition of I-V characteristic @ 253 K.
1° set of measurements
HAMA S13360-3050
HAMA S13360-3075
HAMA S14160-3050
PRO
Single photon detection;
High Photon Detection Efficiency;
Good time resolution;
Insensitive to magnetic field.
Cheap
Low voltage operation
CONS:
Large Dark Count Rate
Prone to radiation damage
luisa.occhiuto@cern.ch INFN 2024 4

## Slide 6
Costum made portable Peltier box
Ultra pure air tanks
Multiplexer
Source Meter
Power supplies
Adapter board
SiPM board
Characterization setup for I-V characteristic installed in Cosenza, University of Calabria.
5 boards analyzed.
Data acquisition of I-V characteristic @ 253 K.
1° step of measurements
HAMA S13360-3050
HAMA S13360-3075
HAMA S14160-3050
PRO
Single photon detection;
High Photon Detection Efficiency;
Good time resolution;
Insensitive to magnetic field.
Cheap
Low voltage operation
CONS:
Large Dark Count Rate
Prone to radiation damage
Irradiation with different energies @ fixed fluence, .
To lower energy: IBA Solid Plate Phantom (RW3).
#Board | Energy scan (MeV) | RW3 thickness (mm)
1 | 138 | 0
2 | 73 | 88
3 | 41 | 116
4 | 20 | 127
5 | 13 | 131
2° set of measurements
luisa.occhiuto@cern.ch INFN 2024 4

## Slide 7
Costum made portable Peltier box
Ultra pure air tanks
Multiplexer
Source Meter
Power supplies
Adapter board
SiPM board
Characterization setup for I-V characteristic installed in Cosenza, University of Calabria.
5 boards analyzed.
Data acquisition of I-V characteristic @ 253 K.
1° step of measurements
HAMA S13360-3050
HAMA S13360-3075
HAMA S14160-3050
PRO
Single photon detection;
High Photon Detection Efficiency;
Good time resolution;
Insensitive to magnetic field.
Cheap
Low voltage operation
CONS:
Large Dark Count Rate
Prone to radiation damage
Irradiation with different energies @ fixed fluence, .
To lower energy: IBA Solid Plate Phantom (RW3).
#Board | Energy scan (MeV) | RW3 thickness (mm)
1 | 138 | 0
2 | 73 | 88
3 | 41 | 116
4 | 20 | 127
5 | 13 | 131
2° step of measurements
Oven annealing: 150 h @ 150 °C
3° set of measurements
luisa.occhiuto@cern.ch INFN 2024 4

## Slide 8: I-V CHARACTERISTIC
253K- no irradiated
253K- annealed
253K- irradiated
luisa.occhiuto@cern.ch INFN 2024 5

## Slide 9: ENERGY SCAN
Overvoltage = Dark current - Vbd
=efficiency of degrader.
Displacement damage for each sensor. A proton at 13 MeV is more harmful than a proton at 138 MeV.
PRELIMINARY
For semplicity we call:
HAMA S13360-3050 == A
HAMA S13360-3075 == B
HAMA S14160-3050 == C
Fraction of damage for each sensor
luisa.occhiuto@cern.ch INFN 2024 6

## Slide 10: CONCLUSION AND OUTLOOK
Pions, kaons can be separated up to 50 GeV for a large range of pseudorapidity.
Below the focalization is not optimal.
Radiation damage is in agreement with the NIEL model.
With annealing there is a recovery of the performance of the sensors independent of the energy used to irradiate them.
The next step is to irradiate the sensors with gamma rays and see how the damage changes
Nσ SEPARATION
NOISE
CHARACTERIZATION
γ RAYS
SIMULATION
OUTLOOK
SiPMs
OUTLOOK
The next step is to add noise and see how the Nσ separation and the resolution change.
luisa.occhiuto@cern.ch INFN 2024 7

## Slide 11: THANKS!
luisa.occhiuto@cern.ch INFN 2024 8

## Slide 12: Backup
luisa.occhiuto@cern.ch INFN 2024 9

## Slide 13: SiPM SENSORS
PRO:
Single photon detection;
High Photon Detection Efficiency;
Good time resolution;
Insensitive to magnetic field.
Cheap
Low voltage operation
CONS:
Large Dark Count Rate
Prone to radiation damage
Sensors: 3x3 pixel
HAMA S13360-3050
HAMA S13360-3075
HAMA S14160-3050
The Dark Dount Rate (signal per unit of time observed in absence of a photon beam) can be reduced by operating at low temperatures ().
Effect of radiation on SiPMs depends of various factor:
Type of radiation
Energy of the particles
Radiation dose
Duration of exposure
Radiation damage by Non-Ionizing Energy Loss (NIEL) leads to displacement damages and build up of crystal defects that results basically in increased DCR http://rd50.web.cern.ch/NIEL/default.html.
Different particles different interaction different damage.
luisa.occhiuto@cern.ch INFN 2024 10

## Slide 14: SiPM SENSORS
PRO:
Single photon detection;
High Photon Detection Efficiency;
Good time resolution;
Insensitive to magnetic field.
Cheap
Low voltage operation
CONS:
Large Dark Count Rate
Prone to radiation damage
Sensors: 3x3 pixel
HAMA S13360-3050
HAMA S13360-3075
HAMA S14160-3050
The hardness factor k is used to normalize the damage caused by different incident particles relative to a reference particle, in this case a 1 MeV neutron.
This allows us to compare the damage caused by particles with different energies on a common scale.
In other words, it tells us how much energy a 1 MeV neutron beam would have to have to cause the same damage.
luisa.occhiuto@cern.ch INFN 2024 11
A few MeV proton is more harmful than a 1 MeV neutron. From 100 MeV damage seems to be compatible between neutrons and protons.

## Slide 15: SiPM SENSORS
PRO:
Single photon detection;
High Photon Detection Efficiency;
Good time resolution;
Insensitive to magnetic field.
Cheap
Low voltage operation
CONS:
Large Dark Count Rate
Prone to radiation damage
Sensors: 3x3 pixel
HAMA S13360-3050
HAMA S13360-3075
HAMA S14160-3050
The hardness factor k is used to normalize the damage caused by different incident particles relative to a reference particle, in this case a 1 MeV neutron.
This allows us to compare the damage caused by particles with different energies on a common scale.
In other words, it tells us how much energy a 1 MeV neutron beam would have to have to cause the same damage.
luisa.occhiuto@cern.ch INFN 2024 12
Where D is the displacement damage cross section.

## Slide 16: ENERGY SCAN
Evaluation of breakdown voltage (Vbd).
  Evaluation of current at 3 Overvoltage.
  Evaluation of difference between current post and pre irradiation.
  Uniform distribution assumption.
Overvoltage = Dark current - Vbd
=efficiency of degrader.
luisa.occhiuto@cern.ch INFN 2024 13